## Slide 1: Ultra low energy ion implantation into transition metal dichalcogenides
B. E. Kardynał
Peter Grünberg Institute 9 (PGI-9),
Forschungszentrum Jülich, Germany
Notes: Add team members

## Slide 2
Acknowledgements
FZJ PGI-9
Minh Bui
Dr Sven Borghardt
Thipwaree Keawphong
Dr Renu Rani
Lanqing Zhou, David Fricker, Zeng Zheng
6/28/2022
2
FZJ PGI-1/IAS-1
Stefan Rost
Dr Christoph Friedrich
Dr Irene Aguilera
Prof Dr Stefan Blügel
Helmholtz‐Zentrum Dresden‐Rossendorf
Prof Dr Arkady Krasheninnikov
Dr Mahdi Ghorbani
FZJ ER-C
Dr Lei Jin
Lidia Kibkalo
FZJ HNF
Dr Jhih-Sian Tu
Janine Worbs
Stephanie Bunte
University of Göttingen
Dr Manuel Auge
Felix Junge
Prof Dr Hans Hofsäss
University of Limerick
Dr Eoghan O’Connell
Mike Hennessy
Eoin Moynihan
Prof Dr Ursel Bangert
Integration of Molecular Components in Functional Macroscopic Systems initiative
Aalto University
Dr Hannu-Pekka Komsa
Arsalan Hashemi
SuperSTEM
Dr Quentin Ramasse

## Slide 3: Spin-valley-polarisation locking
Plan view
Side view
Mo,W
Se,S
MoSe2
K
-K
K
-K
K
-K
Symmetry: trigonal, lack of inversion symmetry
Spin-orbit interactions
Optical readout
Direct bandgap
Strong excitonic effects
Spin-valley qubit
1st Brillouin zone
Notes: Valence spin splitting: 100s meV
Conduction band splitting: up to 40 meV
Spin-valley-photon polarization locking

## Slide 4: Localisation of excitons
Brammy et al. Nat. Commun. 8, 15053 (2017)
L. Yu, Nano Lett. 21, 2376 (2021)
By strain:
On defects:
Klein et al. Nat Commun 10, 2755 (2019)
Hötger et al., Nano Lett. 21, 1040–1046 (2021)
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 5: Why ultra low energy ion implantation?
WHY IMPLANTATION?
Wide range of elements can be used
Clean, performed in vacuum
Post-annealing possible
WHY ULTA LOW ENERGY?
Enough to implant in the ML
Limits number of undesired defects
Enables patterned implantation with free surface
S. Kretschmer et al., J. Phys. Chem. Lett. 13 (2022) 514−519
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 6: Simulation of Se implantation into MoS2
Molecular Dynamic simulation: 128 events
Se adatoms
Se@S
S vacancies
A. Krasheninnikov (HZDR, Dresden)
Bui et al., npj 2D Mater Appl 6, 42 (2022)
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 7: Ultra-low energy ion implantation
MoS2 on SiO2
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 8: Experimental and simulated HAADF images
MoS2 implanted with Se at E~10 eV with 1015 ions/cm2
experimental HAADF STEM image
Eoghan O’Connell et al – IMC 19
simulated HAADF STEM images
1
4
2
3
1
2
3
4
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 9: Optical spectroscopy
~ 0.43 Se/S on top layer
Bui et al. npj 2D Mater Appl 6, 42 (2022)
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 10: Photoluminescence spectra
Annealing: 200oC, 3 h, 5 x10-3 mbar
Annealing conditions selected considering the binding energy of adatoms:
Under investigation:
MoSe2 + S
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 11: DFT calculations of implanted layers
Bui et al. npj 2D Mater Appl 6, 42 (2022)
G
M
K
G
E-EF (eV)
2.0
1.0
0.0
MoS2-0.22Se0.22 ML
M
K
G
E-EF (eV)
1.8
1.7
1.6
1.5
1.4
G
MoSe2
MoSe2-0.33S0.33
Notes: Correct DFT if time allows

## Slide 12: Emission from Cr (E=25eV) implanted MoSe2
T = 10 K
top hBN
Gr back
bottom hBN
ML
V
e-
h+
D0
D0 bound exciton
With the possible options:
the origin of D0 state is not clear.
Cr-Se@Se 41%
interstitial 28%
Cr@Mo 28%
Under investigation:
MoSe2 + P
hBN +He, Ne, Kr
Notes: Very similar to trion.

## Slide 13: Patterned implantation
Vion
Vmask
Cr/Au
Implantation target
Hole
diameter
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 14
Implantation of 25 eV Mn ions into ta-C/Si
Adjustment of all spectra by means of SIMNRA
Laterally controlled ULE ion implantation
M. Auge et al, NIM-B, 512, 96 (2022)

## Slide 15: Summary
Material and process design:
  ion trajectories simulations
  Molecular Dynamics
  DFT calculations
Characterisation:
  TEM
  optical spectroscopies
Ultralow energy implantation into MoS(Se)2 has allowed us to :
  Generate strain on an atomic scale
  Introduce defects
Ultra low energy implantation very flexible / number of applications
Still much to find out !

## Slide 16: TMDs monolayers
G
M
K
G
3
2
1
0
-1
E (eV)
G
M
K
-K
Gate voltage (V)
X-
X+
X0
1.550 1.575 1.660 1.625 1.650 1.675
4.0
2.0
0.0
-2.0
-4.0
Energy (eV)
Min
Max
Plan view
Side view
Mo,W
Se,S
Notes: Lattice: hexagonal. Minimum at K-point -> direct bandgap. El and holes in the metal layer. 2D confinement means very stong Coulomb interactions. X binding energy depends on the environment and is up to 300meV in vacuum. The result: excitons live even at room temperature. Excitons sensitive to the external fields – dipole field penetrates into barriers.

## Slide 17
Grid 2
Hole diameter: 1 µm
Spacing: 2 µm
Patterned implantation: simulations

## Slide 18: Cr implantation in MoSe2 - Molecular Dynamics simulation
Cr-Se@Se 41%
interstitial 28%
Cr@Mo 28%
25 eV
A. Krasheninnikov (HZDR, Dresden)
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 19: Emission from Cr implanted MoSe2
T = 10 K
top hBN
Gr back
bottom hBN
ML
V
e-
h+
D0
D0 bound exciton
With the possible options:
the origin of D0 state is not clear.
Cr-Se@Se 41%
interstitial 28%
Cr@Mo 28%
x3
x1
V = 2.0V
Notes: Very similar to trion.

## Slide 20
Power dependence
D peak decreases relatively to X0 and X-
e-
h+
defect
Bound exciton
Saturation 10 µW
I = Isat . P/(P+Psat)
Defect-band transition
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 21: Photoluminescence excitation
D peak formation in resonance with X0 generation
Excitation E
Notes: In previous measurement we excite with fixed laser wavelength. *run e- h+ animation*
More info can be gained when we see at which exc wavelengths the sample’s absorption contributes most to PL.
*run exc E anim at same time* In this measurement of PLE: vary excitation wavelength and record change in D peak intensity *anim*. This can show the absorption property of emission. In this measurement we scan the laser over the range above X0 to below X-
Intensity of D state: highest at X0 emission energy. The absorption on the other hand is not strong around X-  D emission is predominantly formed by trapping excitons, not trions.
This agrees with previous observation that D peak emission competes with X-.
Defect states: fed by X0 generation, not X-: more evidence the transition is donor-acceptor or acceptor-band.? (Competition beween X- and D?)
2 possible origin: from radiative recombination of excitons bound to charged acceptor (?). Alternative: donor-acceptor transition, or acceptor-band.
More to come with doping dependent measurement

## Slide 22: MoSe2+Cr: DFT
MoSe2 with Cr@Mo
S.Rost
Notes: To see how the defects affect our optical property, we did DFT calculations to calculate the band structures of Cr@Mo and Cr@Se-sub. I should update on Stefan’s calculations for interstitial position.
Cr@Mo: acceptor state near conduction band: “Classic” defect: States localised in real space / delocalized in k-space. If the states are not degenerate, we can host single e- and single photon emission can be achieved
Cr@Se-sub: one localised state mid gap, and a dispersive state below CB
Midgap: classic defect states; Others: hybrid with conduction host states.
As a reminder, these DFT: preliminary results, don’t include many body interaction. So may missing E corrections  we don’t rely too seriously on the exact energy levels of the calculations, but the trend should be clear. In any case we should be able to see see defect states.
DFT: 5x5 cell, relaxed to 1e-4 a.u. . SOC included
#Possibility of magnetic coupling / enhancement
Cr@Se: donor state around midgap and acceptor near conduction band

## Slide 23: MoSe2+Cr: DFT
S.Rost
MoSe2 with CrSe
MoSe2 with Cr-Se@Se
Notes: To see how the defects affect our optical property, we did DFT calculations to calculate the band structures of Cr@Mo and Cr@Se-sub. I should update on Stefan’s calculations for interstitial position.
Cr@Mo: acceptor state near conduction band: “Classic” defect: States localised in real space / delocalized in k-space. If the states are not degenerate, we can host single e- and single photon emission can be achieved
Cr@Se-sub: one localised state mid gap, and a dispersive state below CB
Midgap: classic defect states; Others: hybrid with conduction host states.
As a reminder, these DFT: preliminary results, don’t include many body interaction. So may missing E corrections  we don’t rely too seriously on the exact energy levels of the calculations, but the trend should be clear. In any case we should be able to see see defect states.
DFT: 5x5 cell, relaxed to 1e-4 a.u. . SOC included
#Possibility of magnetic coupling / enhancement
Cr@Se: donor state around midgap and acceptor near conduction band

## Slide 24: Temperature dependence
Normalised intensity (a.u.)
T = 10 K
T = 108 K
A- - band transition
e-
h+
-ve charged acceptor
Bound exciton
Notes: So we have the two possibilies for D emission: exciton bound to A-, or acceptor-band transision.
1st scenario *point on image*: has low binding E, should dissociate as temperature rises
 we heat the system up to 108 K and measure the PL.
At high temperature: D peak dissociates more slowly than trions  not expected from defect bound excitons.
*animation* This, combining with all observations sofar, implies the D peak transistion is likely from A- band transition.
This D peak, while has electrical controlibilty and remain bright at higher temps, is still a broad emission likely from an ensemble of defect sites. This is because the defect density is still high:
We use ~ 1.5 um2 laser spot, which cover about up to 4e4 defects.
For SPE, we need to dilute ion conc for further insight and possibility of isolating a single defect.
This is what we’re working on and hope to have some new data soon.

## Slide 25
MoSe2+Cr D peak: spin-valley locking?

## Slide 26: Raman spectroscopy
Bui et al. npj 2D Mater Appl 6, 42 (2022)
Notes: We then turn to Raman spectroscopy: quick and non destructive measurement technique for Se level in the system, also suitable with samples on SiO2 substrate
In this measurement, laser radiation comes onto the sample and gets scattered inelastically by the lattice vibration of the ML. The measured scattered signal can give information on the lattice structure.
For example, ML MoS2 out of plane vibrational modes A’ show at 404 cm-1 and inplane vibration E’ at 385 cm-1.
*click for animation* Incoporation of Se introduces a mode at at 270 cm-1, caused by the out of plane vibration of S-Mo-Se bond. This can give evaluation of Se presence in the ML. More Se: higher intensity
In addition, Se presence also breaks periodicity of lattice, leading to other development of spectra: e.g. more contribution to phonon lines in LA, or broadening and shifting of peaks. E’ and A’ of MoS2 modes also becomes weaker

## Slide 27: MoS2+Se: discharge
Au contact: necessary to maximize the incorporation rate
Bui et al. npj 2D Mater Appl 6, 42 (2022)
Notes: 2 critical factors for good implantation: metal contact and heating.
1st thing we found: metal contact is essential to define a potential on the sample.
It can also remove charge of implanted ion from ML.
*hover on graph* This graph illustrate the role of contact on implantation results:
Blue curve is the Raman spectrum of an implanted ML with contact, yellow/brown curve is that without a contact.
Blue spectrum shows more Se incorporation rate with higher A’MoSSe.
Without contact: ions implanted on ML build up charge and repel further coming ions. They can have lower energies because of electrostatic repulsion.
At some point, the total number of implanted ions is then limited.  not good for assessing the implant process

## Slide 28: MoS2+Se: heating
Pre-annealing: in-situ before implantation
Post-annealing: in-situ after implantation
Hot implant: implantation during annealing
Bui et al. npj 2D Mater Appl 6, 42 (2022)
Notes: Next crucial factor for implant is heating/annealing.
Pre-annealing: before implant: aims to clean sample by removing some volatile contamination
After implant, there might be some unwanted defects such as adatoms and vacancies. Annealing may promote diffusion of these adatoms into filling the vacancies and increase Se incorporation.
*anim* While these methods give decent Se substitution level, Biggest change comes from implant at elevated temperature, as seen here in the Raman spectra on the right: For hot-implanted sample: A’MoSSe is most intense and the lines’ sharpness indicate good crystallinity preservation.
While the role of temperature is at the moment not well understood, we believe it’s to ease the discharging process by better mobilizing charge carriers.

## Slide 29
DFT: S implantation in selenides
MoSe2 +S
MoSe2-0.33S0.33
M
K
G
E-EF (eV)
2.0
1.0
0.0
-1.0
G
M
K
G
E-EF (eV)
1.8
1.7
1.6
1.5
1.4
G
MoSe2
MoSe2-0.33S0.33
Notes: Correct

## Slide 30: DFT: strain vs implantation
EK/Q (eV)
2.2
2.1
2.0
1.9
1.8
1.7
1.6
1.5
Strained MoS2 ML
-4 -3 -2 -1 0 1 2 3
Lattice strain (%)
z-parameter
0.131
0.130
0.129
0.128
0.127
0.126
Strained MoS2 ML
-4 -3 -2 -1 0 1 2 3
Lattice strain (%)
Q
K
(0.25-z)c
c
Notes: Correct

## Slide 31
DFT: S implantation in selenides
MoSe2 /WSe2 +S
MoSe2-0.33S0.33
G
M
K
G
E-EF (eV)
2.0
1.0
0.0
-1.0
E-EF (eV)
2.0
1.0
0.0
-1.0
G
M
-K
G
K
E-EF (eV)
1.6
1.5
1.4
1.3
1.2
G
M
-K
G
K
WSe2-0.33S0.33
G
M
K
G
E-EF (eV)
1.8
1.7
1.6
1.5
1.4
Notes: Correct

## Slide 32: MoSe2+S
Splitting of A’ mode
Unassigned Raman modes, from presence of disorder (implants)
X0
XD
S+ @ 20 eV, 2.5 x 1014 cm-2
Notes: Correct

## Slide 33: MoSe2+S
PL visible at cryogenic T
Defects dominate
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 34: MoSe2+S
T = 7.7 K
T = 7.7 K
A
B (?)
M. Selig et al. PR Res. 1, 022007(R) (2019)
Notes: Cryo measurement PL shows clearer changes: redshifted X0? Or trion?
*anim* Reflectance: measurement, which reflects the absorption of the compound, A-exciton transition is clear
Additional transition @ 1.83 eV, unclear for now

## Slide 35
Outcome probability from DFT simulation by A.V. Krasheninnikov
Notes: Correct

## Slide 36: Sample
top hBN
MoSe2
Gr back
Au
bottom hBN
ML
Au
MoSe2
ML
Bottom hBN
Top hBN
Gr back
Au
Au
Gr/hBN/MoSe2/hBN on SiO2
20 μm
MoSe2
Gr back
Au
bottom hBN
ML
Au
Cr+: 25 eV
3x1012 cm-2 ~0.26% Cr/Mo
220oC
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 37: Sample preparation
Mechanical exfoliation & stamping using PDMS
Au contact: defines potential on flake
MoS2 on SiO2
Exfoliation
Notes: Valley coherence together with other properties: optically addressable spin-valley qubit.
Probed in very simple structures.
Gamma valley, dispersion – 0.01% of excitons in the light cone
Bohr radius 2 nm
Access on single particle level: confinement of an exciton or trion
The way to do it: localize electron / hole in energy minimum: gating , electrostatic, dielectric, doping

## Slide 38
A slide to say: while WSe2 shows SPE and coherence, it is not easy to interpret because of the role of defects. Show Sven’s data and Prokhor’s data.

## Slide 39: Gating of WSe2 ML
1.65
1.75
50
1.55
0
-50
Gr
WSe2/ MoSe2
SiO2
Vg
p-Si
Excitation
Measured signal
60K
12K
Excitation at 660 nm
Laser power: 10mW
Spot size: 1.5mm
Electron / Hole doping
Notes: Control of doping needed for example to see T dependence.

## Slide 40: Vacancy formation
Tried implanting Kr+ (23 eV, 3e12/cm2, 220oC); no samples came back alive (PL quenched), suggesting high level of damage
Tried annealing
RT Raman & PL can detect
M. Mahjouri-Samani et al. Nano Lett. 16, 5213−5220 (2016)

## Slide 41: Gated WSe2 ML
Electron / Hole doping
Notes: Valley coherence preserved with excitation at energy 132meV above the exciton energy.
Clear asymmetry – sign that band structure is not sufficient.

## Slide 42: Excitation Resonant with X0
hn (eV)
X+ and X- different effective masses, holes are heavier
Phonon resonance between X0 and X- energies.
Vgc (V)
0
50
100
-50
-100
Max
Min
EX: 710 nm
1.74
1.6
X-
Xg-
I
X-’
X+
12K
X-
X+
X+
X-
Xg-
I
X-’
EX: 660 nm
hn (eV)
1.74
1.6
Notes: One reason for asymmetry is the trion binding energy

## Slide 43: EXTRiNSIC EFFECTS ON TMDs
S. Borghardt et al., Phys. Rev. Mater. 1, 054001 (2017)
WSe2/ MoSe2
Various substrates
Si
hBN (< 10nm)
WSe2/ MoSe2
hBN (10-30 nm)
Si/SiO2
Dielectrics renormalize energies
Hydrophobic surfaces needed for good contact
Notes: Picture of Sven, larger labels, add strain analysis

## Slide 44: Device - GatED hBN/MoSe2/hBN
Gr
hBN (< 10nm)
WSe2/ MoSe2
hBN (10-30 nm)
Gr (~10 nm)
Si/SiO2
Vg
Laser
power
hBN
Gr
Gr
ML MoSe2
20 mm
Gate voltage (V)
X-
X+
X0
1.550 1.575 1.660 1.625 1.650 1.675
4.0
2.0
0.0
-2.0
-4.0
Energy (eV)
Min
Max
Notes: Picture of Sven, larger labels, add strain analysis

## Slide 45
Gate voltage (V)
X-
X+
X0
1.550 1.575 1.660 1.625 1.650 1.675
4.0
2.0
0.0
-2.0
-4.0
Energy (eV)
Min
Max
Device - GatED hBN/MoSe2/hBN
hBN
Gr
Gr
ML MoSe2
Notes: Assuming epsilon=3.76 I V=2V, m =0.5 , the potential fluctuations would be 7.6 meV
https://www.nature.com/articles/s41699-018-0050-x

## Slide 46: Gated hBN/WSe2/hBN ML
1.60 1.62 1.64 1.66 1.68 1.70 1.72 1.74
2.0
1.5
1.0
0.5
0.0
-0.5
-1.0
Gate voltage (V)
Energy (eV)
X-
X
X
XX
XD
X+/-
XD+/-
Neutral excitons
Negative trions
X-
XD-
XX-
Phonon assisted trion formation:
Ex – Ex- = 30 - 36 meV
EA’ = 32 meV
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between then of 1.6nm.

## Slide 47: Gated hBN/WSe2/hBN ML
Energy (eV)
2.0
1.5
1.0
0.5
0.0
-0.5
-1.0
Gate voltage (V)
1.60 1.62 1.64 1.66 1.68 1.70 1.72 1.74
X-
X+
X
Positive trions
X
XD
X+/-
XD+/-
XD+
X
X
Phonon blockade of trion formation:
Ex – Ex- = 21 meV
EA’ = 32 meV
Notes: I need bright positive trion
10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 48: Excitons in p-doped hBN/WSe2/hBN ML
1.0
0.5
0.0
-0.5
-1.0
Gate voltage (V)
1.60 1.62 1.64 1.66 1.68 1.70 1.72 1.74
Energy (eV)
X-
X+
X
Xd+
X
X+
Xd+
S.Borghardt et al. arXiv:1911.01092
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 49: Qualitative rate equation For P-doped WSe2
X
X+
Xd+
Xd
CONSTANT RATES
S.Borghardt et al. arXiv:1911.01092
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 50: Sources of localisation
2.0
1.5
1.0
0.5
0.0
-0.5
-1.0
Gate voltage (V)
1.60 1.62 1.64 1.66 1.68 1.70 1.72 1.74
Energy (eV)
X-
X+
X
Sources of localization:
Acceptors
External charge fluctuations
Dielectric constant fluctuations
x30
1.52 1.54 1.56
WSe2/ MoSe2
hBN
Si/SiO2
e
e
S.Borghardt et al. arXiv:1911.01092
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 51: Gated WSe2 ML – linewidth
Gate voltage (V)
X
X+
Exciton – boson like – Gaussian broadening
Trion – fermion – Lorenzian line
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 52
5 Å
HAADF
S
Se
S/Se
10eV, 1019 m-2, no annealing
Se incorporation 1~3%.
Extended defects visible – STEM induced?
Vacancies – small contrast
Single S vacancies: 9%
Double S vacancies: 1.4%
qMo-Se = 43.1o
HAADF
2.0 2.5 3.0 3.5
Energy (eV)
150
100
50
0
EELS counts (a.u.)
Optical properties by EELS
U. Bangert et al., Ultramicroscopy 176, 31 (2017)
STEM-EDX of Se implanted MoS2
Notes: We know the contrast difference in STEM HAADF images is not enough to say we have Se implantation. Therefore, here we analyse x-ray signal in the STEM image map. We focus on the area which contains one brighter dot. Then we detect the x ray signal from the image map. The S signal map shows a hole or a vacancy in the map and the map of Se signal reveals a dot like image. As we overlap this two maps together, we observe a perfect match between the two images and also consistent with the HAADF image. Therefore, we are able to estimate the amount incorporation rate is about 1-3 % by accounting those brighter dots in the STEM images. We also try to estimate the S vacancies which leads to be 9% for single S vacancies and 1.4% for double vacancies. The number of double S vacancies much higher then our expectation, since the energy of ion is not enough to create double S vacancies in one impact. The possibility to have double impacts on same site is only about 0.6-0.7%.
On the other hand, the STEM images only show the Se atom is located at the position which suppose to be S atom in MoS2 lattice. I do not understand what you say in the last sentence. The incorporation rate is much lower than our expectoration and calculation. In this case, EM is design to study things within few atoms to thousands of atoms. To give more insight of this alloy structure in bigger picture, we have to use Raman and PL spectroscopy studies. In addition we need to consider ML implantation with MLs supported on substrates.

## Slide 53: Gated WSe2 ML – linewidth
X
X+
PRB 67, 241307(R) 2003
Notes: 10nm hBN would give 2*10^16 m^-2 carriers, which gives a separation between them of 1.6nm.

## Slide 54: POLARIZATION oF Dark STATES
z-polarized light
Gr
WSe2/ MoSe2
SiO2
Vg
p-Si
Excitation
Measured signal
3 mm
S.Borghardt et al. arXiv:2001.08043

## Slide 55: monolayer OF WSe2
Robust valley coherence only in the absence of charge carriers.
Spin-photon polarization entanglement would need to overcome:
  Electron spin – fine structure splitting.
  Exciton scattering into dark state in the presence of disorder.
Polaronic effects need further study.
Better devices needed for quantum correlations and classical correlations.

## Slide 56: Gated WSe2 ML – linewidth (extended voltage range)
20 mm

## Slide 57: Doping of monolayer TMDs
Homojunction devices
Localisation of excitons
Methods:
  Implantation
  Diffusion
  Electrostatic

## Slide 58: Low energy ion implantation Se into MoS2
Si
SiO2
Metal contact
TMDs
Se+
Se+
Se+
Se+
Monte Carlo simulations predict 70% retention rate.
Isoelectronic with S, forms alloys.
Chemically stable.
Alloys available: good reference point.
Samples: PDMS stamp, CVD.
Potential for electrostatic gating.
Se80+ implantation:
ESe= 10 - 25 eV
Dose = 1 - 20 x 1018 m-2
0.1 - 1Se atom per S atom in MoS2 ML
EVs = 5.9 eV -> min Ese = 7.2 eV
EVMo = 13.4 eV -> min ESe = 13.6 eV
C.Ataca & S. Ciraci, J. Phys. Chem. C, 115, 13303 (2011)
2/10/2020
Notes: We start our studies from Se ion implantation on MoS2 ML instead of other interesting dopants such Nb and Br which predicted by theory calculations. Monte Carlo simulations predict 70% of retention rate at 10eV ion energy so we should be able to create an alloy. Since MoSSe alloys can be synthesized directly, we have good reference point to compare the implanted MLs to. Furthermore, the alloy based lateral heterostructure is still highly desirable for study.In addition, Se will not have dangling bonds and thus the mterials is chemically stable.
We chose ion energy low enough to replace S atom with Se ion in a single impact. If we treat all the collision as elastic and assume that Se ion impacts on the surface is at normal to the ML surface, then to create a S vacancy in MoS2 ML one needs 5.9 eV. 13.4 eV is needed to create Mo vacancy. Se ion is able to deliver this energy if it has 7.2 eV and 13.6eV respectively. Since not all ion impact at normal to the surface, we chose ion energy from 10-20 eV and the dose is in the same order magnitude as S density in MoS2 ML.

## Slide 59: Low energy ion implantation Se into MoS2
Si
SiO2
Metal / graphene
contact
TMDs
Se+
Se+
Se+
Se+
Monte Carlo simulations predict 70% retention rate.
Isoelectronic with S, forms alloys.
Chemically stable.
Alloys available: good reference point.
Se80+ implantation:
ESe= 10 - 25 eV
Dose = 1 - 20 x 1018 m-2
0.1 - 1Se atom per S atom in MoS2 ML
EVs = 5.9 eV -> min Ese = 7.2 eV
EVMo = 13.4 eV -> min ESe = 13.6 eV
Requirements:
Clean surface
Grounding
C.Ataca & S. Ciraci, J. Phys. Chem. C, 115, 13303 (2011)
10/02/2020
Notes: We start our studies from Se ion implantation on MoS2 ML instead of other interesting dopants such Nb and Br which predicted by theory calculations. Monte Carlo simulations predict 70% of retention rate at 10eV ion energy so we should be able to create an alloy. Since MoSSe alloys can be synthesized directly, we have good reference point to compare the implanted MLs to. Furthermore, the alloy based lateral heterostructure is still highly desirable for study.In addition, Se will not have dangling bonds and thus the mterials is chemically stable.
We chose ion energy low enough to replace S atom with Se ion in a single impact. If we treat all the collision as elastic and assume that Se ion impacts on the surface is at normal to the ML surface, then to create a S vacancy in MoS2 ML one needs 5.9 eV. 13.4 eV is needed to create Mo vacancy. Se ion is able to deliver this energy if it has 7.2 eV and 13.6eV respectively. Since not all ion impact at normal to the surface, we chose ion energy from 10-20 eV and the dose is in the same order magnitude as S density in MoS2 ML.

## Slide 60
Optical spectroscopy of Se implanted MoS2
Eion= 20eV, Fluence = 1 x 1018 m-2, Implanted and annealed at 220oC
Eion= 20eV, Fluence = 5 x 1018 m-2, Annealed at 280oC
Annealing : a key to high quality
PL still broadened
Alloy effect? Disorder?
Notes: https://onlinelibrary.wiley.com/doi/epdf/10.1002/adma.201304389
We know the contrast difference in STEM HAADF images is not enough to say we have Se implantation. Therefore, here we analyse x-ray signal in the STEM image map. We focus on the area which contains one brighter dot. Then we detect the x ray signal from the image map. The S signal map shows a hole or a vacancy in the map and the map of Se signal reveals a dot like image. As we overlap this two maps together, we observe a perfect match between the two images and also consistent with the HAADF image. Therefore, we are able to estimate the amount incorporation rate is about 1-3 % by accounting those brighter dots in the STEM images. We also try to estimate the S vacancies which leads to be 9% for single S vacancies and 1.4% for double vacancies. The number of double S vacancies much higher then our expectation, since the energy of ion is not enough to create double S vacancies in one impact. The possibility to have double impacts on same site is only about 0.6-0.7%.
On the other hand, the STEM images only show the Se atom is located at the position which suppose to be S atom in MoS2 lattice. I do not understand what you say in the last sentence. The incorporation rate is much lower than our expectoration and calculation. In this case, EM is design to study things within few atoms to thousands of atoms. To give more insight of this alloy structure in bigger picture, we have to use Raman and PL spectroscopy studies. In addition we need to consider ML implantation with MLs supported on substrates.

## Slide 61: LocAlISATION BY DOPING
Maintains trigonal symmetry
Shallow dopant (A0X, D0X)
Could work for WSe2 and MoSe2
DOS [a.u.] @ P
P in MoSe2 monolayer - relaxed
2.0
0.0
-2.0
Energy (eV)
G
M
K
G
spin up
spin down
-2.0
0.0
2.0
Energy (eV)
G
M
K
G
Cr in MoS2 monolayer - relaxed
3% Se in MoS2 lattice
2
1
0
-1
-2
qMo-Se = 43.1o

## Slide 62: Power dependence

## Slide 63: ADONIS* beam line
  *Anlage zur Deposition
  niederenergetischer Ionen auf Substrate
  (apparatus for the deposition
  of low energy ions on a substrate)