## Slide 2: High-temperature superconducting undulators for compact free electron lasers, CLIC and FCC-ee
Sebastian C. Richter1,2 (PhD candidate)
supervised by Amalia Ballarino1, Daniel Schörling1, Axel Bernhard2 and Anke-Susanne Müller2.
1
2
*
**
This work is supported by:
* The Wolfgang Gentner Programme of the German Federal Ministry of Education and Research (grant no. 05E15CHA),
** The DFG-funded Doctoral School „Karlsruhe School of Elementary and Astroparticle Physics: Science and Technology“.
MSC group seminar
30 June 2022
TE-MSC-SCD
-MDT
-SMT

## Slide 3: Contents
Background and Motivation
About the Project
Simulations of Superconducting Undulators
Experimental Work
  REBCO Tape Bending Experiment
  Vertical Racetrack Undulator
  Helical Undulator
Conclusion and Outlook

## Slide 4: Background: free electron laser
* Schmüser, Dohlus, Rossbach; Ultraviolet and Soft X-Ray Free Electron Lasers, Springer (2008).
(a) Laser
(b) Free electron laser
*
The plane undulator
Undulator
gap

## Slide 5: Background: use case
Employing high-temperature superconductors (HTS) to undulators for the next generation of compact, highly brilliant light sources:
  Potential enhancement of undulator parameters, e.g. B amplitude for given undulator period length (λu)
  Relaxed cryogenic requirements (lower costs), larger margins, compared to LTS, like Nb-Ti or Nb3Sn
Link to CompactLight:
    Hard X-ray FEL (≤ 1 nm),
    Short period undulators (< 20 mm, 1 ≤ K ≤ 3),
    Lower electron beam energy.
A. Mak, P. Salen, V. Goryashko, Undulator Considerations in the Baseline Design of the MAX IV Soft X-Ray Laser, FREIA Report Series 2018 (http://uu.diva-portal.org)

## Slide 6: Background: damping undulator/wiggler
Definition undulator vs. wiggler: K parameter and radiation spectrum
  Kundulator ≲ 1 and Kwiggler >> 1
Energy loss via synchrotron radiation by additional dipole fields.
Wiggler in straight section of a ring:
∫ B ds = 0
* P. Peiffer, “The Status of the Damping Wiggler Project for the CLIC Damping Rings”, The 16th Pan-American Synchrotron Radiation Instrumentation Conference, Chicago (2010).
*
** D. Schoerling et al., “Design and system integration of the superconducting wiggler magnets for the Compact Linear Collider damping rings”, Phys. Rev. ST Accel. Beams (2012).
Link to CLIC and FCC-ee:
    High wiggler B-fields (> 2 T),
    rather long period lengths (> 40 mm).
    K ~ 15 to 20 **

## Slide 7: Background: superconductors
High-Temperature Superconductor (HTS) | 
Here: REBCO (rare-earth barium copper oxide) Tc ≈ 92 K Bc2⊥ ≈ 110 T, Bc2‖ > 240 T tape | 
BꞱ | B∥
Low-Temperature Superconductor (LTS)
State-of-the-art: Nb-Ti (niobium-titanium) Tc ≈ 10 K Bc2 ≈ 14.5 T strand cable
B to strand/cable orientation is not relevant. Critical current is given by:
B or
J
J
* https://lhc-machine-outreach.web.cern.ch/lhc-machine-outreach/components/cable.htm
** J. van Nugteren, High Temperature Superconductor Accelerator Magnets, PhD (2016)
*
**
B  or

More on critical current densities: https://fs.magnet.fsu.edu/~lee/plot/plot.htm

## Slide 8: Motivation
Example: 2D model simulation 15 mm period , 6 mm gap (at 4.2 K)
Potential:
  magnetic field amplitudes B ~ 2 T for periods ~15 mm may be feasible.
Material | Joperation (A/) | Bconductor (T) | Baxis (T)
Nb-Ti | 1076 | 2.8 | 1.3
REBCO all Ʇ | 1530 | 3.0 | 1.7
REBCO all ∥ | 3450 | 6.6 | 3.1
Material |  | Bconductor (T) | Baxis (T)
Nb-Ti | 1076 | 2.8 | 1.3
REBCO all Ʇ | 1530 | 3.0 | 1.7
REBCO all ∥ | 3450 | 6.6 | 3.1
  Reality in between…
  Hard X-ray FEL (λ ≤ 1 nm)
  REBCO data from 2018

## Slide 9: About the project
3 prototype coils:
  Vertical racetrack (VR),
  Horizontal racetrack (HR),
  Helical undulator around the beam pipe (hel.).
Bending radii < 5 mm needed further investigation…
VR
HR
hel.
Beam
2D
gap

## Slide 10: Undulator parameter and ranges
Parameter | Description | Range of interest
Targets |  | 
E | Electron energy | 3 to 8 GeV
 | Radiation wavelength | hard X-ray (≤ 1 nm)
K | Undulator strength parameter: | (1 ≤ K ≤ 3)
Design |  | 
 | Undulator period | 13 mm
g | Gap between magnetic poles | ≤ 6 mm
B | Magnetic field (amplitude) on beam axis | to be maximized
Limits |  | 
Jc | Critical current density in the conductor | 
Bconductor | Magnetic flux density at the conductor | 
Parameter | Description | Range of interest
Targets |  | 
E | Electron energy | 3 to 8 GeV
 |  | hard X-ray (≤ 1 nm)
K |  | (1 ≤ K ≤ 3)
Design |  | 
 | Undulator period | 13 mm
g | Gap between magnetic poles | ≤ 6 mm
B | Magnetic field (amplitude) on beam axis | to be maximized
Limits |  | 
Jc | Critical current density in the conductor | 
Bconductor | Magnetic flux density at the conductor | 

## Slide 11: Simulations of superconducting undulators
Example: HR coil, 13 mm period, 6 mm gap (at 4.2 K)
Adapted from Peter J. Lee
http://fs.magnet.fsu.edu/~lee/plot/plot.htm
Chart: Magnetic Field (T)
| 5 | 10 | 15 | 20
YBCO: B ∥ Tape plane | 4599.7996 | 4264.246 | 3416.6751 | 3085.9004
YBCO: B ⊥ Tape plane | 3664.9998 | 2919.9995 | 2379.9996 | 1796.1537 | 1447.6924 | 1188.462 | 1034.3652 | 956.923 | 851.8301 | 780.8449 | 719.9995 | 679.4359 | 626.087 | 593.2388 | 563.4783 | 535.3843 | 516.5215 | 469.5647 | 433.0766 | 406.956 | 391.3041 | 367.6926 | 360.0003 | 344.3473 | 328.6954 | 322.3077
Nb-Ti | 3319.48 | 2635.2 | 2067.39 | 1761.65 | 1441.35 | 1121.05 | 917.223 | 771.63 | 596.923 | 446.75 | 291.5 | 226.25 | 167.5 | 111.667 | 60
Loadline B Ʇ | 1000 | 1500 | 1900
Loadline B ∥ | 1000 | 1500 | 4300

## Slide 12: Simulations of superconducting undulators
x (mm)
HR, 13 mm period, 6 mm gap (at 4.2 K)
3 T
1.5 kA/, Bconductor
-3 T
4 mm
iron
vacuum
Beam axis
tape
0 T
2D parameter space investigations
B
B

## Slide 13: Simulations of superconducting undulators
x (mm)
0 T
Bmax
3D
→ later more specific…

## Slide 14
coil at 4.2 K | Horizontal racetrack (3D, with iron poles) | Vertical racetrack (3D, with iron poles) | Helical undulator (3D, without iron poles)
undulator period | 13 mm |  | 
gap size g | 6 mm |  | 
Bmax on axis | 2.2 T | 1.7 T | 2.3 T
operating Jc | 2.6 kA/mm2 | 2.3 kA/mm2 | 2.3 kA/mm2
B⊥max at conductor | 5.6 T | 5.6 T | 5.6 T
coil at 4.2 K | Horizontal racetrack (3D, with iron poles) | Vertical racetrack (3D, with iron poles) | Helical undulator (3D, without iron poles)
 | 13 mm |  | 
gap size g | 6 mm |  | 
Bmax on axis | 2.2 T | 1.7 T | 2.3 T
operating Jc | 2.6 kA/mm2 | 2.3 kA/mm2 | 2.3 kA/mm2
B⊥max at conductor | 5.6 T | 5.6 T | 5.6 T
Simulated undulator coil parameters (3D)

## Slide 15: Contents
Background and Motivation
About the Project
Simulations of Superconducting Undulators
Experimental work
  REBCO Tape Bending Experiment
  Vertical Racetrack Undulator
  Helical Undulator
Conclusion and Outlook

## Slide 16: REBCO tape bending experiments
Are bending radii < 5 mm even feasible?!
Bending experiment @KIT
  Bending radii R = {10, 8, 6, 5, 4, 3, 2.5, 2, 1.25, 0.75} mm,
  Optional: half helix twist,
  Bending in RT, then LN2 cool-down.
Cross-check: Helical bending @CERN
  Same procedure and
  Same radii as above.
  Different winding bodies.
S. C. Richter et al., “Bending Radius Limits of Different Coated REBCO Conductor Tapes - An Experimental Investigation with Regard to HTS Undulators”, IPAC 2021.
CERN setup KIT setup

## Slide 17: REBCO tape bending experiment: results
50 μm substrate
60 μm, 30 μm, 25 μm substrate
Besides SSTC ST1911-78 all samples showed no or reversible degradation down to R = 5 mm.
SSTC tape behaved significantly different for different widths.
The thinnest substrate conductors (30 μm and 25 μm) reached the smallest Rmin = 2 mm.
S. C. Richter et al., “Bending Radius Limits of Different Coated REBCO Conductor Tapes - An Experimental Investigation with Regard to HTS Undulators”, IPAC 2021.

## Slide 18: (HR and) VR undulator coil
HR design on hold:
Bending radius (1.25 mm) is too tight.
First VR dummy coils with copper tape
    fully soldered and dry wound,
    investigation of solder paste quality  improved by vertical winding.
75 mm
75 mm

## Slide 19: VR undulator coil: design
Two non-insulated (NI) sub-coils with opposite current direction and separated by insulator.
Innermost turns of both sub-coils are soldered along the curved side (D-shape) to a 10 mm wide coated REBCO tape that connects them electrically.
Magnet current flow: sub-coil 1, spiral to its center, bridge to the innermost turn of sub-coil 2, spiral out.
S. C. Richter et al., “Progress on HTS undulator prototype coils for compact FEL designs”, in IEEE Trans. on Appl. Supercond., 2021.

## Slide 20: VR undulator coil: 3D modelling
The Jc(B,T,Ʇ) surface of REBCO superconductors was based on fits.
The critical current density Jc was defined by considering the worst case scenario: the maximum magnetic field on the conductor Bcond perpendicular to the tape plane,
  At 4.2 K: maximum B = 99.95% Bcond .
Je(4.2 K) = 2071 A/mm2
Je(77 K) = 75 A/mm2
Opera 2020 Based on the Biot–Savart law
S. C. Richter et al., “Progress on HTS undulator prototype coils for compact FEL designs”, in IEEE Trans. on Appl. Supercond., 2021.

## Slide 21: VR undulator coil: manufacturing (I)
4 mm wide and
  100 µm thick Bruker HTS tape (VR coil #1 and #2),
  45 µm thick SuperPower tape (VR coil #3).
The first turn of each tape was fixed by a pin and soldered along the curved side to the c-tape,
  Sn62Pb36Ag2 solder paste @ 185 °C for 5 min.
Winding with controlled winding tension {30 N, 25 N}.
The last turn of each tape was soldered to its penultimate turn along the curved sides,
  97In3Ag solder paste @ 155 °C for 5 min.
S. C. Richter et al., “Progress on HTS undulator prototype coils for compact FEL designs”, in IEEE Trans. on Appl. Supercond., 2021.

## Slide 22: VR undulator coil: manufacturing (II)
A copper lead was pressed on the curved side of each sub-coil with a thin indium foil in between.
Six voltage taps (red points) and two temperature sensors:
  temperature sensors (PT1000) on the outermost turn of each sub-coil.
Indium foil
VR coil #1
VR coil #2, #3
current flow
S. C. Richter et al., “Progress on HTS undulator prototype coils for compact FEL designs”, in IEEE Trans. on Appl. Supercond., 2021.

## Slide 23: VR undulator coils: parameters for LN2
S. C. Richter et al., “Powering Test Results of HTS Undulator Coils at 77K for Compact FEL Designs”, IPAC’22
 | VR coil #1, #2 | VR coil #3
Undulator period λu | 13 mm | 
Sub-coil x-section | 4 mm  5 mm | 4 mm  4.6 mm
HTS conductor with dimensions | Bruker HTS 4 mm x 100 μm | SuperPower 4 mm x 45 μm
Number of turns | 51 | 102
Jec, sim (0.6 T, 77 K) | 75 A/mm2 | 222 A/mm2
Ic, sim (0.6 T, 77 K) | 30 A | 40 A
B0(Ic,sim,d=3.5mm) | 0.14 T | 0.28 T

## Slide 24: Determination of the experimental Ic criterion
VR coils powering tests:
V-I curve of single Bruker HTS tape for 1 μV/cm: Ic(77 K, 0.6 T) = 34.3 A.
  Outermost turn length of 30 cm x 1 μV/cm: 30 μV becomes the criterion.
  Ic ↔ U = 30 μV
Transfer to HTS undulator VR coils:
  30 μV / 15 m = 0.02 μV/cm
  30 μV / 30 m = 0.01 μV/cm

## Slide 25: VR undulator coils: experimental results LN2 I
Powering tests of VR coil #1, #2, and #3:
current ramping with 0.05 A/s and 0.5 A/s until a drift in voltage was measured.
charging: discharging: transversal current hotspot heating transversal current
S. C. Richter et al., “Powering Test Results of HTS Undulator Coils at 77K for Compact FEL Designs”, IPAC’22

## Slide 26: VR undulator coils: experimental results LN2 II
Effective time constant τ:
voltage over time while applying a step function current (plateau 10 A).
The voltage U can be described as: U = (ISC - IR) ∙ R + L ∙ dISC/dt .
For U→0 V: dISC/dt = (IR - ISC) ∙ R/L ⇒ I (t) = I ∙ e- t/τ .
Analog solution: U = a ∙ e-t/τ, with τ = L/R and a = constant.
Effective time constants could be measured:
 | VR coil #1 |  | VR coil #2 |  | VR coil #3 | 
τ | 26 s | 42 s | 32 s | 46 s | (4 s) | 90 s
S. C. Richter et al., “Powering Test Results of HTS Undulator Coils at 77K for Compact FEL Designs”, IPAC’22

## Slide 27: VR undulator coils: experimental results LN2 III
Current steps and overflow
Current steps of 2 A with a 300 s decay time up to 112 A (>> Ic (!)) ,
For I > 70 A all sub-coils showed a stable (transversal) resistance Rr.
Rr | 58 µΩ | 48 µΩ
Ic | 40 A | 30.5 A
Rr | 29 µΩ | 19 µΩ
Ic | 39 A | 35 A
Rr | 400 µΩ | 58 µΩ
Ic | 47 A | 41 A
S. C. Richter et al., “Powering Test Results of HTS Undulator Coils at 77K for Compact FEL Designs”, IPAC’22

## Slide 28: VR undulator coils: LHe setup @ KIT
Powering tests of VR coil #2 and #3 at 4.2 K:
Current leads: up to 1500 A
Quench protection: 1 mV (later 4 mV)
DAQ time: 10 Hz

## Slide 29: VR undulator coils: experimental results LHe I
Powering tests of VR coil #2 and #3 at 4.2 K:
current ramping with 0.25 A/s until a drift in voltage was measured.
S. C. Richter et al., “Powering test results of HTS undulator prototype coils for compact FELs at 4.2 K”, to be presented at ASC 2022.

## Slide 30: VR undulator coils: experimental results LHe II
Effective time constant τ:
voltage over time while applying a step function current (plateau 200 A).
Effective time constants could be measured:
 | VR coil #2 |  | VR coil #3 | 
τ | 74 s | 88 s | (5 s) | 121 s
30-June-22
S. C. Richter et al., “Powering test results of HTS undulator prototype coils for compact FELs at 4.2 K”, to be presented at ASC 2022.

## Slide 31: VR undulator coils: experimental results LHe III
Ic | 930 A | 930 A
Ic | 520 A | 400 A
 ~2.3 kA/mm2
 ~2.3 kA/mm2
Current steps and overflow
Current steps of 20 A or 40 A with a 300 s decay time up to U runaway,
30-June-22
S. C. Richter et al., “Powering test results of HTS undulator prototype coils for compact FELs at 4.2 K”, to be presented at ASC 2022.

## Slide 32: Helical undulator design
Why a helical undulator? → More compact and efficient.
Helical undulator coil with period u= 13 mm,
  4 mm wide coated REBCO tape superconductor,
  Bifilar helix, dry-wound, non-insulated (NI) design,
  Gap ≥ 5 mm, w.r.t. the tapes min. bending radius,
  REBCO always under compression (facing the gap).
Tape fan endings due to different winding angles: α < β, with a constant undulator period/pitch → non-quadratic cross-section.
Very first helical undulator with superconducting tapes → novel winding scheme.
S. C. Richter et al., “Status of a Prototype HTS Helical Undulator Coil for Compact FELs”, IPAC’22

## Slide 33: Helical undulator simulations
Electromagnetic simulations: Opera 2020,
  Worst case B ⊥ tape with Jc(B,T,⊥) fits.
Mechanical simulations: Opera 2020 + ANSYS 2020,
  Lorentz forces + thermal shrinking.
Lorentz forces on the superconducting tape stacks (J = 2 kA/mm2) are counterbalanced and controllable.
Cross-section in the y-z plane of the superconducting tape stacks with By displayed (J = 2 kA/mm2) as color map. Scale in mm.
Y
Z
4.3
By (T)
4.0 3.0 2.0 1.0 0.0 -1.0 -2.0 -3.0 -4.1
S. C. Richter et al., “Status of a Prototype HTS Helical Undulator Coil for Compact FELs”, IPAC’22

## Slide 34: Helical undulator winding
Creation of a winding body for helical tape design including coil ends
Multiple test winding on 3D printed formers,
  0.1 mm thick stainless steel and copper tape.
150 mm
4.2 mm
0.1 mm
S. C. Richter et al., “Status of a Prototype HTS Helical Undulator Coil for Compact FELs”, IPAC’22

## Slide 35: Conclusion & Outlook
The technical potential of HTS for undulators has been demonstrated.
3 VR prototype coils manufactured and successfully tested in LN2/LHe.
  Stable up to Ic and well beyond the design current without any degradation.
  Reasonable time constants maybe suitable for tunable undulators.
Next steps: | Future goals:
Finalize technical design and drawing for a helical undulator. Manufacture the world's first helical undulator from ReBCO tape. | Field quality, Mechanical margins, Beam tracking.
Many thanks to C. Fernandes, J. Mazet, F. Garnier, T. H. Nes, F.-O. Pincot, P.-A. Contat, N. Bourcey, S. Clement, P. Martin Vazquez, P. Rizzo, J. C. Perez, H. Felice, G. de Rijk, D. Standen, G. Lenoir, P. Koziol, C. Barth, G. Succi, F. Pillon, R. Betemps, G. Kirby, A. Grau, D. Saez de Jauregui, N. Glamann, B. Krasch, J. Gethmann, K. Damminsek, … and all other colleagues following and supporting this work!
Thanks for your attention!

## Slide 37: Background: free electron laser
Energy transfer between particle and light: ,
  Continuous: Fixed phase relation between electron motion and field oscillation.
Modulation of particle energy and drift velocity:
  “Microbunching”,
  All particles radiate coherently.
Radiation wavelength: ,
  Undulator parameter .
Schmüser, Dohlus, Rossbach; Ultraviolet and Soft X-Ray Free Electron Lasers, Springer (2008)
saturation length
E = 245 MeV
FEL
z
Back-up

## Slide 38: Simulations of superconducting undulators
Example: 13 mm period short models, 5 periods, 6 mm gap (at 4.2 K)
Back-up

## Slide 39: Simulated undulator coil parameters (3D)
coil at 4.2 K | Horizontal racetrack (3D, with iron poles) | Vertical racetrack (3D, with iron poles) | Helical undulator (3D, without iron poles)
undulator period | 13 mm |  | 
gap size g | 6 mm |  | 
Bmax on axis | 2.2 T | 1.7 T | 2.3 T
operating Jc | 2.6 kA/mm2 | 2.3 kA/mm2 | 2.3 kA/mm2
B⊥max at conductor (Bmax mod) | 5.6 T (7.4 T) | 5.6 T (5.8 T) | 5.6 T (6.4 T)
coil at 4.2 K | Horizontal racetrack (3D, with iron poles) | Vertical racetrack (3D, with iron poles) | Helical undulator (3D, without iron poles)
 | 13 mm |  | 
gap size g | 6 mm |  | 
Bmax on axis | 2.2 T | 1.7 T | 2.3 T
operating Jc | 2.6 kA/mm2 | 2.3 kA/mm2 | 2.3 kA/mm2
B⊥max at conductor (Bmax mod) | 5.6 T (7.4 T) | 5.6 T (5.8 T) | 5.6 T (6.4 T)
Back-up

## Slide 40: VR coil #3 – investigation in raw data
Chart: 
Voltage (V)
Chart: 
Time (s)
Back-up

## Slide 41: HTS undulator - flowchart
Horizontal Undulator, Test coil
Vertical Undulator, Test coil
Helical Undulator, Test coil(s)
Coil 1-#n
Coil 1-#n
Coil 1-#n
Wiggler/undulator, short model (0.1 m)
Wiggler/undulator, long model (0.5 m)
2023
2028
Small coil program
Back-up