## Slide 1: Effect of transverse compressive stress on Nb3Sn Rutherford cables for accelerator magnets
Gilles Lenoir, Kirtana Puthran, Christian Barth, Felix Wolf, Jérôme Fleiter and Amalia Ballarino
TE-MSC-SCD
MSC seminar - 23/06/2022

## Slide 2: Outline
Context, motivation & some literature
Objectives, methodology and specimen
Transverse compressive stress and loadings scenarios
Transport measurements using FRESCA test station
Damage state Metallographic observation and post-mortem analysis
Discussion and conclusion
Perspectives & on-going work

## Slide 3: Context and motivation
Need for higher-field accelerator magnets for HL-LHC and beyond
  Manage mechanical limits as moving to higher fields
  Nb3Sn conductors to exceed Nb-Ti based technologies High Jc LTS RRP 108 /127 ( ~ 2.5 kA/mm2 @ 12 T, 4.2 K) HL-LHC 11T (ø0.7 mm) and MQXF (ø0.85 mm)
   Brittle and strain sensitive material
 Impact of loading and understanding of mechanical mechanism in the conductor
11T schematic cross-section.
© P. Ferracin, IEEE TAS, 2019.
11T conductor block cross-section.
© C. Scheuerlein, IOP SUST, 2019.
RRP 108/127 ø0.7mm from double-stack Rutherford cables.
Courtesy of E. Rochepault based on the ASC plot.
X-ray tomography of double stack [Wolf 18]
Courtesy of A. Ballarino

## Slide 4: Context and motivation
Mechanical sensitivity of the Nb3Sn
  Characterization at cold from [Ekin 87] to [Troitino 21]
    axial strain
    transverse pressure
  Reversible and irreversible critical current degradation from
    Deformation of the copper matrix
    Cracks in Nb3Sn sub-elements
Pre-compressive load applied during manufacturing of magnet to sustain Lorentz forces and prevent movement  For 11 T magnets, global limitation of peak stress during collaring to 150 MPa [Ferracin 19] (not last value)
Relative critical current with applied transverse stress measured using a compressive WASP device [Troitino 2021]
 Effect of pressure applied at Room Temperature (RT) on HL-LHC conductors
19 T, 4.2 K

## Slide 5: A brief glance in literature – Strand scale
  [Ebermann 2019] - Transverse stress applied on strands
    RRP 144/169 ø0.7mm
    Transverse stress applied at RT (hydraulic press in building180)
    Electrical measurements (@ cryolab), metallography (@ EN-MME-MM) and FEM analysis
    Electrical degradation and cracks after 100 MPa
    Cracks in longitudinal CS @ 100 MPa: longitudinal direction
    @ 150 MPa: longitudinal cracks propagating to the surface of the sub-elements
Critical current Ic at T=16.6 K using Ec=100μV/m
SEM micrographs of transverse cross-section of a),b) ref. sample, c),d) 75 MPa, e),f) 100 MPa, g),h) 125 MPa, i),j) 150 MPa and k),l) 200 MPa.
SEM micrographs of longitudinal cross-section of a) to d) 75 MPa, e) to h) 100 MPa, i) to l) 150 MPa.

## Slide 6: A brief glance in literature – Cable scale
  [Ebermann 2018] + PhD thesis (CERN / TU Vienna)
    Electrical measurements in FRESCA after application of transverse stress at RT
    Specimen
      Double-stack configuration
      3 different types of cable
    Metallographic analyses
      Specimen 1 – 11T RRP 144/169 (no mica)
Inverted
Not inverted
Inverted
150MPa 175MPa 200MPa
Transverse optical micrographs
SEM micrographs @200 MPa
  No degradation measured or observed at 150MPa
  Degradation after 175 MPa but not enough material to conclude clearly
  Mainly longitudinal cracks observedshrinkage of supercond. area and not interruption
   Cable H15OC0190 with RRP 144/169 ø0.7 mm
   Limited data in interesting interval 150-175-200 MPa

## Slide 7: A brief glance in literature – Coil scale
  [Balachandran 2021] – Metallographic analyses of 11T dipole coils
    SMC #109 (cable 220B “small gap” RRP 108/127 ø0.7mm)
      Critical current limitation
      Cracks
    10-stack (SMC #105 cable 196A RRP 144/169 & 150/169)
      Loaded transversally at 210 MPa
      Cracks
  Difficult to understand and compare
  Limited conclusions given cost and time
   For the coil, crack distribution and varying orientation indicate multi-axial stress state
  For the 10-stack, cracks oriented along principal planes and principal direction
Transverse cross-section
Top longi. cross-section
Side longi. cross-section

## Slide 8: Objectives and methodology
Data for a few and different architectures
Investigate the correlation between Ic degradation and damage phenomena
  Stress levels for which damage can be observed
  Correlation between Ic degradation and cracks
Evaluate possible extrapolation between scales
Objective
  Data of recent cable configuration
  Investigate the impact of monotonic / cumulated loading
  Develop and propose procedure to study elementary loadings w/ statistical & systematic study of damage
    Ic measurements
    Damage phenomena
      Crack initiation / damage in epoxy / etc.
      Spatial cracks distribution & pattern
Main steps
  Transport measurements under magnetic field of a double-stack specimen after application of pressure at RT
  Metallographic analysis of samples transversally loaded and comparison of damage state and transport measurements
Ic-σtrans for Cable H15OC0190 with RRP 144/169 [Ebermann 19]
Architecture
Ic degradation
Mech. behavior
Design & operating limits

## Slide 9: 11T cable specimen
Strand and cable configuration
  RRP 108/127 ø0.7 mm
  “Small mica gap”
  Keystoned cable
Double-stack configuration
  Preparation
    S2-glass fiber and mica insulation of the bare cable
    Heat treatment
    Vacuum impregnation in epoxy CTD-101K
  Possible configurations
    Inverted – Compensate the keystone
    Non-inverted – Doesn’t compensate the keystone

## Slide 10: Investigated specimens
Specimen for transport measurement – “FRESCA specimen”
  1.8 m long double-stack cable with Vtaps and splices
  Area transversally compressed in high field region always the same
Metallographic samples cut from FRESCA specimen after transport measurements
  Cut with a diamond wire saw
  Samples
    Loaded area of the FRESCA specimen
    Reference samples checked for absence of damage
    60 mm long samples for microscopy to which transverse compressive stress was applied separately after the transport measurements
Schematic layout of the long FRESCA specimen
3
3
Ref. samples
Ref. samples
Loaded area
1
1
2
2
2
2
1
1
2
3

## Slide 11: Transverse stress and loading cases
Transverse pressure
  Applied using hydraulic press at building 180 at CERN developed by F. Wolf and P. Ebermann [Wolf 18] [Ebermann 18]
  Boundary conditions: no constraints on the sides of the specimen
  Evaluation of stress distribution
    Stress from Prescale ﬁlm measurements was within 12.5% from the stress from calibrated load cells [Wolf 18]
    From Prescale film, pressure is lower at the side of the cable  recent analyses showed this depend on the specimen
  Stress case name come from the averaged pressure applied
Loading scenarios
  Transport measurments
    1/ Measurement at virgin state
    2/ Warm up & application of pressure @ RT
    3/ Cool down & measurement in FRESCA
    4/ After the 190 MPa step, specimen loaded to 20 cycles at 190 MPa and measured in FRESCA
  Metallographic analyses
    Selected stress levels applied for transport measurements 140 MPa / 160 MPa / 170 MPA / 180 MPa
    Monotonic and cumulated loadings
Schematic side view of the setup to apply transverse load [Ebermann 18]
130 to 190 MPa w/ 10 MPa step
Increase homogeneity
Evaluate stress distrib.
t
σ [MPa]
130
140
150
0
130
Transport measurement in FRESCA
140
160
170
180
190
20 cycles
150
160
170
180
190 MPa
190 cycled
virgin
 cumulated loading
t
σ [MPa]
130
140
150
0
160
160 monotonic
160 cumulated

## Slide 12: Transport measurements in FRESCA [Verweij 99]
Specimen specification
  Vtap placed in high field region on the two cables
  Transverse pressure applied only on the central part w/o Vtaps
  Bapp // to width & ┴ to thickness of the stack
Experimental procedure for each stress level
  Training - ramped to quench @ (4.2 K, 9.6 T, 300 A/s)
  Measurements
    Decreasing field
    At each field, 8 current runs are performed
  Critical current Ic determined at 4.2 K with .
Schematic cross-section of the FRESCA sample holder [Ebermann 18].
Schematic layout of the long FRESCA specimen
U-I curve of two stress cases measured on each cable

## Slide 13: Transport measurements
Evolution of the relative critical current and n-value for the 2 cables at minimum and maximum applied field with applied stress at RT
  Until 140 MPa
    Ic is increasing due to initial strain state of Nb3Sn
    n is stable
  140 MPa to 160 MPa
    Ic is decreasing from max but still above virgin case
    n is stable
  170 MPa
    Small Ic decreases above/near virgin case
    n is decreasing
  180 MPa & 190 MPa: significant Ic decreases
    180 MPA: ̴2 % below virgin state, ̴6 % below max
    190 MPA: ̴6 % below virgin state, ̴8 % below max
    Reduction of n-value from 90 to < 50
for min and max Bapp
n-value for min and max Bapp

## Slide 14: Transport measurements
Evolution of the relative critical current and n-value for the 2 cables at minimum and maximum applied field with applied stress at RT
  Until 140 MPa
    Ic is increasing due to initial strain state of Nb3Sn
    n is stable
  140 MPa to 160 MPa
    Ic is decreasing from max but still above virgin case
    n is stable
  170 MPa
    Small Ic decreases above/near virgin case
    n is decreasing
  180 MPa & 190 MPa: significant Ic decreases
    180 MPA: ̴2 % below virgin state, ̴6 % below max
    190 MPA: ̴6 % below virgin state, ̴8 % below max
    Reduction of n-value from 90 to < 50
  20 cycles from 0 MPa to 190 MPa
    Strong Ic degradation: ̴16% from virgin case
    No clear evolution of n
for min and max Bapp
n-value for min and max Bapp

## Slide 15: Transport measurements
Field dependence of the critical current for different applied stress with min and max plots of the expected performances derived from single wire data
  Virgin: Ic just within expected range
  ≤170 MPa: within expectations
  180 MPa: min expected performance
  190 MPa: below expectations
  20 cycles at 190 MPa: severely degraded

## Slide 16: Transport measurements
Until 160 MPa Ic is increasing or stable
170 MPa Withing expectation with slight evolution of n
180 MPa & 190 MPa significant Ic decreases
20 cycles from 0 MPa to 190 MPa
for min and max Bapp
n-value for min and max Bapp

## Slide 17: Metallographic analysis - Investigated specimens
  Cut from FRESCA specimen after transport measurements
  Description of samples
    190 cycled - Loaded area of the transport measurement sample
    0 or Reference samples
      Used to validate the absence of damage from
        previous steps (handling, tests)
        Preparation (cutting, grinding, polishing)
      Ref. samples prepared together with analyzed samples to guarantee the preparation
    xxxC or xxxM - 60 mm long samples used to apply transverse stress and compared with transport measurements
       140C / 160M / 160C / 170M / 170C / 180M / 180C
Loading of the 190 Cycled
Exemple of loadings of the metallographic samples
1
2
3
Presented here

## Slide 18: Metallographic analysis – Preparation and analysis
Cutting of samples with diamond wire saw
 impact of cutting evaluated on ref. samples < 20 μm from cutting plane
Preparation of the sample
  Embedded in epoxy resin at cold
  Grinding and polishing with decreasing particle size (SiC papers and water-based diamond pastes)
  Vibro-polishing final step
Observation & Analysis
  Optical microscope for global analysis and small cracks using SEM
  Quantification of cracks on grey scaled stack pictures with color scheme assigned to cracked filaments
    yellow-1crack, orange-2, red-3 and dark red-4 & more
    Doesn’t represent the size of the crack! One yellow coded sub-element may have a 3 μm long crack or a 10 μm long one
Transverse cross-section
Top longi. cross-section
Grinding with P1200 paper
Polishing with 1 μm diamond solution
Vibro-polishing with 0.02 μm SiO2 susp.
Transverse cross-section w/ SEM 190 Cycled
Radial cracks in sub-elements
3 μm
10 μm
Side longi. cross-section

## Slide 19: Metallographic analysis – 190 Cycled
190 cycled heavily damaged
No cracks observed in strands located at the kink
Damaged concentrated in middle & thick side  From Prescale film, pressure is lower on the side of the cable  Thick side more impacted Non-inverted configuration
X-shape damage pattern in strands
    yellow-1crack orange-2 red-3 dark red-4&more

## Slide 20: Metallographic analysis – 190 Cycled
Radial crack
wavy crack
[Balachandran 21]

## Slide 21: Metallo. analysis – 190 Cycled Transverse CS
Large opened cracks
Apparent lower cracks density than [Ebermann 18]
SEM micrographies of the 200 MPa sample [Ebermann 18]
  Cable H15OC0190 with RRP 144/169
Radial crack

## Slide 22: Metallo. analysis – 190 Cycled Longitudinal CS
Side longitudinal – Strands located on the transition layer
wavy crack
Longi/straight crack
Transverse
crack

## Slide 23: Metallo. analysis – 190 Cycled Longitudinal CS
Top longitudinal – First layer of top cable

## Slide 24: Metallo. analysis – 190 Cycled Longitudinal CS
Top longitudinal – First layer of top cable

## Slide 25: Metallo. analysis – 190 Cycled Longitudinal CS
Top longitudinal – First layer of top cable
  [Eberman 18] –longi. cracks because transv. load  degradation due to shrinkage of supercond. area and not interruption
  [Jewell 08] – Ic degradative cracks are transverse
Longitudinal cracks on top longi. CS RRP strand [Ebermann 18]
Transverse cracks on longi. CS RRP strand [Jewell 08]
Longitudinal CS requires time and effort (& luck?) to obtain relevant information
Not adapted for first cracks / damage initiation studies

## Slide 26: Metallographic analysis – 160 Monotonic & Cumulated
160 MPa monotonic
160 MPa Cumulated
    yellow-1crack orange-2 red-3 dark red-4&more

## Slide 27: Metallographic analysis – 160 Monotonic & Cumulated
160 MPa Cumulated
160 MPa Monotonic
Example of cracks in a sub-element of the 160 monotonic sample

## Slide 28: Metallographic analysis – 160 Monotonic & Cumulated
Crack density is more important in the cumulated sample
Center of stack is mainly damaged
Damaged concentrated in middle & thick side  From Prescale film, pressure lower at the side  Non-inverted configuration
160 MPa Cumulated
160 MPa Monotonic
    yellow-1crack orange-2 red-3 dark red-4&more

## Slide 29: Metallographic analysis – 140 Cumulated
Presence of cracks at 140 MPa with a cumulated loading
Transport measurement at 140 MPa cumulated
  Ic max
  no evolution of n-value from virgin
140 MPa Cumulated
10μm

## Slide 30: Metallographic analysis - Outcomes
All samples show cracks, even the lowest one: 140 MPa Cumulated.
Density of cracks more important in cumulated loaded samples than monotonic one.
Damage in cables localized mainly in center, thin side less damaged than thick side.  Non-inverted configuration (can be confirmed with inverted configuration comparison)  From Prescale film, pressure lower at the side (sample dependent)
Cracks
  Initiated from
    Porosities (core & restack)
    Interfaces (Nb/Nb3Sn & core/Nb3Sn)
  Nb barrier & core never cracked
  Pattern of cracks in sub-element
    Cracks are localized in the 45° planes from loading direction.
    Damaged sub-elements orientation does not vary wrt. the rotation of the hexagon structure for high stress levels For low stress levels, hexagon structure and deformed shapes of sub-elements seems to play a role in the degradation
    Majority of the cracks oriented // to loading direction  Cracks ┴ to loading direction appear in severely damage sub-elements localized in zone C
    In strands with less damage (1 to 10 sub-elements affected) cracks localized in A,B & C. As cracks density , localized in C. Heavily damage strands, zone D is reached and multiple cracks

## Slide 31: Other investigation method
Etching of copper matrix
X-ray tomography – CT scan
  Non-destructive method
  Require high resolution to observe cracks
Ion beam abrasion So called Cross-section polisher
  Minimize damage surface
  Allow to look for small cracks
200 MPa step – Spatial resolution 10μm
No cracks visible [Ebermann 18]
Tensile test in-situ SEM on PIT strand Spatial resolution 4μm [Lenoir 17]
Cross-polishing of longitudinal CS of IT strand after interrupted tensile test [Lenoir 17]
Bundle of sub-element of RRP 144/169 longitudinal view [Ebermann 19]
80nm
Etching of an IT strand [Jewell 08]

## Slide 32: Conclusion
Transport measurements & damage state
  Damage in sub-element observed before transport measurements degradation
  No impact of small cracks observed at low stress levels on the transport measurements performed at the stack scale
Cumulated / cyclic loading
  Clear differences in damage occurring in monotonic and cumulated / cyclic loadings
Question
  Effect of cyclic loadings (mech. & thermal) at lower pressure?
   “Sultan” type tests
  Correlation between Ic degradation and damage phenomena  At which pressure / stress level the first cracks appear?  Physical phenomena and damage process involved?
  Extrapolation between strand, stacks (double & 10-stack) and coils scales?
  Can we build magnets with below stress level for which appears first cracks?
  Can we live with some of the cracks?

## Slide 33: Perspectives & on-going work
Numerical twin using the CoCaSCOPE approach [Manil 21]
11 T samples
  Lower stress levels
  Longitudinal cross-section
  Statistics (crack density, size, pattern)
MQXF specimens – K. Puthran
  Inverted stack configuration
  First cracks and stress levels
  Impact of impregnation resin
Statistical & systematic study of damage
  Transport measurements
  Damage phenomena
    Crack initiation / damage in epoxy / etc.
    Spatial cracks distribution & pattern
Stack sample
  Inverted or non-inverted configurations
     both should be done
  Simplified structure allowing to study mechanical and electrical responses under known conditions
  Easier, quicker, cheaper.
Architecture
Ic degradation
Mech. behavior
Design & operating limits
  Experimental procedure
  Metallographic analysis (procedure, tools, etc.)
Elementary loadings
  Transverse
  Bending
  Tensile
Damage analysis
Transport measurement
Numerical simulation

## Slide 34: Effect of transverse compressive stress on Nb3Sn Rutherford cables for accelerator magnets
Gilles Lenoir, Kirtana Puthran, Christian Barth, Felix Wolf, Jérôme Fleiter and Amalia Ballarino
TE-MSC-SCD
Thank you for your attention
[Balachandran 21] S. Balachandran et al., SUST, 2021, 10.1088/1361-6668/abc56a.
[Ebermann 18] P. Ebermann et al., SUST, 2018, 10.1088/1361-6668/aab5fa.
[Ebermann 19] P. Ebermann et al., SUST, 2019, 10.1088/1361-6668/ab2e51.
[Ekin 87] JW. Ekin, Journal of Applied Physics, 1987, 10.1063/1.338986.
[Ferracin 19] P. Ferracion, IEEE TAS, 2019, 10.1109/TASC.2019.2899284.
[Jewell 08] M. Jewell, PhD thesis, University of Wisconsin–Madison, 2008, link.
[Lenoir 17] G. Lenoir, PhD thesis, CentraleSupélec, Université Paris-Saclay, 2017, link.
[Manil 21] P. Manil et al., CERN TE-MSC seminar, 2021, https://indico.cern.ch/event/1085648/.
[Troitino 21] J. Ferradas Troitino et al., SUST, 2021, 10.1088/1361-6668/abd388.
[Verweij 99] A. P. Verweij et al., IEEE TAS, 1999, 10.1109/77.783259.
[Wolf 18] F. Wolf et al., IEEE TAS, 2018, 10.1109/TASC.2017.2780850.