## Slide 1: Diamond-like carbon coatings for cryogenic operation of particle detectors
S. Leardini, Y. Zhou, A. Tesi, M. Morales, D. González-Díaz, A. Breskin, S. Bressler, L. Moleri, V. Peskov
13/06/2022

## Slide 2: Background
Needs in detectors with HV
Solution –> resistive materials
spark-quenching
adjusting the charge-induction profile from moving charges to improve space resolution in tracking detectors
reducing local charging-up
Too conductive -> problem not solved
Too resistive -> charging-up + field deformation

## Slide 3: Objective
Find a suitable material for spark-quenching operating at LAr temperature -> candidate: DLC
Right range of surface resistivity: 10-100 Mohm / sq
Characterize such material and model its behavior with temperature

## Slide 4: Material - 1
- DLC produced at the University of Science and Technology of China
deposition through magnetron sputtering
Procedure: - substrate kept in oven @ 70ºC - surface cleaned with ethanol - vacuum @ 10^-5 mbar - deposition (20-60 min)
From talk by Yi Zhou: https://indico.cern.ch/event/852331/contributions/4611238/attachments/2367150/4042458/Resistive%20Detectors%20with%20DLC.pdf

## Slide 5: Material - 2
- 6 different samples with kapton substrate (named A-F), 2 with FR4 substrate (named “a” and “f”)
~ 10 x 10 cm

## Slide 6: Cryogenic setup - 1
- First measurements done with “Physical property measuring system” (PPMS)
- Able to ensure thermal equilibrium for all the temperatures
- Measured sample ”A” (4 different ~ 1 x 1 cm regions) with 4-point probe
- Able to cover only up to 30 Mohm/sq
I Miccoli et al 2015 J. Phys.: Condens. Matter 27 223201

## Slide 7: Cryogenic setup - 2
Home- made cryostat
Able to measure all the range of resistivities

## Slide 8: Commissioning
10% agreement

## Slide 9: Uniformity (with PPMS)
20% variation

## Slide 10: Linearity

## Slide 11: R-T curves (modeling) - 1
2 R-T curves taken for each sample
Global fit to all the samples with the function with parameter T common for all the samples
0

## Slide 12: R-T curves (modeling) - 2

## Slide 13: R-T curves (modeling) - 3
Expressed “a” as a function of rho_300, logarithmic relation - Expected value for “a” according to variable- range hopping model: 1/4

## Slide 14: R-T curves (modeling) - 4
produced many curves and inverted the fitting function numerically
Got iso-resistivity curves to select the initial rho_300 if we wish some resistivity at a certain temperaure

## Slide 15: Aging
RT : no aging effect after transporting > 2 C / cm^2
LN : < 2% variations
DUNE Far Detector (assuming Ar background, gain =100): 60.5 μC/cm2 in 10 years -variations < factor of 2 in > 1 year -no effect of humidity

## Slide 16: Test in detector (RWELL) – 90 K
Charge multiplication occurring inside the detector in a stable manner!

## Slide 17: Conclusions
- We characterized the DLC material produced at the University of Science and Technology of China focusing on uniformity, linearity, behavior with temperature and aging
The material is well – behaved in all these aspects, looking a very promising material to operate in a detector at LAr temperature (and in all the range up to RT in fact)
We made a predictive parametrization that may facilitate the production of new DLC samples with a desired resistivity at any temperature
We managed to operate a detector at 90 K with a DLC layer obtaining charge multiplication in a stable manner

## Slide 18: Thanks for your attention!