## Slide 1
Nb bulk QPR (A5) and RF disk processing
Oleksandr Hryhorenko / IJCLab – CNRS

## Slide 2: QPR-A5 (HZB)

## Slide 3: QPR-A5 Summary
Surface preparation
BCP removal of 150 µm at RI
800 °C annealing, 4 hours
BCP removal of 10 µm at RI
MP removal of 250 µm (2 steps) at IJCLab
RF evaluation
RF test at HZB = > “Bad” RF performance => Q-disease => Precipitation of hydrides => Surface dislocations “Skeletons”
History of QPR-A5
Improved roughness
Bad RF performance
Standard path (applied on QPR sample)
What step brings Hydrogen during MP and how to mitigate it without chemistry?
EP removal of 50 µm at CEA (remove skeletons)
800 °C annealing, 3 hours (hydrogen degassing)
EP removal of 25 µm at CEA (due to C contamination caused by furnace)
~ 150 nm peak to valley difference
~ 10-15 um in-plane size
NbHx Pits
Trace of NbHx
segregations
along the scratch
Q-disease mitigation treatment
2 phases of precipitations:
Peaks
Valleys

## Slide 4: Q-disease analysis (studies on samples)
Precipitation of Hydrides
Step 1: removal of 250 µm
Step 2: polishing 2 hours
Hydrides are not observed
Too damaged or no Q-disease
Hydrides are observed
Q-disease
Q-disease analysis
Q-disease test
~10-12h
LN2
39.5°C

## Slide 5: Q-disease analysis (studies on samples)
Step 1: removal of 250 µm
Step 2: polishing 2 hours
Hydrides are not observed
Too damaged or no Q-disease
Hydrides are observed
Q-disease
Q-disease analysis
Mitigation treatment
Annealing + test: 800C for 3 h
Hydrides are not observed
Now no Q-disease
BCP + test: removal of 5 µm
Hydrides are not observed, but revealed strain is presented
Now no Q-disease
Precipitation of Hydrides
Q-disease test
~10-12h
LN2

## Slide 6: Q-disease analysis (studies on samples)
Step 1: removal of 250 µm
Step 2: polishing 2 hours
Hydrides are not observed
Too damaged or no Q-disease
Hydrides are observed
Q-disease
Q-disease analysis
Mitigation treatment
Annealing + test : 800C for 3 h
Hydrides are not observed
Now no Q-disease
BCP + test : removal of 5 µm
Hydrides are not observed, but revealed strain is presented
Now no Q-disease
Step 2+15 min+test
Q-disease analysis: prolongation
Step 2+15 min+test

## Slide 7: Q-disease analysis (studies on samples)
Step 1: removal of 250 µm
Step 2: polishing 2 hours
Hydrides are not observed
Too damaged or no Q-disease
Hydrides are observed
Q-disease
Q-disease analysis
Mitigation treatment
Annealing + test : 800C for 3 h
Hydrides are not observed
Now no Q-disease
BCP + test: removal of 5 µm
Hydrides are not observed, but revealed strain is presented
Now no Q-disease
Step 2+15 min+test
Step 2+120 min+test
Q-disease analysis: prolongation
Step 2 is not a source of hydrides as passivation process prevents hydrogen penentration + reduced temperature processing
Step 2+15 min+test
Any comments?

## Slide 8: Perspectives
RF evaluation in perspective at HZB
Surface preparation
BCP removal of 150 µm at RI
800 °C annealing, 4 hours
BCP removal of 10 µm at RI
MP removal of 250 µm (2 steps) at IJCLab
EP removal of 50 µm at CEA (remove skeletons)
800 °C annealing, 3 hours (hydrogen degassing)
EP removal of 25 µm at CEA (due to C contamination caused by furnace)
History of QPR-A5

## Slide 9: RF disk (STFC)

## Slide 10: RF disk (STFC) Summary
Summary:
Performed a heat treatment (800°C for 3h) to reduce the H phase
No need to use light chemical removal (SiO2 particles were removed by recleaning), no C contamination
NEXT STEP:
RF disk test at STFC (Daniel Seal)
RF disk
QPR
Samples

## Slide 11
Thank you for your attention