## Slide 1
5th IFAST WP9 Meeting

## Slide 2
Deposition of 6 GHz cavity

## Slide 3: Deposition of NbTiN inside the 6 GHz
Deposition parameters:
Power 150 W
Current 0.23 A
Voltage 658 V
Dep Temp 650 C
Pulsed DC
Frequency 350 KHz
Dual Time 1.1us
Deposition time 1 h 30 min
Dep pressure 2.6 x10-2 mbar mag current 7.54 A

## Slide 4: SEM of NbTiN film at cavity equator
Element | Weight% | Atomic% | 
Ti K | 25.77 | 39.49 | 
Cu K | 5.13 | 5.93 | 
Nb L | 69.09 | 54.58 | 
Totals | 100.00 |  | 
Element | Weight% | Atomic% | 
Ti K | 25.40 | 38.99 | 
Cu K | 5.39 | 6.24 | 
Nb L | 69.21 | 54.77 | 
Totals | 100.00 |  | 

## Slide 5: Deposition of Nb thin film inside 6 GHz cavity
Deposition parameters:
Power 150 W
Current 0.23 A
Voltage 658 V
Dep Temp 650 C
Pulsed DC
Frequency 350 KHz
Dual Time 1.1us
Deposition time 1 h 30 min
Dep pressure 2.6 x10-2 mbar
mag current 7.54 A

## Slide 6: Deposition of Nb3Al on copper disk
Element | Weight% | Atomic% | 
Al K | 22.83 | 49.22 | 
Cu K | 8.53 | 7.81 | 
Nb L | 68.63 | 42.97 | 
Totals | 100.00 |  | 
Chart: 
 | 0.2485
 | 0.028463