## Slide 1: First-principles calculations on investigating the behavior of metal surfaces under high electric field
CERN 20.04.2022
Ye Wang
Institute of technology, University of Tartu

## Slide 2: Outline
Field-induced atomic strcuture modifications:
  The behavior of Cu nanoparticles under electric field
  Carburized W surface reconstructions:
    The application of WC surfaces
    Identify the atomic structures of WC surfaces
    Investigate the properties of WC surfaces with electric field
Conclustions and Outlook

## Slide 3
Increase the bond distance between Cu pair
without electric field
with electric field(10.28GV·m−1)
with electric field(15.42GV·m−1)
potential well
potential well
potential well
Preliminary Estimates

## Slide 4
without electric field
with electric field (5.14GV·m−1)
Cu nanoparticles
Electric Field

## Slide 5
Carburized W{110} surfaces are known to produce two globally ordered reconstructions, R(15 × 3)-C/W(110) and R(15 × 12)-C/W(110)
R(15 × 3)-C/W(110):
Violet Rectangle
R(15 × 12)-C/W(110):
Large Rectangle with
Solid Green Line
W(110)/C-R(15×3) and W(110)/C-R(15×12) have been extensively studied both experimentally and theoretically since 1960s​
Both structures have been nicely used as the templates for the growth and self-assembly of metal nanostructures, for instance, Ag, Au, Co, Cu and C60, etc.​
Motivation

## Slide 6
The application of WC surfaces for nanotechnology:
  Promising for nanofabrication due to their nano-patterned periodicity
  Electric fields induce surface rearrangement and diffusion, their behavior need to be understood
Interesting behavior under high electric field:
  The work function of W(110)/C-R(15×12) seems to be lowered
  What is the main reason causing this behavior?
Problem: the exact atomic structure of W(110)/C-R(15×12) surface is still unknown
  Find out what the structure is
  Identify the W(110)/C-R(15×3) surface and reconstruction mechanism
Motivation

## Slide 7
STM image of carburized W{110}
1h
2h
5h
16h
(a)-(c) shows the temporal evolution of the STM images of R(15 × 3) reconstruction,
(d) denotes the STM image of the R(15 × 12) reconstruction
by Kim et. Al

## Slide 8
Atomic Structure
The Simulated STM image within the Tersoff-Hamann approximation
Close-up STM image
R(15×3)-C/W(110)
Large-scale STM image
the number of the W atoms at the surface layer of R(15×3)-C/W(110) is 14

## Slide 9
Large-scale STM image
R(15×12)-C/W(110)
According to the hypothesis of Kim et al., Block B is a clean W slab, and it is originated from two neighboring A-blocks by removing the subsurface carbons.
Thus, the total number of W on the R(15×12) surface is 56.
Atomic Structure within DFT calculations
Close-up STM image
A
A
B
A: R(15×3)-C/W(110)
B: clean W(110)

## Slide 10
STM image of carburized W{110}
1h
2h
5h
16h
(a)-(c) shows the temporal evolution of the STM images of R(15 × 3) reconstruction,
(d) denotes the STM image of the R(15 × 12) reconstruction
by Kim et. Al
Our Hypothesis: the unit cell of R(15×12)-C/W(110) is composed of C+C+B

## Slide 11
C block – a metastable structure of R(15×3) reconstruction

## Slide 12: Conclusions and Outlook
We identify the atomic structure of the R (15 × 12) surface and reveal the reconstruction mechanism of the R (15 × 3)
Our results provide an important understanding of the carburized W{110}, open a new avenue for exploring self-organization properties of various metal nanostructures
Outlook: After we have confirmed the atomic structure, we aim to explain experimental results about metastable hypothesis under electric field

## Slide 13
Achnowledgments
ERA Chair ”MATTER”
Thank you for your attention!

## Slide 14
DFT to study the properties of metal surfaces under electric field
Gaussian:
Object: metal nanoparticles, non-periodic
Method: localized basis sets
Result analysis: Molecular Orbital Theory
VASP:
Object: metal surfaces, periodic in x, y z direction
Method: plane wave basis sets
Result analysis: Band Structure