## Slide 1: Microscopic analysis of Cu electrodes from the Large Electrode System
CERN, 20.04.2022
S. Oras
Tartu University, Institute of Technology
MATTER laboratory

## Slide 2: Outline
Characterization of Cu electrodes
  Description of electrodes
  SEM
  EDX
  AFM + FEM
Heat-induced growth of CuO nanowires
Future plans

## Slide 3: Characterization of Cu electrodes

## Slide 4: Description of electrodes
We have received 3 pairs electrodes in total.
  2 Pairs of soft and hard Copper with different conditioning and plasma treatment history from Helsinki.
  And another pair without conditioning and plasma treatment from CERN.
Phys. Rev. Accel. Beams 23, 033102

## Slide 5: SEM

## Slide 6: SEM: Cathode
Soft Cu
Soft Cu

## Slide 7: SEM: Anode
Soft Cu
Hard Cu
Soft Cu

## Slide 8: EDX
EDX (Energy-dispersive X-ray spectroscopy) inside SEM.
Performed by Aile Tamm and Helle-Mai Piirisoo.

## Slide 9
Spectrum | C | O | Na | Mg | S | Cl | K | Ca | Ti | Cu | Total
Spectrum A | 2.89 | 0.61 |  |  |  |  |  |  | 0.28 | 96.22 | 100.00
Spectrum B | 2.79 | 0.63 |  |  |  |  |  |  | 0.36 | 96.22 | 100.00
Spectrum A
Spectrum B
Mapping was done in several locations on both electrodes.
(This spectra is from cathode.)
EDX: Mapping

## Slide 10
Elemental composition of a regular surface of untreated Cu electodes 0185 and 0186 in wt.%:
High amount on C especially on anode.
 | C | O | Ti | Cu | Total
0185 (cathode | 2.90 | 0.73 | 0.32 | 96.06 | 100.0
0186 (anode) | 7.57 | 0.91 | 0.78 | 90.74 | 100.0
EDX: Summary

## Slide 11: AFM
Atomic Force Microscope (AFM)
(Dimension Edge by Bruker/Veeco)
equipped with Kelvin probe
(mapping the work function)

## Slide 12: AFM: Crater topography vs work function
Work function
Topography

## Slide 13: AFM+FEM: Field enhancement
AFM images as input for Finite Element Method (FEM) simulation
Field enhancement up to 5 times due to topology.
Field enhancement capped at 3
Field enhancement simulation

## Slide 14: Heat-induced growth of CuO nanowries

## Slide 15: Growth of CuO nanowires
CuO nanowires can be synthesized by heating Cu in the presence of oxygen* in the temperature range 400°C-700°C.
*Nano Lett., Vol. 2, No. 12, 2002

## Slide 16: Cu sample with CuO nanowires:
Inner structure after heat-treatment Cut by Focused Ion Beam (FIB), analysed by EDX (NSFL, IPUT)
Dorogov, et. al, Appl. Surf. Sci. 246, 423 (2015).

## Slide 17: Tungsten oxide nanowires
Tungsten Oxide nanowires grown in vacuum on tungsten filament used in SEM.
Estimating the amount of molecules in CLIC

## Slide 18: Future plans
Plans with current electrodes:
  Cut the electrode to see if the carbon is on the surface or is it in bulk.
Plans for new electrodes:
  We need a new pair of electrodes without excessive C.
  We make EDX and microscopy in Tartu. Then we do conditioning and/or plasma in Helsinki. We look at results in Tartu.
We receive heating stage for microscope in September. We can observe in real-time IF growth of CuO wires happen in Cu in vacuum.

## Slide 19
Achnowledgments
ERA Chair ”MATTER”

## Slide 20: Mapping large craters
Mapping of the most interesing part is almost impossible.
Image of crater with artefacts
¾ of image with dull tip