## Slide 1: Compact Linear Collider: Investigation of electrical breakdown phenomena using multiscale and multiphysics simulations
Veronika Zadin1, Andreas Kyritsakis1, Flyura Djurabekova2, Tauno Tiirats1, Sergei Vlassov1, Sven Oras1, Ye Wang1
CBC 2022
1. Institute of Technology & Institute of Physics, University of Tartu, Estonia
  ERA Chair MATTER, http://www.matter.ee
  veronika.zadin@ut.ee
2. University of Helsinki, Finland
flyura.djurabekova@helsinki.fi

## Slide 2: University of Tartu: ERA Chair MATTER
Essential tools
Multi-scale simulations
SEM, TEM, AFM
In-situ Nanomanipulation
Functional materials in extreme environments
Study of Nanostructures
Materials Under High EM field
Vacuum Breakdown
Surface diffusion under high field
Nanomanipulation & Nanofabrication using electric fields
Biomedical Applications
V. Zadin, University of Tartu

## Slide 3: ERA Chair MATTER: Team in action
Veronika Zadin, PhD, prof., coordinator, advanced computer simulations
Andreas Kyritsakis, PhD, ERA Chair holder, associate prof., advanced computer simulations
Sergei Vlassov, PhD, associate prof., Nanomanipulation team lead
Veikko Linkko , PhD, associate prof., Biomedical team lead
Sven Oras, PhD, Postdoc
Edgars Butanovs, PhD, Postdoc
Tauno Tiirats, PhD, Postdoc
Mihkel Veske, PhD, engineer
Mart Ernits, MSc, PhD student
Ye Wang, MSc, PhD student
Elyad Darmechi, MSC, PhD student
Roni Koitermaa, MSC, PhD student
Mikael Rinne, Engineer, BSc student
Theophilus Odubena, BSc student
Ihar Suvorau, BSc student
Kristi Koitla, BSc student
Margit Meiesaar, supporting staff
V. Zadin, University of Tartu

## Slide 4: CLIC – Compact Linear Collider in https://clic.cern/
Surface damage in CLIC accelerating structures after the breakdown
CLIC:
collision energies 0.5-5 TeV
Proposed length 50 km requires E ~ 100 MV/m causing vacuum breakdowns
 BD mechanisms must be understood
Applications:
CLIC collider in CERN
vacuum switches
novel nanofabrication applications
x-ray sources
medical linear accelerators
RF components for microwave devices
V. Zadin, University of Tartu

## Slide 5: How we decode the nature …
V. Zadin, University of Tartu
DFT
Molecular dynamics
Mesoscale modeling
Finite Element Analysis
Distance
1Å
1nm
1μm
10nm
1mm
femtosec
picosec
nanosec
microsec
seconds
years
Time

## Slide 6: Breakdown initiation mechanisms
Key problem 1: understanding the mechanism leading to the appearnce of the field emitter
Fatique damage
Subsurface defects
Emission current measurements
Field enhancement factor β
Key problem 2: understanding actual formation of field enhancement factor ~100
Field emitters with height to radius ratio ~100 (100 nm tall with 1 nm diameter) needed????
A. Descoeudres, et al.,
Phys. Rev. ST Accel. Beams. 12 (2009)
L. Laurent et al.,
Phys. Rev. ST Accel. Beams. 14 (2011)
A. Pohjonen, F. Djurabekova, et al.
J. Appl. Phys. (2013)
e-
V. Zadin, University of Tartu

## Slide 7: Unlocking BD onset
KIMOCS
Gold model systems,
Surface behaviour
In situ SEM:
Heating & diffusion
Local El. field
MD, DFT, FEMOCS, GETELEC
Surface stability, estimation of possible phenomena
FEM modeling,
Upscaling in X and t
Expectations of experimental conditions
V. Zadin, University of Tartu

## Slide 8
The emission currents & thermal effects of electron emission
Electron Emission by General Thermal Field model
Thermionic emission: high temperature, low field
Field emission: low temperature, high field
Combined effects: general thermal field equation
  Joule heating (volumetric heat deposition)
  Nottingham heat (surface heat deposition)
V. Zadin, University of Tartu
Electron emission and heating by GETELEC Code:
https://github.com/AndKyr/GETELEC
A. Kyritsakis, F. Djurabekova, Comput. Mater. Sci 128 15 (2017)
Two heat deposition components
V. Zadin, University of Tartu
Notes: Kristjan Eimre will speak more later …

## Slide 9: Sharp emitter effects
General barrier formula:
V. Zadin, University of Tartu

## Slide 10: GETELEC
More details: A. Kyritsakis et. al., Comput. Meter. Sci. 128, 15–21 (2017)
GETELEC
Local Field
Radius
Input
Temperature
Work function
Current density
Nottingham heat
Output
e- Energy spectra
V. Zadin, University of Tartu

## Slide 11: Code implementation
GETELEC
Local Field
Radius
Input
Temperature
Band structure
Current density
Nottingham heat
Output
e- Energy spectra
No analytical solutions for our integrals!
Nested self-consistent
Pre-calculated
Later retrieve by interpolation
Material + Potential Barrier
V. Zadin, University of Tartu

## Slide 12: WWW.GETELEC.ORG
V. Zadin, University of Tartu

## Slide 13
V. Zadin, University of Tartu

## Slide 14
V. Zadin, University of Tartu

## Slide 15: Concurrent ED-MD: FEMOCS
V. Zadin, University of Tartu
Mesh generation “on the fly” when MD system changes
Solve for E, T, J et al.
Feedback to MD electrostatic forces + heating
https://github.com/veskem/femocs
Fine elements:
Deal.II library
Molecular Dynamics:
PARCAS MD
LAMMPS

## Slide 16: Specifics of FEMOCS algorithm
Atoms (MD)
FEM mesh
Electric Field
Field emission,
Particles (e), Positions, Injections
PIC
Current distribution
Temperature distribution
Velocity
perturbration
Sur. charge distribution
Force perturbation
V. Zadin, University of Tartu
M. Veske et. al, Phys. Rev. E 101, 053307 (2020)

## Slide 17: Heating and El. field calculations
  [1] A. Kyritsakis, F. Djurabekova, Comput. Mater. Sci 128 15
Surface Current density Js and
Nottingham heat PN distributions
GETELEC [1]
Temperature
distribution T(z)
MD velocity perturbation (Berendsen thermostat)
Conductivities σ,κ(Τ)
V. Zadin, University of Tartu
Heating: Joule and Nottingham
Track particles:
Interpolate charge density:
Collide particles (Monte Carlo method):
  (… and many other collision types)
Solve Poisson equation (FEM)
Calculate surface currents and inject new particles
Repeat for desired number of time steps
The Electric field Calculation: Space Charge Screening effects

## Slide 18: Static surface under el. field
Field Emission Microscopy experiment
Collaboration with Dr. Hirofumi Yanagisawa(Max-Planck Institute of Quantum Optics)
Surface faceting and protrusion formation
Possible mechanism for emitter formation
H. Yanagisawa, V. Zadin et al. https://arxiv.org/abs/1605.05393
V. Zadin, University of Tartu

## Slide 19: Current understanding
V. Jansson, et. al., Nanotechnology 31, 355301 (2020)
Fujita et al., Phys. Rev. 75, 2007
V. Zadin, University of Tartu

## Slide 20: Field assisted surface diffusion: the experiment
V. Zadin, University of Tartu

## Slide 21: Conclusions
FEMOCS – concentrates our best current understanding of BD onset
  Still has significant limitations – emitter must be pre-created
GETELEC – best currently available tool for field emission calculation & analysis
  Nottingham heat
  Metals & semiconductors
  Web interface to make it usable by wider audience
Whole multiscale range of simulations most probably needed to understand true reasons of BD initiation
Tight integration with in-situ microscopy experiments critical!
V. Zadin, University of Tartu

## Slide 22
Thank You for Your attention!
ERA Chair MATTER with funding from the European Union’s Horizon 2020 research and innovation programme under grant agreement No 856705.
Supproted by:
Estonian research council grants:
PUT 57 & PUT 1372
Special thanks to:
Alvo Aabloo
Elyad Darmechi
Tarmo Tamm
Simon Vigonski
Sergei Vlassov
Mihkel Veske
Kristjan Eimre
Kristian Kuppart
Sven Oras
Artur Tamm
Robert Aare
Tarvo Metspalu
Ye Wang
Aile Tamm
Faiza Summer
Helle-Mai Piirsoo
Walter Wuench
Flyura Djurabekova
Ville Jansson
Kai Nordlund