## Slide 1: HRMT-56: Experimental Results on Irradiated Graphitic Materials for HED

## Slide 2: Agenda
Irradiated Materials Overview
The HRMT-56 Experiment
Results Analysis
Conclusions

## Slide 3: LHC TDE Configuration & Operational Runs
Courtesy of E.Farina & A.Lechner

## Slide 4: Irradiated Materials Overview

## Slide 5: TDE Low-Density Core: Sigraflex®
~1630 sheets of Sigraflex®, 2 mm thick (L20012-C)
Sigraflex stack of sheets
SIGRAFLEX
Notes: Add expanded graphite (reduced speech)

## Slide 6: Alternative Options for HL-LHC Dump Core
Low-Density Carbon-based materials such as Graphite and Carbon-Carbon - C/C
C/Cs advantages:
+ Densities and properties can be “tailored”.
+ Hight RT as of compared to Graphite (Better mechanical properties).
+ Non-fragile behaviour (also wrt crack propagation).
C/C
Graphite
Brittleness
- Adjustable mechanical and thermomechanical properties.
- 30 grades from 6 different EU producers under assessment.
- 3D Carbon/Carbon composites for beam intercepting devices at CERN (F.X.Nuiry et al.)
- Full Scale Proton Beam Impact Testing of new CERN Collimators and Validation of a Numerical Approach for Future Operation (M.Bergeret, F.X.Nuiry et al.)
Notes: Consideration as the best alternative to compose the dump core

## Slide 7
C/C Tailoring of Industrial grades
Chart: Density dist. For HRMT-56 CC Grades
| <1 g/cc | 1.0 - 1.1 g/cc | 1.4 - 1.5 g/cc | 1.6 - 1.7 g/cc | > 2 g/cc
Sales | 1 | 5 | 15 | 10 | 1
Chart: HTHT range dist. on HRMT-56 CC Grades
| < 2000 C | 2000 - 2200 C | 2200 - 2500 C | 2500 - 2800 C | 2800 - 3000 C
HTHT ranges | 5 | 22 | 0 | 5 | 2
Density and HTHT influence mechanical and thermomechanical properties of grades
Higher density:
- Similar CTE
- Higher Thermal Conductivity
- Stronger (↑ σT ) but stiffer (↑ E)
(Relation depends on specs. For each material)
Higher T during HTHT:
- Stability to material throughout T span (Specially wrt CTE values)
- Increases Thermal Conductivity
- Increases mechanical properties (↑σT /E) but up to a limit related to Graphitization
Characterizations required as inputs for simulations

## Slide 8: The HRMT-56 Experiment

## Slide 9
HiRadMat-56 [HED = High-Energy Dumps]
Beam parameters:
440 GeV / 1.2e11 ppb
HRMT-56 tank CAD model
HRMT-56 tank CAD model – cut view
beam
Beam gotten w44/21 (November 2021)
Complete Pulse List attained successfully – 77 pulses in total (~2,65x1015 protons)
Notes: Add two/three legends
Add BEAM
4 TS
440GeV a 1.2e11 p+

## Slide 10
Target Station A & B: HL-LHC TDE
HL-LHC Beam Dump material targets (1)
beam
Target St.A | Number | Length | Instrumented
Total Targets | 13 | 21 mm | No
Total TiB2 Diluters | Long = 5 | 250 mm | No
 | Short = 8 | 80 mm | Yes (5  [1x] PT100)
1
Target St.B | Number | Length | Instrumented
Total Targets | 9 | 20 mm | No
 | 2 | 150 mm & 75 mm | No
Total TiB2 Diluters | Long = 3 | 250 mm | No
 | Inter. = 1 | 120 mm | Yes ([1x] PT100)
 | Short = 8 | 80 mm | Yes (3  [1x] PT100)
HL-LHC Beam Dump material targets (2)
beam

## Slide 11
Target Stations C & D: FCC-ee + TCDQ/S & Sigraflex®
beam
FCC-ee & TCDQ/s material targets
Target St.C | Mat. | Number | Length | Instrumented
Total Targets | C | 2 | 30 mm | Yes [x1] – LDV. Int
 |  | 6 | 20 mm | Yes [x3] - LDV. Ext
Total Diluters | TiC | Long = 1 | 300 mm | Yes ([1x] PT100)
 |  | Short = 1 | 60 mm | Yes ([1x] PT100)
Total Diluters | TiB2 | Long = 3 | 250 mm | No
 |  | Short = 3 | 80 mm | Yes (3  [1x] PT100)
LHC-TDE Sigraflex for Run3 targets
beam
Target St.D | Number | Length | Instrumented
Total Targets | 2 | 220 mm | Yes ([1x] PT100)
 | 3 | 320 mm | Yes ([1x] PT100)

## Slide 12
Peak Energy Density into target train (Courtesy of E.Farina & A.Lechner)
Targets
21 mm of C/C - Ø 60 mm
(3 slices)
Diluter up  250 mm TiB2 Ø20mm / (20 mm slices)
Diluters mid & down  80 mm TiB2 Ø20mm / (20 mm slices)
Peak E dose = 2.75 kJ/g
Peak E dose = 2.62 kJ/g
Peak E dose = 2.32 kJ/g
1.1 g/cm3
1.5 g/cm3
1.7 g/cm3
beam
Example of Target Train for HRMT-56 beam impact
Target Station A & B: HL-LHC TDE

## Slide 13
Diluters TiB2

## Slide 15: PIE - Results Analysis

## Slide 16: TDE Low-Density Core: Sigraflex®
HRMT- 43 (2018) test
One single beam impact
One sheet
Sample was in Air
Sample was unconstrained
24 mm
beam
0.5 mm thickness
Energy deposited ~ 2.46 kJ/g (in 7.2 µs)
LHC Run3 peak energy density
- Delamination & flakes fracture within the bulk
Bump of over 200 µm of both sides (-> permanent damage)
Experimental conditions were not fully controlled
Investigation of SIGRAFLEX samples exposed in the HiRadMat facility: https://edms.cern.ch/document/2380563/1
SEM
u-CT scan

## Slide 17
HRMT-56 [HED] – Sigraflex studies (N2 and VACUUM)
BEAM 1 =
0.25 x 0.25 mm
Constrained configuration - Uncompressed
1.2 g/cm3, t = 2 mm
Free sheets:
t = 2/1/0.5 mm, 1.0 g/cm3 t = 2/1/0.5 mm, 1.2 g/cm3
Diluter of TiB2: Ø20mm Length 20 mm
Constrained - Uncompressed
1.2 g/cm, t = 2mm
Constrained configuration – Compressed 5%
1.2 g/cm3, t = 2 mm
50 mm
50 mm
10 mm
Max. Peak E = 2.7 kJ/g
Max. Peak E = 2.6 - 2.7 kJ/g
Max. Peak E = 2.60 – 2.37 kJ/g
Max. Peak E = 3.2 kJ/g
Sigraflex 1.2 (= 1.1) Target
BEAM 2 =
1 x 0.34 mm
Diluter of TiB2: Ø20mm Length 250 mm
Constrained - Uncompressed
1.2 g/cm, t = 2mm
Free sheets:
t = 2/1/0.5 mm, 1.2 g/cm3
Max. Peak E = 1.85 – 1.5 kJ/g
Sigraflex 2.1 (= 2.2) Target
Max. Peak E = 3 kJ/g

## Slide 18
Constrained configuration - Uncompressed
1.2 g/cm3, t = 2 mm
Free sheets:
t = 2/1/0.5 mm, 1.0 g/cm3 t = 2/1/0.5 mm, 1.2 g/cm3
Diluter of TiB2: Ø20mm Length 20 mm
Constrained - Uncompressed
1.2 g/cm, t = 2mm
Constrained configuration – Compressed 5%
1.2 g/cm3, t = 2 mm
50 mm
50 mm
10 mm
Max. Peak E = 2.7 kJ/g
Max. Peak E = 2.6 - 2.7 kJ/g
Max. Peak E = 2.60 – 2.37 kJ/g
Max. Peak E = 3.2 kJ/g
Sigraflex 1.2 (= 1.1) Target
BEAM 1 =
0.25 x 0.25 mm
HRMT-56 Sigraflex ® targets type1 (N2 and VACUUM)

## Slide 19
SOLO layers (HRMT-56)
Chart: 1.1 solo LAYERS in N2 [UM/UM]
Upst_3s | 0.046 | 0.037 | 0.062 | 0.015 | 0.029 | 0.03
Dwst_3s | -0.0385 | -0.038 | -0.05 | -0.0185 | -0.027 | -0.058
Empty | 0
Upst_1s | 0.042 | 0.036 | 0.056 | 0.0115 | 0.019 | 0.034
Dwst_1s | -0.025 | -0.036 | -0.028 | -0.019 | -0.03 | -0.062
Empty2 | 0
Layer Thickness / Multi-shot vs. Single shot effect in N2
Relation between layer thickness and damages observed
No clear sign of major effect related with multi-pulses events
x
Specimens much less affected than in HRMT-43
Damaged confined to entry/exit surfaces
Bulk intact
HRMT-56 [HED] – Sigraflex studies
2 mm thick
1 mm thick
0,5 mm thick
2 mm thick
1 mm thick
0,5 mm thick

## Slide 20
SOLO layers (HRMT-56)
Chart: in N2 vs. Under vacuum solo LAYERS [UM/Um]
| 1 | 2 | 3 | 4 | 5 | 6
Upst_3s_N2 | 0.046 | 0.037 | 0.062 | 0.015 | 0.029 | 0.03
Dwst_3s_N2 | -0.0385 | -0.038 | -0.05 | -0.0185 | -0.027 | -0.058
Empty | 0
Upst_3s_VAC | 0.022 | 0.009 | 0.03 | 0.008 | 0.005 | 0.01
Dwst_3s_VAC | -0.01 | -0.017 | -0.07 | -0.005 | -0.005 | -0.01
Empty2 | 0
Relation between layer thickness and damages observed
Samples irradiated in N2 more damaged than those under vacuum
Specimens much less affected than in HRMT-43
Damaged confined to entry/exit surfaces
Bulk intact
HRMT-56 [HED] – Sigraflex studies
Layer Thickness / Response in N2 vs. under Vacuum
2 mm thick
1 mm thick
0,5 mm thick
2 mm thick
1 mm thick
0,5 mm thick

## Slide 21
Chart: solo LAYERS Out of plane deformation [UM]
Upst_3s_N2 | 92 | 37 | 31
Dwst_3s_N2 | -77 | -38 | -25
Empty | 0
Upst_3s_VAC | 44 | 9 | 15
Dwst_3s_VAC | -20 | -17 | -35
Empty2 | 0
HRMT-43_Ups_G27 | 0 | 0 | 237
HRMT-43_Dwst_G27 | 0 | 0 | -225
 | HRMT-43 | HRMT-56
Material purity | TH/Z grade (C > 99.85%) – F05010TH | NH/C grade (C > 98%) – F05010C
Density | 1.0 g/cm3 | 1.0 g/cm3
Environment* | Air | Nitrogen (also under vacuum)
Beam Spot Size (σx , σy) | “0.25x0.25 mm” | 0.28x0.24 mm (SOLO layers)
Conditioning of Samples** | Workshop (“humid”) | N2 environment and Flushing (“dry”)
Sample thickness | 0.5 mm | 0.5 mm (also 1 mm and 2 mm)
Out of plane deformation | 200 – 250 ums | 20 – 30 ums
Radius of affected area | 0.8 mm | 0.28 mm
Beam Intensity // Peak Energy Density // Event type | G27-G28  1.218e11 ppb, 288b // ̴ 2.47 kJ/g // (1 pulse event) | 1.208e11 ppb, 288b // ̴ 2.45 – 2.35 kJ/g (per pulse) // (3 pulses / 1 pulse)
*TDE environment is N2 at slight overpressure to Pa.
**Sigraflex Dump conditioning is “somewhere between” dry and humid
SOLO layers (HRMT-43 vs. HRMT-56)
HRMT-56 [HED] – Sigraflex results
2 mm thick
1 mm thick
0,5 mm thick

## Slide 22
Diluter of TiB2: Ø20mm Length 250 mm
Constrained - Uncompressed
1.2 g/cm, t = 2mm
Free sheets:
t = 2/1/0.5 mm, 1.2 g/cm3
Max. Peak E = 1.85 – 1.5 kJ/g
Sigraflex 2.1 (= 2.2) Target
Max. Peak E = 2.8 kJ/g
BEAM 2 =
1 x 0.34 mm
HRMT-56 Sigraflex ® targets type2 (N2 and VACUUM)

## Slide 23
SOLO layers (HRMT-56)
Asymmetric Beam in N2 – Surface effects
E_density = 2.37 – 2.45 kJ/g
Density = 1.0 g/cc
Thickness = 0.5 mm
N2 / Symmetric beam
Density = 1.0 g/cc
Thickness = 2 mm
N2 / Asymmetric beam
E_density = 1.8 – 1.85 kJ/g 0
E_density = 1.6 – 1.7 kJ/g
Density = 1.0 g/cc
Thickness = 1 mm
N2 / Asymmetric beam
E_density = 1.5 – 1.55 kJ/g
Density = 1.0 g/cc
Thickness = 0.5 mm
N2 / Asymmetric beam
SOLO layers in N2 + asymmetric beams  bulk delamination
Effect of thickness on extent of delamination
Recent results. On-going progress.
E_density = 2.8 kJ/g
Density = 1.0 g/cc
Thickness = 2 mm
N2 / Asymmetric beam
Stacked

## Slide 24
Density = 1.0 g/cc
Thickness = 2 mm
N2 / Asymmetric beam
E_density = 1.8 – 1.85 kJ/g 0
E_density = 1.6 – 1.7 kJ/g
Density = 1.0 g/cc
Thickness = 1 mm
N2 / Asymmetric beam
E_density = 1.5 – 1.55 kJ/g
Density = 1.0 g/cc
Thickness = 0.5 mm
N2 / Asymmetric beam
Asymmetric Beam in N2 / Vacuum
E_density = 1.8 – 1.85 kJ/g 0
Density = 1.0 g/cc
Thickness = 2 mm /
VAC / Asymmetric beam
E_density = 1.6 – 1.7 kJ/g 0
Density = 1.0 g/cc
Thickness = 1 mm /
VAC / Asymmetric beam
E_density = 1.5 – 1.55 kJ/g 0
Density = 1.0 g/cc
Thickness = 0,5 mm /
VAC / Asymmetric beam
N2 layers damaged in the bulk / Vacuum layers just superficial damage
Effect of thickness on extent of delamination
Recent results. On-going progress.

## Slide 25
STACKED layers
Conclusions STACKED layers in N2/Vacuum:
Practically no damage observed (coherent with LHC TDE Autopsy Results)
Compressed/Uncompressed results are very similar
- Vacuum samples “untouched”
Results on Sigraflex® (HRMT-56)

## Slide 26: Conclusions

## Slide 27
Sigraflex® shows no damage up to 2.7 - 3.2 kJ/g when irradiated in N2 & Vacuum for 3 (or 1) shots and in STACKED configuration for any beam impact
  Run3 parameters are compatible with tested conditions for Sigraflex (doubt on what cumulative damages would appear after ‘00s shots at Run3 & beyond (HRMT-HED2 (2024))
  HRMT-56 SOLO layers results do not show bursting-out effect shown in HRMT-43 for symmetric beam impacts
  HRMT-56 SOLO layers show bursting-out effect for asymmetric beam impacts:
      No bulk effect on samples under Vacuum / Layers impacted in N2 show same extent of damage as those of HRMT-43
      Boundary conditions and environment play indeed a role in bursting out of plane – even more than peak energy density.
 Technically going with stacked Sigraflex ® sheets is a valid choice for Run3
Alternatives based on CFC materials would be available and are performing well.
Full assessment of C-based materials under beam Impact (being) done (CC / C-SiC / Sigraflex / Graphite)