## Slide 1
Glyn Kirby , Ariel , Arnaud, Devide
4th May 2020

## Slide 2: Base line design (no taper)
Central field : 3.000 T
Peak field inner/outer coils : 3.531 , 3.452 T
Load line Fraction inner/outer coils : 72.921% , 72.021%
Integral on 1m rad axis Tm : By -2.8, Bx -2.804 e-07, Bz 4.093 e-3
Errors: heavily curved magnet ( Beam tracking WG, I say more later)
Current : 218.372 A
Inductance : 13.172 H
7 strand insulated rope
Strand and cable for then magnet : ~15.59 km strand , ~2.22 km rope.
1m rad of curvature cold!!.
90 deg end to end angle at the outside of the magnet
Former : Spar 5 mm, min wall 0.5 mm
***Fine tuning in progress but this is very close ***

## Slide 4
Combined Function correction
Dipole = 204 mm
Quad = 2.45 mm
Sextupole = 0.2 mm
Rad 118 mm
CF mm
Flat dipole not the best
But one option

## Slide 5: With clean dipole through aperture.

## Slide 6: Channel layouts
3 x 7 strand ropes
21 wires ~ 5 kA
Je 61.09 %
24 wires
710 A
Je 78.54%
22 wires
710 A
Je 83.8%
6 x 7strand ropes 42 wires
~5 kA
Je 61.09 %
Some channels with different packing lay out that have been looked at
19 strand rope
13.5 kA
Je < 59.6 %
12 ropes
84 wires
118 A
Je 63%

## Slide 7: Log Stacking
Layout in channel | Je %
Log stacking | 83.8
Rectangular stacking | 78.45
7 strand rope | 61.09
19 strand rope | 59.6
Test channels 7 strand rope and 36 strand log stacking
Fusillo 84 strand log stacking with chisel base to add stacking
Thanks to Ariel for the log stacking tests
Thanks to the Upsala team for the rope image

## Slide 8: Wire insulation & Performance
11kV wire insulation!
Strong bond to wire!
CERN 1.9:1 filaments 6 um
Prototype stock CERN wire
Magnet SS 55%
~ 4 mm pitch
Wire insulation is key!
55% overlap 2 layers + 3 layer spiraling spacer rib !

## Slide 9: Conductors
6 Non insulator strands in rope with a Cu or Invar core, the core cannot have superconductor due to inductive current and joint problems.
But insulation may stop resin getting in so ?
Open insulation old idea.
7 insulated strands
82 insulated strands in channel, winding with rope may be an advantage.
Base line design today
New design of non insulated rope.
Heavily competed,
large strand !
Nice but ????????
Insulated strands
compacted strands into a rope & then insulated
Non-Insulated strands
12 ropes
249 A 14 H
14 ropes
1627 A, 0.4 H
Open insulation

## Slide 10
Log stacking v classical
12 – 7 strand ropes
We plan winding tests!
6 x 7strand ropes 42 wires
~5 kA
Je 61.09 %
12 ropes
84 wires
118 A
Je 63%

## Slide 11: Tapered aperture & coil makes assembly easy! And may give radial pre-stress option !?
10 mm taper on radius over 1.571m, 0.366 deg
0.022 mm step between channels
Axial to radial force magnification = x 156
Exaggerated view of taper
Not corrected for dia. change
After correction for dia. change

## Slide 12: Peak field due to spar thickness or more precisely the gap between coils
Spar thickness
Peak field volume
In this image the peak field has started to be leveled away from the ends
As the SPAR reduces in thickness the layers get closer and at 5 mm (for this coil) both inner and outer coil peak field are equal further reduction in the gap increases peak field
Decreasing coil gap

## Slide 13: The basics of selecting the CCT angle

## Slide 14: First look at winding table idea!
Vertical table in Bat 927
Need to add one stepper motor and control, identical to what we have just made for the hts winging tool in Bat 230.
3 axis
2 axis
Thanks to Oliver for the animated models

## Slide 15: Solid Aluminum Support Design to fit into CERN Test Station
LBNL design.

## Slide 16: Added later by Spanish team

## Slide 17: Beam tracking in 3 Tesala
Bean energy 1.3 GeV, particle rest mass 0.938 GeV, 3T central field, Beam > 50 deg

## Slide 18: Beams like the Curved Corrected Harmonics

## Slide 19: Thankyou