## Slide 1
Pedro Morales Sanchez
20/05/2022
Brazing discs and prototype review

## Slide 2: Test
Gap | Ratio
0.03mm | 4.3/0.96
Ø0.5mm
Ø0.8mm
T18VG1-DISK-11WDSDVG1
08/12/2021
Pedro M | Smartcell structure development

## Slide 3: Programed tests
Different materials / temperatures / ratios / companies
Thanks to Bodycote and Fritz Motschmann for their collaborative approach to this project.

## Slide 4: Visual inspection
No overflow
Diffusion
No remarkable problem

## Slide 5: Leak test
Leak test OK of all parts after brazing cycle

## Slide 6: Ultrasounds analysis
H2 dry/ AuCu50/ Bodycote
H2 dry / AuCu50/ CERN
Vacuum/ Palcusil-5/ CERN
Vacuum/ Palabraze-840/ CERN
Brazing tests (15 September 2021) · Indico (cern.ch)

## Slide 7: Ultrasounds analysis
H2 dry/ AuCu50/ Bodycote
H2 dry / AuCu50/ CERN
Vacuum/ Palcusil-5/ CERN
Vacuum/ Palabraze-840/ CERN
Brazing tests (15 September 2021) · Indico (cern.ch)

## Slide 8: Metallographic evaluation - Gold
Brazing tests (15 September 2021) · Indico (cern.ch)
#1
1000 deg in the contact area we can see crossing grains. Bonding achieved with low pressure (less 0.05MPa) and very short time cycle
The material stops at the bonding surface

## Slide 9: Metallographic evaluation - Gold
Brazing tests (15 September 2021) · Indico (cern.ch)
#1
#1
#2
Bodycote
Temp: 1000 oC
Time: 5-10min
#8
#9
CERN
Temp: 978.9 oC
Time: Time: 5-10min

## Slide 10: Metallographic evaluation - Gold
Brazing tests (15 September 2021) · Indico (cern.ch)
#1
Another point we can demonstrate is that when the ratio of BFM in the groves is low it can lead to empty areas
Ratio below 1

## Slide 11: Metallographic evaluation – Palcusil5 (Silver)
Brazing tests (15 September 2021) · Indico (cern.ch)
#4
That is the lowest temperature reached in the study and still we can observe a good continuity but we cannot see any CG.

## Slide 12: Metallographic evaluation - Palcusil5 (Silver)
Brazing tests (15 September 2021) · Indico (cern.ch)
#7
Another outcome we can see from this study is that the BFM stops as soon is reaching the end of the channels generating a rounding in the corners and a flat area in the straights surfaces

## Slide 13: Metallographic evaluation - Palcusil5 (Silver)
#4
#5
#6
#7
At CERN
Temp: 815 oC
Time: 10-15 min
We can see there is some continuity in all surfaces in contact.
As we can see in the pictures no crossing grains (CG) are observed. The red region in the UT correspond to non CG.

## Slide 14: Metallographic evaluation - Palcusil5 (Silver)
#7
We see the material stops at the end of the brazing grooves but it generate some diffusion of the Pd or Ag in a range of 2-4mm.
SP1
SP2

## Slide 15: Metallographic evaluation – Pallabraze840 (Silver)
#12
Brazing tests (15 September 2021) · Indico (cern.ch)
That is a medium temperature (870C) and still we can observe a good continuity.
The curious thing we have observe here is that there is material squeezing in the narrow gap between the discs and reaching the RF area

## Slide 16: Metallographic evaluation – Pallabraze840 (Silver)
Brazing tests (15 September 2021) · Indico (cern.ch)
#13
In this picture we can see how the material is going into the gap a in the previous pair.
Here we have a small hint in the middle of one grain that wants to cross but nothing else

## Slide 17: Metallographic evaluation – Pallabraze840 (Silver)
#11
#13
#12
At CERN
Temp: 870 oC
Time: 15-20 min
We can see that the continuity in UT is almost comparable to the gold bunch BUT here, we see that the material diffusion is enter the interface and cover all possible gaps.

## Slide 18: Conclusions
During gold cycles, up to 1000 deg, we observe a good bonding and material remain in the brazing volume.
A sharp edge if very efficient stopping the BFM.
We see that Pallabraze is a safer choice in terms of diffusion because it covers all interface and It allows us to use it in two cycles.
Palcusil5 is a material with a good balance to ensure a good leak despite of having some diffusion in a range of 2-4mm. Only one cycle.
The weight in all tests has not been something influencing the result (<0.05MPa-0.005MPa) or at least we cannot confirm it we the samples we have.

## Slide 19: Smartcell prototype
Ordered a prototype for checking we are going in the right direction (or not).
The prototype has been ordered at CERN to be done completely at CERN
The material used for the prototype is Cu OFE laminated, from CERN Store: 44.09.56.210.1  8880851 - Material Request
 Job J3073539 - Smartcell assembly prototype

## Slide 20
Smartcell prototype

## Slide 21: Smartcell prototype
Very sharp edge
Chamfer
Ratios >= 2
Silver Pallabraze is working ok from the perspective of UT analysis, maintaining the temperature very low during the whole process and if we choose it, we have the advantage of having two steps for brazing.

## Slide 22: Smartcell prototype
#7
The material used for the prototype is Cu OFE laminated

## Slide 23: Smartcell prototype
#7

## Slide 24: Smartcell prototype
#7

## Slide 25: Smartcell prototype
#7
Shift of two cells during the brazing cycle

## Slide 26: Smartcell prototype
#7
Worst part is we got a leak in the second interface

## Slide 27: Smartcell prototype

## Slide 28: Smartcell prototype analysis
#7

## Slide 29: Smartcell prototype analysis
#7

## Slide 30
#1
#2
#4
#5
#6
#3
#9
#10
#7
#8
#11

## Slide 31: Smartcell prototype analysis
#7

## Slide 32
#1
#2
#4
#5
#6
#3
#9
#10
#7
#8
#11
0.8mm
0.8mm
0.8mm
0.8mm
1.1mm

## Slide 33: Smartcell prototype analysis
#7

## Slide 34: Smartcell prototype analysis
#7

## Slide 35: Smartcell prototype analysis
#7

## Slide 36: Smartcell prototype analysis
#7
Disc test
Smartcell test

## Slide 37: Conclusions
The alignment method needs to be improved. New V in granite.
The brackets during brazing do not work properly. More weight.
The BFM silver alloys allow us to use non H2 furnace and lower temperature but on the other hand, they diffuse till the edge (RF region included).
The machining finish is very important to get an homogeneous and good enough continuity between copper parts.

## Slide 38
Thanks for your attention.
Questions??
Thanks to Nuria Catalan, Anastasiya Magazinik, Joel Sauza, Fritz Motschmann, Bodycote, Serge Lebet and all participants from materials, especially Anite Pérez and Enrique Rodriguez