## Slide 1
A. Zampa, P. Tixador and A. Badel
14th July 2022
Current redistribution in the surrounding of a defect during an inhomogeneous quench on a 2G HTS tape

## Slide 2
Context
Influence of local inhomogeneities in the REBCO layer
Current redistribution around a dissipative zone
Conclusions
OUTLINE
1
1
2
3
4
5
Experimental observations of inhomogeneous quenches

## Slide 3
Context
Influence of local inhomogeneities in the REBCO layer
Current redistribution around a dissipative zone
Conclusions
OUTLINE
1
2
3
4
5
Experimental observations of inhomogeneous quenches
1

## Slide 4
Current
Time
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Ic
OPERATION OF A R-SFCL
2
1
2
3
4
5
Context

## Slide 5
Current
Time
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Normal operation
Ic
In
OPERATION OF A R-SFCL
1
2
3
4
5
2
Context

## Slide 6
Time
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Current
Ic
In
Time
OPERATION OF A R-SFCL
Normal operation
1
2
3
4
5
2
Context

## Slide 7
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Current
Ic
In
Dissipative state
Time
OPERATION OF A R-SFCL
Normal operation
1
2
3
4
5
2
Context

## Slide 8
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Current
Time
Ic
In
Dissipative state
OPERATION OF A R-SFCL
Normal operation
1
2
3
4
5
2
Context

## Slide 9
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Zsfcl
Current
Time
Ic
In
Dissipative state
OPERATION OF A R-SFCL
Normal operation
Clearing Fault Time
1
2
3
4
5
2
Context

## Slide 10
Benefits of Resistive-type Superconducting Fault Current Limiter (R-SFCL)
Current
Time
Normal operation
Clearing Fault Time
Vsfcl
Igrid
Vgrid
Z
load
Zgrid
Zsfcl
Ic
In
● A theoretical "infinite" maximum prospective current
● An easier fault current interruption in DC transmission (also AC)
Dissipative state
OPERATION OF A R-SFCL
Normal operation
1
2
3
4
5
2
Context

## Slide 11
REBCO TAPES FOR R-SFCL
3
Substrate
Buffer layers
REBaCuO
Stabilizer
Low cryogenics costs (Tc=92 K)
High resistance per unit length
High current density (600 A/cm,w at 77 K)
Courtesy of Nexans® - THEVA
1
2
3
4
5
Context
No copper stabilization !

## Slide 12
Ic is inhomogeneous along the tape length
Data from THEVA (77 K, self-field)
Current
Time
Normal operation
Ic
In
Dissipative state
Time
Normal operation
Ic
In
Dissipative state
Ic dependencies - Ic(x,T,|B|,θ)
INHOMOGENEITY OF THE IC IN REBCO TAPES
4
Current
1
2
3
4
5
Context

## Slide 13
Context
Influence of local inhomogeneities in the REBCO layer
Current redistribution around a dissipative zone
Conclusions
OUTLINE
6
1
2
3
4
5
Experimental observations of inhomogeneous quenches

## Slide 14
Sample from Theva (77 K)
1
2
3
4
5
6
I
A HTS tape from THEVA with multiple voltage taps connected to a power supply shows inhomogeneous voltages along its length
7
OBSERVATION THROUGH VOLTAGE MEASUREMENTS
Experimental observations of inhomogeneous quenches
2
1
3
4
5

## Slide 15
VISUALIZATION OF A TAPE DURING A QUENCH
8
Experimental set-up to observe the very beginning of a quench
Experimental observations of inhomogeneous quenches
2
1
3
4
5

## Slide 16
9
Sample Superpower ® 67 mm
Cryostat (77 K)
Fault current set-up
Data recorder
High-speed camera
50 000 fps
Pulse
Igrid
Vgrid
Z
sfcl
Zgrid
+
-
Help from A.Derbey & B.Sarrazin
Help from J.Vessaire & M.Gibert
10 ms
Experimental observations of inhomogeneous quenches
2
1
3
4
5
VISUALIZATION OF A TAPE DURING A QUENCH

## Slide 17
10
67 mm
12
mm
Images recorded
for 10 ms
Experimental observations of inhomogeneous quenches
2
1
3
4
5
VISUALIZATION OF A TAPE DURING A QUENCH

## Slide 18
Context
Influence of local inhomogeneities in the REBCO layer
Current redistribution around a dissipative zone
Conclusions
OUTLINE
11
1
2
3
4
5
Experimental observations of inhomogeneous quenches

## Slide 19
RECOGNITION OF LOCAL INHOMOGENEITIES
12
Work carried out by S.Holleis and M.Eisterer from TU Vienna
Measurement of the remnant field after magnetization
Inversion of the magnetic problem gives
y
x
3
1
2
4
5
Influence of inhomogeneities in the REBCO layer

## Slide 20
RECOGNITION OF LOCAL INHOMOGENEITIES
13
3
1
2
4
5
Influence of inhomogeneities in the REBCO layer
Local Ic based on magnetization does not describe all the dissipation phenomena
x
x
x
Positions of bubble columns and inhomogeneities match well
Work carried out by S.Holleis and M.Eisterer from TU Vienna
y
y
y
IEEE TAS

## Slide 21
NON-EPITAXIAL GROWTH OF THE REBCO LAYER
3
1
2
4
5
Influence of inhomogeneities in the REBCO layer
14
Work carried out by S.Holleis and M.Eisterer from TU Vienna

## Slide 22
Context
Influence of local inhomogeneities in the REBCO layer
Current redistribution around a dissipative zone
Conclusions
OUTLINE
15
1
2
3
4
5
Experimental observations of inhomogeneous quenches

## Slide 23
3D FEM ELECTRO-THERMAL MODEL
16
Width (12 mm)
Top silver layer (2 µm)
REBCO layer (1.5 µm)
Hastelloy C276
(100 µm)
Bottom silver layer (1 µm)
Silver on lateral side (1 µm)
Buffer layers (2D/interface)
Thermo-electrical model developed by C.Lacroix & F.Sirois from EPM
Idc
Vsource
R
sfcl
Rcircuit
Xcircuit
+
-
60 mm
● Temperature and current dependence of REBCO layer under Tc
4
1
2
3
5
Current redistribution around a dissipative zone

## Slide 24
3D FEM ELECTRO-THERMAL MODEL
16
Thermo-electrical model developed by C.Lacroix & F.Sirois from EPM
● Temperature and current dependence of REBCO layer under Tc
4
1
2
3
5
Current redistribution around a dissipative zone
● Inhomogeneous critical current density (x,y)

## Slide 25
x
y
z
I
I
I
20
40
0
12
TEMPERATURE EVOLUTION ALONG THE WIDTH
17
x (mm)
z
y (mm)
3 ms
4
1
2
3
5
Current redistribution around a dissipative zone
0 mm
60 mm

## Slide 26
x
y
z
I
I
I
20
40
0
12
TEMPERATURE EVOLUTION ALONG THE WIDTH
17
x (mm)
z
y (mm)
3 ms
4
1
2
3
5
Current redistribution around a dissipative zone
0 mm
60 mm

## Slide 27
CURRENT DENSITY EVOLUTION ALONG THE WIDTH
18
0
12
20
40
0
12
20
40
0
12
20
40
x (mm)
y (mm)
x (mm)
x (mm)
y (mm)
3 ms
3 ms
3 ms
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
y (mm)
I
I
I
I
I
I
I
I
I
With an increasing transport current!

## Slide 28
CURRENT DENSITY EVOLUTION ALONG THE WIDTH
18
0
12
20
40
0
12
20
40
0
12
20
40
x (mm)
y (mm)
x (mm)
y (mm)
x (mm)
y (mm)
3 ms
3 ms
3 ms
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
I
I
I
I
I
I
I
I
I
With an increasing transport current!

## Slide 29
0
12
0
60
60
Temperatures similar on each side of the tape…
TEMPERATURE EVOLUTION ALONG THE LENGTH
19
x (mm)
y (mm)
0
12
0
60
x (mm)
y (mm)
70 K
260 K
70 K
260 K
10 ms
10 ms
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
I
I
I
With an increasing transport current!
I
I
I

## Slide 30
CURRENT DENSITY EVOLUTION ALONG THE LENGTH
20
0
12
x (mm)
y (mm)
0
12
x (mm)
y (mm)
0
0
0
60
0
60
The current density is not identical on the top and bottom silver layers
Temperatures similar on each side of the tape…
10 ms
10 ms
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
I
I
I
With an increasing transport current!

## Slide 31
CURRENT DENSITY EVOLUTION ALONG THE LENGTH
21
y (mm)
10 ms
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
I
I
I
I
I
I
0
60
x (mm)
12
y (mm)
10 ms
x (mm)
12
0
60

## Slide 32
CURRENT DENSITY EVOLUTION ALONG THE LENGTH
22
4
1
2
3
5
Current redistribution around a dissipative zone
x
y
z
I
I
I
I
I
I
y (mm)
10 ms
x (mm)
12
0
60
2
y (mm)
10 ms
x (mm)
12
0
60
2

## Slide 33
CONCLUSIONS
23
5
1
2
3
4
Conclusions & Perspectives
Inhomogeneous and homogeneous dissipation regimes are successive behaviors
Positions of dissipation spots and zones of non-epitaxial growth of the REBCO are in good agreement
Ic as a function of the position should be improved to describe dissipation phenomena
Thermo-electrical mechanism of quench onset
Three practical outputs of the study :
Assessment of the impact of a lack of stabilizer on one side
Voltage taps positions for Ic measurement (superconductor side VS substrate side)
Evaluation of the NZPV through data processing