## Slide 1: HTS solenoids at PSI
Jaap Kosse, Bernhard Auchmann, Michal Duda, Jeroen van Nugteren, Stephan Mueller,
Henrique Rodrigues, Stephane Sanfilippo
12/10/22
Work supported by the Swiss State Secretariat for Education,
Research and Innovation SERI

## Slide 2: CHART2 MagDev @ PSI
CHART2 MagDev at PSI:
  creates magnet-development infrastructure
  LTS (Nb3Sn) technology development for the internat. high-field magnet project
  HTS (REBCO) superbend demonstrator
  bulk-HTS (REBCO) undulators
  HTS capture solenoid for a positron source
“Swiss Accelerator Research and Technology – CHART” is a Swiss research network with PSI as a host institute and CERN, EPFL, ETHZ, and UniGE as additional members (http://chart.ch)
HTS winding
LTS re-reeler
3D Scanning
LTS winding
Heat treatment
Impregnation
Loading / Assembly
Storage
Instrumentation
1)
2)

## Slide 3: CHART2 MagDev: Technology Solenoid Program
Rapidly develop infrastructure for HTS coil manufacturing and testing
via NI coil technology license agreement with Tokamak Energy
Winding
Soldering
Testing
Cryogen-free test station (2 kA)
Tensioning system developed by Francois-Olivier Pincot,
Jacky Mazet, CERN
Pre-tinning support by Davide Uglietti, PSI
Modeling

## Slide 4
NI HTS Technology Solenoid
Stacked, single layer pancakes
Axial joints
4 coils, 12 mm SuperOx tape
Solder-potted coils
r_i 25 mm
r_o 50 mm

## Slide 5
18 T by 4 stack at 2 kA, 12 K

## Slide 6: Cryogen-free test setup
stack of 4 NI HTS coils with thermal/current
connectors
HTS leads
1st cryocooler
4K coldhead
2nd cryocooler
20K coldhead
radiation shield
top plate

## Slide 7: Modeling
Screening currents
NI charging effect
Cool-down and ramping
COMSOL 2D axisymmetric model
H-formulation based on [1]
coupled with thermal model
[1] R Mataira et al, “Finite-element modelling of
no-insulation HTS coils using rotated anisotropic resistivity”, 2020
Disadvantage of axial joints
During ramp
z
r
Note: examples of P3 solenoid

## Slide 8: CHART2 MagDev: Technology Solenoid Program
Rapidly develop infrastructure for HTS coil manufacturing and testing
via NI coil technology license agreement with Tokamak Energy
Winding
Soldering
Testing
Cryogen-free test station (2 kA)
Tensioning system developed by Francois-Olivier Pincot,
Jacky Mazet, CERN
Pre-tinning support by Davide Uglietti, PSI
Modeling

## Slide 9: PSI Positron Production (P3) Experiment
Target and HTS Adiabatic Matching Device
6 GeV beam from SwissFEL linac
Solenoids
Beam diagnostics
RF Cavities
Concept design of P3
N. Vallis, PSI [3]
SuperKEKB Factory (State of the art, 3 GeV) [1] | 0.5
FCC-ee requirements [2] | 2 (incl. safety factor 2)
P3 simulations [3] | 3 (0.4 T RF sol.)-8 (1.5 T RF sol.)
[1] K. Akai, K. Furukawa, and H. Koiso, "Superkekb collider", 2018.
[2] I. Chaikovska et al., "Positron source for FCC-ee", 2019.
[3] N. Vallis, “PSI The P3 experiment: a Positron Source Demonstrator for FCC-ee”, 2022
Goal: experimentally validate high yield in context of FCC-ee, in 2025
Magnetic field [T]
Yield
Yield optimization Y. Zhao, Cern

## Slide 10
NI HTS coils
Target
e-
e+
e-
NI magnet
Compact DC
Radiation
FCC-ee P3
Target power 13 kW 1 W
Shielding ~2 cm tungsten [1] none
P3 experiment is unshielded & will not test radiation robustness
NI HTS solenoid for P3
72 mm warm bore
Coil r_i/r_o 61/115 mm
Conduction cooled, 15 K by RDK 500B #1
1.2 kA leads cooled by RDK 500B #2
15 T bore, 21 T max
[1] B. Humann, CERN

## Slide 11
Copper/lead mass
~200 kg
Neon could work
~40 L
Rely on thermal buffer in case of fault
Case: HTS lead burn-out,
no thermal buffer
Case: HTS lead burn-out,
thermal buffer
J. van Nugteren, Little Beast Engineering
T [K]
T [K]
B [T]
B [T]
Time [s]
Time [s]
Time [s]

## Slide 12: Main worry: axial compressive stress
We’ll probably do destructive tests on our small soldered solenoids in LN2 to measure
[1]
[1] 10.1109/TASC.2020.2966157

## Slide 13: Conclusions
PSI team created infrastructure to wind, solder, test and model HTS coils
Test coil stack reached 18 T
Scaled-up version to be used in positron source experience at PSI in 2025

## Slide 14: Quench event
5 min
Triggered by thermal runaway, due to badly clamped joint