## Slide 1: An R&D path for the muColl silicon tracker
Request for the muColl tracker
State of the art of LGAD-based 4D sensors
Path forward for a muColl tracker based on UFSD_RSD
N. Bartosik, N. Cartiglia, N. Pastrone INFN, Torino

## Slide 2
Setting the stage: resolution and occupancy
Fairly stringent requests for resolutions
Very high occupancy in the vertex detector
To be combined with:
As low as possible material budget
As low as possible power consumption
(strips)
(macropixels)

## Slide 3: First design innovation: low gain avalanche diode (LGAD)
High field obtained by adding an extra doping layer
E ~ 300 kV/cm, closed to breakdown voltage
The low-gain mechanism, obtained with a moderately doped p-implant, is the defining feature of the design.
The low gain allows segmenting and keeping the shot noise below the electronic noise, since the leakage current is low.
The gain layer:
a parallel plate capacitor with high field
zoom
Drift area with gain
0.5 – 2 mm long
Low gain is the key ingredient to good temporal resolution
LGAD optimized for timing are often called Ultra-Fast Silicon Detector (UFSD)

## Slide 4: Summary of UFSD temporal resolution
Resolution without gain
There are now hundreds of measurements on 45-55 mm-thick UFSDs
 Current sensor choice for the ATLAS and CMS timing layers

## Slide 5: UFSD: State-of-the art
Physicist
No gain area ~ 50 um
JTE + p-stop design
CMS && ATLAS choice
Not 100% fill factor
Hit contained in a single pixel
Very well tested
High Occupancy OK
Rate ~ 50-100 MHz
Rad hardness ~ 2-3E15 n/cm2
Trench-isolated design
Almost 100% fill factor
Hit contained in a single pixel
Temporal resolution (50 mm) : 35-40 ps
High Occupancy OK
Rate ~ 50-100 MHz
Rad hardness: ~ 1E15 n/cm2
No gain area ~ 5 um
HPK2
16x16 array
2.1 cm

## Slide 6: Second design innovation: resistive read-out
The signal discharges to ground
The AC pads offer the smallest impedance to ground for the fast signal
The signal is formed on the n+ electrode ==> no signal on the AC pads
-+
-+
-+
-+
-+
-+
Fast signal
long RC
short RC
Fast signal
long RC
short RC
In resistive readout the signal is naturally shared among pads (4-6) without the need of B field or floating pads
Thanks to the internal gain, full efficiency even with sharing
Results presented here are from the FBK RSD2 production

## Slide 7: RSD principle of operation in motion

## Slide 8: Example of signal sharing
Pad 1
Pad 2
Pad 4
Pad 3
0 2 4 6 8
Time [ns]
0 2 4 6 8 10
Time [ns]
0 2 4 6 8 10
0 2 4 6 8 10
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
60
40
20
0
-20
Amplitude [mV]
60
40
20
0
-20
1
2
4
3
P 1
Pad 1
The laser is shot at the position of the red dot: the signal is seen in 4 pads
50-mm thick RSD,
Gain ~ 20

## Slide 9: Experimental set-up
The Particulars TCT laser setup has been used:
  IR laser generates a signal in the RSD,
  simulating the passage of a MIP
  laser spot size ~ 8 μm
  Laser temporal precision: ~ 8 ps
  movable x-y stage provides reference positions of the laser shots, precision: σ Laser~ 2 μm
Sensors are read out with 16-ch fast analogue board, developed at FNAL
The signals are recorded with16-ch CAEN Digitizer (5 Gs)
Amplitude [mV]
Amplitude of pre-signal samples
RMS noise level ~ 1.1 mV

## Slide 10: RSD2 structures used in this analysis (FBK - RSD2 production)
Pitch = 1300 mm
Pitch = 450 mm
200 x 340 mm2
In this study, the perfomance of sensors with electrodes shaped as crosses is presented.
4 different dimensions: 200, 340, 450, and 1300 mm
Pitch = 0.45 mm

## Slide 11: RSD position resolution (FBK RSD2 production)
RSDs at gain = 30 achieve a spatial resolution of about 2-3% of the pitch size:
RSD:
1300 x 1300 mm2: sx ~ 30 mm
450 x 450 mm2: sx ~ 5 mm
Compared to a standard pixel
1300 x 1300 mm2: sx ~ 920 mm
450 x 450 mm2: sx ~ 320 mm
Chart: RSD2 crosses: spatial resolution when the total AC amplitude = 60 mV
| 1300 | 450 | 340 | 200
1300 um | 40 | 15 | 13 | 10
 | 9.6519


Chart: RSD2 crosses: spatial resolution for 4 different pitch sizes
| 29 | 53 | 69 | 154
1300 um | 95 | 50 | 33 | 15.4
450 um | 34 | 25.3 | 19.9 | 15.5 | 10.6 | 10.1 | 8.4 | 7.9 | 10.6
340 um | 44.8 | 34.1 | 21.87 | 19.9 | 13.85 | 12.8 | 10.6 | 7.4 | 6.33
200 um | 45.9 | 26 | 24.13 | 18.5 | 15.9 | 10.5 | 8.5 | 7.8 | 5.2 | 4.4
gain = 30

## Slide 12: RSD temporal resolution (FBK RSD2 production)
Chart: RSD2 Crosses: time jitter for 3 different pixel sizes
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185
Calculated Jitter | 240 | 120 | 80 | 60 | 48 | 40 | 34.2857 | 30 | 26.6667 | 24 | 21.8182 | 20 | 18.4615 | 16 | 14.1176 | 12.6316 | 11.4286 | 10.4348 | 9.6 | 8.8889 | 8.2759 | 7.7419 | 7.2727 | 6.8571 | 6.4865
1300 x 1300 um^2 | 56.745 | 32.8786 | 23.4028
450 x 450 um^2 | 36.3716 | 28.9083 | 22.7264 | 17.598 | 16.4973 | 15.3704 | 14.2113
200 x 340 um^2 | 54.8016 | 56.5406 | 39.4137 | 30.3111 | 18.6773 | 15.7493 | 12.0416 | 8.6626 | 7.7775
gain = 30
The resolution depends mostly upon the signal size and weakly on the pixel size
RSDs at gain = 30 achieve a temporal jitter of about 20 ps

## Slide 13: RSD2 performance summary

## Slide 14: Final goal of RSD R&D: a completely new tracker
The design of a tracker based on RSD is truly innovative:
It delivers ~ 20 -30 ps temporal resolution
For the same spatial resolution, the number of pixel is reduced by 50-100
The electronic circuitry can be easily accomodated
The power consumption is much lower, it might even be air cooled (~ 0.1-0.2 W/cm2)
The sensors can be really thin
Standard tracker
RSD-based tracker

## Slide 15: Matching UFSD-RSD capabilities to the muColl requests
High occupancy and levels.
TI-LGAD can be used up to 1-2E15 n/cm2
R&D in radiation harness needed to cover the full radiation field
Low occupancy and radiation levels. Ideal for macro-pixels.
Pixel size, spatial, and temporal resolutions are a perfect fit for present RSD technology
RSD will strongly reduce the number of pixels
Very Low-occupancy and radiation levels. Long strips do not provide accurate temporal resolution.
Propose to replace it with RSD macro pads

## Slide 16: Conclusions
In Torino we are continuing the development of TI-LGAD and RSD for applications to the muColl tracker
UFSD and RSD offer very good combined spatial and temporal performances
These designs are a good fit to the need of the muColl design
Cell size | Number of cells | Thickness | Detector
To be decided |  | 50 um | TI_LGAD
200 um x 2 mm | 1/8 # of present design | 50 um | RSD
200 um x 2 mm | Similar to the present design | 50 um | RSD
Very difficult (impossible?) to achieve good timing with strips
Better to use macro-pads?
Proposed detector