## Slide 1: FBK LGAD Technology for fast timing
FBK LGAD group: A. Bisht, G. Borghi, M. Boscardin, M. Centis Vignali, F. Ficorella, O. Hammad Ali, G. Paternoster
paternoster@fbk.eu
1st MONOLITH Workshop on silicon sensors for timing and their applications
Genève, 5-6 Sept. 2022
UFSD group
INFN Torino, Univ. of Turin, Univ. of Piemonte Orient, Univ. of Trento, FBK Trento, Univ. of California at Santa Cruz.

## Slide 2: Introduction and Motivation
LGAD Technology developed at FBK since 2015
Developed together with INFN Turin and University Trento for 4d-tracking
More than 15 batches produced since 2015
High Luminosity LHC (HL-LHC, operational in 2026):
  Luminosity: ×5 compared to LHC  150-200 events per bunch crossing
  Timing and spatial resolution of standard silicon tracking sensors not sufficient: 10-15% of vertexes composed of 2 events
Requirements for silicon timing detectors in HL-LHC:
  Timing resolution: 30 ps (rms)
  Low spatial granularity: ~1 mm (timing information assigned to the track)
  High radiation hardness: > 1·1015 neq·cm-2
Motivation

## Slide 3: LGAD Technology
p-
n+
oxide
metal
p
E Field
Silicon detectors with internal charge multiplication
Gain: 10-20
Gain layer provides high-field region
Depleted thickness: 20 - 100 µm (epi or Si-Si wafers)
Time resolution 30 ps with thin 50 µm sensor
Improve SNR of the system (when the sensor shot noise is not dominating)
Low Noise and power consumption
n+
metal
p
p
p++
Technological features
Main functionalities
20 - 100 µm

## Slide 4: LGAD Fabrication Technology
Fabricated on 6 inches Wafers
Custom CMOS-like Technology
Fabricated in the FBK internal facility (ISO 9001:2015 certified)
Single pads,
Pad arrays;
Strips;
Other pixelated detectors….
Large area detectors
Up to ~ 3x3 cm2

## Slide 5: FBK LGAD Technology Roadmap
UFSD
Fast timing and radiation resistance
4D-tracking at HL-LHC
iLGAD (double-sided)
Fine-segmentation, Thin-Entrance window
RSD (Resistive
Silicon Detectors)
TI-LGAD (trench-isolated)
Soft x-ray detection
New red-out paradigm: high temporal- and space-resolution with reduced # of channels
4D-tracking
Fine segmentation, fast-timing, radiation resistance
4D-tracking, soft x-ray
Different designs, optimized for different applications

## Slide 6: UFSD: Recipe for fast timing
Key factors governing time resolution of LGADs.
Both design & technology
HR p-type
n+
oxide
metal
Gain layer
n+
metal
Gain layer
p
LR p-type
Thickness
Gain
Drift velocity of e- in the bulk
Pad geometry (weighing field)

## Slide 7: Recipe for fast timing
Gain
Gain depends on GL dose and Bias Voltage
High Gain reduces the jitter
At too high gain the time resolution is dominated by Landau noise
Target gain should be reached at a Bias where the e- velocity in the bulk is saturated (E > 3e4 V/cm)
For 50 µm the target is G~10 at V > 200 Volts
Sadrozinski et al 2018 Rep. Prog. Phys. 81 026101
timing
Bulk Efield
Rule: use the minimum gain that allows
reaching the minimum value in time resolution
Landau floor
jitter
Working point

## Slide 8: Recipe for fast timing
Thickness
Reducing Thickness ->
Higher slew-rate
Lower Landau and Time-walk
High capacitance
Less radiation resistance (SEB)
Trade off ~ 50 um
Sadrozinski et al 2018 Rep. Prog. Phys. 81 026101

## Slide 9: Recipe for fast timing
Latest test with ultra-thin LGADs 35 m and 25 m
F. Carnesecchi, arXiv:2208.05717
Ultra-thin sensors produced at FBK (EXFLU project)
Characterized at INFN Bologna, INFN Turin and CERN
35µm thick LGADs approach 20ps time resolution (mainly thanks to Landau noise reduction)
No further improvement moving to 25 µm. Possible causes:
  higher substrate doping (not saturated electrons velocity in the bulk)
  Higher noise of the sample
Wafers from eXFlu0 production
Thickness

## Slide 10: Radiation Hardening
Initial Acceptor removal
Increasing Fluence
During irradiation the Gain of LGADs is reduced
The mechanism can be explained with a reduction of the acceptor concentration in the Gain Layer
It is possible to partially compensate the gain-loss by increasing the bias voltage
Gain is completely lost after 1e15 neq/cm2
Possible microscopic mechanism: Boron de-activation due to Si interstitial
(𝒅𝒐𝒏𝒐𝒓−𝒍𝒊𝒌𝒆)

## Slide 11: Radiation Hardening
Carbon Co-implantation for acceptor removal mitigation
Carbon co-implantation Optimization
Carbon Dose
Carbon implantation depth
Thermal load Boron/Carbon for activation and diffusion
Carbon Enables competing mechanism
(donor-like)
No Carbon
+ Carbon (optimal dose)
(neutral)
Many split on C dose
Boron
Carbon
Carbon implanted only in the Gain Layer at the same depth (overlapping to Boron)
Boron removal
Carbon co-implantation

## Slide 12: Radiation Hardening
Carbon co-implantation for acceptor removal mitigation
Radiation resistance improving
Acceptor removal coefficient
Different carbon doses and Thermal Load
[M. Ferero, INFN To, 37th RD50 Workshop ]
Higher initial boron Density
Recipe for high radiation resistance
Using optimized Carbon dose
Increase boron density (w/o increasing the gain too much)

## Slide 13: Radiation Hardening
Gain layer optimization
Higher initial boron Density
Low thermal budget
Higher Boron concentration -> lower c factor
Shallow B implant (more dose for the same gain)
Narrower (low diffused) B profiles
Boron depth: Shallow (~1um) or Deep
Thermal diffusion (low or high)
Disadvantages of a Shallow gain layer:
• Worst gain recovery than deep-gain implant, using external bias
Shallow GL
Deep GL

## Slide 14: Radiation Hardening
Carbon Co-implantation for acceptor removal mitigation
Shifting (or adding) an additional Carbon implant deeper than the Gain Layer (Carbon shield)
More tests are ongoing…
Boron
Boron
Carbon
Boron
Boron
Carbon
Carbon
Carbon
i) No Carbon
ii) Carbon in the Gain Layer (GLC)
iii) Carbon shield (CS)
iv) GLC + CS
(the right place to add Carbon has still to be understood…)
First tests on GLC + CS show a further decreasing of the c factor of ~ 20%.

## Slide 15: Recipe for fast timing
Time resolution
< 30 ps up to 1e15 neq/cm2
< 40 ps up to 2.5e15 neq/cm2
Demonstrated radiation resistance and time resolution for HL-LHC

## Slide 16: Recipe for fast timing
Production qualification
ATLAS - HGTD
CMS - ETL
Full sensors ~ 2 x 2 cm2
15 x 15 and 16 x 16 arrays
1.3 mm2 pads
UFSD 4 batch for final sensor qualification

## Slide 17: Novel LGAD schemes for fine-segmentation
Segmented Standard LGAD
Trench-Isolated LGAD
n+/p+
Multiplication region
n+
Gain layer
Epi-silicon (p-)
Support wafer (p+)
Epi-silicon (p-)
Support wafer (p+)
    JTE and p-stop are replaced by a single trench (< 1 um wide)
    Trenches act as a drift/diffusion barrier for electrons and isolate the pixels.
Trench Isolated - LGAD Technology
    No-gain region at the pixel border due to isolation and termination structures: JTE and p-stop
    Dead distance for charge multiplication ~ 40 - 80 μm
no-gain region ~ 60um
no-gain region < 5 um

## Slide 18: Novel LGAD schemes for fine-segmentation
Trench Isolated - LGAD Technology
Pixels 55 × 55 µm2 (Medipix/Timepix)
FF > 80%
Inter-pad distance
Measured with TCT setup (red laser)
Pixel 1
Pixel 2
laser scanning
Interpixel distance in the range 2-10 um (depending on the layout split)
Measured at INFN TO (courtesy of M. Ferrero)

## Slide 19: Novel LGAD schemes for fine-segmentation
Trench Isolated - LGAD Technology
Pixels 55 × 55 µm2 (Medipix/Timepix)
FF > 80%
Time Resolution (jitter)
Measured with TCT setup (red laser)
Not-degradated time resolution wrt standard LGADs
Time resolution (laser setup) < 10 ps
M. Senger – VCI 2022
Jitter (s)
Bias (Voltage)

## Slide 20: RSD – Resistive Silicon Detectors (aka AC-LGADs)
Resistive n+
Thin coupling dielectric layer
AC pads
p+ implant
DC Bias Pad
Main Technological Features
Not-segmented p-gain implant
Resistive n+ implant
AC Metal pads
Segmented Standard LGAD
n+
Gain layer
Epi-silicon (p-)
Support wafer (p+)
Resistive Silicon Detectors
RSD is not just an LGAD with AC-pads. It is a different way to read-out the signal and to segment the sensor

## Slide 21: RSD – Resistive Silicon Detectors (aka AC-LGADs)
The signal spreads on several pads, with amplitude inversely proportional to the hit distance
N. Cartiglia
TCT Measurements with IR Laser Setup
Laser Spot
How does it works
Chart: RSD2 crosses: spatial resolution when the total AC amplitude = 60 mV
| 1300 | 450 | 340 | 200
1300 um | 40 | 15 | 13 | 10
 | 9.6519


the resolution is 3% of the pixel size
RSD2 production

## Slide 22: RSD – Resistive Silicon Detectors (aka AC-LGADs)
N. Cartiglia
Time resolution
Chart: RSD2 Crosses: time jitter for 3 different pixel sizes
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185
Calculated Jitter | 240 | 120 | 80 | 60 | 48 | 40 | 34.2857 | 30 | 26.6667 | 24 | 21.8182 | 20 | 18.4615 | 16 | 14.1176 | 12.6316 | 11.4286 | 10.4348 | 9.6 | 8.8889 | 8.2759 | 7.7419 | 7.2727 | 6.8571 | 6.4865
1300 x 1300 um^2 | 56.745 | 32.8786 | 23.4028
450 x 450 um^2 | 36.3716 | 28.9083 | 22.7264 | 17.598 | 16.4973 | 15.3704 | 14.2113
200 x 340 um^2 | 54.8016 | 56.5406 | 39.4137 | 30.3111 | 18.6773 | 15.7493 | 12.0416 | 8.6626 | 7.7775
The temporal resolution does not depend on the pize size, only on the total amplitude.
(total amplitude = sum of the amplitudes of the 4 read-out electrodes at the pixel corner)
RSD2 crosse overall result:
Spatial resolution ~ 3% pitch size
Temporal resolution ~ 35 ps, regardless of pitch size

## Slide 23: RSD – Resistive Silicon Detectors (aka AC-LGADs)
Final GOAL
23
The design of a tracker based on RSD: It delivers ~ 30 ps temporal resolution and excellent spatial resolution with large pixels
For the same spatial resolution, RSD trackers use 50-100 fewer pixels
The electronic circuitry can be easily accommodated
The power consumption is much lower;
Standard tracker
RSD-based tracker

## Slide 24: Conclusions
In the last years FBK developed LGADs technology for 4D-tracking
Last developments in LGAD lead to time resolution ~30ps up to fluences of 2.5e15 neq, mainly thanks to the using of thin substrates and initial acceptor removal mitigation
The radiation resistance can be further increased by optimizing Carbon co-implantation or dopant co-implantation
The new TI-LGAD technology preserves the time resolution of LGADs scaling down the pixel size to few tens of microns.
RSD technology can combine the 30ps time resolution, few microns space resolution and radiation hardness with a reduced number of read-out channels.

## Slide 25: Thank you for your attention
paternoster@fbk.eu
Acknowledgements
Part of the work has been performed in the framework of RD50
Some batches have been produced in the framework of convenzione INFN/FBK
Horizon 2020, grant UFSD669529
Progetto PRIN2017, MIUR, 4DInSide, Prin2017
Progetto FARE, MIUR, R165xr8frt_fare
Dipartimenti di Eccellenza, Torino Physics Dep. (ex L. 232/2016, art. 1, cc. 314, 337)
UFSD group
INFN Torino, Univ. of Turin, Univ. of Piemonte Orient, Univ. of Trento, FBK Trento, Univ. of California at Santa Cruz.

## Slide 26: Radiation Hardening at extreme fluences
Psphorous/Boron co-doping
GOAL: operate LGADs at fluence > 1016 neq/cm
eXFlu project (V. Sola, INFN To)
F= 1e16 neq/cm2
Gain layer is obtained by co-implanting Boron and Phosphorous
1*B -> 5*B + 4*Ph
No acceptor removal after F= 1e16 neq/cm2
It works under the assumption (cA  cB)
Production to be completed in October 2022

## Slide 27: LGAD – Radiation hardness
[Ryan Heller, 38th RD50 Workshop]
[Gordana Lastovicka-Medin, 38th RD50 Workshop]
Death of highly irradiated LGADs at test beam
Probably due to a rare, large ionization events producing large current in narrow path
Mortality is function of sensor thickness and voltage only (Gain is not necessary for death mechanism)
Fatal voltage: > 600V for 50 um Sensors
Fatal Voltage becomes lower for thinner sensors
SEB = Single Event Burnout
Thickness

## Slide 28: TI-LGAD Production Batch: Electrical characterization
TCT Setup with IR Laser
200V and RT
2x2 pixels
1.3 mm2 pixels
ATLAS/CMS Timing Layer
+ light
Dark current ~ 10 pA/mm2
Automatic IV characterization
GAIN

## Slide 29: Temporal resolution
Chart: RSD2 Crosses: time jitter for 3 different pixel sizes
| 5 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45 | 50 | 55 | 60 | 65 | 75 | 85 | 95 | 105 | 115 | 125 | 135 | 145 | 155 | 165 | 175 | 185
Calculated Jitter | 240 | 120 | 80 | 60 | 48 | 40 | 34.2857 | 30 | 26.6667 | 24 | 21.8182 | 20 | 18.4615 | 16 | 14.1176 | 12.6316 | 11.4286 | 10.4348 | 9.6 | 8.8889 | 8.2759 | 7.7419 | 7.2727 | 6.8571 | 6.4865
1300 x 1300 um^2 | 56.745 | 32.8786 | 23.4028
450 x 450 um^2 | 36.3716 | 28.9083 | 22.7264 | 17.598 | 16.4973 | 15.3704 | 14.2113
200 x 340 um^2 | 54.8016 | 56.5406 | 39.4137 | 30.3111 | 18.6773 | 15.7493 | 12.0416 | 8.6626 | 7.7775
The temporal resolution does not depend on the pize size, only on the total amplitude.
(total amplitude = sum of the amplitudes of the 4 read-out electrodes at the pixel corner)

## Slide 30
Chart: RSD2 crosses: spatial resolution when the total AC amplitude = 60 mV
| 1300 | 450 | 340 | 200
1300 um | 40 | 15 | 13 | 10
 | 9.6519


Chart: RSD2 crosses: spatial resolution for 4 different pitch sizes
| 29 | 53 | 69 | 154
1300 um | 95 | 50 | 33 | 15.4
450 um | 34 | 25.3 | 19.9 | 15.5 | 10.6 | 10.1 | 8.4 | 7.9 | 10.6
340 um | 44.8 | 34.1 | 21.87 | 19.9 | 13.85 | 12.8 | 10.6 | 7.4 | 6.33
200 um | 45.9 | 26 | 24.13 | 18.5 | 15.9 | 10.5 | 8.5 | 7.8 | 5.2 | 4.4
Spatial resolution as a function of the signal amplitude for 4 pitch sizes
Executive summary: the resolution is 3% of the pixel size
(total amplitude = sum of the amplitudes of the 4 read-out electrodes at the pixel corner)

## Slide 31
Latest FBK RSD production RSD2
RSD2 crosse overall result:
Spatial resolution ~ 3% pitch size
Temporal resolution ~ 35 ps, regardless of pitch size
The key feature of RSD2 is to design the electrodes to have as little metal as possible and to maximize sharing among the read-out pads at the corner of the pixel

## Slide 32
(B)
(A)
Example of uniformity in the time resolution over the whole pad
Plot obtained by shooting laser shots (TCT system) over the whole pixel surface and comparing the trigger time with the reconstructed time