## Slide 1: MARTHA - Monolithic Array of Reach Through Avalanche photo Diodes
R. Richter, A. Bähr, J. Damore, Ch. Koffmane, R. Lehmann, J. Ninkovic, G. Schaller, M. Schnecke, F. Schopper, J. Treis

## Slide 2: MPG HLL
Central facility of the Max Planck Society
40 scientists, engineers and technicians
+ guest scientists, and students
sensor
  simulation
  design
  fabrication
camera
  design
  assembly
  test
New Building
  IPP Campus Garching
  currently moving
  1500 m² cleanroom area
  600 m² ISO3 & ISO4 area
  6/8 inch silicon process

## Slide 3: MPG HLL – some examples
electron (7GeV)
positron (4GeV)
Vertex Detector
2 layers DEPFET + 4 layers DSSD
DePFETs at KEK - Japan
DePFET for particle tracking
curtesy Belle2 collaboration
WFI on Athena
DePFET - X-ray imaging spectroscopy
curtesy ESA
We also produce
-SDD (silicon drift detectors)
-Diodes
-Avalanche Diodes
-Strip Detectors
-etc.
XMM-Newton
  pnCCD
  X-ray imaging spectroscopy
  curtesy ESA
DePFET -planetary science
curtesy ESA
MIXS on BepiColombo

## Slide 4: Martha - APDs for soft X-Rays
(Soft X-ray) Photon Counting For applications at FELs
(HLL) thin entrance window + avalanche multiplication
homogeneous gain
high k-factor (low excess noise)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel

## Slide 5: Martha - Interpixel isolation
Interpixel isolation requirements
Isolation
Suppress edge break down
Reduction of E-fields at interface
(oxide charge up, H-bond cracking)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
?

## Slide 6: Strip array 50µm pitch (2D simulation)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
MOS Isolation
450µm
10µm
HF region extends over pixel gaps
Reach-through APD
50 µm pitch
MOS isolation
Based on HLL „standard“ technology

## Slide 7: Strip Array (2D Simulation)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
MOS Isolation
450µm
10µm
HF region extends over pixel gaps
100µm

## Slide 8: Strip Array (2D Simulation)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
MOS Isolation
450µm
10µm
HF region extends over pixel gaps
100µm

## Slide 9: Strip Array (2D Simulation)
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
MOS Isolation
450µm
10µm
HF region extends over pixel gaps
Avalanche (breakdown) at edges
Approach not usable
100µm

## Slide 10: 2D Simulation Edge Breakdown Suppression
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
p+ cathode
p multiplication layer (ML)
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
100µm
100µm

## Slide 11: Edge Breakdown Suppression
deep implant (6 µm)
extend ML
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
100µm
Deep Implant
Field-Drop Layer
Notes: high energy implant + low bulk doping ensures
flat ‘plate capacitor like‘ electric field distribution
Wide high field region -> lower e-field (same gain)
-> lower k factor -> lower excess noise factor

## Slide 12: 2D Simulation Edge Breakdown Suppression
HF region
extends over
pixel gaps
HF region and
field drop layer
extend over
pixel gaps
VMOS=3V

## Slide 13: Simulated signal Evolution (Current)
full signal formed faster in reference structure
(generated drift to backside)
‘anti cross talk‘
450m
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
100µm
solid - with avalanche
dashed - without avalanche
generate test charge Qtest = 1.3x10-16 C

## Slide 14: Simulated signal Evolution (charge)
-> M = 14.8
450m
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
100µm
solid - with avalanche
dashed - without avalanche
generate test charge Qtest = 1.3x10-16 C

## Slide 15: Gain in the Gap region
450m
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
100µm
variation of injection position in x
generate test charge Qtest = 1.3x10-16 C

## Slide 16: Gain in the Gap region
reduce gap size
reduce gain inhomogeneity
450m
p multiplication layer (ML)
p+ cathode
p- drift region
n+ contact
n+ contact
left pixel
right pixel
450µm
10µm
n field drop layer
100µm
variation of injection position in x
generate test charge Qtest = 1.3x10-16 C

## Slide 17: What happens in the gap region? Gap loss gets ‘compensated’
not at implant edges (no edge BD)
field peaks

## Slide 18: Final Array
Expected features
Gain up to 20
Collection efficiencies: > 99%
Pixel pitch: given by bump bond technology
and ro electronics space consumption (ATLAS 50µm)
Position resolution: <<
Time resolution:
Leading edge trigger: <50ps
Full signal formation 50ns (450µm)

## Slide 19: Prototype production
Pixel Strips Diodes MGR Diodes
production finished
tests started
Aims
proof of principle
Efficiency, gain, cross talk, noise
find reliable narrow guard ring structure
(in view of buttable arrays)
n+ pixel or strips
backside p+ entrace window
non structured, no Al
Vframe
Vinn_guard
Vbias
via CE
p- bulk
high field
MOS grid

## Slide 20: APD Diodes with and without Gaps
n field drop layer
p multiplication layer
N+
N+
N+
n field drop layer
p multiplication layer
N+
N+
N+
N+
p multiplication layer
plane diode
diode with gaps
and FDL
diode with gaps
but without FDL
diodes 2x2mm²
Edge breakdown suppression
works as intended

## Slide 21: Homogeneity of high energy implantation (multiplication region)
R. J. McIntyre, 1985
Typical Reach-Through APD IVs
diodes with gaps
point of inflection VA
p multiplication region fully depleted
no difference between diodes and gap diodes
(preliminary)
VA

## Slide 22: summary
MARTHA – a new approach for an APD pixel array
operated in RT proportional mode
no inter pixel dead space
suitable for large pixel arrays
low excess noise due to HE high field implantation
First prototyping – small APD arrays and strips
will be tested further soon

## Slide 23: Outlook
tAPD 20µm
p-
p
n+ anodes
high field region
t_handle_wafer ≈ 400µm
light entrance window
thin p+ cathode
next steps:
proof of concept measurements (started)
discussions with potential users and ASIC designers
MARTHA sensors can also be produced on thinned wafers
  improved timing capabilities
Notes: tAPD = 20µm: drift times (triggering electrons + amplified holes) ≈ 0.5ns
ED100V: 1.46 * 1010 cm-2 (450µm), ≈ 3 * 1011 cm-2 (20µm)
To switch on the gain from 1 to 10: Dp < 2 * 1011 cm-2 (tHF = 5.5µm) or ≈ 65V
Build a 20µm detector with M = 1 @Vdepl and M ≈ 10 @65V overbias
play around with thicker sensors and wider tHF …

## Slide 24: Thanks for your attention
R. Richter, A. Bähr, J. Damore, Ch. Koffmane, R. Lehmann, J. Ninkovic, G. Schaller, M. Schnecke, F. Schopper, J. Treis

## Slide 25: Backup Slides

## Slide 26: Pixel Capacity
expected pixel capacity
50um Pixel 3um gap: ca. 35fF
50um Pixel 10um gap: ca. 20fF

## Slide 27: HLL thin entrance window
fully depleted
  sensitive over the complete bulk
  thickness 50 .. 450 .. 1000 µm
  thin, non-structured entrance window
  QE > 90% for 0.3 keV < E < 15 keV
  radhart @ soft X-rays (self shielding)
backside irradiation
  100 % fill factor
  optional light (& UV) filter
integrated first amplifier
  low noise
  fast readout
  emi robust

## Slide 28: Optimization for soft X-ray detection (low excess noise)
deep implant (6 µm)
extend ML
Excess noise factor
F = M * k + (2 - ) (1 - k)
k < 1
The lower E the lower k
the lower the noise but the lower gain!
A. Pilotto et. al. (2022)
Notes: high energy implant + low bulk doping ensures
flat ‘plate capacitor like‘ electric field distribution
Wide high field region -> lower e-field (same gain)
-> lower k factor -> lower excess noise factor

## Slide 29: MPG HLL
Central facility of the Max Planck Society
40 scientists, engineers and technicians
+ guest scientists, and students
At present
Siemens Campus Neuperlach Munich
1000m2 of clean room area
330m2 of ISO3 area
Full 6 inch silicon process line
1500m2 of clean room area
600m2 of ISO3 & ISO4 area
8 inch silicon process line
New building
IPP Campus Garching
in autumn 2023 – move started