## Slide 1: Single-electron counting, fully depleted charge-coupled devices for dark matter detection
Steve Holland
Lawrence Berkeley National Laboratory
December 7th, 2023

## Slide 2: Outline
Fully depleted CCDs: basic concepts and applications in astronomy
Direct Dark Matter detection with single-counting Skipper CCDs / Multiple-amplifier sampling CCDs

## Slide 3: DOE Stage III Dark Energy Survey (2013-2019)
Dark Energy Camera: FNAL/LBNL
570 Mpixels
250 um thick, fully depleted CCDs
Teledyne DALSA Semiconductor/LBNL
DOE Stage 3 Dark Energy project
HyperSuprime CAM
870 Mpixels
200 um thick, fully depleted CCDs
Hamamatsu Corporation
Satoshi Miyazaki (PI) and Yukiko Kamata (CCD testing)
National Astronomical Observatory of Japan
Cryogenic operation ~ 140K
~ 100 kpixels/sec
HEP detector spinoff

## Slide 4: DOE Stage III Dark Energy Survey (2013-2019)
Dark Energy Camera
1st light Sept 2012
1.1M + images to date
150 mm high resistivity Si
(15 um)2 pixels

## Slide 5
HyperSuprimeCam – 116 2k x 4k, (15 µm)2-pixel CCDs (870 Mpixels)
CCDs from Hamamatsu Corporation / Subaru 8-m Telescope
Full moon for scale

## Slide 6: Fully depleted CCDs 101
CCD fabricated on a high-resistivity silicon substrate that is fully depleted by the application of a substrate bias
Merging of CCD / p-i-n detector
  HEP spinoff
Typical thickness for astronomy is 200 – 250 µm
Thick device results in high near-infrared response
Main advantage for astronomy
  Detect high redshift objects
Not to scale

## Slide 7
Near IR – Silicon becoming transparent, Eph< Si bandgap (~ 1.1 eV)
Blue end – Strong absorption in dead layers (n+ of p-i-n structure)

## Slide 8
Dark Energy Spectroscopic Instrument
DOE Stage 4 Dark Energy project

## Slide 9: Backside layers: LBNL CCDs
TEM cross-sectional image
SiO2
ZrO2
ITO
In-situ doped polysilicon
Silicon substrate
n+ polysilicon
High-r n-type substrate
AR coating design by Don Groom

## Slide 10
MEDICI simulations
Potential minimum (collecting phase)
Relatively insensitive to Vsub
Capacitor voltage divider effect
Wide range of Vsub possible
Vsub = 80V
Vsub = 30V
Fully depleted CCDs / 2D simulations

## Slide 11
Fully depleted CCDs in space applications
Transiting Exoplanet Survey Satellite
Launch date April 18, 2018
4 x 4096 x 4096 (15 um)2 pixels
100 um thick
Fabrication at MIT Lincoln Laboratory
Xtend soft x-ray imaging telescope
XRISM
Launch date Sept 6, 2023
4 x 1028 x 1028 (24 um)2 pixels
200 um thick
Fabrication at Hamamatsu Corp
https://doi.org/10.1117/12.2626894
https://doi.org/10.1117/12.2560348
https://doi.org/10.1016/j.nima.2020.164676
https://doi.org/10.1002/asna.20230139

## Slide 12: Dark Matter detection with CCDs
Proposed by Juan Estrada et al of FermiLab (2008)
    https://doi.org/10.48550/arXiv.1105.5191
  Low noise / improves low-energy detection threshold
    Si bandgap ~ 1.1 eV
  Thick CCDs for larger mass/CCD
  Expected dark-matter particle interactions
    Nuclear recoil (silicon nucleus)
    Scattering off electrons
Si

## Slide 13: Dark Matter detection with CCDs
  1st underground engineering run / one 4 Mpixel DECam CCD
    https://doi.org/10.1016/j.physletb.2012.04.006
      2 e- noise (2012) now deep sub-electron (Skipper CCDs)
      250 um thick (2012) now 650-725 um (all fully depleted)
      Dark current orders of magnitude less than astronomy CCDs
      All processing at foundry
        ~ 5 – 6 um backside P layer from the gettering process
    SENSEI / DAMIC-M / OSCURA are 0.1/1/10 kg scale

## Slide 14
LBNL Dark Matter CCD development
SENSEI@SNOLAB
2 km underground
100 g scale experiment
1 lot of 25 wafers
Full fabrication at DALSA
6k x 1k / (15 um)2 / 650 um thick
1st science run was
9/2022 – 4/2023
Copper cryostat
Lead shield

## Slide 15
Parameter | DESI | SENSEI1
CCD format Thickness | 4k x 4k (15 um)2 250 um | 6k x 1k (15 um)2 650 um
Read noise | 2.5 – 3.0 e- rms | 0.13 e- rms See note 1
Dark current | ~ 1 e-/pixel-hour (133K) | ~ 1.6 x 10-4 e/pix-day (135K) See note 2
Exposure time | 15 minutes | 20 hours
Readout time | 1 minute | 7.7 hours
1
DESI (astronomy) vs SENSEI (DM)
Note 1: Skipper CCD with 300 samples / pixel
Note 2: Cold Cu, some shielding / 100 m underground
Number quoted is the single-electron event rate
PRL 125.171802

## Slide 16: Skipper CCD operation
Multiple, nondestructive reads of the charge (floating-gate)
Noise ∝ Inverse square root of the number of samples
  1990 results
    0.5 e- noise but no improvement after 256 samples
Invented by Jim Janesick
  U.S. patent 5250824 (1993)
Based on the floating-gate amplifier (1970’s)
https://doi.org/10.1117/12.19452
https://doi.org/10.1117/12.19457

## Slide 17
Floating-gate amplifier
LBNL implementation (floating-gate amplifier)

## Slide 18: Version 2 Skipper CCD tested at FermiLab
2nd version (LDRD 2013)
  0.068 e- after 4k samples (2017)
FG amplifier CCDs
https://doi.org/10.1103/PhysRevLett.119.131802

## Slide 19: Version 2 Skipper CCD tested at FermiLab
2nd version (LDRD 2013)
  Low-level light charge histogram (FermiLab)
FG amplifier CCDs

## Slide 20
Measurements and animation from FermiLab

## Slide 21
[e-]
x [pixel]
y [pixel]
Skipper-CCD basics
Measurements and animation from FermiLab

## Slide 22: Dark Matter detection with CCDs
Following topics
  “Dark current” / background single-electron rates
    Astronomy versus dark matter CCDs with shielding
  Particle ID via energy deposit and spatial signature
  Depletion of thick CCDs (650 – 725 um thick)
  Faster readout Skipper CCDs for astronomy
Lead shield
HyperSuprime Cam
Astronomy
SENSEI
Dark Matter

## Slide 23
CCD DM background count rates not dominated by SHR electron-hole generation (dark current)
  IR shielding (cold Cu surrounding the CCD) / Underground / Pb shielding
  Carefully chosen, low-background radiation materials near the CCD
Publications
2018 Surface run prototype CCD
  PRL 121.061803
2019 Underground prototype CCD
  PRL 122.161801
2020 Underground science CCD
  PRL 125.171802
2022 Surface IR and Pb shield
  PhysRevApplied.17.044050
2022 Cherenkov / e/h recombination
  PhysRevX.12.011009

## Slide 24: Dark Matter detection with CCDs
Following topics
  “Dark current” / background single-electron rates
    Astronomy versus dark matter CCDs with shielding
  Particle ID via energy deposit and spatial signature
  Depletion of thick CCDs (650 – 725 um thick)
  Faster readout Skipper CCDs for astronomy
Lead shield
HyperSuprime Cam
Astronomy
SENSEI
Dark Matter

## Slide 25: Dark Matter detection with CCDs
Fully depleted CCDs for dark-matter detection cont’
  Particle identification for background suppression
    Spatial correlation and energy measurement

## Slide 26: Dark Matter detection with CCDs
Fully depleted CCDs for dark-matter detection cont’
  Radioactive contamination in the silicon substrate
    Decay chain products spatially correlated (double b event below)
              Candidate 32Si – 32P event
              Cosmogenic activation of silicon
              Rejected by spatial / energy / decay time correlation
https://iopscience.iop.org/article/10.1088/1748-0221/10/08/P08014

## Slide 27: Dark Matter detection with CCDs
Following topics
  “Dark current” / background single-electron rates
    Astronomy versus dark matter CCDs with shielding
  Particle ID via energy deposit and spatial signature
  Depletion of thick CCDs (650 – 725 um thick)
  Faster readout Skipper CCDs for astronomy
Lead shield
HyperSuprime Cam
Astronomy
SENSEI
Dark Matter

## Slide 28: Dark Matter detection with CCDs
CCD mass is limited by the standard wafer thickness
    675 µm for 150 mm, 725 µm for 200 mm wafer
    Depletion voltage goes as (thickness)2 and (resistivity)-1
Two advances for thick CCDs
  Improvements in the production of float-zone silicon
    Higher resistivity / lower depletion voltage
  LBNL high-voltage compatible CCD designs
    DOI: 10.1109/TED.2009.2030631 and https://doi.org/10.1117/12.672393

## Slide 29
Enabling technology: Float-zone silicon
Si Ingot
Melt
Zone
Heater
Vdepl ~ 90 – 120V for 15 – 20 kohm-cm and 725 um thick (200 mm)

## Slide 30
OSCURA
Observatory of Skipper CCDs Unveiling Recoiling Atoms
Technology transfer of the LBNL p-channel fully depleted technology to Microchip Technology (above left) and Lincoln Laboratory (above right)
    200 mm wafers with step-and-repeat photolithography
    10 kg scale (~20k 1Mpix CCDs, 10x more pixels than Rubin/LSST)
LBNL Dark Matter CCD development

## Slide 31
Enabling technology: Float-zone silicon
Blue table entries are 150-mm diameter
Red are 200-mm diameter wafers
Si Ingot
Melt
Zone
Heater
Link to Topsil Float-Zone silicon
Year Acquired | Topsil Crystal # | Resistivity r (kW-cm) | Lifetime t (ms)
2009 | 2142946 | 5.5 – 7.0 | 4.4
2009 | 2143310 | 5.0 - 6.0 | 16.3
2009 | 2144322 | 14.0 - 20.0 | 3.4
2014 | 22-0572-10 | 20.0 - 28.0 | 7.3
2015 | 33-0203-20 | 22.0 - 26.0 | 21.4
2019 | 31-1062-10 | > 10.0 | 22.4
2020 | 33-1751-30 | > 10.0 | 18.9
2020 | 32-1345-20 | 18.0 – 20.0 | 23.5
2020 | 34-1802-10 | 17.7 – 22.4 | 18.4

## Slide 32
HV-compatible CCD design (SNAP)
30 minute dark exposure
650 um thick
(10.5 um)2 pixels
133K
200V Vsub

## Slide 33
ATLAS detector group at LBL 1995
H. Spieler, D. Nygren, C. Haber, S. Holland, N. Palaio
Prototype detector development and fabrication at LBNL
More HEP heritage
High-voltage CCD designs assisted by HEP cont’

## Slide 34
More HEP heritage
High-voltage CCD designs assisted by HEP cont’
  Work on n on p detectors at LBNL introduced us to concepts that were helpful for the future HV CCD effort
    E.g. P stop floating potentials had relevance to CCDs

## Slide 35
More HEP heritage
High-voltage CCD designs assisted by HEP cont’
  Work on n on p detectors at LBNL introduced us to concepts that were helpful for the future HV CCD effort
    E.g. P stop floating potentials had relevance to CCDs
Parasitic Static Induction Transistor present in fully depleted CCDs

## Slide 36
More HEP heritage
High-voltage CCD designs assisted by HEP
  Floating guard rings and topside substrate contact
  Standard power-semiconductor method, but our first exposure to this was via strip / pixel detector development
Topside n+ substrate contact beyond the depletion edge
Backside contact is not practical
  Insulating anti-reflection coatings
  Back illumination
CCD pixels
TED.2002.806476

## Slide 37: Dark Matter detection with CCDs
Following topics
  “Dark current” / background single-electron rates
    Astronomy versus dark matter CCDs with shielding
  Particle ID via energy deposit and spatial signature
  Depletion of thick CCDs (650 – 725 um thick)
  Faster readout Skipper CCDs for astronomy
Lead shield
HyperSuprime Cam
Astronomy
SENSEI
Dark Matter

## Slide 38
Faster readout for Skipper CCDs
Loosely based on the “Distributed amplifier concept” described in the original 1973 FG-amplifier paper

## Slide 39
Faster readout for Skipper CCDs
Loosely based on the “Distributed amplifier concept” described in the original 1973 FG-amplifier paper

## Slide 40
Faster readout for Skipper CCDs
Multiple-amplifier sensing CCD
8 and 16 amplifier prototypes under test

## Slide 41
Faster readout for Skipper CCDs
https://doi.org/10.48550/arXiv.2308.09822
FNAL 8 amps
LBNL 16 amps
  Overhead to get to the Mth amp, then conventional CCD readout
  Interest for spectroscopic astronomy applications, e.g. DESI II
    Read once per amp with ~ 1 e- after averaging (16 amplifiers)
  In progress: 16 amplifier x 4 corner layout design for 4k x 4k FD CCD
    Photolithography stitching

## Slide 42
DECam: Fabrication at Teledyne DALSA Semiconductor and LBNL
Teledyne DALSA Semiconductor fabricated fully depleted CCDs for
  SENSEI and DAMIC/DAMIC-M Dark matter CCDs (all DALSA)
  Dark Energy Spectroscopic Instrument
    20 4k x 4k (15um)2 pixels with LBNL, 10 with STA / U of Arizona
  ~ 1/3 of the 100 um thick, fully depleted CCDs for Rubin Observatory/LSST
      DALSA / Semiconductor Technology Associates (STA) / U Arizona
      Remainder of the Rubin CCDs from e2V

## Slide 45
More HEP heritage
In red attendees at the LBNL Atlas SCT meeting (1995)

## Slide 46
More HEP heritage
High-voltage CCD designs assisted by HEP cont’
  Collaborators in 1995
  Also Sally Seidel and Grant Gorfine (U New Mexico)
    Testing of LBNL devices at UNM