## Slide 1
Pedro Morales Sanchez
07/09/2022
Brazing discs and prototype review

## Slide 2: Summary
Different materials / temperatures / ratios / companies

## Slide 3: Ultrasounds analysis
H2 dry/ AuCu50/ Bodycote
H2 dry / AuCu50/ CERN
Vacuum/ Palcusil-5/ CERN
Vacuum/ Palabraze-840/ CERN
Visual inspection
Leak test

## Slide 4: Metallographic evaluation - Gold
Brazing tests (15 September 2021) · Indico (cern.ch)
#1
#1
#2
Bodycote
Temp: 1000 oC
Time: 5-10min
#8
#9
CERN
Temp: 978.9 oC
Time: Time: 5-10min

## Slide 5: Metallographic evaluation – Silver base material
#4
#5
#6
#7
At CERN
Temp: 815 oC
Time: 10-15 min
We can see there is some continuity in all surfaces in contact.
As we can see in the pictures no crossing grains (CG) are observed. The red region in the UT correspond to non CG.

## Slide 6: Metallographic evaluation - Palcusil5 (Silver)
#7
We see the material stops at the end of the brazing grooves but it generate some diffusion of the Pd or Ag in a range of 2-4mm.
SP1
SP2

## Slide 7: Second round of test - Palcusil5 (Silver)
Data: ???
Time holding: 5 hours
Temperature holding: 700 deg
Time brazing: 5-10 min
Temperature brazing: 715 deg
Leak test  OK
UT report  EDMS 2756054 (S. Bonnin EN/MME)

## Slide 8: Second round of test - Palcusil5 (Silver)
We have lost some flatness after the brazing
We have lost some copper material as always

## Slide 9: Second round of test - Palcusil5 (Silver)

## Slide 10: Second round of test - Conclusions
We have been able to confine the material avoiding it to reach the RF area
We have tested a method to get a bonding surface with a low temperature cycle and a low pressure (0.04Mpa)
We see the holding time too large so is worth to explore how much can we reduce this time to make something more industrial friendly

## Slide 11
Smartcell prototype

## Slide 12
Smartcell prototype
Quotations from VDL and LT-Ultra. Very tight the dispute honestly
We are going to do the 4 prototypes with LT-Ultra but we will do at CERN the premachining, all the metrology but the final one after diamond machining and the heat treatment.

## Slide 13
Smartcell prototype
The material is already ordered and the machining is about to start
The material is 10mm laminated copper sheet
We have checked that the difference between the 10mm and 15mm sheet is not significant as we can see, and the accumulation of stress is not an issue. Is very homogeneous.
10mm
15mm

## Slide 14
Thanks for your attention.
Questions??
Thanks to Nuria Catalan, Anastasiya Magazinik, Joel Sauza, Fritz Motschmann, Ruben Brown and all participants from materials, especially Anite Pérez and Enrique Rodriguez