## Slide 1
Outline:
Main characteristics of the FRESCA2 cable
Main characteristics of the strand
Strand stability, an issue to avoid magnet quench at low field
Procurement strategy
Conductor choice, properties and procurement strategy
Luc Oberli

## Slide 2: Main characteristics of the FRESCA2 cable
The cable was defined with the following requirements:
The transport current has to be high enough to achieve with enough margin a central field of 13 T at 4.2 K in a large aperture dipole, but with a maximum current of 16 kA to be compatible with the power supply installed in the FRESCA test facility.
The cable has to be flexible enough to facilitate the winding of the coil, not only for a block coil structure but also for a cosf dipole.
The cable has to be produced with the cabling machine installed at CERN (maximum 40 spools).
To satisfy all these requirements and for other reasons which will be given later in this presentation, the strand diameter was fixed to 1 mm and the number of strands to 40.

## Slide 3: Main characteristics of the FRESCA2 cable
Cable width | (mm) | 21.4
Cable mid-thickness at 50 MPa | (mm) | 1.82
Keystone angle | (degree) | 0
Cable transposition pitch | (mm) | ≈ 120
Number of strands | (-) | 40
IC (12 T, 4.2 K) | (A) | 31420
IC (15 T, 4.2 K) | (A) | 15170
n-value @ 15 T and 4.2 K | - | 20
RRR after HT | - | > 120
Minimum cable unit length | (m) | 260
Cable width calculated to compact only slightly the strands on the width.
Nd/2cosf + 0.732 d
The critical current of the cable is calculated taking into account a degradation of 10 % due to cabling.

## Slide 4
The cable has to be flexible enough to wind the coil having a bending radius as small as 45 mm and to make the jump between the 2 layers of each double-pancake.
The reduction of the strand diameter to 1.0 mm has given a flexible cable.
The transposition pitch of the cable was determined from cabling test done with Cu strands to have a cable mechanically stable.
Main characteristics of the FRESCA2 cable

## Slide 5
 |  | NED | FRESCA2
Strand diameter | (mm) | 1.25 | 1.00
Sub-element diameter | (mm) | < 50 | < 50
Copper to non-Copper volume ratio | - | 1.25 | 1.25
JC(12 T, 4.2 K) | (A/mm2) | 3000 | 2500
JC(15 T, 4.2 K) | (A/mm2) | 1500 | 1250
n-value @15 T and 4.2 K | - | > 30 | > 30
RRR (after full reaction) | - | > 200 | > 150
Piece length | (m) | > 1000 | > 400
Main characteristics of the strand
Following the results obtained by the NED program on a strand of 1.25 mm in diameter, where only one supplier has been able to produce the conductor with 288 sub-elements and with a Jc around 1400 A/mm2 at 15 T and 4.2 K, the performances of the strand in term of Jc have not been pushed too high.

## Slide 6
Strand stability: an issue to avoid magnet quench at low field
The stability of the Nb3Sn strand could be an issue with high Jc, large sub-element diameter and low RRR.
Stability improves as strand diameter is reduced, as measured at 4.3 K on the RRP 54/61 strand having sub-element of ~ 80 mm in diameter at a strand diameter of 0.8 mm.
For this reason, the strand diameter was fixed to 1.0 mm as a compromise between the need to have a high transport current and the need to avoid magneto-thermal instabilities at low field.
The sub-element diameter has also to be small enough to reduce the flux jumps at low fields and a maximum value of 50 mm was specified.

## Slide 7
Analysis of B. Bordini (CERN), conservative model used to predict the stability of a 0.8 mm strand with 80 mm sub-element diameter
Stability improves as the RRR of the strand is increased from around 8 to 120, it is beneficial both at 4.2 K and at 1.9 K.
The RRR of the virgin strand has to be large enough to have some guaranty not to get “hot-spots” in the cable, in particular near the cable edge. RRR degradation over a length of ~ 1 mm is sufficient to create severe instability and to impair the current capability of the strand.
For these reasons, the request on the RRR value is high. A minimum value of 150 was specified.
Strand stability: effect of RRR

## Slide 8
Bruker-EAS has developed for NED a 1.25 mm strand with 50 mm sub-elements diameter achieving around 1400 A/mm2 at 15 T and 4.2 K.
OST has developed for LARP a 1.0 mm strand with 66 mm sub-elements diameter achieving around 1300-1400 A/mm2 at 15 T and 4.2 K.
Nb3Sn Strand Procurement strategy
Two suppliers have the technology to develop a Nb3Sn strand (in a short time) meeting the specification for the FRESCA2 cable:
Bruker-EAS and Oxford Superconducting Technology (OST).
The procurement is divided in 3 steps:
a 1st step called “qualification phase”
a 2nd step called “pilot production”
a 3rd step for the full production
The objective is to have at the end of the first 2 steps the qualification of the 2 suppliers.

## Slide 9
Nb3Sn Strand Procurement strategy
First Step: qualification phase
A first order for 9 km of PIT strand placed by CERN to Bruker-EAS in March 2010
Three billets fabricated, one with round filaments and two with hexagonal filaments.
Jc achieved: Jc(15T, 4.2K) @ 1350 A/mm2 and Jc(12T, 4.2K) @ 2450 A/mm2.
Kilometer long strand piece lengths obtained.
RRR @ 196 – 260 for the billet 09Y04
RRR @ 40 - 67 for the billet 09Y05
Magnet load line

## Slide 10
Nb3Sn Strand Procurement strategy
Second Step: pilot production
2 orders (2 X 15 km) will be placed by CEA to Bruker-EAS and OST
Price enquiry sent in December 2010, deadline for answering end of January 2011
Minimum piece lengths required > 400 m
RRR > 100 required to OST and RRR > 150 required to Bruker-EAS
Two orders placed by CERN:
10 km of PIT strand placed to Bruker-EAS in August 2010 (delivery expected before June 2011)
Strand with round filaments, RRR > 150 and minimum piece length > 150 m
10 km of RRP strand placed to OST in September 2010 (delivery expected before October 2011)
Difficulties seen by OST to guarantee simultaneously Jc, RRR and long strand piece lengths for a strand of 1 mm in diameter with 50 mm sub-element diameter .
order accepted by OST with the following restrictions: RRR > 75 and minimum piece length > 150 m.
First Step: qualification phase

## Slide 11
Thank you for your attention !
Third Step: 35 km strand production
On the basis of CERN order results, CEA will launch a 35 km strand production (mid of 2011) to one supplier.
Nb3Sn Strand Procurement strategy

## Slide 12
Critical Current
SF+M Instability
SF Instability
Magnet
Load Line
Magnet
Design Field
  At 4.2 K the combination of the Self-Field Instability with the Magnetization Instability at low fields is the most dangerous
Magneto-Thermal Stability
by courtesy of B. Bordini (CERN)