## Slide 1: EuCARD-WP7-HFM Dipole Conceptual Review Nb3Sn dipole protection
Philippe FAZILLEAU
CEA/iRFU/SACM
January 20, 2011 @ SACLAY

## Slide 2: Introduction
Cold mass 293 kg and Energy 5.4 MJ
i.e. energy density 18.4 J/g

## Slide 3: Introduction
Uniform dissipation
All magnet [118 MJ/m3]  Tmean = 126 K
  1 pole  Tmean = 182 K
  1/2 pole  Tmean = 276 K
Adiabatic hot spot criteria
importance of the detection
J(T) : overall current density,
T : time,
r(q) : overall resistivity,
g : density, q : temperature,
C(q) = specific heat.
Vmax = 1000 V, I = 10,5 kA  Rdump = 95 mΩ
 qmax = 228 K

## Slide 4: Detection
The quench propagation and detection depends mainly on:
The propagation velocities
But for Nb3Sn @ (13.2 T, 4.2 K) Tcs= 8 K Tc = 11,96 K [Summers]
 Tt = 9,98 K so vl = 10,8 m/s
Tt = Tcs vl = 19,4 m/s
Tt = Tc vl = 6,7 m/s (conservative case)
The detection thresholds; voltage and time thresholds :
Ud = 100 mV
td = 100 ms

## Slide 5: Calculations : QTRANSIT code
home made code (fortran),
checked on several magnet (CMS, ALEPH, ATLAS, QPOLES…),
3D simulation of the quench thermal transient in the magnet,
based on the quench propagation velocities and the resistance growth with time,
material property dependences on temperature, magnetic field and RRR,
Computes voltages, temperatures and resistance rise in the winding,
Includes quench heaters.
transverse
propagation
longitudinal
propagation

## Slide 6: Electrical protection circuit
protection principle based on the extraction of the magnetic stored energy into a dump resistor,
takes benefit of quench heaters (if needed),
grounding circuit ± Vmax/2 to ground,
Inductances computed with ROXIE.
DP1
DP2
DP3
DP4

## Slide 7: Computation hypothesis
heaters location
quench
ignition
or
or



Do we need heaters ?

## Slide 8: Nominal case – no heaters
t = 0 s
t = 24 ms
t = 59 ms
t = 2,37 s
A quench starts to
expand in DP1
Vresistive > Ud
Detection of the quench
Switches open
End of the discharge
t = 124 ms
DP2 starts to quench
t = 221 ms
DP4 starts to quench
t = 415 ms
t = 424 ms
t = 429 ms
DP3 starts to quench
t = 711 ms
DP1
DP2
DP3
DP4
The worst case (Tmax and Vmax) occurs for a quench ignition in a corner of DP1,
The contactors open 100 ms after the detection (Ud > 100 mV),

## Slide 9: Nominal case – no heaters
The high temperature gradient within the magnet could induce mechanical issues
 Heaters could solve it by spreading the quench more uniformely.

## Slide 10: Nominal case – with heaters
The worst case (Tmax and Vmax) occurs for a quench ignition in a corner of DP1,
The contactors open 100 ms after the detection (Ud > 100 mV),
The heaters are effective 50 ms after this time (150 ms after the detection).
t = 0 s
t = 24 ms
t = 59 ms
t = 1,97 s
A quench starts to
expand in DP1
Vresistive > Ud
Detection of the quench
Switches open
End of the discharge
t = 124 ms
DP2 starts to quench
t = 200 ms
t = 265 ms
DP1
DP2
DP3
DP4
t = 174 ms
Heaters effective

## Slide 11: Nominal case – with heaters
Heaters have strongly decrease the temperature gradient (factor 2),
they slightly increase the voltage at the terminals of 2 double-pancakes.

## Slide 12: Quench behaviour – 1 T, 5 T, 10 T, 13 T
Detection
Threshold voltage Ud = 100 mV
A quench starts in a corner of DP1
Time to reach the threshold
Length of the quenched zone
Discharge results
Time threshold td = 100 ms, Rdump = 95 m, No heaters

## Slide 13: Dump resistor parametric study

## Slide 14: Fault scenario
A quench is fired in a corner of DP1,
No detection:
 no dump into the external resistor
 no heaters
t = 0 s
t = 59 ms
t = 0,981 s
A quench starts to
expand in DP1
End of the discharge
DP2 starts to quench
t = 221 ms
t = 378 ms
DP1
DP2
DP3
DP4
DP4 starts to quench
t = 384 ms
t = 388 ms
DP3 starts to quench
t = 568 ms
t = 2,2 s

## Slide 15: Fault scenario

## Slide 16: Conclusion
The ratio E/M of the dipole is high but manageable with a good detection system,
A study of the detection lead to thresholds values of 100 mV and 100 ms,
The use of heaters is not necessary as Tmax < 250 K, Vmax < 500 V; but the high temperature gradient within a coil could induce mechanical issues,
Heaters lower the temperature gradient, the maximal temperature and slightly increase the maximal voltage at the terminals of the double-pancakes,
The study of the protection at different currents does not show any issues; a thermal study will be led for the use of heaters and the ignition of the quench at the lowest current values.
The fault scenario shows that the magnet will not burn-out even if it will experiment high temperatures (up to 354 K) and high temperature gradient (251 K).
The presence of the HTS insert and its implications on the protection will be studied.