## Slide 1
L. Burmistrov, M.Heller, T. Montaruli, C. Trimarelli, Jan Swakon (for IFJ PAN proton facility)
(on behalf of NUSES collaboration)
A SiPM based camera for the Terzina telescope on board the NUSES space mission
Outline:
The NUSES mission.
Intro.
The Terzina telescope
SiPM intro.
Simulation of the instrument
Radiation hardness
Annealing
rr

## Slide 2
GSSI is leading the mission
This map some time ago

## Slide 3
Ivan De Mitri
Riccardo Nicolaidis
See talks from :
Andrea Di Salvo
See talks from :
Poster by : Pillera (zirè-FTK)

## Slide 4
The NUSES mission composed of two payloads.
Two main components :
ZIRE
TERZINA
ZIRE`
TERZINA
Telescope
60 x 60 x 50 cm3
TERZINA weight < 30 kg
Monitors the fluxes of low energy cosmic rays (< 250 MeV),
Electrons and protons to study Van Allen radiation belts
Space weather and the magnetosphere-ionosphere-litosphere couplings
And much more ….
60 cm
50 cm
ZIRE`
Demonstrator of Cherenkov light detection produced by Extensive Air Showers
First measurement of showers with Cherenkov light from space (E>100PeV)
Proves the technology for detecting Earth skimming muon and tau neutrinos
Measure the background conditions
Further Development of SiPM technology for space
TERZINA
60 cm

## Slide 5
Camera vs POEMMA
TERZINA Telescope
primary mirror daim.: 0.4m
POEMMA Telescope
primary mirror daim.: 4m
Probe
POEMMA
SiPM part
(Detection of Cherenkov light)
TERZINA SiPM photo detection plane
y (mm)
x (mm)
John F. Krizmanic
arxiv:2008.04984v2
~ 12 x 6 cm2

## Slide 6
SiPM vs ma-PMT (PMT)
Operation voltage <100 V ~1000V
Currents ~1 muA ~100 muA
Power per cm2 ~mW ~0.1W
Weight per cm2 of sensitive area ~10 g ~100g
Total integrated charge infinite 200 Q
Time resolution <100 ps < 1 ns
Special resolution ~1 mm ~10 mm
Photo detection efficiency @ 400 nm > 50 % < 50 %
Variation with temperature very sensitive low
Need of pre-amplifier/PMT gain 0.1 mV 5 mV
Radiation resistance low good
Single photon response PMT vs SiPM
SiPM
PMT
PMT
Prompt cross-talk within one channel
Change sharing between anodes.
Large variation of the response defined by secondary emission

## Slide 7
Parametric SiPM simulation
Prompt cross talk.
After pulsing
SiPM all the cells are connected in parallel
Delayed crosstalk imposed in other pixels is not simulated.
In simulation we include as well :
Gain variation, electronic noise, pre-amplifier, ADC.

## Slide 8
Single p.e. avalanche tree
Trial parameters for generator testing:
Probability of the cross talk is set to 0.2
Probability of the after-pulse is set to 0.15
And after pulse decay time 15 ns.
After pulse
Single
Photo electron
p.e.
Cross
Talk
After
pulse
Crosstalk
Recurrent process
Clearly saturated due to cell recovery time
Final result waveform.
Initial p.e.

## Slide 9
S
Experimental setup

## Slide 10
SiPM characterization : V break down (Vbd)
Break down voltage – defines when SiPM start to detect light. It is a function of a temperature.
Vbd calculated with :
Second log derivative
Forward biasing.
Measure the quenching resistor
Vbd

## Slide 11
SiPM characterization : IV curves for different mu-cell sizes.
Vbd as a function temperature
Cell size
Current at same V
Temperature
Vbd
~32.6 V (20°C)
~31.2 V (-20°C)
Temperature coefficient is 33mV/oC

## Slide 12
SiPM characterization : response on very large number of photons from laser (~10 ps).
“Forward” (positive)
“Forward” (pos.)
Rise time of the
signal is 200 ps !!!
Reverse (negative)
Reverse (neg.)

## Slide 13
SiPM characterization : decay time of the slow component. Preamplifier optimization.
Laser vs
Laser + int. sphere
Normalized single p.e. shape after amplification.
Zoom

## Slide 14
SiPM characterization : DCR (dark current rate), (CT) optical cross-talk, PDE(photo detection eff.)

## Slide 15
Resin samples
Acknowledgments: IFJ-PAN and Jan Swakon (responsible for proton irradiation campaign).
https://web.infn.it/EURO-LABS/
https://www.ifj.edu.pl/

## Slide 16
IV measurements after each irradiation step
IV_PCB1_S3_25um_wores_ch01_K2400_n1

## Slide 17
Results after irradiation test
We observe linear increase of the DCR with irradiation dose.
We observe linear increase of the DCR with irradiation dose.
Standard characterization of the SiPM is impossible after irradiation.
The PDE measurements can be done only with large number of photons, as a consequence large systematical are expected for this measurements.
30 % of the expected dose are coming from protons.
We “simulate” 10 years on the orbit (planed mission duration is 3 years).
No change of the quenching resistor has been observed.
No optical degradation of the resin samples have been observed.
No change of the Vbd behavior as a function of temperature measured.

## Slide 18
Annealing at 40 oC
Dry air
Climatic box, where we can vary the temperature from -20 to 80 oC
The irradiated samples are stored at -20 oC
to avoid room temperature annealing.
We use the climatic chamber for temperature control.
Measurements IV measurements were done every 2-5 hours (excluding nights).

## Slide 19
How much light do we produce in the photo sensor window
Amplitude 237 mV @ 106 amplification
Imaging the Fe ion

## Slide 20
Bare SiPM or SiPM with thin window ?
Mu-cell operates in geiger mode
Thikness of the protective window 400 – 40 mum
Can we make it thinner ? 10 mum ?
Can we completely remove it ?
Window
Perpendicular track at maximum will produce 4 p.e. equivalent signal
This effect can be vanished by removing the window :-) ...
If the bare surface is not planar very thin resin can form micro-lenses need to have additional R&D.

## Slide 21
Conclusions
We present the parametric simulation of the SiPM used in the full simulation chain.
The radiation test with 50 MeV protons up to 30 Gy integrated dose (corresponds to 10 years on the orbit).
SiPM are promising photo sensors to be used for space base experiments.
We present full chain of different activities for Terzina telescope on board the NUSES space mission.
We characterize SiPM with different mu-cell sizes with and without resin.
SiPM annealing at 40 oC has been studied.

## Slide 22
Backup

## Slide 23
Cathode
Anode
Rq
APD