## Slide 1: Accelerator Magnet R&D in CHART D. M. Araujo, B. Auchmann, A. Brem, M. Daly, M. Duda, R. Felder, C. Hug, O. Kirby, J. Kosse, T. Michlmayr, G. Montenero, H. G. Rodrigues, G. Rolando, S. Sanfilippo, S. Sidorov, D. Sotnikov with support from CERN, ETHZ, FNAL, LBNL, Tokamak Energy Ltd, UniGE, uTwente
02.03.2023 – Magnet Seminar
Work supported by the Swiss State Secretariat for Education, Research and Innovation SERI.

## Slide 2: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 3: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 4: CHART – What, Who, How?
http://chart.ch
“CHART, the Swiss Center for Accelerator Research and Technology, was founded to support the future oriented accelerator project Future Circular Collider (FCC) at CERN and the development of advanced accelerator concepts in Switzerland beyond the existing technology. […] The high field magnet R&D has strong synergies with PSI projects […]” [Application for support of the Swiss Accelerator Research and Technology Initiative, 2018]

## Slide 5: CHART – What, Who, How?
Members:
CHART Council: approves projects and receives reports.
CHART Executive Board: implements and reports on progress.
Funding: For a given research period, CHART members pledge funds and apply jointly for additional funding from SERI and ETH Council.
  CERN’s pledge is the biggest individual amount and makes up 37% of the overall CHART2 envelope (2019-2024).
  Projects are defined in CHART Project Proposals and, if they receive CERN funding, addenda with the FCC Feasibility Study or the HFM Programme.
Notes: Implications of the national effort:
  Only in a national effort can multiple institutes as well as national funding agencies be persuaded to set aside funds – most of these resources would be lost otherwise.
  Projects with academic experts can be hard to set up when complementary funding is required. In CHART, the complementary funds are pre-allocated.
  Geographic vicinity eases collaboration, but the national character does not preclude (at all) international collaboration, as many of the following slides will illustrate.
  Multiple lines of funding come with multiple lines of accountability and reporting (local instititue, CHART Council and SERI, HFM Programme).

## Slide 6: CHART – What, Who How?
Topics and FTEs of ongoing HFM projects in CHART:
FCC Feasibility Study and other CHART projects:
  FCC / LHC Lumi
  FCCee Beam Dynamics Simulation
  FCChh Stability
  FCCEe SPIN POL
  FCCee Lumi
  Muon Collider Feasibility Studies
  FCCee Injector
  FCC Geodesy
  FCCee CPES – cryogenic power supply development (1 FTE)
  FCCee HTS4 – HTS Short Straight Section Demo for FCCee (4 FTE)
  HTS Bulk Undulator – bulk REBCO undulator technology (2 FTE)
  FCC Geology 3D Model

## Slide 7: CHART HFM Strategic Guidelines
Provide relevant input to the next ESPPU.
Aim for meaningful innovation.
Fast-track key technology R&D with academia and industry.
Use fast-turnaround minimum viable products as innovation funnel.
Where required, invest in infrastructure early to maximize its impact.
Increase the cross-linking among CHART members to reach full potential as a distributed research network.
Ensure optimal communication, coordination, and collaboration within CHART, with CERN, and the HFM Programme.
Realize synergies for PSI’s scientific and medical programs.

## Slide 8: CHART Acc. Magnets – Technology Pillars
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS/HTS conductor R&D, Characterization
Cable
Rutherford / Roebel production
WireChar
WireDev
MagDev1
MagDev2
FCCee Injector
FCCee HTS4
Notes: UniGE has experience in rod-type internal tin wire manufacturing

## Slide 9: CHART Acc. Mag. – Enabling Technology R&D
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS and HTS strand/tape R&D, Procurement, QA
Cable
Rutherford / Roebel production
X-ray tomography
Billet manufacturing
Notes: Grenoble, synchrotron and HMF
CERN
  Manufacturing infrastructure
  Modeling wire to cable performance

## Slide 10: CHART Acc. Mag. – Enabling Technology R&D
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS and HTS strand/tape R&D, Procurement, QA
Cable
Rutherford / Roebel production
Model-Based Systems Engineering,
Multi-scale modeling
MagNum MagComp
Notes: Grenoble, synchrotron and HMF
CERN
  Manufacturing infrastructure
  Modeling wire to cable performance

## Slide 11: CHART Acc. Mag. – Enabling Technology R&D
Polymer R&D
Insulation and composite R&D REBCO NI Coil Technology
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS and HTS strand/tape R&D, Procurement, QA
Cable
Rutherford / Roebel production
MagRes
MagComp

## Slide 12: CHART Acc. Mag. – Enabling Technology R&D
Additive manufacturing
Coil interfaces
Lab 4.0
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS and HTS strand/tape R&D, Procurement, QA
Cable
Rutherford / Roebel production
MagAM

## Slide 13: CHART Acc. Mag. – Enabling Technology R&D
Powered sample tests in background field
Quench Protection
Signal Analysis
Cryogenic Powering
Mechanical Assembly
Mechanical loading
Magnet Design
FCC-hh / HE-LHC conceptual and technical
Coil Manufacturing
Nb3Sn and HTS coils
Testing
LTS and HTS magnet tests
INJECTION
Strand / Tape
LTS and HTS strand/tape R&D, Procurement, QA
Cable
Rutherford / Roebel production
FCCee CPES

## Slide 14: 2020 Update of the European Strategy for Particle Physics
  “Europe, together with its international partners, should investigate the technical and financial feasibility of a future hadron collider at CERN with a centre-of-mass energy of at least 100 TeV and with an electron-positron Higgs and electroweak factory as a possible first stage. “
  “The technologies under consideration include high-field magnets, high-temperature superconductors, plasma wakefield acceleration and other high-gradient accelerating structures, bright muon beams, energy recovery linacs. The European particle physics community must intensify accelerator R&D and sustain it with adequate resources. A roadmap should prioritise the technology, taking into account synergies with international partners and other communities such as photon and neutron sources, fusion energy and industry. Deliverables for this decade should be defined in a timely fashion and coordinated among CERN and national laboratories and institutes.“
http://cds.cern.ch/record/2721370

## Slide 15: LDG Roadmap for HFM R&D
Accelerator R&D Roadmap published in Jan 2022.
  https://arxiv.org/abs/2201.07895
Input for CHART Roadmap and HFM Programme

## Slide 16: From A. Siemko, Intro to HFM RD3 Meeting

## Slide 17: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 18: CHART1 Goals
CHART1 goals (mid-2016 to mid-2019) :
  the design of an optimised 16 T Canted Cosine Theta (CCT) dipole magnet, as an option for the FCC hadron collider main magnet;
  the development (design and prototype) of a high-field dipole magnet with CCT technology; and
[B. Auchmann et al., Electromechanical Design of a 16-T CCT Twin-Aperture Dipole for FCC, IEEE Trans. on Appl. SC 28 (April, 2018) no. 3.]
[M. Benedikt et al., FCC Conceptual Design Report, Vol. 3 – The Hadron Collider (FCC-hh), pp. 50-52, submitted to Eur. Phys. J. ST, (December 2018).]

## Slide 19: CHART1 Goals
CHART1 goals (mid-2016 to mid-2019):
  the design of an optimised 16 T Canted Cosine Theta (CCT) dipole magnet, as an option for the FCC hadron collider main magnet;
  the development (design and prototype) of a high-field dipole magnet with CCT technology (February 2017 – October 2019)
[G. Montenero et al., Coil Manufacturing Process of the First 1-m-Long Canted-Cosine-Theta (CCT) Model Magnet at PSI, IEEE Trans. on App. SC., Vol 29(5), 2019.] [G. Montenero et al., Mechanical Structure for the PSI Canted-Cosine-Theta (CCT) Magnet Program, IEEE Trans. on Appl. SC., Vol 28(3), 2018.]

## Slide 20: Mechanical Structure
Al shell 25 mm
Vertically split yoke, OR 250 mm
Vertically split Al-bronze pad
Protective Al shell 5 mm
Vertical and horizontal keys
Bladder locations
Closed pad gap
Open yoke gap
Al-bronze former
Bladder and Key technology chosen for tuneability and relative simplicity.
  Closed and pre-loaded pad gap for maximum-rigidity cage around coils.
  Aluminum bronze pads to match coil differential contraction.
Notes: show loading concept via reaction forces

## Slide 21: CHART1 MagDev Lab

## Slide 22: CHART1 MagDev Lab
90 m2 laboratory refurbished, equipped, commissioned for construction of CD1 06/2017-06/2018.
Production-readiness review (http://indico.psi.ch/event/cd1prr).
Vacuum Impregnation
Coil reaction
Portal crane
4-m winding/instrum/assembly bench
Winding table
Storage

## Slide 23: CD1 Winding and Insulation Issues

## Slide 24: CD1 IL Former after Heat Treatment
Insulation has turned resistive (1-3 Ω mandrel to cable).
Cable clamping caused mandrel deformation by +/- 1.5 mm in central section.

## Slide 25: IL Splicing an Instrumentation
Splicing followed closely the LBNL procedure.
Repeated trials led to a smooth operation. Visually, all looks good.
IL has only two v-taps in the winding, and two more on each splice.

## Slide 26: IL/OL Sliding Planes
Sliding planes installation without incidents.
Need to improve heating towards the extremities (coil mounting acts as heat sink).

## Slide 27: Re-machining OL
Outer-layer spar was reduced from 3 mm to 2 mm.
QA shows minimal distortion of the former.
Test-assembly successful.

## Slide 28: OL Winding and Reaction
Winding without incidents. Glass-ribbon reinforcement on pole surfaces provided good insulation.
Pre-reaction, the cable was below the former OD everywhere.
Resistance cable/former was again ~3 Ω. There is no distinct weakness, but all glass braid has turned resistive.
After reaction, numerous turns, especially towards the ends, stuck out from the mandrel OD by as much as 0.7 mm.

## Slide 29: Splicing and Instrumentation OL
OL splicing was carried out without incidents. Visual inspection is good.
OL is equipped with 5 v-taps and a spot heater, as well as 2 v-taps per splice.

## Slide 30: Coil Assembly
OL wrapped in glass ribbon.
IL and OL aligned by Al block.
G10 shims between IL and OL to avoid axial slipping.
Teflon mesh between Al shell and coil.

## Slide 31: Impregnation
Following mostly the LBNL impregnation scheme,
adjusted for our thin Al shell,
and using a peristaltic pump to slow down injection.

## Slide 32: Intra-layer Splicing and Assembly in Pads
Intra-layer splicing produced a cable stack slightly wider than anticipated.
Visual inspection looks good.
Wrapping imp. coil with two layers 125-µm-thick Kapton and assembly inside pads proved difficult.
Pads-to-Al-shell insulation tested up to 800 V.

## Slide 33: Mechanical Assembly – Loading
Assembly went “as advertised”.
The yoke halves are sprayed with Steel-It, inserted, and locked into the Al shell.
The yokes are turned and lifted on the table.
The pads are inserted and loaded with nominal shims.
The keys entered at the predicted bladder pressure of 100 bar for vertical and 350 bar for horizontal keys.
The strain gauges equally tracked very well with simulations.
Horizontal loading took only 1 hour.

## Slide 34: Loading and Strain Gauges

## Slide 35: CD1 Complete
A wonderful team effort came to an end.
Without the incredible openness and generosity of LBNL colleagues we could not have reached this milestone!

## Slide 36: Test of CCT5 at LBNL
CCT5 was tested before CD1 was complete.
It has many of the same design features.
Long training was explained by
  De-bonding of cables from channel walls
  And cracks in the glass-epoxy insulation.
CD1
Courtesy D. Arbelaez, LBNL.
 | CD1 | CCT5
ID | 63.6 mm | 90 mm
Spar | 3/2 mm | 7.4/3 mm
Layer interface | Sliding plane | Bend & Shim
Mechanical structure | Bladder & Key | ID Spar and Al shell
Resin | FSU Mix 61 | FSU Mix 61

## Slide 37: Record Field after a Long Delay
October 2019, the CD1 magnet was finalized and shipped to LBNL, Berkeley, US, for testing.
An Odyssey began:
The magnet was blocked for 3 months in US customs and the transport crate was heavily damaged by a fork lift.
COVID delayed the start of testing by 6 months.
After several ramps, the LBNL test station had technical problems. The repair grew into an upgrade project.
After the return of the test station, the PSI magnet lost in priority over other delayed LBNL projects.
Upon invitation by CERN, the magnet was shipped there and arrived in November 2021.
A dangerous electrical incident at CERN interrupted all testing at CERN for several months.
Upon resumption of testing, HiLumi magnets received priority.
CD1 was eventually tested at CERN in November 2022.
It reached 10.1 T in the bore at 94% of Iss at 1.9 K; 9.9 T and 100% of Iss at 4.5 K..
Courtesy F. Mangiarotti (CERN) and M. Daly (PSI).
Bottom line: Stress-management works – no conductor degradation from handling, assembly, powering, cycling.

## Slide 38: BOX Data (see below) for Iss Determination

## Slide 39: CD1 and CCT4/5
Courtesy F. Mangiarotti (CERN), D. Arbelaez (LBNL), M. Daly (PSI).

## Slide 40: CD1 CLIQ Tests
Safely assess CLIQ efficiency on short CCT magnet.
Numerous voltage and capacitance values tested at increasing current values.
0
0.05
- 0.05
- 0.1
- 0.15
- 0.2
0
2
4
6
8
10
Time [s]
Current [kA]
CLIQ settings
200V; 40 mF
EE = 200ms
Courtesy F. Mangiarotti

## Slide 41: CD1 Spot Heater Test
All tests at 4.5 K
Circuit: 10 mF capacitor charged to:
  27 V (8 kA and above)
  35 V (6 kA)
  45 V (4 kA)
10.5 Ohm resistance
Outer Layer
I [kA] | t100mV [ms]
4 | 310
6 | 100*
8 | 32
10 | 15
12 | 7.0
14 | 4.1
16 | 2.3
2.2 2.3
Courtesy F. Mangiarotti

## Slide 42: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 43: MagDev Laboratory
New extension to building WLHA next to SLS2.0.
Hand-over in August 2020.
Infrastructure (hall and equipment) was excluded from cost-sharing with CERN.

## Slide 44: MagDev Laboratory Layout
HTS winding
LTS winding
Re-reeler
3D Scanning
Heat treatment
Impregnation
Loading / Assembly
Storage
Instrumentation
Autoclave 10 bar, 250ºC to arrive April 2022. For the time being no loading press.

## Slide 45: MagDev and HTS4 Team
Christoph Hug Technician LTS
Michael Daly Engineer LTS
André Brem
Material Scientist
Douglas Araujo
Engineer LTS
Henrique Rodrigues
Technician ReBCO
Thomas Michlmayr
CAD, Technical Design
Design
Materials
Processes
Instrumentation, Protection, Testing
Dmitry Sotnikovs Engineer HFM ReBCO
Oliver Kirby Internship LTS
Jaap Kosse
Engineer HTS4 ReBCO

## Slide 46: MagDev1
Clean reaction
BigBOX constr. and test
Pcubed concept. design

## Slide 47: BOX Program
BOX (BOnding eXperiment) program with uTwente has shown a wide variety of results, from complete conductor degradation (no impregnation) to substantial training (epoxy) to no-training (wax, Stycast), with 18 BOX samples successfully manufactured and tested to date.
Pictures by M. Daly, S. Sidorov, S. Otten
Notes: LBNL is preparing a wax impregnated subscale CCT magnet

## Slide 48: BOX Program Sections
Cleaner BOXes perform better.
Weak CTD101K (5x lower K1c) outperforms standard CTD101K.
Terribly processed filled CTD101K by far outperforms standard CTD101K.
K1c alone cannot predict performance.
  Tg (glass transition) and Tc (curing) may be equally important.

## Slide 49: Accoustic data taken on all BOX samples

## Slide 50: PostMortem Analysis
Quantify defects after wire-saw cutting and polishing.
[Courtesy of O. Kirby, M. Daly.]
Voids
Surface defects (de-bonding)
Cracks

## Slide 51: PostMortem Analysis - First 7 Data sets
Low K1c CTD101k
MY750
Mix61
CTD101k
CTD101k
Sedimentation
Stycast
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9
Voids 0-3
Cracks 4-6
Wire OD 7-8
Channel 9

## Slide 52: BOX Compression
Courtesy S. Ott et al.
Courtesy M. Daly
Successful systems can be characterized and benchmarked against CTD101-K in U Twente’s transverse-compression setup.
CTD 101-K measurements reproduce previous results of Twente U-shaped samples.
Paraffin wax’s lower modulus and yield increase degradation.

## Slide 53: Wax Sub-scale Layer tested at LBNL
All data courtesy of D. Arbelaez for the LBNL CCT program.
  Sub_2: epoxy in inner and outer, inner with thin spar
  Sub_3, epoxy in inner and outer, inner with thick spar
  Sub_5, wax in inner, epoxy in outer, outer layer re-used from sub_3
Wax inner layer did not show any training quenches.
Also Stycast will be investigated.
The wax-impregnated Sushi by Wigner institute (HU) is being prepared for testing.

## Slide 54: CCT4FCC Pros and Cons
Design:
  Mechanical support of each turn  reduced coil stress and avoidance of stress-induced degradation.
  Easy field quality (on paper).
  Ideally suited for LTS/HTS hybrid magnets due to easy stacking of heterogeneous layers.
  Simpler external mechanical structure  more iron between the apertures and better magnetic separation  less cross-talk.
  Hope to fix training: getting one turn “right”, the entire magnet would work; no discontinuities towards the end regions
Fabrication:
  Simple and safe coil-manufacturing process; little tooling needed; coil always protected by former.
Instrumentation and protection:
  Efficient CLIQ protection as every turn is a high-field turn.
  Co-winding of instrumentation (fibers, wires, etc.) is supposedly easy.
Design:
  Every turn must be glued to metal surfaces; delamination would preclude good performance.
  Reduced efficiency by winding angle, rib thickness, and spar thickness.
  Check FQ variation along z-axis due to lack of control on turn position.
  Some axial strain on cable in every turn.
  No radial pre-compression possible.
Fabrication:
  Tricky winding on small ID with wide cable.
  Difficult to obtain reliable insulation.
  Difficult to keep cable in groove on small IDs.
  Interplay between former and cable during reaction.
Instrumentation and protection
  No heater protection possible.
Scaleup:
  Involved former manufacturing; cost and time consuming; difficult to scale to 15 m.
  Difficult assembly and alignment for long magnets – assembly gaps reduce performance.

## Slide 55: Alternatives to CCT – Low-Pre-Stress CT
Initially, the plan was to abandon stress management due to the training.
A Low-Pre-Stress Cosine Theta configuration was studied in collaboration with G. Vallone (LBNL).
2D studies looked promising:
  A standard cos-theta coil inside a rigid structure of optimized thermal contraction for little pre-stress after cool-down.
  2-layer coils like 11-T saw peak stresses on coil OD, little stress-enhancement on ID midplane.
  4-layer coil results showed strong dependence on wedge position in the outer layers.
  Recall: FNAL 15-T magnet has no wedges in the outer layers. Hence they plan to use SM-CT to enhance outer-layer stiffness.
3D studies revealed problems:
  The additional motion of a low-pre-stress configuration leads to prohibitive stress concentrations.
  Possibly low transverse pre-stress should be combined with conventional axial loading.
New 3-D coil-end generator (G. Vallone) is available from this work.
Courtesy G. Vallone http://indico.psi.ch/e/magdev1review

## Slide 56: Stress Managed Alternatives to CCT
Same scale, 50 mm aperture
Conductor area (1/4) = 2445.4 mm2
Conductor area (1/4) = 2709.3 mm2 (+ 10.8 % conductor)
HF cable (28 x 1.0 mm ) Layers 1 and 2
LF cable (40 x 0.7 mm)
HF cable (28 x 1.0 mm ) Layer 1 and pole coils
LF-1 cable (40 x 0.7 mm) Layer 2
LF-2 cable (30 x 0.7 mm) Layers 3 and 4
1
2
3
4
1
2
3
4
Pole coil
Courtesy of D. M. Araujo – images for illustration purposes only; these are snapshots of comparative design studies – not fully optimized designs.
Following wax and later Stycast BOX results, the focus shifted back to stress management.
SM CT (Cosine Theta) and SM CC (Common Coil) were studied, using FNAL 15 T cable/strands.

## Slide 57: Stress-Managed Common Coil Option
Advantages:
  Synergies with HTS program.
  Individual-layer impregnation with low-field splices.
  In preliminary study, less conductor than SM CT option.
  Easier axial mechanics.
  Potential route to react&wind.
Disadvantages
  More difficult transverse mechanics.
  More difficult to wind into slots.
SEQV Max 146 MPa
SEQV Max 910 MPa
Preliminary study at 14.5 T
Courtesy of D. M. Araujo – images for illustration purposes only; these are snapshots of comparative design studies – not fully optimized designs.

## Slide 58: BigBOX
Brookhaven DCC17 magnet provides 9.2 T field.
A 13-turn Nb3Sn hardway-bend racetrack coil will see ~120 MPa with ~25% margin on one straight section.
This corresponds to the most strenuous operating condition expected for a stress-managed coil.
BigBOX was delivered 06/2022.
Test expected soon ...
Courtesy of D. M. Araujo

## Slide 59: Materials R&D
Elimination of pyrolyzed organic residues.
  Combustion in vacuum above 580ºC for highest efficiency.
  Minimum oxygen injection, controlled through CO, CO2 sensors and electrical measurements.
  RRR tests show 8% reduction.
  BOX test for super-clean surfaces will follow. Cable-stability test needed.
Spray/dip-coating and glazing process with heat-resistant insulating paint.
Low K1c CTD101K.
No-bond epoxy/wax blend.
Courtesy A. Brem.

## Slide 60: Materials R&D
Cryogenic tribology with BAM Berlin.
Wax characterization at ETHZ.
Filled-wax/epoxy process development
  Particle functionalizing, dispersion.
  Vacuum bag filling.
  VPI for the most reliable impregnation process.
Courtesy A. Brem.

## Slide 61: Outlook
2023-2024 will see the sub-scale program, that shall tune and validate manufacturing processes and discover major design issues (3-4 magnet tests).
2024-2026 will see the ultimate- field program (at lest 1 magnet test).
Material sample and powered-sample R&D will continue in support of large- scale magnets.
Collaboration remains a center-piece of our methodology. CHART collaborations, close exchanges with the CIEMAT’s common-coil program, and open exchanges and cooperation throughout the HFM Programme will remain a priority.
Materials and Composite Samples (not powered)
Powered Samples and Mechanical Models
Sub-scale Magnets
Short Magnets Ultimate Field (14…16T)
Long Magnets Ultimate Field Magnets (14…16 T)
2023-2024
2024-2026

## Slide 62: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  HTS Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 63: 4-Stack Technology Solenoid in the Cryogen-Free Test Station
Successful test in cryogen-free test station of 4-pancake HTS NI solenoid, built in-house at PSI and using licensed Tokamak Energy Ltd technology.
Coil reached 18.2 T in the center, 20.3 T on the conductor at the maximum current of the power converter of 2 kA.
Stack of 4 NI HTS coils with thermal/ electrical connectors
HTS leads
1st cryocooler
4K coldhead
2nd cryocooler
20K coldhead
thermal
connectors
radiation shield
top plate
Cu leads
Diameter: 100 mm
Aperture: 50 mm
SC type: ReBCO
# tapes: 2
# turns: 2 x 170
SC length: 2 x 49 m
Courtesy of M. Duda, J. Kosse, H. Rodrigues

## Slide 64: 4-Stack Technology Solenoid in the Cryogen-Free Test Station
field
current
coils voltage
2 kA 3h
18.2 T
1.6 mV
over 4 coils
~800 nohm
slow ramp
down with
0.5 A/s only
A B C D
0-A:
fast ramp up with 1 A/s
voltage over coils increasing because of current radial path
A-B:
slower ramp up with 0.2 A/s to stabilize coils voltage increase
B-C:
2 kA 3h plateau
coils voltage decreasing because of current redistribution
field is increasing – not reaching plateau
C-D:
slow ramp down with 0.5 A/s to avoid quench back
Courtesy of M. Duda
Gained experience with NI coils.
Thermal runaway as consequence of bad electro- thermal contact (indium contact sheet was re-used).
Axial contacting plates needed to be re-soldered.
No SC degradation observed.

## Slide 65
HTS NI target solenoid, to demonstrate
high-yield positron source concept
  stable DC operation,
  high thermal conduction due to solder impregnation to extract heat deposited in coils,
  radiation robustness due to absence of insulators.
Manufacturing Q3’23-Q2’24
Experiment at PSI’s SwissFEL 2025/26
Coil diameter | 122 mm inner, 219 mm outer
Stored energy | 331 kJ
Operating current | 1.17 kA
Charging constant | 11 hours
15 T in 72 mm warm bore
21 T on conductor
15 K conduction-cooling
Solid-state (Pb) thermal buffer
5 coils from 12 mm ReBCO
target
FCCee Injector Study:P3 (PSI Positron Production)
Courtesy J. Kosse, T. Michlmayr, H. Rodrigues

## Slide 66: Solder Impregnation Technology
Fluxed Winding
Soldering from top
Rosin Flux
200 Celsius
+ 30 min cycle
Problems:
Dry patches inside
Time
Fluxed-Hot-winding
Pre-tinned tape
Rosin Flux
200 Celsius
~ 25 min cycle
Problems:
Small empty voids
Time
Fluxed winding
Pre-tinned tape Bath soldering in vacuum
Removable mandrel
GSP-2533 Flux
210 Celsius
~ 3 min cycle / ~ 5 mbar
Problems: Unequally spaced turns
Courtesy of H. Rodrigues (PSI)
Fluxed winding
Pre-tinned tape
Bath soldering in vacuum
Removable mandrel
Tightening during soldering
GSP-2533 Flux
220 Celsius
~ 3 min cycle / ~ 5 mbar
Problems: Tbs

## Slide 67: HTS for HFM
How to make cable for HTS accelerator magnets (e.g (15 m long, 16+ T, 4.2-20 K)?
  How to deal with ramp losses?
  How to guarantee sufficient integral field quality?
  How to protect the magnets?
Material development for insulated tape stack.
Numerical studies for transient effects in cross-section.
Insulated tape-stack cable manufacturing.
Technology racetracks.
Hybrid configuration of SM-CC beyond 2025.
Ultimately HTS-only SM-CC.
Close technical exchange with MSC has started.
Materials and Numerical Design Studies
Powered Cable Samples
Technology Racetrack Coils
Short Hybrid HTS/LTS Magnets (15…17 T)
Short All-HTS Magnets (16…20 T) (4.2…20 K)
Q4’24

## Slide 68: HTS4: HTS short straight sections for FCC-ee
By using HTS sextupoles and quadrupoles instead of the RT baseline, HTS4 aims to:
Reduce energy consumption from up to 80 MW (43 MW in CDR) to <10 MW
Increase dipole filling factor
Enhance optics flexibility
Challenges:
Accelerator-grade field quality with HTS
Balance cooling power with conductor volume
High-reliability cryocooler-based operation
Low heat-load powering
Mitigation of radiation issues on electronics
Sub-scale coils and 1-m prototype module to be constructed and tested at PSI
CCT variant courtesy M. Koratzinos

## Slide 69: MagDev2 (2023-2024) Under Preparation
Application to SERI for support of CHART 2025-2028 under preparation.
RD4
RD3
RD2
HFM

## Slide 70: Overview
CHART and HFM
CHART1: Canted Dipole 1 (CD1)
CHART2:
  MagDev Lab
  Technology R&D and Stress-management
  HTS Technology Solenoid, Pcubed
  HTS4
  HTS HFM
MagXX family of CHART projects

## Slide 71: D-MAT SMG: MagRes
Development of fracture-tough resins.
Best-in-class K1c with multi-hour pot-life.
Made from readily available components.
Courtesy P. Studer and Prof. T. Tervoort

## Slide 72: ETHZ D-MAVT/pd|z and inspire AG: MagAM
Enhanced functionality in coil components through design for Additive Manufacturing
  Interpenetrating Phase Layers for improved bonding.
  Compliant endspacers.
  Locally tunable modulus for.
Courtesy P. Beutler

## Slide 73: D-ITET IEF: MagNum
Enhanced reproducibility, traceability, and sustainability through Model-Based Systems Engineering for accelerator magnets.
pyMBSE package and a bundle of standard tools and best practices are now supported and maintained by MSC group.
Pilot projects under way at CERN, ETHZ, LBNL, and PSI.
Courtesy M. Maciejewski

## Slide 74: D-MAT SMG: MagComp
Started in December 2022, MagComp will attempt to
  mechanically characterize 10-stacks produced at PSI with different epoxies/waxes.
  perform detailed subscale modeling.
  extract 3D anisotropic elasto-plastic constitutive relations.
  link with related efforts through HFM RD4.
Courtesy D. Araujo, X. Kong

## Slide 75: D-ITET PES: FCCee CPES
In support of FCCee HTS4, CPES develops a cryogenic power supply which, in its first iteration, may reduce heat load to the cryo-cooler by 50%.
CPES development follows specifications provided by CERN power-supply specialists.
The CPES unit may incorporate magnet protection functionality.
Cold-testing and integration studies at PSI cryogen-free test station.
Courtesy J. Huber

## Slide 76: Conclusion
CHART supports the goals of the HFM Programme and carries out magnet development for FCCee.
The MagDev laboratory is fully operational with a dedicated and focused team.
We aim to build a Nb3Sn ultimate-field demonstrator by 2026.
We believe that the stress-managed approach to be a unique contribution to the HFM community’s effort and improve the overall risk-balance.
Our HTS program supports FCCee, creates synergies for PSI, and its HFM activity is designed for full synergy with the LTS program.
Coordination, communication, and collaboration are key for gettting the most out of the CHART network and for being a constructive partner in HFM.
We are grateful for support throughout the community, in particular CERN, FNAL, LBNL, uTwente!
The challenges are real and ieads are plentyful – it is an exciting time to do magnet R&D! We are looking forward to our exchanges in the HFM R&D Fora!

## Slide 77
Spare Slides

## Slide 78: Fast-Turnaround R&D Programme as an Innovation Funnel
HFM R&D has suffered from slow turnaround and late feedback on technological choices.
“We propose to structure the magnet R&D as a succession of meaningful fast-turnaround demonstrations, ranging from non-powered material […] samples […] towards ultimate specifications. In this way, new technologies can be tested under realistic conditions at the earliest possible stage, the smallest relevant scale and cost, and the fastest pace.“
Materials and Composite Samples (not powered)
Powered Samples and Mechanical Models
Sub-scale Magnets
Short Magnets at Intermediate Field
(11…12T)
Long Robust Magnets (11…12T)
Short Ultimate Magnets (14…16T)
Long Robust
Ultimate Magnets (14…16 T)
HTS Samples and Technology
HTS Design Studies
(LTS/HTS hybrid , all-HTS)
Sub-scale HTS Magnets
HTS Demonstrator Magnets
(16…20 T)
Hybrid LTS/HTS R&D Magnets
(4.2 K)
All-HTS
R&D Magnets
(4.2…20 K)
Examples of multi-scale demonstrators for LTS and HTS magnet R&D, adapted from Figs. 2.11 and 2.12.

## Slide 79: Non-contained Wax in U-Shaped Sample at uTwente

## Slide 80
[Copper Development Organization, Guide to Nickel Aluminium Bronze for Engineers, 2019]

## Slide 81: CD1 Protection: Energy Extraction & CLIQ
Assess protection of CD1 with EE only and, CLIQ with a EE delay.
Based on Jiani’s PhD Thesis.
Typically, EE tested and triggered at lower currents and extraction (MIITs) calculated.
CLIQ assessed by triggering at lower currents to gauge max current in inner coil.
Significantly lower quench integral than expected.
CLIQ tests have larger quench integral because we added some energy extraction delay.
CLIQ 300V 10 mF

## Slide 82: CD1 Protection: Energy Extraction & CLIQ
Assess protection of CD1 with EE only and, CLIQ with a EE delay.
Based on Jiani’s PhD Thesis.
Typically, EE tested and triggered at lower currents and extraction (MIITs) calculated.
CLIQ assessed by triggering at lower currents to gauge max current in inner coil.
Significantly lower quench integral than expected.
CLIQ tests have larger quench integral because we added some energy extraction delay.

## Slide 83: Resistance to Mandrel
CD1, after reaction and impregnation, had a resistance of approx. 3 Ohms to the mandrel.
Coil to mandrel resistance greatly improves when cold.
This transition was noticed for each thermal cycle.

## Slide 84: RRR measurements
Fast and uniform transition
RRR (293/20) values:
  All magnet: 270 +- 6
  Outer layer: 290 +- 10
  Inner layer: 250 +- 10

## Slide 85: CD1: Splice Resistance