## Slide 1: WP6, Results and Outcomes from Latest WP6 Test Campaigns in Radiation Facilities
André M. P. Mattos (IES/University of Montpellier)
Almudena Lindoso (UC3M)
RADNEXT 2nd Annual Meeting – 9-10 May 2023
https://indico.cern.ch/e/radnext-2023

## Slide 2: Outline
IES/UM: Test Campaigns
  CHARM: RISC-V/SoC
    Power and logging challenges
  ChipIr: RISC-V/SoC/FPGA
  PSI: SRAM
    Setup, capabilities, and results
Conclusions
UC3M: Test Campaigns
  CHARM: SoC
  ChipIr:
    Microprocessors/SoC
    FPGAs
    GPUs
  UltraScale+
Publications
Conclusions

## Slide 3
IES/UM: Test Campaigns

## Slide 4: IES/UM: Test Campaigns
 | Source | Facility | Date | Experiment
1st year | Protons | PSI | 12/21* | SDRAM/HyperRAM
 | Heavy Ions | RADEF | 02/22 | SRAM
 | Neutrons | ChipIr | 05/22* | RISC-V/SoC/NoC
 | Protons | PARTREC | 06/22* | RISC-V/SoC
2nd year | Mixed-Field | CHARM | 10/22 | RISC-V/SoC
 | Neutrons | ChipIr | 11/22* | RISC-V/SoC
 | Protons | PSI | 12/22 | SRAM
 | Laser | ESTEC | 05/23 | SRAM
*Test campaigns through TA calls
CHARM
CHARM
Irradiation room
Control room

## Slide 5: > CHARM: RISC-V/SoC
Characterization of a fault-tolerant RISC-V system-on-chip in flash-based FPGAs
  Two different board designs with same FPGA family, but different power regulators
  Both boards with external SEL protection and current monitoring
  External robust communication fixtures were used to extend the logging interfaces
  Similar setups and conditions, but two very distinct experimental characteristics
  Despite that, there is good correlation between results considering the useful operation time
[2] [Accepted] André M. P. Mattos, Douglas A. Santos, et. al., “Using HARV-SoC for Reliable Sensing Applications in Radiation Harsh Environments”, IWASI, 2023.
[1] [Under review] Douglas A. Santos, André M. P. Mattos, et. al., “Enhancing Fault Awareness and Reliability of a Fault-Tolerant RISC-V System-on-Chip”, Electronics, 2023.
SMF2000:
M2S010
SDRAM
HARSH:
M2S025
3x SDRAM

## Slide 6: > CHARM: RISC-V/SoC >> Power regulators
 | TLV62565 | EP53A7HQI | LM317
Device type | Switching regulator | Switching regulator | Linear regulator
Board critical TID | ~ 19 krad | > 36 krad | > 36 krad
# SELs | 1 | 1 | 1
# Transients | 1 | 7 | 6
Observations | After critical TID, it was not operational, but current limited. After 29 krad, it had unlimited consumption | Steady current increase (voltage decrease) ~ 6.5% | Steady current decrease (voltage increase) ~ 8.5%
75 mA
135 mA
124 mA
80 mA
TLV62565
EP53A7HQI
LM317
SEL
Transients
Limited
Unlimited
~150mA

## Slide 7: > CHARM: RISC-V/SoC >> Logging interface
Robust interface: UART ↔ RS-485
  UART with flow control
  RS-485 transceiver
  IO buffer
  Flexible and easy to use (transparent)
  RJ45 connector/cable for physical connection
    Robust and often available in patch panels
 | ChipIr [Neutrons] | PARTREC [High-energy protons] | CHARM [Mixed-field]
High-level failures | None¹ | Desynchronization¹ | None²
Observation | Cable: 125m (with patch panel connections) Baud Rate: 3Mbauds | Only one occurrence: IO buffer caused the flow control to unsync data | 
¹Functional testing only (loopback) with direct irradiation, ²Only usage (no specific testing)
UART → RS-485
RS-485 → UART
DUT
HOST COMPUTER
≈
Irradiation room
Control room
UART → USB

## Slide 8: > ChipIr: RISC-V/SoC
Characterization of a fault-tolerant RISC-V system-on-chip in a SRAM-based FPGA
  Adaptation from the flash-based port
  External bitstream memory required
  Sensitive configuration memory
    Custom scrubbing and correction (alternative to the SEM IP) with integration to the SoC
Zybo:
Zynq-7000 family
Flash
SDRAM
 | SoC in Flash-based FPGA [Microchip] [M2S010] | SoC in SRAM-based FPGA [Xilinx] [Zynq-7010]
Total Fluence [n/cm²] | 1.80x10¹² | 5.83x10¹⁰
Mean Fluence to Failure [n/cm²] | 2.06x10¹⁰ | 3.60x10⁸
Cross Section [cm²] | 4.98x10‾¹¹ | 2.78x10‾⁹
~ 200x difference in robustness
[3] [Under review] Douglas A. Santos, Pablo M. Aviles, André M. P. Mattos, et. al., “Hybrid Hardening Approach for a Fault-Tolerant RISC-V System-on-Chip”, RADECS, 2023.

## Slide 9: > PSI: SRAM
Investigation on radiation-induced single-event latch-ups in SRAM memories on-board PROBA-V mission
  Understanding the flight behavior and error rates
Utilization of an experimental approach attending the target environment
  RADEF: Heavy Ions
  PSI: Protons
  ESTEC: Laser (further investigation of the observed phenomena)
Development of an experimental setup for enhanced observability
[5] [Under review] André M. P. Mattos, Douglas A. Santos, et. al., “Instrumentation and Methodology for In-Depth Analysis of Single-Event Latch-up on Memory Devices”, Journal of Instrumentation, 2023.
[4] [Under review] André M. P. Mattos, Douglas A. Santos, et. al., “Investigation on Radiation-Induced Single-Event Latch-up in SRAM Memories on-Board PROBA-V”, RADECS, 2023.

## Slide 10: > PSI: SRAM >> Test Setup
Enhanced experimental setup
  Precise timing and current measurements
  Coherent monitoring between memory errors and current measurements
  Many test modes with realistic stimuli
  Robust and flexible test setup

## Slide 11: > PSI: SRAM >> Experimental features
Dynamic test: current behavior
  Correlation with each test operation within a dynamic test cycle
  Current values during SEL events
*Data from heavy ions experiment

## Slide 12: > PSI: SRAM >> Results
Error accumulation during SEL events
  Example within a dynamic test
  50ms “hold time” and 200ms “cut time”
Event cross sections
  Good correlation between lots
  Weibull fitting

## Slide 13: Conclusions
Tests at CHARM presented many setup challenges to be addressed before the campaign
Tests at ChipIr provided more insights on the capabilities of Flash- and SRAM- based FPGAs for radiation testing
Tests at PSI allowed the elaboration of an enhanced setup and provided practical insights
We are currently working in the first WP6 milestone, which will summarize the setup preparation experience obtained in these first 2 years of the project
We intend to elaborate more publications using the acquired data and experience

## Slide 14
UC3M: Test Campaigns

## Slide 15: UC3M: Test Campaigns TA RADNEXT
 | Source | Facility | Date | Experiment
1st year | Protons | PSI | 12/21 | µp/FPGA/SoC
 | Neutrons | ChipIr (1/3) | 05/22 | µp/FPGA/SoC/GPUs
2nd year | Neutrons | ChipIr (2/3) | 09/22 | µp/FPGA/SoC/GPUs
 | Mixed field | CHARM | 10/22 | µp/SoC
 | Neutrons | ChipIr (3/3) | 11/22 | µp/FPGA/SoC/GPUs
3rd year | Protons | PARTREC | 09/23 | µp/FPGA/SoC
 | X-ray (microbeam) | ESREF | Under review | µp/FPGA/SoC/Memories
CHARM
2 commercial boards (zybo)
Microprocessor hardening techniques
Complex setup
After 6.31krad (~20 hours), board non responsive
CHARM
Completed

## Slide 16: > ChipIr: Experimental setup
Experiments UC3M, complex COTS systems:
  8x SoC Xilinx Zynq-7000 (28 nm): Microprocessors, FPGA, SoC
  6x Jetson Nano (20 nm): Quad-core A57 & NVIDIA Maxwell GPU
  1x SoC Xilinx UltraScale+ (16 nm FinFET)
Experimental
Setup (May)
Several experiments
per board type
ChipIr

## Slide 17: > ChipIr: Experimental setup
Experiments UC3M, complex COTS systems :
  8x SoC Xilinx Zynq-7000 (28 nm): Microprocessors, FPGA, SoC
  6x Jetson Nano (20 nm): Quad-core A57 & NVIDIA Maxwell GPU
  1x SoC Xilinx UltraScale+ (16 nm FinFET)
Experimental
Setup
(November)
ChipIr
ChipIr
8x Zybos
6x Jetson
UltraScale+

## Slide 18: > ChipIr: Experimental setup
UltraScale+
GPU
Zynq & UltraScale+: serial communication
GPU: Ethernet connection
External host (Raspberry Pi) to control the
experiments & Power cycles
UltraScale+: SEL detector
Zynq

## Slide 19: > ChipIr: Evaluation of events vs board location
Zynq 7000
3 Different hardening techniques
  PL
  SoC (PL+PS)
NIR_RRR_SEM behaves differently
  Includes Xilinx SEM IP:
  Detects & corrects PL errors
Board position | SEM corrections | PL+PS events
5 | 978 | 205
6 | 1119 | 214
Experiment | ∆ Errors (%)
dCR_RRR (PL) | - 13.37 (+3 positions)
NIR_RRR_noSEM (SoC) | - 47.50 (+5 positions)
NIR_RRR_SEM (SoC) | +4.21
SoC (PL+PS)
PL

## Slide 20: > ChipIr: Cross-section
Comparison different particles/ different complex systems
 | FPGA Zynq-7000 | Microprocessors Zynq-7000 | SoC Zynq-7000 | GPU Experiment 1 (6 benchmarks) | GPU Experiment 2 (12 benchmarks)
Total Fluence [n/cm²] | 2.72x1011 | 2.57x1011 | 3.38x1011 | [1.51x1010 , 9.30x1010 ] | [3.56x1011, 1.17x1012 ]
Cross-section [cm²] Neutrons ChipIr | 1.38x10-9 | 9.64x10-9 | 1.28x10-8 | [9.68x10-9, 1.56x10-9 ] | [8.48x10-9, 3.53x10-9 ]
 | FPGA Zynq-7000 | Microprocessors Zynq-7000
Cross-section [cm²] Protons PSI | 4.42x10-10 | 1.38x10-9
Cross-section [cm²] Protons CNA | 1.86x10-10 | 5.61x10-10
ChipIr experiments/benchmarks:
  FPGA: 3
  SoC: 1
  GPUs: 12
  Microprocessor: 3
    2 soft-core (RISC-V)
    1 hard-core (Cortex A9)
Similar experiments
Previous Results
RADECS DW 22
ChipIr

## Slide 21: > ChipIr: Cross-section
Comparison CHARM/ChipIr complex system microprocessor-based hardening technique
  Based in:
Microprocessor Hardening technique |  | CHARM | ChipIr
 | Fluence [particles/m2] | 5.67x1011 | 2.57x1011
 | Cross-section [cm2] (Total events) | 2.35x10-9 | 9.64x10-9
 | Cross-section [cm2] (Undetected errors) | 1.23x10-11 | 5.84x10-11
 | Error rate [errors/hour] | 114.12 | 105.13
 | Time [hours] | 11.66 | 23.56
Up to 2 orders
of magnitude
improvement
P. M. Aviles, A. Lindoso, J. A. Belloch, M. Garcia-Valderas, Y. Morilla and L. Entrena, "Radiation Testing of a Multiprocessor Macrosynchronized Lockstep Architecture With FreeRTOS," in IEEE Transactions on Nuclear Science, vol. 69, no. 3, pp. 462-469, March 2022
doi: 10.1109/TNS.2021.3129164.

## Slide 22: > ChipIr: SoC UltraScale+
Small number of events
Microlatchup (under SEL stablished limit=500 mA)
The same test was performed at CNA (15 MeV protons)
  Small number of events
    Flux was increased: TID effects observed (persistent current degradation)
  No SEL observed
Additional tests will be performed in the next TA campaigns (PARTREC)
CNA
ChipIr
CNA
CNA

## Slide 23: Publications
RADECS 2022 Data Workshop: P. M. Aviles, L. A García-Astudillo, J.A. Belloch, L. Entrena, A. Lindoso, “Comparative of proton radiation data for 28 nm Zynq-7000 SoC”
IEEE TNS (Special issue RADECS 2022) : L. A. García-Astudillo, A. Lindoso, et al., "Evaluating Reduced Resolution Redundancy for Radiation Hardening in FPGA designs"
doi: 10.1109/TNS.2023.3268825
Under Review:
RADECS 2023
  D. A. Santos, P.M. Aviles, A.M.P. Mattos, M. Garcia-Valderas, L. Entrena, A. Lindoso, L. DiLillo, “Hybrid Hardening Approach for a Fault-Tolerant RISC-V System-on-Chip”
  G. Leon, J.M. Badia, J.A. Belloch, M. Garcia-Valderas, A. Lindoso, L. Entrena, “Analysing the influence of memory and workload on the reliability of GPUs under radiation”
Journal publications & conference communications in progress

## Slide 24: Conclusions
Successful test of complex systems in different facilities
  SoC, hard-core & soft-core microprocessors, FPGA and GPUs
Combine different experiments/different boards & sensitivities for a radiation campaign
Challenges in testing complex devices:
  SoC
  GPUs
Comparison of irradiation campaigns results for different facilities/particles
Developing guidelines for non-expert end users

## Slide 25: Thanks for your attention!
Image Source: IES/UM
André M. P. Mattos (IES/UM):
andre.martins-pio-de-mattos@etu.umontpellier.fr
Almudena Lindoso (UC3M):
alindoso@ing.uc3m.es