## Slide 1: RMM1a,b magnet Assembly and test results of the RMM1a,b magnet, a CERN technology demonstrator towards Nb3Sn ultimate performance
Emma Gautheron, Juan Carlos Perez, Susana Izquierdo Bermudez, Davide Tommasini, Hélène Felice, Michael Guinchard, Carlo Petrone, Gerard Willering, S. Mugnier, G. Campagna
24.10.2022 – Oral sessions – Nb3Sn Dipole Magnets – 1LOr1C-01

## Slide 2: Content
RMM magnet program
Mechanical design and assembly
Powering tests

## Slide 3: Context
Scope of the eRMC and RMM magnet program

## Slide 4: RMM: Racetrack Model Magnet
Explore the Nb3Sn technology for high field accelerator magnets
RMM is a demonstrator:
    Nb3Sn in high field (Btarget > 16 T)
    Mechanical preload study
    Close cavity Ø 50 mm
  Towards Nb3Sn ultimate performance:
    Conductor type HL-LHC
    Bshort sample = 18.8 T at 1.9 K
    RMM1b reached 16.7 T Bp (88 % of SS)
Lcavity_tot = 526 mm
Lcavity_D50 = 431 mm

## Slide 5: RMM: a big dipole magnet
Courtesy of E. Todesco
Chart: Equivalent coil width (mm)
| 9 | 16.5 | 15 | 19 | 14.5 | 30 | 34
Nb-Ti | 3.5 | 4.3 | 4.4 | 4.5 | 6 | 9 | 10.07
Nb3Sn | 9.5 | 10.8 | 12 | 13.8 | 13.5 | 14 | 14.5 | 16.5
oblique line | 0 | 18
Relatively large coil width with low current density
Notes: Ezio’s comments:
The line of 450 A/mm2 corresponds to the case of an ironless magnet – therefore it is there just to guide the eye and give an order of magnitude
If a magnet sits on the 450 A/mm2 line, it does not mean that this is its actual overall current density as the presence of iron reduces the current
In some magnets, grading is used, so for instance in the LHC dipole inner layer is at 360 A/mm2 and outer layer is at 440 A/mm2 – obviously this complexity is not visible in the plot

## Slide 6: RMM: a big dipole magnet
0.8 m
1.2 m

## Slide 7: RMM: part of a more global strategy
Racetrack Coils
Racetrack Coils
with Cavity
Racetrack Coils
with Cavity
and Flared ends
 eRMC magnet
 RMM magnet
 DEMO magnet (?)

## Slide 8: Magnetic design RMM
1 mm diameter wire, Cu/Sc ~ 1
40-strand Rutherford cable
eRMC pole in magnetic stainless steel ST 430
Bp/Bo ~ 1
Rcoil aperture = 31 mm
3D design [6] : Peak field in the straight section
Chart: eRMC & RMM Load lines
| 0 | 2.26206928 | 3.7250829200000002 | 4.9484206500000001 | 6.0941077799999999 | 7.1928363900000001 | 8.2717790400000002 | 9.3421110600000006 | 10.4064578 | 11.4658727 | 12.522071 | 13.5764212 | 14.631514299999999 | 15.6851334 | 16.737435000000001 | 17.788520500000001 | 18.8395121 | 19.889980099999999 | 20.939469299999999 | 21.988032100000002 | 23.0359035
eRMC 2D Load w/SF | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
RMM 2D Load w/SF | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20
102,min,1.9K | 130.045 | 109.843 | 93.0007 | 78.7486 | 66.5589 | 56.0549 | 46.9588 | 39.0597 | 32.194 | 26.2323 | 21.0702 | 16.6225 | 12.8187 | 9.5996 | 6.9151 | 4.7226 | 2.9851
102,min,4.3K | 104.5986 | 87.0404 | 72.4732 | 60.222 | 49.8232 | 40.9449 | 33.3422 | 26.8286 | 21.2592 | 16.5191 | 12.5156 | 9.1728 | 6.4276 | 4.2272 | 2.5267 | 1.2876 | 0.4769
12.3 kA
17.1 T
13.6 kA
18.8 T

## Slide 9: Mechanical Design and Assembly
Targets for pre-load, Fuji tests and final assemblies into RMM1a & RMM1b

## Slide 10: Mechanical design RMM
Preload target: powering at 11.8 kA – i.e. 16.5 T Bp and 16.3 T Bo
  Preload strategy:
    Transverse: Small coil-pole detachment at powering
    Axial: 80 % of the Lorentz forces in the rods at cold
Upper stress limit: 150 MPa Von Mises in the coil blocks
RT preload:
Cold:
Powering:
Coil VM stress: 82 MPa max
Coil-Pole transverse pressure: 20 MPa min
ANSYS APDL 3D Finite Element Model
Coil VM stress: 153 MPa max
Coil-Pole transverse pressure: 65 MPa min
Coil VM stress: 143 MPa max
Coil-Pole transverse pressure: 10 MPa min

## Slide 11: Summary of assembly iterations
Dummy assembly
Characterization of the mechanical structure
Aluminum coils
RMM1a
Coil pack & contact optimization
Fuji assemblies at half lateral preload & shimming fine-tuning
 16.6 T Bp at 1.9 K
RMM1b
Longitudinal re-assembly
Machining of the rods & reduction of the longitudinal preload target
 16.7 T Bp at 1.9 K
eRMC1a
Coil pack & contact optimization
Coil rails’ machining & lateral coil shimming
 16.5 T Bp at 1.9 K
2019-2020 [8]
2018-2019 [7]
2021
2022

## Slide 12: Summary of assembly iterations
Dummy assembly
Characterization of the mechanical structure
Aluminum coils
(2018-2019)
RMM1a
Coil pack & contact optimization
Fuji assemblies at half lateral preload & shimming fine-tuning
(2021)
RMM1b
Longitudinal re-assembly
Machining of the rods & reduction of the longitudinal preload target
(2022)
eRMC1a
Coil pack & contact optimization
Coil rails’ machining & lateral coil shimming
(2019-2020)

## Slide 13: Reminder – eRMC1a performance
Courtesy of S. Ferradas Troitino
20 A/s
Reusing the 2 eRMC coils for the RMM magnet:
102
101
eRMC 102
RMM
eRMC1a
RMM1a,b
eRMC 101

## Slide 14: Summary of assembly iterations
Dummy assembly
Characterization of the mechanical structure
Aluminum coils
(2018-2019)
RMM1a
Coil pack & contact optimization
Fuji assemblies at half lateral preload & shimming fine-tuning
(2021)
RMM1b
Longitudinal re-assembly
Machining of the rods & reduction of the longitudinal preload target
(2022)
eRMC1a
Coil pack & contact optimization
Coil rails’ machining & lateral coil shimming
(2019-2020)

## Slide 15: Coil pack – Contact optimization
Coil rail
Machining of the coil rails:
eRMC coils’ width reduced by 50 um after cold (SS)
RMM coil machined to their average width
 all coils within 50-100 um in width in the straight section
Fuji tests & shimming optimization:
Pole-to-pole contact
   fine-tuned shims
Transverse preload uniform on the coil straight sections
  eRMC coils: +150 um on each side
  RMM coil: +100 on each side
Notes: + based on Faro arm measurements

## Slide 16: Preloading of the coil pack
Bladders
Bladders & Keys – RT preload driven by the monitored strain on shell midplane / on rod

## Slide 17: Preloading of the coil pack
Bladders
Bladders & Keys – RT preload driven by the monitored strain on shell midplane / on rod
Chart: Interference (mm)
| 0 | 1.2 | 1.6 | 1.7
FEA | 0 | 1053.9842 | 1053.9842 | 1815.0275
measurements_midplane | 266.3667 | 262.0333 | 261.75 | 283.5167 | 304.8667 | 313.3 | 332.9 | 359.1 | 409.65 | 435.15 | 482.1 | 519.8333 | 581.6167 | 615.8833 | 669.1833 | 725.7333 | 754.0833 | 817.0167 | 859.2167 | 891.5167 | 957.2 | 987.45 | 976.1667 | 967.65 | 964 | 1405.6667
Room temperature (RT)
1.9 K
Final RT preload step
Following steps
D+1
D+4
cryostat
1.9 K
RT preload
D+4
cryostat
1.9 K
RT
1.9 K
Chart: Rods εz [μm/m]
| Loading [28/10/2021] | Relaxing after loading [01/11/2021] | Check on HFM insert [19/11/2021] | Cooldown [29/11/2021]
RAZ | 569.5 | 536.6 | 536.9 | 679.236
RBZ | 569.7 | 511.3 | 511.1 | 591.836
RCZ | 568.6 | 519.4 | 514.1 | 683.836
RDZ | 577 | 541.5 | 541.8 | 555.772
FEA Strain Z (um/m) | 568 | 568 | 568 | 658
AVG Strain Z (um/m) | 571.2 | 527.2 | 525.975 | 627.67
Measured
77 % of L.F.
 Transverse:
 Axial:
At cold: magnet less preloaded than expected & asymmetry in the rods

## Slide 18: Rods’ behavior – during cool down
Courtesy of S. Mugnier
900
800
700
600
500
Cooldown – RMM1a
Warm-up
Tue 23
Thu 25
Sat 27
Mon 29
Wed 1
Nov 2021
Rods εz [um/m]
RA
RB
RC
RD
Observations during cool down:
Asymmetry of traction strain
Jumps in the rod strain gauges’ signals
RA_Z
RB_Z
RC_Z
RD_Z
 Interference between rods and yoke at this level of transverse interference

## Slide 19: Rods’ behavior – during cool down
Courtesy of S. Mugnier
900
800
700
600
500
Cooldown – RMM1a
Warm-up
Tue 23
Thu 25
Sat 27
Mon 29
Wed 1
Nov 2021
Rods εz [um/m]
Observations during cool down:
Asymmetry of traction strain
Jumps in the rod strain gauges’ signals
RA_Z
RB_Z
RC_Z
RD_Z
 Interference between rods and yoke at this level of transverse interference
 Mechanical iteration: RMM1b
Machining of the rods (from Ø64 to 60 mm)
Longitudinal reassembly only
New axial target of 70 % of LF at cold
Courtesy of S. Mugnier
Courtesy of G. Campagna for the calculations
900
800
700
600
500
Rods εz [um/m]
Fri 19
Sun 21
Aug 2022
RA_Z
RB_Z
RC_Z
RD_Z
Cooldown – RMM1b

## Slide 20: Summary of assembly iterations
Dummy assembly
Characterization of the mechanical structure
Aluminum coils
(2018-2019)
RMM1a
Coil pack & contact optimization
Fuji assemblies at half lateral preload & shimming fine-tuning
(2021)
RMM1b
Longitudinal re-assembly
Machining of the rods & reduction of the longitudinal preload target
(2022)
eRMC1a
Coil pack & contact optimization
Coil rails’ machining & lateral coil shimming
(2019-2020)

## Slide 21: Powering Tests at Cold
Training, magnetic and mechanical performance, RMM1a & RMM1b

## Slide 22: Training at 1.9 K
Chart: RMM1b
| 1 | 2 | 3 | 4 | 5 | 6 | - | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
I (kA) | 11.497 | 11.59 | 11.674 | 11.719 | 11.756 | 11.81 | 11.81 | 11.855 | 11.887 | 11.936 | 11.935 | 11.69 | 11.693 | 11.823 | 11.81 | 11.41
Bp(T) | 16.1165 | 16.2317 | 16.3357 | 16.3915 | 16.4373 | 16.5042 | 16.5042 | 16.56 | 16.5996 | 16.6603 | 16.6591 | 16.3556 | 16.3593 | 16.5203 | 16.5042 | 16.0087
16.7 T Bp (88 % SS)
16.0 T Bp (93 % SS)
16.1 T Bp (84 % SS)
Chart: RMM1a
| 1 | 2 | 3 | 4 | 5 | - | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17
I (kA) | 10.9 | 11.466 | 11.509 | 11.6 | 11.7 | 11.81 | 11.78 | 11.774 | 11.838 | 11.888 | 11.847 | 11.86 | 11.818 | 11.869 | 11.783 | 11.819 | 11.904 | 11.55
15.4 T Bp (80 % SS)
16.6 T Bp (87 % SS)
16.2 T Bp (94 % SS)
4.5 K
4.5 K
Courtesy of G. Willering & C. Bockstiegel
Precursors in quenches
No sign of degradation in the V-I measurements

## Slide 23: Voltage spikes during current ramps
RMM1a – last ramp at 1.9 K
RMM1b – ramp 1
RMM1b – ramp 2
RMM1b – ramp 3
RMM1b – ramp 4
RMM1b – ramp 5
RMM1b – ramp 6
RMM1b – ramp 7
RMM1b – ramp 8
RMM1b – ramp 9
RMM1b – ramp 10
Spikes starting from 11.2 kA in all the current ramps
Courtesy of G. Willering

## Slide 24: Mechanical performance
RMM1a - Quench 17 (11.90 kA)
Axially:
7 % of the longitudinal Lorentz forces seen by the rods
Transversally:
Change of slope around 15.5 T
Vibrations observed from 11 kA

## Slide 25: Quench locations
RMM LOWER
RMM UPPER
eRMC 102 LOWER
eRMC 102 UPPER
eRMC 101 LOWER
eRMC 101 UPPER
RMM1a & RMM1b: a total of 32 quenches
The magnet quenches in the straight section.
Only 4 quenches in the RMM coil.
eRMC 101 alone: 8
eRMC 102 alone: 18
RMM alone: 2
Simultaneous quenches: 4
22 quenches in eRMC 102 LOWER:
Pole turn
1st block
(high field region)

## Slide 26: RMM1b – Record field in the bore
Courtesy of C. Petrone & M. Liebsch
Magnetic measurements :
    7 induction coils and 3 cross calibrated Hall sensors
    On a Printed Circuit Board (PCB), inside the aperture
16.50 T measured
Chart: Event #
| 1 | 2 | 3 | 4 | 5 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17
RMM1a - measured | 15.2586 | 15.9351 | 15.9866 | 16.0443 | 16.1665 | 16.3163 | 16.304 | 16.3826 | 16.4413 | 16.3918 | 16.411 | 16.3578 | 16.4229 | 16.317 | 16.3586 | 16.4614
RMM1b - measured | 15.968 | 16.183 | 16.236 | 16.28 | 16.346 | 16.4 | 16.439 | 16.498 | 16.496 | 16.2005 | 16.2058 | 16.3608 | 16.3456
Chart: Event #
| 1 | 2 | 3 | 4 | 5 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17
RMM1a - measured | 15.2586 | 15.9351 | 15.9866 | 16.0443 | 16.1665 | 16.3163 | 16.304 | 16.3826 | 16.4413 | 16.3918 | 16.411 | 16.3578 | 16.4229 | 16.317 | 16.3586 | 16.4614
RMM1a - calculated | 15.2166 | 15.896 | 15.9476 | 16.0568 | 16.1769 | 16.2729 | 16.2657 | 16.3425 | 16.4025 | 16.3533 | 16.3689 | 16.3185 | 16.3797 | 16.2765 | 16.3197 | 16.4217
RMM1b - measured | 15.968 | 16.183 | 16.236 | 16.28 | 16.346 | 16.4 | 16.439 | 16.498 | 16.496 | 16.2005 | 16.2058 | 16.3608 | 16.3456
RMM1b - calculated | 15.9332 | 16.1456 | 16.1997 | 16.2441 | 16.3089 | 16.3629 | 16.4013 | 16.4601 | 16.4589 | 16.1648 | 16.1685 | 16.3245 | 16.3089
Notes: Measured 0.04 T more than calculated in the bore
0.3 % of error

## Slide 27: Conclusion
    Exploration of high field in the straight section of a Nb3Sn dipole block configuration
    Record field of 16.7 T (88 % of the short sample limit)
    No sign of conductor degradation
    Spikes observed in the differential voltage measurements during current ramps starting from 11.2 kA
    Change of slope observed in the mechanical measurements
    Suspicion of mechanical limitation
    Next step: transverse preload increase

## Slide 28: References
[1] J. C. Perez et al., "16 T Nb3Sn Racetrack Model Coil Test Result," in IEEE Trans. on Appl. Supercond., vol. 26, no. 4, pp. 1-6, June 2016, Art no. 4004906, doi: 10.1109/TASC.2016.2530684.
[2] E. Rochepault and P. Ferracin. Nb3Sn accelerator magnets, chapter CEA-CERN block type dipole magnet for cable testing: FRESCA2. Particle Acceleration and Detection Series. Springer, 2019. https://doi.org/10.1007/978-3-030-16118-7_12
[3] M. Benedikt. Future Circular Collider: The integrated program (FCC-int), 2018. https://fcc-cdr.web.cern.ch/reports/EPPSU18_FCCint.pdf
[4] EUROCIRCOL-fcch2020project.
[5] S. Izquierdo Bermudez, R. Ortwein, J. C. Perez and E. Rochepault, "Design of ERMC and RMM, the Base of the Nb3Sn 16 T Magnet Devel-opment at CERN," in IEEE Trans. on Appl. Supercond., vol. 27, no. 4, pp. 1-4, June 2017, Art no. 4002004, doi: 10.1109/TASC.2017.2651403.
[6] E. Rochepault, S. Izquierdo Bermudez, J. C. Perez, D. Schoerling and D. Tommasini, "3-D Magnetic and Mechanical Design of Coil Ends for the Racetrack Model Magnet RMM," in IEEE Trans. on Appl. Super-cond., vol. 28, no. 3, pp. 1-5, April 2018, Art no. 4006105, doi: 10.1109/TASC.2018.2807803.
[7] M. G. Pérez et al., "Mechanical Tests, Analysis, and Validation of the Support Structure of the eRMC and RMM Magnets of the FCC R&D at CERN," in IEEE Trans. on Appl. Supercond, vol. 30, no. 8, pp. 1-7, Dec. 2020, Art no. 4004507, doi: 10.1109/TASC.2020.3005355.
[8] J. C. Perez et al., "Construction and Test of the Enhanced Racetrack Model Coil, First CERN R&D Magnet for the FCC," in IEEE Trans. on Appl. Supercond, vol. 32, no. 6, pp. 1-5, Sept. 2022, Art no. 4005105, doi: 10.1109/TASC.2022.3163064.

## Slide 29
Thank you for your attention
Contact: emma.lucie.gautheron@cern.ch
A special and warm thank you to Juan Carlos Perez and Helene Felice for their support and supervision.
Many thanks to the complete 927 team, particularly Hugues Dupont and Nicolas Eyraud for their patience and rigor in the magnet assembly process.

## Slide 30: Additional slides

## Slide 31
530
800
RMC
ERMC/RMM
RMC
ERMC
RMM
16 mm closed cavity
50 mm closed cavity
Courtesy of D. Tommasini

## Slide 32: Conductor
53 km of 1.0 mm, RRP wire delivered in 2016 (scrapped OST for Hi-lumi)
4 billets 120/127
sub element size 64 m
Cu/nonCu 1.05-1.10:1
5 billets 150/169
sub element size 55 m
Cu/nonCu 1.05-1.10:1
RRR > 120 with exception of billet 18213 (RRR 90-100)
Courtesy of D. Tommasini

## Slide 33: Strand & Cable Parameters
 | eRMC #101 | eRMC #102 | RMM #101
Strand Type | RRP 120/127 | RRP 150/169 | RRP 120/127
B. Bordini, J. Fleiter & A. Bonasia
1 mm diameter wire, Cu/Sc ~ 1
40-strand cable
Bare cable width x thickness: 20.95 x 1.82 mm (as built)
Assumed growth during HT: 0.8 % (width), 3.6% (thickness)
SS core 14 mm wide x 25 um thick
Mica 44 mm + S2 636, Braided, 0.145 mm

## Slide 34: Insulation
Courtesy of D. Tommasini
Considering the needs for the FCC, we wanted to reinforce the state of the art (11 T) with thicker layers (150 μm).
0.150 +0.00/-0.02 mm Mica-Glass Insulation
Insulation tests preformed to define the best parameters:
  S2 glass 636 11 TEX yarn
  14 yarns (ply) per bobbin
  32 bobbins
  Speed (angle) set to guarantee full coverage and appropriate thickness
yarns

## Slide 35: Magnetic design 2D
eRMC
RMM
eRMC pole in magnetic stainless steel ST 430
90 turns/quadrant
RMM pole in titanium Ti-6Al-4V
132 turns/quadrant
Rcoil aperture = 31 mm
Rclosed cavity aperture = 25 mm
 | eRMC | RMM
Nominal current Inom [kA] | 13.1 | 11.4
Overall current density [A/mm2] | 282 | 245
Bore field [T] | 15.7 | 16.0
Peak field [T] | 16.0 | 16.2
Stored energy at Inom [MJ/m] | 1.5 | 2.1
112 %;214 %
118 %; 2 20 %
119 %;221 %
S. Izquierdo Bermudez et al., "Design of ERMC and RMM, the Base of the Nb3Sn 16 T Magnet Development at CERN"

## Slide 36: Mechanical Design – Overview
FE model in 2D and 3D
Coil block material properties: isotropic linear with a rigidity of 25 GPa at RT and cold
Friction of 0.15 in all contacts; except in yoke-shell which was fine tuned with a dummy assembly and is of 0.1
Impregnated coil as bonded contacts; except coil-pole contact as standard sliding with separation allowed
3 steps:
  RT preload: interference in keys + rods
  Cool down: with CTE coil block isotropic of 3.8 mm/m
  Powering: Lorentz forces from Opera 3D at 11.81 kA i.e. 16.5 T Bpeak

## Slide 37: Shell overall behavior (RMM1a vs RMM1b)
 Similar shell behavior between RMM1a and RMM1b assemblies
Courtesy of S. Mugnier and M. Guinchard

## Slide 38: Rods overall behavior
 The rods unbalance at cold disappears in 1b version. Quite similar behavior between RMM1a and RMM1b assemblies
Courtesy of S. Mugnier and M. Guinchard

## Slide 39: Mechanical response - during a quench TRANSVERSAL
Quench #17 (1.9 K)
Imax = 11.90 kA
Relative Strain
Absolute Strain
10.8 kA / 15.3 T
All vibrations at
11.0 kA / 15.5 T
6 MPa

## Slide 40: Mechanical response - during a quench LONGITUDINAL
Quench #17 (1.9 K)
Imax = 11.90 kA
Absolute Strain
Relative Strain
6 MPa

## Slide 41: V-I measurement RMM1a

## Slide 42: Protection- Quench back studies
Specific energy extraction studies were performed for current between 1000 and 10000 A for both a resistance of 80 mΩ and 60 mΩ.
The measured quench integral is lower then expected from LEDET simulations. Assuming the inductive components were well calculated, one can assume that the quench back effect is stronger than expected.
LEDET simulations courtesy Emmanuele Ravaioli

## Slide 43: Protection- Quench back studies
60 mOhm
80 mOhm
A lot of data from all segments is available for model refinement.
Here one can see in some of the smaller segments the quench(back) start in several segments varying as function of energy extraction resistance.