## Slide 1: Nanophotonic particle detectors
Our group: photonics and quantum tech experiment & theory
Ido Kaminer
FET OPEN
available ERC-funded positions for experienced postdocs
+ how quantum optics can contribute to scintillators and Cherenkov detectors

## Slide 2: Nanophotonics
Image sources: Capasso (Harvard), Soljačić (MIT), Joannopoulos (MIT), Johnson (MIT), Polman (AMOLF), Vuckovic (Stanford), Vahala (Caltech), Englund (MIT) research groups.

## Slide 3: Applications of nanophotonics
LED and lasers
Particle accelerators
Flat optics
Thermal emitters
Photonic computing
nanophotonic scintillators

## Slide 4: Apply nanophotonics to scintillator science?
Control light-outcoupling
  Nanophotonic scintillators
Enhance light-emission
  Purcell scintillators
Inspiration from quantum optics?
  Nanophotonic Cherenkov detectors, with S. Easo @ LHCb X. Lin, Nature Physics (2018), Nature Comm (2021)

## Slide 5: Apply nanophotonics to scintillator science?
Control light-outcoupling
  Nanophotonic scintillators
Enhance light-emission
  Purcell scintillators
Inspiration from quantum optics?

## Slide 6: X-ray scintillation enhancement
Large scale patterns (430x430 microns)
SEM
Roques-Carmes*, Rivera*, et al., Science (2022)

## Slide 7: Setup at MIT (based on a micro-CT)
Source
Specimen
Scintillator
+
Objective
CCD
Roques-Carmes*, Rivera*, et al., Science (2022)

## Slide 8: X-ray scintillation enhancement
Roques-Carmes*, Rivera*, et al., Science (2022)

## Slide 9: X-ray scintillation imaging
Roques-Carmes*, Rivera*, et al., Science (2022)

## Slide 10: Other x-ray scans
TEM Metallic grid
TEM Metallic grid
Human hair
Human hair
Flower bud
Leaf
Leaf
Flower bud
Roques-Carmes*, Rivera*, et al., Science (2022)

## Slide 11: Apply nanophotonics to scintillator science?
Control light-outcoupling
  Nanophotonic scintillators
Enhance light-emission
  Purcell scintillators
Inspiration from quantum optics?

## Slide 12: The Purcell effect
The spontaneous emission rate depends on the EM environment
E. M. Purcell Phys. Rev. (1946)
The Purcell factor
For a dipole in a cavity:
General design rule: highest Q and smallest V
Micropillar
Microdisk
P. Lodahl et al. Rev. Mod. Phys. (2015)

## Slide 13: Purcell effect for scintillation applications
Large V for the optical modes
Low Q for good extraction
But we cannot use the Q/V design rule
The scintillator needs:
Use of the Purcell effect in an untraditional manner
We proposed the concept of Purcell-enhanced scintillators
Yaniv Kurman
Kurman, et al. "Photonic-crystal scintillators: Molding the flow of light to enhance X-ray and γ-ray detection." PRL 125, 040801 (2020).

## Slide 14: The Photonic-crystal scintillator
Use of the photonic band gap to increase emission in desired angles while reducing emission into undetectable directions
Joannopoulos, et al., Molding the flow of light (2008)
Kurman, et al. "Photonic-crystal scintillators: Molding the flow of light to enhance X-ray and γ-ray detection." PRL 125, 040801 (2020).
Yaniv Kurman
Angular Purcell Enhancement

## Slide 15: Experimental realization
Co-dopant sensitizer
Neta Lahav
Lu2O3:Eu-Bi
SiO2
Growth method: sol-gel,
layer by layer
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)
Morales Ramírez et al., J. Mater. Res. 28, 1365 (2013)
Nedelec, J. Nanomaterials 2007, 036392 (2007)
Review: Sol-Gel Processing of Nanostructured Inorganic Scintillating Materials

## Slide 16: Building a new scintillation lab
X-ray
Roman Schütz
optical
fiber
to spectrometer
@ Technion
scintillator
rotating to extract lifetime
analyze angle-depedence
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)

## Slide 17: Proof-of-concept measurements
Faster emission
From to
More photons
Angular emission
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)
Light yield
LYSO (literature): 22000 ph/MeV
Lu2O3 bulk (literature): 19750 ph/MeV
Our thin film: 14550 ph/MeV
With our PhC structure: 26000 ph/MeV

## Slide 18: Robustness to fabrication errors
Specific structures
Ensemble average with scattering
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)

## Slide 19
Enhanced X-ray imaging
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)

## Slide 20: Purcell nanophotonic scintillators
Kurman*, Lahav*, Schuetz*, et al. Purcell enhancement of X-ray scintillation, in preparation (2022)

## Slide 21: High resolution X-ray detectors: breaking their intrinsic trade-off
regular scintillator
vs photonic-crystal scintillator
Shultzman*, Segal*, et al., Purcell-Enhancement of X-ray Imaging and Phosphor-Screens, under review (2022)

## Slide 22: Apply nanophotonics to scintillator science?
Control light-outcoupling
  Nanophotonic scintillators
Enhance light-emission
  Purcell scintillators
Inspiration from quantum optics?

## Slide 23: Inspiration from quantum optics
Sensitive light detectors:
  number-resolved single-photon detectors
Ultrafast light detectors:
  tens of ps time res
But it’s not just about counting the photons!
More information in photon correlations
  Can we use this information to improve the bottom line? image quality?
The duration of Cherenkov pulses (entanglement!)
  Karnieli et al., Science Advances (2021)
Photon bunching in scintillators

## Slide 24
Quantum optical characterization of scintillators

## Slide 25: Quantum optical characterization of scintillators

## Slide 26
available ERC-funded positions for students and postdocs
Kurman, et al. PRL 125, 040801 (2020)
Roques-Carmes*, Rivera*, et al., Science (2022)
Karnieli et al., Science Advances (2021)
Shultzman*, Segal*, et al., under review (2022)
Kurman*, Lahav*, Schuetz*, et al., in preparation (2022)
More on Cherenkov detectors, quantum optics, and other ideas:
kaminer.technion.ac.il

## Slide 27: Why we like doing physics with free electrons
Radiation sources
Nearfield optical microscopy
Shaping single-electron wavepackets
Shentcis et al. Nature Photonics (2020)
Dahan*, Nehemia* et al. Nature Physics (2020)
tunable X-rays
Wang et al. Nature (2020)
Kurman et al. Science (2021)
Dahan et al. Science (2021)
4D imaging
the free-electron comb