## Slide 1: Development of DLC-RPC for Radiative Decay Counter of MEG II Experiment
Atsuhiko Ochi1, Sei Ban2, Kei Ieki2, Rina Onda2, Wataru Ootani2, Atsushi Oya2, Masato Takahashi1, and Kensuke Yamamoto2
1Kobe University
2The University of Tokyo
7th MPGD Conference at Weizmann Institute , 14/12/2022

## Slide 2: Contents
Introduction : MEG II and RDC
DLC-RPC : first prototype
DLC-RPC : new prototype with HV line
Summary and prospects

## Slide 3: MEG II experiment on PSI
Lepton flavor violation search
  μ  eγ
  Already searched for < 4.2 x 10-13 level (MEG I)
Upgraded experiment : MEG II
  Up to < 6 x 10-14 level of branching ratio
A.M. Baldini et al., arXiv 1801.04688

## Slide 5: Radiative Decay Counter (RDC)
Detector for tagging BG-
  When BG- have a signal-like energy (), most of e+ have a low energy (-) → RMD e+ distributed on the muon beam axis
Downstream
RDC
Upstream
RDC
Under development
Already
installed

## Slide 6: Requirement for upstream RDC
Upstream RDC
Signal: Positron of 1-5 MeV (Rare), >90% efficiency
Background: Muon of 28 MeV (100M cps)
Size: 20 cm diameter
Timing resolution: ~ 1ns
Material budget: < 0.1% X0
Hit rate : Maximum count rate is ~ 4Mcps/cm2
Radiation hardness for > 30 weeks operation
Position resolution: doesn’t need

## Slide 7: Our Solution : DLC-RPC
Surface RPC with DLC electrodes (DLC-RPC)
  DLC sputtered on 50 µm-thick polyimide (PI) foils
  Material budget meets the requirement
  Electrodes decoupled by Polyimide substrate
  HV applied for each layer independently
DLC: Diamond-Like Carbon
Gas flows inside chamber
~400 μm
Signal readout
+HV
-HV
+HV
-HV
+HV
-HV
+HV
-HV
Design draft
Polyimide 50mm
DLC
Pillar

## Slide 8
by K. Yamamoto

## Slide 9: Prototype of DLC-RPC
Detailed properties and performances are published in
Atsushi Oya et al 2022 J. Phys.: Conf. Ser. 2374 012143
Manufactured using MPGD techniques

## Slide 11
(Dec. 2020)

## Slide 13: Aging studies using neutron/X-ray
Fast neutron radiation facility at Kobe Univ.
  Date: 20th June – 3rd July, 2022
  3MeV d + Be target -> 8B + n
  neutrons with peaks at 2.5 MeV
X-ray generator at KEK Platform-C
  Date: 29th August – 7th October, 2022
  Cu target with monochromator
    Cu K line (8.0 keV)
  Specs:
    Tube voltage: 20 – 60 kV Tube current: 2 – 30 mA

## Slide 14: Preliminary results using aging studies
Neutron irradiation : 165 mC/cm2
X-ray irradiation : 272 mC/cm2
There are no significant changes in signal while those irradiation
However, those irradiations are ~103 times smaller than expected dose in MEG II
We need more intense source
After irradiation tests, we found fluorine attachment on the DLC surface. But no effect found on the signals and gains.
NON-irradiation sample DLC
C1s | 78.50
N1s | 3.92
O1s | 17.19
Si2p | 0.25
S2p | 0.06
P2p | 0.09
%
Irradiation sample DLC
C1s | 76.85
N1s | 0.62
O1s | 14.44
F1s | 6.11
Si2p | 1.25
S2p | 0.06
Ca2p | 0.57
%
Fluorine

## Slide 15: New prototype with HV feed lines

## Slide 16: New prototype are tested in beamline Just Now
Testbeam campaign using MEG II beamline
  13th – 18th Dec. 2022

## Slide 17: Summary and prospects
Surface RPC with ultra-low mass (0.1% X0) has been developed for MEG II upstream RDC, using DLC and MPGD techniques
High rate capability (>1M cps/cm2) has been attained for m+ beam
Aging effect is not seen up to 272mC/cm2
New design with inline electrodes are being tested Just NOW
DLC-RPC will be installed in MEG II at 2023
These researches are supported by
Grant-in-Aid for Scientific Research (No. 21H04991)
Kobe Univ. Reseach Facility Center for Science and Technology
KEK Detector R&D Center Platform C
RD51 collaboration

## Slide 18: Backup