## Slide 1: Iron Based Superconductors: status and prospects
Dongliang Wang, Yanwei Ma
Institute of Electrical Engineering, Chinese Academy of Sciences,
Beijing, China
1st High Temperature superconductors for Accelerator Technology (HiTAT) workshop, Mar 9-10, 2023

## Slide 2
Outline
Background on iron-based superconductors (IBS)
Development of high Jc PIT 122 IBS wires
Recent advances in long-length wires, joints, pancake & racetrack coils, cables
Conclusions and outlook
1
2
3
4

## Slide 3
High performance:
High Tc~55 K
High Hc2~100 T, Hirr very close to Hc2
Small anisotropy, γ<2
High Jc~6 MA/cm2 & Jc-depairing~160 MA/cm2
 | Bi-system | YBCO | IBS 122 | MgB2
γ | 50-90 | 5-7 | 1-2 | 2
ξab | 2.3 | 2.1 | 2.4 | 8
Gi | 1 | 10-2 | 10-4 | 10-5
Varieties of Iron-based superconductors (IBS)
Prof. Hideo Hosono 2008
At 20 K,
the Hc2 can be >70 T
where IBS outperform both MgB2 and Bi-2223.
Iron-Based Superconductors (IBS)
3

## Slide 4
IBS are considered as “Cheap conductor for high fields”
--Jan Jaroszynski, Supercond. Sci. Technol. 32 (2019) 070501
The cost of IBS wire can be four to five times lower than that of Nb3Sn, making it more expensive than NbTi, but with much higher critical parameters than Nb3Sn.
From a practical point of view, IBS are ideal candidates for applications.

## Slide 5
High Jc of IBS wires: Very weak field dependence in high field region
122 IBS wire:
Large Jc, at B > 20T
Jc shows very weak field dependence in high fields
Ic data of Sr-122 tape,
measured in 2013 at HFLSM, Sendai

## Slide 6
IBS have potential for high-field applications
MRI
(14 T)
ITER
J. Shimoyama, SuST 27 (2014) 044002
Working Temp:
4.2 K – 30 K
Accelerator (20 T)
Development of high-performance conductors is essential
>1GHz NMR
>23.5 T
10 m, 15 T (4.2 K)
6

## Slide 7: Misorientation dependence of Jc : GBs are less detrimental to current flow
M. Putti presented at EUCAS-2015
YBCO θc≈ 3° vs 122 IBS θc≈ 9°(The critical angle of GBs)
Misorientation angle of IBS grains < 9°usually do not impede the Jc flow
Highly textured templates are not necessary: PIT and low-cost CCs are possible
Iida et al., Appl Phys Rev 5 (2018) 031304
θGB dependence of inter-grain Jc for various IBS bicrystals
Notes: These features are highly beneficial for the realization of cheaper conductors for high-field magnets at low temperatures.
Bicrystal experiments on Ba-122 and Fe(Se,Te) revealed the metallic nature of grain boundaries. The critical angle above which inter-grain Jc falls off is around 9.

## Slide 8
－Low cost, simple deformation process
Final Product
1. Many types of sheaths of Ag, Cu, Fe, and Ag-based composites (Ag/Fe, Ag/Cu, Ag/stainless steel) can be employed.
2. For BSCCO, Ag is the only material that is inert to the BSCCO superconductor and permeable to oxygen at the annealing temperature.
122 PIT wires are expected to be much cheaper than BSCCO conductors:
800-900oC
Fabrication process for IBS wires and tapes
(Powder-in-tube method )
Notes: The PIT process is very attractive from the aspect of applications, taking advantage of the low material costs and the relatively simple deformation techniques.

## Slide 9
Outline
Background on iron-based superconductors (IBS)
Development of high Jc PIT 122 IBS wires
Recent advances in long-length wires, joints, pancake & racetrack coils, cables
Conclusions and outlook
1
2
3
4
9

## Slide 10
Huang et al., SuST 31 (2018) 015017
Latest: Record Jc of HP Ba122 tape= 1.81×105 A/cm2 at 4.2 K, 10 T
Powder-In-Tube 122 tapes: High Jc
High Jc values were achieved in hot pressed (HP) Ba122/Ag tapes
At 4.2 K, 10 T: Jc ~ 1.5×105 A/cm2, Ic=437 A, γ = 1.37
18 T: Jc ~ 105 A/cm2
27 T: Jc ~ 5.5×104 A/cm2
The grains are aligned along the c-axis,
most of the misorientation angles are 5-20
No apparent in-plane texture was found
EBSD

## Slide 11
improved by ~ 5 times
High-Jc Ba-122 HIP wires improved by GR+HIP
packing
Ba0.6K0.4Fe2As2 powder
Ba122/Ag+Cu
Ag tube
groove rolling
groove rolling
a
b
cold work
HIP sintering
700 oC,
150 MPa,
4 hours
c
mono-core wires
4.7×104 A/cm2
(4.2 K, 10 T)
Guo et al., SuST 34 (2021) 094001
3.3×104 A/cm2
(latest result)
2 times higher
Physica C 585 (2021) 1353870
tape-in-tube method
JMCC 11 (2023) 1460
by enhancing the texture
Cu/Ag sheath

## Slide 12
Cu/Ag sheathed Ba-122 tapes with practical level Jc
Liu et al., Sci. China Mater. 64 (2021) 2503
Jc (4.2 K, 10 T) = 1.1×105 A/cm2
d
HIP sintering
740 oC,
150 MPa,
1-4 hours
well textured grains
high core density
high transport Jc
Jc exceeding 105 A/cm2 for the first time for Cu/Ag sheathed tapes
A scalable and cost-effective fabrication route!

## Slide 13
Comparison of hysteresis loops for HP and HIP 122 tapes
HP Temperature (880℃)
Grain size: ~3 m
Lotgering orientation factor F: 0.87
Hv: ~140
HIP Temperature (740 ℃)
Grain size: ~0.5 m
Lotgering orientation factor F: 0.46
Hv: >230
Hot Pressing
Hot Isostatic Pressing
Much room for the Jc improvement
Courtesy: S. Awaji
Chart: Magnetic field B (T)
| 0.5 | 1 | 1 | 1.5 | 2 | 3 | 4 | 5 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18
Bup | 103.227 | 67.432 | 66.798 | 62.62 | 64.364 | 70.948 | 76.537 | 77.974 | 78.911 | 79.736 | 80.711 | 80.939 | 80.203 | 79.286 | 78.352 | 76.471 | 74.647 | 72.831 | 70.946 | 69.612 | 68.141 | 66.35
Bdown | 209.886 | 155.59 | 136.162 | 124.972 | 114.235 | 107.874 | 106.424 | 99.272 | 95.199 | 92.605 | 89.393 | 87.002 | 85.749 | 84.829 | 82.302 | 79.631 | 76.68 | 74.962 | 74.372 | 72.899 | 70.601
Jc=1.1×105 A/cm2 (10 T)
Courtesy: C. Senatore
Jc=1.8×105 A/cm2 (10 T)
Fraction with θ<10o:~42 %
Fraction with θ<10o:~10 %
HP Ba-122/Ag
HIP Ba-122/Ag/Cu
Bonura et al., SuST 33 (2020) 095008

## Slide 14
Powder-In-Tube 122 tapes: High Jc & high strength
High Jc values were achieved in Stainless Steel (SS)/Ag/Ba122 tapes, due to higher core density (Hv~230), the Jc is 8×104 A/cm2 at 4.2 K and 10 T .
1.08 m long SS/Ag/Ba122 tape shows good Jc uniformity, the lowest Jc is over 7×104 A/cm2.
Jc distribution of 1.08 m SS/Ag/Ba-122 tape
Dong et al., IEEE TAS 29 (2019) 7300504
High n value：
@10 K，10 T，n~47

## Slide 15
Critical current density of SS/Ag composite tapes
The highest Jctrans >0.1 MA/cm2 at x=0.458 @ 4.2 K, 10 T
Grain boundary transparency parameter =Jcinter/Jcintra continuously increases with doping
Grain boundaries are contaminated by FeAs, doping enhances proximity effect and inter-grain Jc.
Cheng et al., Mater. Today Phys. 28 (2022) 100848
Stainless steel/Ag/Ba1-xKxFe2As2 tapes were made with a wide doping range (0.25≤x≤0.6)
8 %
4 %
47 %
Best Jctransport
slightly overdoped
12.5 %
Proximity effect

## Slide 16
-- analyzed by Prof. Larbalestier group at FSU
The state-of-art high Jc tapes still contain many contaminated GBs which disconnect the Ba122 grains. The Jc can be largely improved if we can eliminate these secondary phases.
significant O
segregation
FeAs
Dark GBs
Bright GBs
EDS line scan
Ba-O
K depletion
Courtesy of F. Kametani
Dark GBs
Bright GBs
HAADF
Fe particle
Many clear GBs in HP-122 tape
Bright field STEM for HP Ba-122 tapes: Second phases at GB
Notes: The second problem annoying us is the dirty grain boundary. ovides a continuous path for supercurrent.
These oxide phase or GB wetting phase are harmful to inter-grains transport. I suggest that these second phases mainly come from the oxidized starting materials
How to remove impurities is an urgent problem to be solved next.

## Slide 17
NEXT STEP for iron-based PIT wires？
Most GBs are contaminated by FeAs, largely limiting intergrain current transport
  Slightly overdoping is a good way to enhance Jctrans
Clean GBs without FeAs phase is always the best choice!
  ~100% may be achieved in the GBs without FeAs (misorientation angle <9o)
Clean grain boundaries
Dirty grain boundaries
Mater. Today Phys., 28, 100848 (2022)
But how to remove FeAs ?

## Slide 18
New record high Jc in PIT SS/Ag Ba122 tapes
High Jc @ 4.2 K :
  Jc~2.2×105 A/cm2 @ 10 T
  Jc>105 A/cm2 even @ 24 T
High mechanical strength
Low material cost
Easy fabrication process scalable to long length tapes
Special technique to remove FeAs wetting phase, details will be published soon.
Very promising to be used in high field magnets!
Hot-pressed tape
SS/Ag tape by NIMS
No published data
New record！
NIMS
IEE

## Slide 19
Outline
Background on iron-based superconductors (IBS)
Development of high Jc PIT 122 IBS wires
Recent advances in long-length wires, joints, pancake & racetrack coils, cables
Conclusions and outlook
1
2
3
4

## Slide 20
Powder-In-Tube 122 tapes: Long length
100 m long, 7-core Ba122 tapes are fabricated by rolling process, and the Jc is continuously improving.
In 2022, the Jc of long wires has been increased above 6104 A/cm2 @ 4.2 K, 10 T by optimizing fabrication process
Supported by the Strategic Priority Research Program of Chinese Academy of Sciences (Grant No. XDB25000000)
@4.2 K, 10 T, transport Jc >60000 A/cm2

## Slide 21
High-performance joints were developed for IBS tapes, with a high critical current ratio (CCR) of 95%.
The IBS joint was tested in a closed-loop coil, showing a low resistance of 2.7×10-13 Ohm.
Meet the application requirements in persistent mode MRI magnets.
High-quality IBS joint
Zhu et al., SuST 35 (2022) 03LT01
IBS closed-loop coil test
for persistent current operation
95 % @ 4.2 K, 10 T
Cold pressing
Powder-In-Tube 122 tapes: Superconducting joints

## Slide 22
Powder-In-Tube 122 tapes: Pancake coils
Qian et al., Physica C 580 (2021) 1353787
New IBS pancake coils have been made, measured up to very high fields reaching 62 A @ 4.2 K, 30 T
35 T water-cooled magnet
(Hefei, China)

## Slide 23
Parameters | Values (mm)
Thickness of coil winding | 57.6
Width of coil | 235.2
Width of coil winding | 4.66
Length of straight part of coil | 200
Thickness of SS tape | 0.3
Turns | 96
Bending radius | 60
7-filaments IBS 100-m long tapes
Very promising for next generation accelerator!
Tapes’ Parameters | Values (mm)
Thickness of IBS tape | 0.33
Width of IBS tape | 4.5
Non-SC/SC ratio | 5
Metal-as-insulation technique
Wind & react > 800 oC
Ic~65 A @ 4.2 K, 10 T
  87 % of the short sample at 10T
IBS Racetrack coils made using the 100 m long tapes
720 mm257 mm
65 A
Zhang et al., SuST 34 (2021) 035021
Jc(coil) = 87% Jc(short tape) @ 10 T

## Slide 24
Pyon et al., SuST 26 (2023) 015009
Ic of the whole coil wires are 30 and 18 A in self-field, corresponding H = 1.75 and 1.0 kOe for mono- and 7-core wires
A high Jc of 71 kA/cm2 (Ic ~67 A) at 4.2 K, 10 T was measured in short segments picked up from the mono-core coil
Rapid increase in dissipation starts above 53 and 47 A for mono- and 7-core wires
HIP process is applied
(Wind & React)
17~18 m mono- and 7-core Ba-122 wires
Wires covered by glass sleeve are wound on SS bobbins
segments of mono-core wire segments of 7-core wire
Powder-In-Tube HIP 122 wires: Coils

## Slide 25
FeSe0.5Te0.5 coated conductor tape and coil
FeSe0.5Te0.5 single pancake coil (SPC) was fabricated and tested under magnetic field
One-meter FeSe0.5Te0.5 coated conductor tapes can be fabricated via PLD
The transport critical current of the SPC was 108 A at self-field and 17 A at 10 T, which is as same as the tape.
Wei et al., SuST 36 (2023) 04LT01
(a)
Bare tape
Encapsulated tape
SPC
hybrid coil
test device
laser
metal tape
heater
Target
One-meter long
PLD

## Slide 26
Cable design
Schematic illustration of the transposed cable and the fabrication steps
The advantages of the designed cable:
High current-carrying compacity
Low dynamic loss
High mechanical stability
High Field Model Dipole Magnet: HTS Cable R&D
REBCO transposed cable reached 2 kA
J. Wang et al, Superconductivity 3 (2022) 100019
IBS transposed cable reached 1.3 kA
Courtesy of Prof. Qingjin Xu

## Slide 27
Platform for kilometer-scale IBS wire
HIP furnace
Currently, a platform for the preparation of kilometer-scale long IBS wire is constructing in China.
Plant layout, ~3000 square meters
Wire drawing machine
Tape rolling machine
HIP furnace
Equipment in place

## Slide 28
Conclusions
Currently, iron-based wires and tapes are in the rapid development stage of research and development.
Transport Jc of 122-type IBS wires has been significantly improved, and has surpassed the practical level at 4.2 K & 10 T with a maximum of 2.2×105 A/cm2.
Transport Jc of 100-m-class Ba-122 IBS tapes was further improved to > 6×104 A/cm2 at 10 T & 4.2 K.
Highlights some remarkable advances of IBS relevant to practical applications, including superconducting joints, cable, the first IBS inserted coils and racetrack coils.
We believe that Fe-based wires are very promising for applications in high magnetic fields, e.g. >20 T at 4.2 K or >10 T at 20-30 K.

## Slide 29
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
IBS solenoid at 24 T
Racetrack at 8 T
The engineering current density of the long-length IBS still needs a significant improvement, to reach the similar level as ReBCO or Bi-2212 conductors.
The materials of stabilizer should be shifted to copper or any other low-cost metals to realize the low cost of IBS.
Structure and fabrication methods of IBS and corresponding coils should be further optimized to minimize the Jc degradation at high field and high stress.
Many other issues like detailed magnetic and mechanical properties study of IBS, quench detection and protection of the IBS coils/magnets and etc.
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA IBS Cable
2022
IBS Technology: Status and Outlook
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Courtesy of Prof. Qingjin Xu

## Slide 30
Contributors:
Xianping Zhang, Chao Yao, Chiheng Dong, Dongliang Wang, Zhongtang Xu, He Huang, Shifa Liu, Zhe Cheng, Yanchang Zhu, Meng Han, et al.
Institute of Electrical Engineering, CAS
Collaborators:
S. Awaji (Ic-B measurement)
HFLSM, Tohoku University, Japan
F. Kametani, C. Tarantini, E. Hellstrom, D. Larbalestier (STEM and GBs)
NHMFL, FSU, USA
Haihu Wen (Pinning properties)
Nanjing University, China
Huajun Liu (In-field Ic measurement)
IPP-CAS
W. K. Kwok, U. Welp (Irradiation)
Argonne National Laboratory, USA
T. Kiss (Characterizing local microstructure and homogeneity of wires)
Kyushu University, Japan
Qingjin Xu (Coil design and fabrication)
IHEP-CAS
J. Hänisch, B. Holzapfel (Jc rising mechanism)
ITEP-KIT, Germany
C. Senatore (Ic (T,B) measurement)
DQMP, Univ. Geneva

## Slide 31
Projects on IBS & Financial support
MoST funded “Next Generation High-field Magnet Technology Based on Iron-based Superconductor” within the National Key R&D Program of China
NSFC funded “High-performance Fe-based Superconducting Materials for High Magnetic Field Applications”
within Major International (Regional) Joint Research Project
CAS funded“Science and Technology Frontier Research for the Next Generation Superconducting Magnet Applications” within the Strategic Priority Research Program of CAS

## Slide 32
From a movie：Avatar
Thank you for your attention!

## Slide 33
Strategies to further improve Jc in 122 PIT wires
To further reduce secondary phases at GBs.
To improve the texture degree,
especially increase the fraction of misorientation
angle <9o.
To further increase flux pinning force: (1) decrease grain size to make more GBs,
(2) increase point pinning sites, e.g. irradiation
or the introduction of nano-particle inclusion.
HP
Rolled
Courtesy: M. Bonura
& C. Senatore
Courtesy: M. Eisterer
Neutron Irradiation of
Ba122 Single Crystals
Ba122 tape

## Slide 34
122 tapes – Strain properties
The Ic of 122 tapes exhibits less strain sensitivity than that of the Nb3Sn, which is important for ITER application.
Liu et al., SuST 30 (2017) 07LT01
Reversible critical currents under a large compressive strain of ε = –0.6%
Sr-122/Ag tapes
7-filament Sr-122/Ag/Monel tapes
Almost no Jc degradation under a large compressive strain of 0.6%
Yao et al. 2017 SuST 30 075010

## Slide 35
122/Ag IBS tapes
The critical bending diameter is 4.4 cm for Sr-122/Ag tapes in thickness of 0.3 mm.
For high strength Ba-122 tapes, the bending diameter is even smaller, only of 2~3 cm.
width ~ 4.5 mm, thickness = 0.3 mm
Cooperated with Prof. Huajun Liu in IPP-CAS
SUS/(Ag-Sn)/Ba-122 tapes
Courtesy of H. Kumakura
Straight
Bent
Straighten
Bending test of 122 IBS tapes
--Heated samples

## Slide 36
Good retention above Ф15 mm
Rapid decrease of Ic in the D10 sample
Ratio = Ic (bending) / Ic (pristine~135A）
Bending diameter of 7-filament 122/Ag tapes
By courtesy of Prof. Q. Xu at IHEP-CAS
Cracks
Cracks in the D10 sample
Li et al., IEEE TAS 32 (2022) 7300304

## Slide 37
122/Ag tape – Magnetization AC loss
Kovac et al., Cryogenics 116 (2021) 103281
The AC loss for 7-core tapes reduced by ~50% at 20 K,
due to the negligible eddy current losses by using more resistive AgSn alloy outer sheath.
Due to highly conductive Ag sheath, large eddy current losses (ecl) was observed for single-core tape
single-core tapes
single-core tapes vs 7-core tapes
Q 1-Ba122/Ag – ecl = Q1-Ba122/Ag - Qecl Ag-99%
(Ag-etched)
*The difference observed between the extracted Q ecl (red lines) and those measured for etched Ag (green lines) could be attributed to different Jcs due to sample degradation

## Slide 38
κ ∝B-α
Thermal properties are dominated by the sheath materials
The thermal conductivity ranges from 1 to 1000 W/m K by adjusting the sheath materials
  @4.2 K：Cu/Ag: 400 W/m K at 0 T; >100 W/m K at 9 T--magnets
  SS/Ag: ~10 W/m K-- current leads
Atoms diffusion between different sheathes and superconducting cores
Supercond. Sci. Technol. 33, 075010 (2020)
Thermal conductivity of composite Ba122 tapes

## Slide 39: Jc anisotropy of 122/Ag tapes
The Ic in applied magnetic fields is slightly higher in the perpendicular field (Ic ) than in the
┴
parallel field (Ic ).
//
The anisotropy ratio (Г= Ic /Ic ) is quite low, less than 2, very good for applications.
⊥ ∥
Senatore et al., SuST 33 (2020) 095008
4.2 K
Awaji et al., SuST 30 (2017) 035018
10 15
Temperature (K)
Ic < Ic only at low temperature and fields
//
5
20
1.0
I / I
C C
//

~2
1.5
2.0
B= 10 T
B= 19 T
~1.5
~1

## Slide 40: n value of 122 tapes
I/Ic
Measured by Prof. Yang Univ. of Southampton, UK
At 20 K, the n value was over 30
At 4.2 K, 10 T, the n value was over 20
Measured by Dr. Oguro HFLSM, Tohoku Univ., JP
Measured by Prof. Kiss Kyushu Univ., JP

## Slide 41
Low AC loss (Multifilament)
Thermal stability (Thermal quench)
Good mechanical strength (Lorentz force)
Scalable production (powders & wires)
Small aspect ratio: round wire
Low cost——Conundrum for HTSC
What makes a good superconducting wire?
Intrinsic
Extrinsic
Superconductors
Nature 414 (2001) 368
Characteristics:
Conductor design
Low anisotropy
High Jc, Hc2
Chemically stable
Commercial superconducting wires and tapes
Bi2223
YBCO
Bi2212
NbTi
Nb3Sn
MgB2
Ag