## Slide 1
AC loss in round cables with helically arranged HTS tapes
Fedor Gömöry
Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, Slovakia
Contributions:
Mykola Solovyov, Marek Mošať, Tomáš Kujovič, Ján Šouc
Institute of Electrical Engineering, Slovak Academy of Sciences, Bratislava, Slovakia
Tiemo Winkler, Kei Sugita
GSI Helmholtzzentrum für Schwerionenforschung GmbH, Darmstadt, Germany
Marc Dhallé, H.J.G. Krooshoop
TNW-EMS, University of Twente, Enschede, The Netherlands
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva

## Slide 2
Motivation
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Foreseen for SIS100 (FAIR):
F Kaether et al., (2021) 12th Int. Part. Acc. Conf.
doi:10.18429/JACoW-IPAC2021-TUPAB378
H G Khodzhibagiyan and A A Smirnov,
Proc. the 12th Int. Cryogenic Engineering Conf. (ICIC’12),
Southampton, UK, Jul. 1988, pp. 841–844. doi:10.1016/
B978-0-408-01259-1.50162-5

## Slide 3
Motivation
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Requirements on the cable:
13.2 kA at 1.9 T
Flexible
Forced flow of coolant
Low loss
LHe (4.5 K)
?
Forced flow of coolant
Flexibility
Transport capacity
AC loss
Possible alternative: CORT
(Conductor-On-Round-Tube)
REBCO tapes
Central tube
X Wang et al., Supercond. Sci. Technol.
34 (2021) 015012

## Slide 4
Outline
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Formula for estimating hysteresis loss in a round HTS cable
Comparison with low-Tc versions
Discussion and issues for further research

## Slide 5
Formula for estimating hysteresis loss in round HTS cable
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Step 1: single tape (critical current Ic, width w) in perpendicular magnetic field
Assumption: magnetic field variation higher than the penetration field -> saturation of screening currents
magnetic moment at saturation
Bmax sin(2ft)
w
L
hysteresis loss per cycle and unit length:
m [Am2]
ms
-ms
Bmax
-Bmax

## Slide 6
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Step 2: tape is wound in helical fashion, orientation of magnetic field changing from 0 to 360 degrees
hysteresis loss per cycle and unit length of the tape:
Step 3: tape is wound in helical fashion, at lay angle a
hysteresis loss per cycle in one tape in 1 meter of CORT:
a
for the cable length Lc is needed the tape length
Assumption: magnetic field variation higher than the penetration field -> saturation of screening currents
Formula for estimating hysteresis loss in round HTS cable

## Slide 7
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Assumption: magnetic field variation higher than the penetration field -> saturation of screening currents
Step 4: to reach the necessary critical current, in CORT there are N tapes
loss in unipolar cycle is ½ of the loss in full cycle
hysteresis loss per cycle in N tapes in 1 meter of CORT:
Formula for estimating hysteresis loss in round HTS cable
Notice: the formula(s) are valid for also for other cables from transposed CC tapes

## Slide 8
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Experimental data:
Formula for estimating hysteresis loss in round HTS cable
M Majoros et al., Supercond. Sci. Technol.
27 (2014) 125008
K Yagotintsev et al., Supercond. Sci. Technol. 33 (2020) 065009
Numerical modeling:
Y Sogabe and N Amemiya, IEEE Trans. Appl. Supercond.
28 (2018) 8200705

## Slide 9
Experimental verification (AC field 72 Hz applied at 77.3 K)
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
3 samples:
2 x 5 tapes
(SCS3050-AP, 3 mm)
Opposite layers
Coinciding layers
Heat-shrink tubing
Kapton™ tape bandage
Carbon tube
(former)
Superconducting tapes
Coinciding layers, stacked tapes
tube: epoxy+ Carbon fibre
E Cuninková et al., IEEE Trans. Applt. Supercond., accepted
https://ieeexplore.ieee.org/document/10056272

## Slide 10
Experimental verification (AC field 72 Hz applied at 77.3 K)
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
derived assuming Ic = const
Modification for Ic(B):
+
Bmax,1
Bmax,2

## Slide 11
Experimental verification (AC field 72 Hz applied at 77.3 K)
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Coinciding layers
Opposite layers
Stacked tapes
3 samples: 2 x 5 tapes

## Slide 12
Experimental verification (AC field 72 Hz applied at 77.3 K)
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Coinciding layers
Opposite layers
Stacked tapes
3 samples: 2 x 5 tapes

## Slide 13
Experimental verification (72 Hz at 77.3 K, 1 mHz at 4.2 K)
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Coinciding layers
Opposite layers
Stacked tapes
3 samples: 2 x 5 tapes
Ic0(77.3 K) = 135 A
Ic0(4.2 K) = 2520 A

## Slide 14
Comparison with the low-loss NbTi version
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Assuming w = 3mm and df = 3 µm:
In similar way, hysteresis loss in NbTi version, the filaments with diameter df :
Condition of equivalent transport capacity of the cable:
Current CC cables have little chance in low-field (<10 T) accelarators
D Uglietti et al., Cryogenics 110 (2020) 103118

## Slide 15
Competing in AC loss with the Nb3Sn version
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
The best Nb3Sn (filament diameter 50 µm), still no coupling:
Considering further 50% contribution from coupling loss in Nb3Sn strands,
plus some coupling loss because of inter-strand connections,
current target for CC cable can be formulated as:
Hysteresis loss reduction to 5% of the present value
No additional coupling loss introduced
E Barzi and A V Zlobin, 2015 FERMILAB-PUB-15-274-TD
E C Collings et al., IEEE Trans. Appl, Supercond. 28 (2018) 4006504
D Schoerling et al., IEEE Trans. Appl, Supercond. 29 (2019) 4003109

## Slide 16
Goal: 20x reduction of hysteresis loss
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Possible ways:
filamentized tape: 150 µm filaments
???
Additional benefit by operating at higher temperatures:
at 20 K the cost of cooling > 4x lower than at 4.2 K
flattening the cable, corresponding magnet design
H Piekarz et al., Nuclear Inst. and Methods in Physics Research, A 943 (2019) 162490
L Rossi and C Senatore Instruments 2021, 5(1), 8
Y Li et al., IEEE Trans. Appl, Supercond. 33 (2023) 4400405

## Slide 17
Conclusions
AC loss in round cables from helically arranged HTS tapes I.FAST WP8 Task 8/6 Collaboration Presented at the 1st HiTAT workshop / 9-10 March 2023 at CERN, Geneva
Magnetic hysteresis is a serious drawback of CC tapes intended for use in pulsed magnets
With a substantial modification of the tape architecture (filamentization) CC could compete with Nb3Sn
in high-field (> 10 T) accelerators