## Slide 1
ReBCO Roebel cable
relevant to accelerator-type demonstrator magnet
EuCARD2
A. Kling, U. Mirasch, A. Drechsler, A. Kudymow, W. Goldacker
a A. Usoskin, A. Rutt
L. Rossi, L. Bottura, G. Kirby, J. van Nugteren
A. Kario, M. Dhallé, S. Otten
C. Senatore
Y. Yang

## Slide 2
Optimization of Roebel cables for use in magnets
CEA Saclay - Cos-theta design
C. Lorin et al.
B(T)
CERN- block coil design
J. van Nugteren et al.
B(T)
Wl
Wc
Tp
Conductor
choice
Cable design
Coil
design

## Slide 3
Cable lengths relevant to accelerator demonstrator
Wilfried Goldacker
Andera Kling assembling 24m Roebel cable
Reel-to-reel system for up to 100 m with possibility for upgrade up to 200 - 300 m
Modular system with room for extension to full-cable assembly in one run (no need for laboratory use)
Controllable tension on the tapes and cable
Suitable for different tapes, cable architectures and dense packing (tape material, no. of strands, transposition length)
Cabling direction
Point of cabling

## Slide 4
Coated conductors performance at 4.2 K
Target performance for RE123 tape at 4.2 K in perpendicular magnetic field:
Jeng = 450 A/mm2 at 15 T
Jeng = 400 A/mm2 – 600 A/mm2 at 20 T

## Slide 5
Development of the punching process
Wl
Wc
Ri
Tp
α
200 µm
Tape directions
Reel with
punched strand
Reel with
REBCO
Punching die
1
2
2. Shearing and cracking
3. Break through
Charging of
the punch
Punching
direction
Cu
Stainless Steel
REBCO
20 µm

## Slide 6
Search for optimal geometry with good alignment of the strands in the cable
Wl = 5.5, 5.9
Wc = 5.5, 5.9
Ri= 10
Tp = 126, 226, 300, 426
α
Horizontal gap
Vertical gap
870 µm
421 µm
174 µm
240 µm

## Slide 7
Measurement
window
Defined length
Shift error
- correction
Signal to feed rolls
Reel-to-reel measurement system of tape geometry and transposition length feed-back system
width variations
camber
Tape geometry measured
Feed back for punching
Transposition length set by a reel feed ( ± 0.05 mm precision)
Transposition error correction planned

## Slide 8
Burr size dependence on punched material and die clearance
17 µm die clearance:
7 µm die clearance:
100 μm stainless steel tape
100 μm stainless steel tape
Bruker CC, 100 μm stainless steel substrate
SuperPower CC, 50 μm Hastelloy substrate
1.
One-step punching TL = 300 mm
2
1
Punching in one-step:
Within CERN collaboration agreement
Reduced tape transport error
Possibility of adjustment to the tape width
Tooling clearance 5 µm +/-2 µm

## Slide 9
Homogeneous thickness of the cable with reduced dog – boning effect
The average critical current per unit width degraded by 6% after punching and copper plating.
No local defects were found.
Chart: Critical current per unit width
| 1-10 | 1-2 | 2-3 | 3-4 | 4-5 | 5-6 | 6-7 | 7-8 | 8-9 | 9-10
Before punching | 10.7917 | 10.8 | 11.1167 | 10.9583 | 10.8083 | 10.2833 | 10.9083 | 10.8833 | 10.9417 | 10.8333
After punching | 10.2364 | 10.2182 | 10.6545 | 10.2727 | 10.3091 | 9.7455 | 10.4727 | 10.1455 | 10.4364 | 10.4
After copper plating | 9.8545 | 10.1818 | 10.5273 | 10.1273 | 10.0909 | 9.4 | 10.4 | 10.1273 | 10.4727 | 10.3091

## Slide 10
Assembled and delivered cables
2 m cable for Ic measurement at 4.2 K (punch and coat)
24 m Roebel cable from Bruker material for Feather-2 winding (punch and coat)
Superconducting cables of 5 - 6 m using tapes from: Bruker, SuperPower, SuNAM and SuperOx
Dummy cables: stainless steel and copper tapes
Cable 130 m, used tape material 2 km
Superconducting cables:
Cable 54 m, used tape material: 0.5 km
G. Kirby, CERN
5 m SC cable
Bruker tape

## Slide 11
Out-of-plane Roebel cable and single tape bending
Measurements at LN2, self-field
REBCO inside / compressive bending
Ic of the Roebel cables:
SuperPower: 1427 A
Bruker: 658 A
SuperPower
20 µm Cu, 50 µm Hastelloy
Bruker
20 µm Cu+, 100 µm SS
Chart: 
| 20 | 16.670000000000002 | 14.29 | 12.5 | 11.11 | 10 | 9.09 | 8.33 | 7.69 | 7.14 | 6.67 | 6.25 | 5.88 | 5.56 | 5.26 | 5
SuperPower tape | 0.99335 | 0.99141 | 0.99086 | 0.98864 | 0.98587 | 0.98282 | 0.97977 | 0.97617 | 0.97091 | 0.96675 | 0.95317 | 0.94874 | 0.94735 | 0.94403 | 0.94015 | 0.93682
SuperPower cable | 1 | 0.99525 | 0.98615 | 1.0094 | 1.0061 | 1.0038 | 1.0028 | 1.0023 | 1.0009 | 0.99823 | 0.99624 | 0.99461 | 0.99227 | 0.98763 | 0.97967 | 0.95196 | 0.94387
Bruker tape | 1 | 1.0031 | 0.97248 | 0.91284 | 0.85856 | 0.7974 | 0.72477 | 0.65061 | 0.58792 | 0.53211 | 0.47554 | 0.43578 | 0.39373 | 0.33639 | 0.21483 | 0.10168 | 0.05581 | 0.019878 | 0.012997
Bruker cable | 1 | 0.99949 | 1 | 0.99929 | 0.99757 | 0.99858 | 0.99615 | 0.99494 | 0.99362 | 0.99099 | 0.98866 | 0.98471 | 0.98005 | 0.97478 | 0.96647 | 0.95766 | 0.94136 | 0.91755 | 0.90216 | 0.88332 | 0.85972 | 0.83085 | 0.79672 | 0.75438 | 0.70384 | 0.64307
Aligned block coil
Cos-theta
coil
Irreversibility point
Bending radius [mm]
Reduced critical current
Bending machine for single tapes:
REBCO inside
REBCO outside
Bending machine for cables:
2R
REBCO inside

## Slide 12
Mechanical properties - increased delamination strength with punch-and- coat method in Roebel
bridge
straight
6 x 4 mm2
Punched after coating
Punch-and-coat strand
Delamination strength (MPa)
straight
bridge
4 x 4 mm2
Delamination strength (MPa)
Punched after coating
Punch-and-coat strand
Maximum force 2.5 kN, LN2
Tape/strand soldered with InSn to Cu block
Delamination is a weak point of ReBCO tape and Roebel strand.

## Slide 13
J. Fleiter, A. Ballarino, L Bottura, P. Tixador, Supercond. Sci. Technol., Vol. 26, No. 6, 2013.
Bruker
SuperPower
P. Gao et al 2019 Supercond. Sci. Technol. 32 055006
Impregnated ReBCO Roebel cable withstand stresses up to 400 MPa
Importance of study ReBCO cables in transverse stress to understand the limits for future high field magnets
Relevance of electromagnetic and thermal cycling effect on critical current of ReBCO cables

## Slide 14
Losses are dominated by hysteresis, inter-tape coupling is not visible
Hysteresis scales with H0/Hp as expected (Norris strip)
Tapes are magnetically coupled, i.e. as a monolithic conductor, but not quite fully
Hysteresis and coupling in Roebel cable

## Slide 15
Feather-M2
ReBCO Roebel cables and the coils
F.J. Mangiarotti et al, Feather magnets test overview, 2020.07.08 – EuCARD2/ARIES Roebel cable experience workshop
Feather-M0
J. van Nugteren, High temperature superconductor accelerator magnets https://research.utwente.nl/en/publications/high-temperature-superconductor-accelerator-magnets

## Slide 16
Roebel cable fabrication for magnet use:
Punch and coat method at Bruker with regular thickness of the Roebel cable
Strand geometry control system - increased precision in transposition length
One step- punching tool within CERN collaboration agreement result in ideally punched tape edge thanks to suitable clearance
The 24 m long Roebel cable with Bruker tape delivered to CERN for Feather-2 coil winding.
Bending in easy direction without permanent degradation down to 4.0 mm (SuperPower), 9.4 mm (Bruker), where bending close to tape properties
Impregnated Roebel cable with-stands transverse pressures in excess of 150 MPa
Roebel or not, geometry quality of ReBCO tape, strands contribute to wind ability, homogeneity and mechanical performance of the coil!
Homogeneity of electro-mechanical properties of ReBCO cables, including delamination and edge effects need to be studied!