## Slide 1: Muon Collider Magnets
L. Bottura, F. Boattini, B. Caiffi, S. Mariotto, L. Quettier, M. Statera
on behalf of the Muons Magnets Working Group
10 March 2023

## Slide 2: Scope of the talk
Why muons ?
The four magnet challenges of the muon collider
A short digression on HTS
Summary

## Slide 3: Collider Choices
Hadron collisions: compound particles
  LHC collides 13.6 TeV protons
  Protons are mix of quarks, anti-quarks and gluons
  Very complex to extract physics
  But can reach high energies
Lepton collisions: elementary particles
  LEP reached 0.205 TeV with electron-positron collisions
  Clean events, easy to extract physics
  Lepton collisions  precision measurements
  Hard to reach high energies
e+e-

## Slide 4: Energy Limit
Electron-positron rings are multi-pass colliders limited by synchrotron radiation
Hence proton rings are energy frontier
Electron-positron linear colliders avoid synchrotron radiation, but are single pass
Typically cost proportional to energy and power proportional to luminosity,
Novel approach: muon collider
Large muon mass suppresses synchrotron radiation => multi-pass
Fundamental particle requires less energy than protons
But lifetime at rest only 2.2 μs (increases with energy)
Therefore the muon collider is part of the European Accelerator R&D Roadmap
N
S
N
S
accelerating cavities

## Slide 5: Muon Collider: Physics ?
Equivalence between proton (hadron) and muon (lepton) center of mass energy at collision for selected production and decay channels
https://doi.org/10.48550/arXiv.2203.07261
Muon collisions in the range of 10 TeV have comparable discovery potential to hadron collision in the range of 100 TeV

## Slide 6: Muon Collider: Sustainable ?
K.Long et al, Nature Physics, v.17, p.289, 2021
A muon collider at 10 TeV can provide the highest integrated luminosity per unit energy consumption

## Slide 7: Muon Collider: Affordable ?
D. Neuffer and V. Shiltsev 2018 JINST 13 T10003
A muon collider at 10 TeV profiting from the LHC infrastructure could be the most cost-effective energy frontier collider

## Slide 8: Proton-driven Muon Collider Concept
Credits to US-DOE MAP
Produce a low emittance muon beam…
… collide !
… accelerate muons…
Steady state
Steady state
Pulsed
Steady state
Pulsed
Time
Beam intensity
100…200 ms
protons
muons
pions

## Slide 9: The four magnet challenges – 1
20 T, 200 mm
Radiation heat load ≈ 5…10 kW
Radiation dose: 80 MGy
Large stored energy o(1) GJ, mass o(300) tons, cost o(100) M
Considerable RT and cryogenic heat load: RT power o(1) MW
Radiation dose o(80) MGy and radiation damage o(10-2) DPA

## Slide 10: Target and capture – 1/3
Attempt to reduce the mass (CAPEX) of the system, and increase operating temperature to improve cryogenic CoP (OPEX)
US-MAP 2010 design
LTS (14 T) + NC (6 T)
US-MAP 2011 design
LTS (14 T) + NC (6 T)
H.G. Kirk, PAC 2011
MuCol 2022 design
HTS (20 T, 20 K)
A. Portone, P. Testoni, J.Lorenzo Gomez (F4E)
C. Accettura, L. Bottura, A. Kohleimainen (CERN)

## Slide 11: Target and capture – 2/3
US-MAP
Proposal
EM = 2.9 GJ
Top = 4.2 K
Mcoils = 200 tons
Mshield = 300 tons
P = 12 MW
EM = 1 GJ
Top = 10…20 K
Mcoils = 110 tons
Mshield = 196 tons
P = 1MW
A. Portone, P. Testoni, J.Lorenzo Gomez (F4E)
C. Accettura, L. Bottura, A. Kohleimainen (CERN)

## Slide 12: Target and capture – 3/3
Operating current: 58 kA
Operating field: 20 T
Operating temperature: 20 K
SOLDERED HTS STACK
COPPER FORMER
COOLING CHANNEL
COPPER SLEEVE
STAINLESS STEEL JACKET
38
25
8
M. Takayasu et al., IEEE TAS, 21 (2011) 2340
Z. S. Hartwig et al., SUST, 33 (2020) 11LT01
HTS conductor design
MIT “VIPER” conductor

## Slide 13: The four magnet challenges – 2
> 40 T, 60 mm
Total 1 km, o(1600) units of solenoid magnets up to o(20) T requires compact windings and careful cost optimization
UHF solenoids, with field beyond state-of-the-art o(40…60) T, calls for novel HTS technology

## Slide 14: Final cooling – 1/3
Probe the limits of UHF solenoid magnets for the final cooling (performance)
Make windings compact to reduce mass (CAPEX)
I. Dixon, NHMFL
Cartoon design of 40 T, 32 mm user facility solenoid (developmental)
Cross section of
32 T, 32 mm user facility solenoid
at NHMFL
R&D test
achieved 25.4 T
At NHMFL
LTS/HTS hybrids
Images of
32.35 T, 21 mm user facility solenoid
at CAS-IEE

## Slide 15: Final cooling – 2/3
Probe the limits of UHF solenoid magnets for the final cooling (performance)
Make windings compact to reduce mass (CAPEX)
B. Song, SST
REBCO insulated coil
achieved 24.1 T
at CAS-IPP
All-HTS
R&D NI coil achieved 18 T
at PSI
J. Kosse, PSI
J.-B. Song, LNCMI
R&D NI insert coil achieved 32.5 T
at LNCMI

## Slide 16: Final cooling (40 T) – 3/3
B. Bordini, CERN
Inner Ring
Outer Ring
‘Modular’ Coil
1 % Field Homogeneity
Bore
Support Plate
‘Correction’ Coil
T. Mulder, CERN
B. Bordini, CERN
A. Dudarev, CERN
smax = 600 MPa
40 T solenoid design

## Slide 17: The four magnet challenges – 3
NC ±1.8 T, 400 Hz, 100 mm x 30 mm
SC < 10T, ≈ 100 mm
Energy storage and power management o(50) GW
Ramp linearity control, requirement (TBD)
Medium field o(10 T) SC dipoles subjected to radiation load

## Slide 18: The four magnet challenges – 4
16 T peak, 150 mm
Radiation heat load ≈ 5 W/m
Radiation dose ≈ 20…40 Mgy
Large bore o(150mm), high field o(10…20T) arc and IR magnets result in large e.m. stress o(300…400MPa) and require novel stress management concepts
Significant Energy deposition o(5 W/m) and dose o(40 MGy)
Stress managed dipoles and quadrupoles

## Slide 19: A short digression on HTS
Reduce energy consumption
(FCC-ee 350 MW, FCC-hh 580 MW)
Increase energy efficiency
(COP at 1.9 K is about 1000)
Risk with helium supply chain
(FCC-hh would require 900 tons of lHe)
Infrastructure (magnet) cost
(FCC-hh quoted at 9 BCHF)
Operate SC magnets at higher (gas) cryogenic temperature
Avoid large liquid helium bath and operate at gas temperatures
Reduce SC unit cost
Increase coil current density to decrease conductor inventory
Compact HTS windings
Target JE 1000 A/mm2
Operation in gaseous He
Range of 15…25 K
5 T at 2800 A
JE = 250 A/mm2
16 T at 2800 A
JE = 850 A/mm2
Calculation example
(T. Lecrevisse, CEA)

## Slide 20: Conductor cost
Grateful thanks to fusion !
Impressive cost/performance reduction in HTS !
Based on CERN orders and requests for quotations 2010-2022
Normalised costs are referred to performance at 12 T, 4.2 K, not corrected for inflation

## Slide 21: HTS for accelerators – DRAFT
 |  | Specification | Target
Minimum Jnon-Cu (4.2 K, 20 T) | (A/mm2) | 1500 | 3000
Minimum Jnon-Cu (20 K, 20 T) | (A/mm2) | 600 | 1250
s(IC) | (%) | 10 | 5
Minimum copper RRR | (-) |  | 20
Minimum Unit Length (UL) | (m) | 200 | 500
Minimum bending radius | (mm) | 15 | 10
Allowable slongitudinal non-Cu | (MPa) | 800 | 1000
Allowable compressive stransverse | (MPa) |  | 400
Allowable tensile stransverse | (MPa) |  | 25
Allowable shear ttransverse | (MPa) |  | 20
Allowable peel speel | (MPa) |  | TBD
Allowable cleavage scleavage | (MPa) |  | TBD
Range of allowable elongitudinal | (%) | -0.1…0.4 | -0.1…+0.5
Internal specific resistance rtransverse | (nW/cm2) |  | 20
Width: 4…12 mm
Substrate (non-magnetic alloy): 40…60 mm
Copper stabilizer (total): 20…40 mm
Total tape thickness: 60…100 mm

## Slide 22: HTS for accelerators – comments
Use non-Cu as basis of comparison independent of the amount of stabilizer added
JE targets are within reach, comparable to fusion specifications
Main attention on mechanics, which is a major challenge of high fields. Need to understand and characterize systematically
Other parameters may be important, but we do not know yet

## Slide 23: Summary
A muon collider at the energy frontier of high energy physics needs (among others)
  High fields (dipoles and quadrupoles from 16 T up to 20 T, solenoids from 20 T up to 40 T and more)
  Energy efficiency (increase operating temperature to profit from Carnot, minimal cryogen usage)
  Economics (high JE, compact magnets, to reduce construction costs, sustainable Maintenance and Operation)
HTS may offer it all, provided…
  We develop a new magnet technology palette, higher current density, higher operating temperature (large degree of innovation required), using present conductor: do not wait for better
  Deploy rapidly for users: they get to know the features of the new devices, cope and (may) adapt demands
  Profit from cost reduction: one more “factor two reduction” possible ? That would be disruptive (HTS/LTS cross over)
Notes: The reason for this talk is that we have received a strong recommendation from the group that proposes priority for particle physics in Europe. The recommendation, received in March 2020 and approved at the Council session of June 2020, contains a very strong statement on the need to ramp-up R&D effort on high-field accelerator magnets

## Slide 24: Acknowledgements
Grateful thanks to many:
C. Accettura, N. Amemiya, B. Auchmann, J.S. Berg, A. Bersani, A. Bertarelli, F. Boattini, B. Bordini, P. Borges De Sousa, M. Breschi, B. Caiffi, X. Chaud, F. Debrais, A. Dudarev, M. Eisterer, S. Fabbri, S. Farinon, P. Ferracin, H. De Gersem, A. Kario, A. Kolehmainen, J. Kosse, J. Lorenzo Gomez, R. Losito, S. Mariotto, M. Mentink, T. Mulder, R. Musenich, D. Novelli, T. Ogitsu, M. Palmer, J. Pavan, H. Piekarz, A. Portone, L. Quettier, E. Rochepault, L. Rossi, T. Salmi, H. Schneider Muntau, C. Senatore, M. Statera, H.H.J. Ten Kate, P. Testoni, G. Vallone, A. Verweij, M. Wozniak, A. Yamamoto, Y. Yang, Y. Zhai, A. Zlobin
and the Muon Magnets Working Group at large
For discussion, development of concepts, design and anlyses, comments and critics, participation and fun !

## Slide 26: Muon beam generation
Absorber
RF field
“cooled” muon
Decreased p⊥
Increased p//
p⊥
p//

## Slide 27: Target and capture – 4/4
Under study (among others)
  Magnetic configuration
  Mechanical support of coils and W-shield (195 tons)
  Integration in a cryostat
  Cooling and cryogenics
  ….
2750 tons
2750 tons
100 tons
100 tons
50 tons
50 tons
A. Kohleimainen (CERN)
A. Portone, P. Testoni, F4E

## Slide 28: Many questions…
A. Kohleimainen (CERN)
Target
Coil module
W Shield
Thermal shield
Thermal shield
Pre-compression structure
Vacuum requirements ?
Composition, cooling ?
Beam OK ?
Maintenance ?
Add space for beam dump ?

## Slide 29: Solenoid manufacturing
Double pancake winding before HTS tape soldering
Joints and inlet/outlet (at low field)
HTS tape soldering by injection of solder at low end of each turn
Unspringing for insulation (cf. ITER TF coil manufacturing)
Stacking of double pancakes and impregnation of the module
A. Kohleimainen (CERN)

## Slide 30: 6D cooling
On-axis field and field profile B(s)
Aperture and clearances
Energy deposition, radiation dose, DPA’s
Good starting point, magnet work will start in 2023
https://indico.cern.ch/event/1147941/contributions/4851978

## Slide 31: Thermonuclear fusion
ITER Central Solenoid Model Coil
13 T in 1.7 m (LTS)
MIT/CFS SPARC TF Coil prototype
20 T at 20 K (HTS)
Large bore (2 m), high-field solenoids (13 T) and toroids (20 T), cooled by a forced-flow of helium, adapted to the removal of significant nuclear heating and AC loss. Both LTS (Nb3Sn) and HTS (REBCO) technologies are developed up to the level of industrial readiness. The push is towards higher fields solenoids (flux swing) and toroids (fusion power). Particularly interesting the operation at 20 K, improving on cryogenic efficiency with respect to liquid and supercritical helium at 4.5 K.

## Slide 32: Magnetic Resonance Imaging
Large bore (800 mm), high-field (11.7 T) and high-homogeneity solenoids, in persistent- or quasi-persistent mode. LTS (Nb-Ti) technology is dominant, with interest in MgB2 and HTS, especially for cryo-free operation. Nb3Sn is considered for a next step, with interest in increased fields (e.g. full-body, 14 T MRI).

## Slide 33: High Magnetic Field Science
LNCMI resistive
(poly-helix) insert
for hybrid magnets
10…20 T in 30…50 mm
NHMFL 45 T hybrid
NHMFL series connected hybrid
36 T in
LNCMI outsert magnet for the 43 T hybrid
8.5 T in 1.1 m

## Slide 34: High Magnetic Field Science
HTS insert of NHMFL all SC 32 T
32 T in 40 mm (15 T LTS + 17 T HTS)
NHMFL HTS Little Big Coil
45.5 T in 14 mm (14.5 T HTS + 31 T resistive)
LNCMI/CEA Nougat
HTS insert
32.5 T in 50 mm
(12. 5 T HTS + 20 T resistive)
Sunam NI one-body
HTS magnet
26.4 T in 35 mm
(26.4 T HTS multi-width)
Small bore (< 50 mm), ultra-high-field (32 T) solenoids. LTS (Nb-Ti/Nb3Sn) outsert with HTS insert, or all-HTS technology is considered, various options for HTS (insulated, non-insulated or partially-insulated). The push is towards higher fields to explore physical phenomena in an affordable installation (all-SC). Existing projects for all-SC 40 T steady state (EMFL, NHMFL), and target all-SC 60 T steady state

## Slide 35: Nuclear Magnetic Resonance
Bruker ASCEND 1.2 GHz
28.2 T in 54 mm (LTS+HTS)
JEOL 1.02 GHz
24 T (LTS+HTS)
Small bore (< 50 mm), ultra-high-field (28.2 T) solenoids. LTS (Nb-Ti/Nb3Sn) outsert with HTS insert. The push is towards higher fields to improve resolution of the resonance spectra as well as acquisition speed. Next target is 1.5 GHz (35 T).

## Slide 36: Work in progress (mCol CM 2022)
Cartoon design of 40 T, 32 mm user facility solenoid (planned)
Cross section of 32 T, 32 mm user facility solenoid (existing)
R&D test
achieved 25.4 T
I. Dixon, NHMFL
R&D NI coil achieved 18 T at PSI
NI solenoid design for 40 T
J.-B. Song, LNCMI
J. Kosse, PSI
B. Bordini, CERN
R&D NI insert achieved 32.5 T at LNCMI
There is a technology path towards compact 40 T solenoids
Higher fields may be possible (upper limit around 55 T ?), but the magnets will be:
More complex
Larger
More expensive ?!?

## Slide 37: Accelerator magnets – 1/4
Powering based on a two harmonics circuit
but… expensive AF!
Field ramp linearity can be obtained driving the magnets into saturation (≈ 0.1 T)
Field quality ?
Losses ?
Reproducibility ?
F. Boattini, CERN
US-MAP

## Slide 38: Accelerator magnets – 2/4
To limit the stored energy, power, and voltage the string of NC dipoles will be “broken” in many individually powered circuits
A capacitor discharge is largely influenced by
  Capacitor temperature
  Ageing
  Any other changes in R-L-C characteristics
Active control will be necessary (active filter)
The specification on the field tracking can have a significant impact on the design and cost of the active filter in the power converter
Tracking on the 24 main circuits of the LHC achieved control accuracy of ppm’s of nominal current

## Slide 39: Accelerator magnets – 3/4
 | Active power (MW/m) | Reactive power (MVA/m) | Energy in gap (J/m) | Energy in air (no gap) (J/m) | Energy in coils (J/m)
Hourglass magnet | 0.15 | 15.7 | 3.8 | 1.2 | 0.07
H-magnet (3 coils) | 0.36 | 16.3 | 3.8 | 1.3 | 0.55
H-magnet (2 coils) | 0.18 | 19.9 | 3.9 | 3.1 | 0.14
Windowframe magnet | 1.24(*) | 14 | 3.7 | 0.7 | 1.49
The magnet stored energy is directly proportional to iron gap and pole width: keep them as small as possible
Fe-Co seems the only practical way to reach fields in the range of 1.8 T, but may pose RP issues (to be quantified)
Higher loss but marginally lower stored energy
Highly optimized cross section
Configuration to be studied
Does not seem interesting
M. Breschi, R. Micelli, P. Ribani (UniBo), F. Boattini (CERN)
Fe-Co saturation curve
(*) mainly due to skin effect, can be limited by subdividing the copper conductors

## Slide 40: Accelerator magnets – 4/4
SC magnets
  10 T is an “unfortunate” number for Nb-Ti
    LHC heritage, resulting from the years if competition with the SSC. Only a couple of models (MFISC, FRESCA) and 10m prototypes made it to (or close to) 10 T
    LHC ultimate field (magnet design) is set at 9 T. This field level was reached in a large part of the series production
    For practical reasons the LHC dipoles operate at 8 T
    Set the Nb-Ti design dipole field to 8…9 T (see later)
  NOTE: 16 T is similarly un “unfortunate” number for Nb3Sn
    Set the Nb3Sn design dipole field to 13…14 T (see later)

## Slide 41: Magnet powering alternatives
1 + 3
1 + 3 + 5
< 1 %
< 0.1 %
B11
B13
B15
BSC
Local correction
B11
B11
B11
B11
B11
B11
B11
B13
Global correction
Compatible with beam specs ?

## Slide 42: Collider magnets – 1/3
On-axis peak field | 10 T
On-axis peak gradient | 300 T/m
Bore diameter | 150 mm
Magnetic length | 15 m
Field Quality | 10 units
Technology | LTS/HTS
Temperature range | 1.9/4.2 K (LTS) or 10 to 20 K (HTS)
The combination of these three is not possible
DIPOLE
QUADRUPOLE
Gmax=175 T/m @ R=75 mm
Weq=120 mm !!!
Bmax15.4 T @ 4.2 K
Weq90 mm !!!
B=13…14 T
G=160…170 T/m
S.Mariotto, B.Caiffi, D. Novellini, INFN

## Slide 43: Collider magnets – 2/3
Work in progress to provide analytical expression for the magnet design limits
  Maximum field and gradient vs. magnet aperture in LTS and HTS
  Combined function limits B+G and B/G
Proposal: take provisionally 9 T for NbTi and 14 T for Nb3Sn
Margin limit
Stress limit
Dipoles
Quadrupoles

## Slide 44: The need for energy
CERN uses today 1.3 TWh per year of operation, with peak power consumption of 200 MW (running accelerators and experiments), dropping to 80 MW in winter (technical stop period)
Electric power is drawn directly from the French 400 kV distribution, and presently supplied under agreed conditions and cost
Supply cost, chain and risk are obvious concerns for the present and future of the laboratory

## Slide 45: Energy efficient cryogenics
The 60…80 K range would be a dream…
LHC
(FCC)
ESS
Need efficient cryo-plant and heat removal scheme in the range of 10…20 K (see work at ESS)
This could be the best range of operating temperature of a future HEP collider
RHIC
Tevatron
HERA
LHC
HTS may be the only path towards a future collider
Nb-Ti
8T
5T
Nb3Sn
16T
12…14T
HTS
40…60T
20…40T
a few T
1.9
4.2
77
Credits to P. Borges De Sousa and R. Van Weelderen, CERN

## Slide 46
Future helium supply is limited and entails a substantial economical and availability risk
F. Ferrand, CERN

## Slide 47: The need for economics
A large component in the magnet cost is the amount of superconductor (coil cross section)
High-field superconductors are (significantly) more expensive than good-old Nb-Ti
Need to work in two directions:
  Reduce the coil cross section (increase J !)
  Reduce unit conductor cost
HTS may offer both
j
w
Rin

## Slide 48: On a slimming diet !
Reduce 16 T FCC-hh dipole x-section by factor 2
900 A/mm2
720 A/mm2
630 A/mm2
Achieve 20 T with the 16 T FCC-hh dipole x-section
550 A/mm2
380 A/mm2
580 A/mm2
540 A/mm2
480 A/mm2
Single coil conductor cross section
Multiply by ≈20 for kUSD/m

## Slide 49: New winding technology needed
5 T at 2800 A
JE = 250 A/mm2
16 T at 2800 A
JE = 850 A/mm2
920 µm
HTS windings can profit from “NI” technology
T. Lecrevisse, CEA

## Slide 50: Collider magnets – 3/3
A first attempt to compile a physical radial build for the various components in the collider bore and magnet, to be continued
S.Mariotto, B.Caiffi, D. Novellini, INFN

## Slide 51: Collider wobbles
h: beam height
p: wave period
Neutrino emission angle ≈ h/p
The same angle can be obtained changing p and h by the same ratio
p = 600 m
h = 150 mm
Mechanical actuation
p = 60 m
h = 15 mm
Magnetic steering ?
MB
10 T
5 m
MB
10 T
5 m
dy
3 T
1 m
dy
3 T
1 m
MB
10 T
5 m
dy
3 T
1 m

## Slide 52: MuCol EU study

## Slide 53: MuCol EU study

## Slide 54: Muons Magnets WG
Twenty-one meetings to date, with participants from m ost collaborating institutes and universities
Since April we meet:
  to “learn” about the previous work (MAP) and advances in relevant fields,
  to discuss in an informal setting initial ideas and options, and
  in preparation of upcoming activities, in particular the EU MuCol
Site: https://indico.cern.ch/category/13958/
Mailing list: muoncollider-magnets@cern.ch

## Slide 55: Tasks
The organization of the tasks overlaps with the EU MuCol study
The scope of the work in most tasks, however, extends beyond the EU proposal (e.g. target solenoid study, HTS tape procurement and measurements, test of HTS pancakes, …)
Most tasks activities also rely on advances and synergy with other projects and programs (e.g. HFM, UHF solenoid R&D, HTS fusion magnets R&D, HTS generators R&D, …)
Task 1
Technical Coordination and Integration
Task 2
Target, Capture and Cooling Magnets
Task 3
Fast Cycled Accelerator Magnets
Task 4
Collider Ring Magnets
Magnet Systems

## Slide 56: The Team and the work – 1/4
Participants
  CERN (LB, SF)
  CEA (LQ)
Activities
  Periodic meeting of the “muons magnets Working Group”
  Machine configuration (“magnet catalogue”)
  Interface to physics, radiation, vacuum, cryogenics, safety and RP
  Review of radiation hardness of superconductors and insulation systems (joint activity with radiation studies)
  Documentation and reporting
Task 1
Technical Coordination and Integration
Task 2
Target, Capture and Cooling Magnets
Task 3
Fast Cycled Accelerator Magnets
Task 4
Collider Ring Magnets
Magnet Systems

## Slide 57: The Team and the work – 2/4
Participants
  INFN (MS)
  CEA (LQ, PhD)
  CERN (AD, BB, TM, LB, AK, CA, AB)
  CNRS (XC)
  F4E (AP, PT)
  KIT (TA)
  PSI (JK)
  SOTON (YY, post-doc)
  UNIGE (CS)
  TWENTE (HTK, AK, post-doc)
Activities (≈ 12 months)
  Conductor review and specification
  Design of target and capture channel solenoids
  Design of final cooling solenoid
  Procurement and electro-mechanical characterization (UHF) of test HTS material
  Pancake model coils, engineering design, manufacturing solutions, mechanical and powering tests
Task 1
Technical Coordination and Integration
Task 2
Target, Capture and Cooling Magnets
Task 3
Fast Cycled Accelerator Magnets
Task 4
Collider Ring Magnets
Magnet Systems

## Slide 58: The Team and the work – 3/4
Participants
  CERN (FB, LB, TECH)
  UNIBO (MB, PR, RM)
  LNCMI (JB)
  TWENTE (HTK, AK)
  TUDa (HVG, post-doc)
Activities (≈ 12 months)
  Power converter conceptual design and optimization, including energy storage
  Components tests (capacitors)
  Conceptual design and 2D optimization of resistive magnets for RCS
  Initiate detailed 2D/3D analysis of resistive magnets for RCS, including saturation, end effects, anomalous loss
  Conceptual design of SC magnets for RCS
  Study of HTS options for pulsed magnets
Task 1
Technical Coordination and Integration
Task 2
Target, Capture and Cooling Magnets
Task 3
Fast Cycled Accelerator Magnets
Task 4
Collider Ring Magnets
Magnet Systems

## Slide 59: The Team and the work – 4/4
Participants
  INFN (SM, BC, DN)
  CERN (LB)
  UNIMI (SM)
Activities (≈ 12 months)
  Establish limits of SC dipoles and quadrupoles, considering LTS and HTS as well as combined function options
  Agree on arc dipole specification
    Field and gradient
    Aperture
    Nested/asymmetric windings
    Operating conditions
  Initiate conceptual design of main arc magnet
Task 1
Technical Coordination and Integration
Task 2
Target, Capture and Cooling Magnets
Task 3
Fast Cycled Accelerator Magnets
Task 4
Collider Ring Magnets
Magnet Systems