## Slide 1: HTS Program at PSI B. Auchmann, A. Brem, M. Daly, M. Duda, M. Koratzinos, J. Kosse, T. Michlmayr, H. G. Rodrigues, D. Sotnikov
10.03.2023 – HiTAT (https://indico.cern.ch/event/1220254)
This work was performed under the auspices of and with support from the Swiss Accelerator Research and Technology (CHART) program (www.chart.ch).

## Slide 2: Overview
Solder-impregnated NI solenoid
P3 adiabatic matching device for operation in SwissFEL
FCCee HTS4 demonstrator study
HTS HFM study
Outlook

## Slide 3: CHART – What, Who, How?
http://chart.ch
“CHART, the Swiss Center for Accelerator Research and Technology, was founded to support the future oriented accelerator project Future Circular Collider (FCC) at CERN and the development of advanced accelerator concepts in Switzerland beyond the existing technology. […] The high field magnet R&D has strong synergies with PSI projects […]” [Application for support of the Swiss Accelerator Research and Technology Initiative, 2018]

## Slide 4: MagDev Laboratory Layout
HTS winding
LTS winding
Re-reeler
3D Scanning
Heat treatment
Impregnation
Loading / Assembly
Storage
Instrumentation

## Slide 5: NI Solder-Impregnated Technology Solenoid
Greg Brittles
Axial joints
Goal: Rapidly develop infrastructure for HTS coil manufacturing and testing
via NI coil technology license agreement with Tokamak Energy.

## Slide 6: HTS Infrastructure and Team @ MagDev Lab
Henrique Rodrigues
Engineer P3 ReBCO
Dmitry Sotnikovs Engineer HFM ReBCO
Jaap Kosse
Engineer HTS4 ReBCO
Winding
Vacuum Solder Impregnation
Testing
Cryogen-free test station (2 kA)
Tensioning system developed by Francois-Olivier Pincot,
Jacky Mazet, CERN
Pre-tinning support by Davide Uglietti, EPFL-SPC
Modeling
Mike Koratzinos
Project lead HTS4

## Slide 7: Modular Technology

## Slide 8: 4-Stack Technology Solenoid Cold Test

## Slide 9
Successful test in cryogen-free test station of 4-pancake HTS NI solenoid, built in-house at PSI and using licensed Tokamak Energy Ltd technology.
Coil reached 18.2 T in the center, 20.3 T on the conductor at the maximum current of the power converter of 2 kA and 12 K coil temp.
Hall probes were qualified at UniGE up to 19 T.
Stack of 4 NI HTS coils with thermal/ electrical connectors
HTS leads
1st cryocooler
4K coldhead
2nd cryocooler
20K coldhead
thermal
connectors
radiation shield
top plate
Cu leads
Diameter: 100 mm
Aperture: 50 mm
SC type: ReBCO
# tapes: 2
# turns: 2 x 170
SC length: 2 x 49 m
Courtesy of M. Duda, J. Kosse, H. Rodrigues
4-Stack Technology Solenoid Cold Test

## Slide 10: 4-Stack Technology Solenoid Cold Test
field
current
coils voltage
2 kA 3h
18.2 T
1.6 mV
over 4 coils
~800 nohm
slow ramp
down with
0.5 A/s only
A B C D
0-A:
fast ramp up with 1 A/s
voltage over coils increasing because of current radial path
A-B:
slower ramp up with 0.2 A/s to stabilize coils voltage increase
B-C:
2 kA 3h plateau
coils voltage decreasing because of current redistribution
field is increasing – not reaching plateau
C-D:
slow ramp down with 0.5 A/s to avoid quench back
Courtesy of M. Duda

## Slide 11: 4-Stack Technology Solenoid Cold Test
Courtesy of M. Duda
current
HTS leads temp
coils temp
78 K
12 K
2 kA 3h
external
heater OFF
heating while
current
discharge
A B C D
0-A:
fast ramp up with 1 A/s
coils temp regulated by external heaters
A-B:
slower ramp up with 0.2 A/s to stabilize coils temperature
B-C:
2 kA 3h plateau
temperature of Cu-HTS leads joint increasing because of joule heating
coils temperature stable at 12 K
C-D:
slow ramp down with 0.5 A/s

## Slide 12: Quench in 4-Stack Technology Solenoid
Thermal runaway as consequence of bad electro-thermal contact (indium contact sheet was re-used).
C4
Cu
Cu
HTS lead
HTS lead
C3
C2
C1
V_c4
V_c3
V_c2
V_c1
V_out
V_in
V taps arrangement
Courtesy M. Duda

## Slide 13: Quench in 4-Stack Technology Solenoid
1.99kA
0.5A/s
1A/s
external heater OFF
temp sensor
detachment
coils 2&3?
25K
28K
2min
5min
35K
0.1A/s
0.2A/s
10A/s
2A/s
5A/s
0.5A/s
Courtesy M. Duda

## Slide 14
bad contact heating too much
c4 voltage rise
Quench in 4-Stack Technology Solenoid
Courtesy M. Duda

## Slide 15
14.4T
14.6T
14.1T
Quench in 4-Stack Technology Solenoid
Courtesy M. Duda

## Slide 16: Performance Reduction in 4-Stack after Quench
Maximum field decreased to 17.3 T
No sign of SC degradation. No current-sharing.
    Are there fewer turns with azimuthal current?
  Individual pancake tests in LN2 confirmed performance decrease in hottest coil.
  Axial connection plates were replaced.
  A 5th coil is under preparation and we may soon assemble a 5-stack.
    Inner copper ring was eliminated,
    Solder impregnation was improved,
    QA procedure is in place to validate all connections prior to high-current powering.
Courtesy M. Duda

## Slide 17
15 T in 72 mm warm bore
21 T on conductor
15 K conduction-cooling
Solid-state (Pb) thermal buffer
5 coils from 12 mm ReBCO
target
HTS NI target solenoid, to demonstrate
high-yield positron source concept
  stable DC operation,
  high thermal conduction due to solder impregnation to extract heat deposited in coils,
  radiation robustness due to absence of insulators.
Manufacturing Q3’23-Q2’24
Experiment at PSI’s SwissFEL 2025/26
FCCee Injector Study:P3 (PSI Positron Production)
Courtesy J. Kosse, T. Michlmayr, H. Rodrigues

## Slide 18
Simulations based on time-dependent 2D EM model from [1], coupled with 2D thermal and lumped thermal network.
PSI Positron Production HTS NI target solenoid
[1] Mataira, R.C., Finite-element modelling of no-insulation HTS coils using rotated anisotropic resistivity.
Superconductor Science and Technology, 2020. 33(8)
Courtesy J. Kosse
2D EM + Thermal

## Slide 19
PSI Positron Production
HTS NI target solenoid
Reminder: magnet will operate at 1170 A
Saturated regime
Power supply failure
Charging
Bore field [T]
Power supply current [A]
Model parameters (contacts, turn-turn-resistivity) based on 18 T test solenoid data
Courtesy J. Kosse

## Slide 20
Thermal buffer sized to allow safe internal dissipation of stored energy at currents below 1300 A.
PSI Positron Production
HTS NI target solenoid
Max coil temperature [K]
Power supply failure
Quench
Slow ramp-down
Courtesy J. Kosse

## Slide 21
System CAN1 ramp to 2000 A, but the magnetic energy can’t safely be extracted in fault scenario (cooler failure, power cut, failing lead).
➡ Aim for prevention instead of protection.
PSI Positron Production. HTS NI target solenoid
1170 A
2000 A
Very high current density
around quench front
During ramp after ramp during fault
During ramp after ramp during fault
[kA/mm2] [K]
[kA/mm2] [K]
1 … From EM-thermal point of view, mechanical restrictions apply.
Courtesy J. Kosse

## Slide 22
Stresses at 1170 A
PSI Positron Production. HTS NI target solenoid
Axial stress[MPa]
Hoop stress [MPa]
Radial stress [MPa]
Fat solenoid some positive radial stress, despite overbanding
Limit >200 MPa for non-soldered NI pancake [1]
[1] Joshi, S.,. IEEE Transactions on Applied Superconductivity, 2020. 30(4): p. 1-5
Courtesy J. Kosse

## Slide 23: HTS4: HTS short straight sections for FCC-ee
By using HTS sextupoles and quadrupoles instead of the RT baseline, HTS4 aims to:
Reduce energy consumption from up to 80 MW (43 MW in CDR) to <10 MW
Increase dipole filling factor – decrease SR
Enhance optics flexibility
Challenges:
Accelerator-grade field quality with HTS
Balance cooling power with conductor volume
High-reliability cryocooler-based operation
Low heat-load powering
Mitigation of radiation issues on electronics
Sub-scale coils and 1-m prototype module to be constructed and tested at PSI
CCT variant courtesy M. Koratzinos

## Slide 24: HTS4: HTS short straight sections for FCC-ee
Are magnets operated by cryocoolers reliable enough to enable high availability?
First estimates say YES, IF redundancy is implemented
Total system coldhead reliability >0.999 over 3 year period possible
 | 0.0000 |  |  |  |  | 
 | 0.9817 | 0.0000 |  |  |  | 
 | 1.0000 | 0.9462 | 0.0000 |  |  | 
 | 1.0000 | 0.9998 | 0.8954 | 0.0000 |  | 
 | 1.0000 | 1.0000 | 0.9995 | 0.8321 | 0.0000 | 
 | 1.0000 | 1.0000 | 1.0000 | 0.9991 | 0.7594 | 0.0000
 | 0.0000 |  |  |  |  | 
 | 0.9817 | 0.0000 |  |  |  | 
 | 1.0000 | 0.9462 | 0.0000 |  |  | 
 | 1.0000 | 0.9998 | 0.8954 | 0.0000 |  | 
 | 1.0000 | 1.0000 | 0.9995 | 0.8321 | 0.0000 | 
 | 1.0000 | 1.0000 | 1.0000 | 0.9991 | 0.7594 | 0.0000
number of required operational coolers
Installed coolers per magnet

## Slide 25: D-ITET PES: FCCee CPES
In support of FCCee HTS4, CPES develops a cryogenic power supply which, in its first iteration, may reduce heat load to the cryo-cooler by 50%.
CPES development follows specifications provided by CERN power-supply specialists.
The CPES unit may incorporate magnet protection functionality.
Cold-testing and integration studies at PSI cryogen-free test station.
Courtesy J. Huber

## Slide 26: HTS for HFM
How to make cable for HTS accelerator magnets (e.g (15 m long, 16+ T, 4.2-20 K)?
  How to deal with ramp losses? Cryogenic concepts?
  How to guarantee sufficient integral field quality?
  How to protect the magnets?
Material development for insulated tape stack.
Numerical studies for transient effects in cross-section.
Insulated tape-stack cable manufacturing.
Technology racetracks.
Hybrid configuration of SM-CC beyond 2025.
Ultimately HTS-only SM-CC.
Close technical exchange with MSC has started.
Materials and Numerical Design Studies
Powered Cable Samples
Technology Racetrack Coils
Short Hybrid HTS/LTS Magnets (15…17 T)
Short All-HTS Magnets (16…20 T) (4.2…20 K)
Q4’24

## Slide 27: Conclusion
CHART MagDev is gradually building up experience in HTS technologies.
A solder-impregnated NI solenoid, built in collaboration with Tokamak Energy Ltd, reached 18.2 T and survived a quench with an as-yet unexplained reduction in performance.
NI coil technology is being refined and applied to the P3 adiabatic matching device which will operate in a beamline by 2025.
Muon collider cooling solenoids have many similarities, and a PhD under the HorizonEurope MuCol project will soon start at PSI.
Other synergetic activities are under discussion in Swiss academia.
HTS4 aims at energy efficient accelerator magnets with related challenges.
HFM R&D is starting, and it is intriguing to re-think what “accelerator-quality” means in an all-HTS accelerator.
We need to improve on instrumentation, modeling.
We are still at the very beginning of this journey …

## Slide 28
Extra Slides

## Slide 29: Cryogen-Free Test Stand – Warm-Lead Cooling
Cryostat insert with two cryocoolers
Radiation shield with MLI
Vacuum vessel with pumps
Electronic rack
vacuum control/monitoring
temperature control/monitoring
voltage signals recording
quench detection system
2kA 10V power converter
Powering cables (500A single cable)
Cooling with 2 cryocoolers
  RDK-415D – samples/coils (1.5W@4.2 K and 35W @ 50K)
  RDK-500B – current leads (160W@70K)
DAQ
  2 nanovolt channels
  16 high precision channels
  32 fast sampling channels
FPGA based quench detection system with interlock and safety matrix
10 cernox temp sensors
5 hall probes (calibrated at various temperatures up to 20T)
Water chiller
Top copper lead temperature reduced from 56ºC to 8ºC.
Courtesy of H. Rodrigues

## Slide 30: Optimized Thermal/Electrical Contacts
Numerous optimizations of contacts enabled the 12 K operating temperature at 2 kA operation.
Courtesy of H. Rodrigues

## Slide 31: Solder Impregnation Technology
Fluxed Winding
Soldering from top
Rosin Flux
200 Celsius
+ 30 min cycle
Problems:
Dry patches inside
Time
Fluxed-Hot-winding
Pre-tinned tape
Rosin Flux
200 Celsius
~ 25 min cycle
Problems:
Small empty voids
Time
Fluxed winding
Pre-tinned tape Bath soldering in vacuum
Removable mandrel
GSP-2533 Flux
210 Celsius
~ 3 min cycle / ~ 5 mbar
Problems: Unequally spaced turns
Courtesy of H. Rodrigues
Fluxed winding
Pre-tinned tape
Bath soldering in vacuum
Removable mandrel
Tightening during soldering
GSP-2533 Flux
220 Celsius
~ 3 min cycle / ~ 5 mbar
Problems: Tbs
Baseline:

## Slide 32: Implementing Lessons Learned on Test Station
Courtesy H. Rodrigues