## Slide 1: Quench protection techniques for HTS coils
Mariusz Wozniak
10th March 2023

## Slide 2: Quench Protection – Goals and increasing complexity
Quench protection is a technique used to prevent any potential damage to a magnet, its circuitry, and surrounding components, when a portion of the magnet undergoes an irreversible transition to a normal state.
This is achieved by managing the stored magnetic energy in a way that mitigates any potential damage.
The scope of “any potential damage” predominantly means:
voltages and temperature (in most cases) -> Nb-Ti
voltages, temperatures, and conductor level stresses -> Nb3Sn
voltages, temperatures, conductor level stress and often superconductor level stress and for NI coils, a potential for a force density redistribution -> YBCO
Each measure above needs its safe operational range. These are extremely resource intensive to establish, if can be fully established at all.
A proper quench protection analysis of an HTS often exceeds the expertise of a single person and the capabilities of a single software tool. Quench protection of HTS is a multidisciplinary team effort!
Notes: Explain that quench protection is about managing stored magnetic energy and the fact that this is getting more complex for YBCO as many more additional aspects need to be taken into account.
Emphasize need for team of people with various skills that are needed for proper quench protection simulations.
Emphasize that the limits for the measures are not well establish and it will be lots of work to do so.

## Slide 3
Managing Stored Magnetic Energy - Basics
For exponential decay:
Required τ for J0 ≈ JCu of HTS conductor:
500 A/mm2:
1000 A/mm2:
Note above assumes adiabatic conditions, no current sharing, and zero NZPV in HTS
For double the initial current density J0, a quadrupling of RE is roughly expected, so quadrupling of energy extraction initial volage, i.e.:
L
RQ
RE
Power source
t1
I
Quench
Notes: Introduce the basic of quench protection with the

## Slide 4: Managing Stored Magnetic Energy - Approaches
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
Active (requires quench detection)
Passive
By-pass
Passive
Notes: After having introduced the energy extraction, Continue through this structure, introduced constant resistance and constant voltage extraction.

## Slide 5: Managing Stored Magnetic Energy - Approaches
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
Active (requires quench detection)
Passive
By-pass
Passive
This indicates that :
magnet energy is predominantly being removed
with active method (Q. detection required)
removal by electric terminals of the magnet
resistor or varistor is used
Notes: After having introduced the energy extraction, Continue through this structure, introduced constant resistance and constant voltage extraction.

## Slide 6
Energy extraction is very effective
Requires quench detection and active system, that are quite involved for HTS and add to the system cost
Voltage needed for energy extraction:
RE=const.: 2
RE=R0(I)β : 3
L=const.
RQ≈0
Resistor ->
Varistor ->
Extraction voltage, for a constant voltage EE is 33% lower than a constant-R extraction for the same effect (in principle).
L
RQ
RE
Power source
t1
I
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive
Notes: After having introduced the energy extraction, Continue through this structure, introduced constant resistance and constant voltage extraction.

## Slide 7
A relatively high dB/dt is needed to remove energy by the magnetic coupling. Electric Energy Extraction can be used to create the high dB/dt.
The effectives of magnetic coupling is higher for varistors than resistors [1]
This might be an interesting avenue for HTS CCT magnets
[1] Eberhard P H et al (1977), “Quenches in large superconducting magnets,” Proceedings of the Sixth International Conference on Magnet Technolgy MT-6, Bratislava, pp 654-661.
L
LC
M
RQ
RE
RC
Power source
t1
I
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 8
T-t-T = Turn-to-Turn
Propagation in conductor
(simplifying as adiabatic) [5]:
[5] Superconducting Magnets: M.N. Wilson, pub. Oxford University Press (1983) ISBN 0-019-854805-2
The method works very well for many LTS magnets and is passive and simple
However, due to large enthalpy margin, the quench propagation along the HTS conductor is relatively slow (typically ~ cm/s).
The normal zone does not develop substantial resistance to cause substantial dI/dt (dB/dt) so AC loss contribution is negligible and due to large MQE it is rare for HTS to quench due to AC loss (i.e. like in quench-back of LTS)
In short, this method of protection is not a good idea for HTS
The protection methods for LTS are not ‘just’ extrapolation of LTS technology
Large enthalpy margin
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 9
[1] Christian Lacroix, et al. Supercond. Sci. Technol. 27 (2014) 055013 (6pp)
[2] Frederic Sirois, presentation just before this one.
The current flow diverters also belong to this category [1, 2]
They are very effective at speeding up the NZPV and reducing the time constant τ and reducing Tmax
This helps with distributing the stored energy in the coil structure.
This is completely passive system, very attractive indeed!
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 10
[1] A. Gavrilin et al. Comprehensive quench analysis of the NHMFL 32T all-superconducting magnet, CHATS 2015, Bologna, Italy
[2] T. Mulder et al. External Coil Coupled Loss Induced Quench (E-CLIQ) System for the Protection of LTS Magnets, IEEE TAS, Conference proceedings of ASC22.
[3] E. Ravaioli. Optimisation of CLIQ for HTS, WAMHTS-2, 2015, https://indico.cern.ch/event/396905/contributions/1837520
[4] K. Ijagbemi et al. Evaluation of Frequency Loss Induced Quench Protection Prototype at 77 K Using HTS Coils,
IEEE TAS, Early Access, 1 – 6, 2023, https://doi.org/10.1109/TASC.2023.3252497
Many possibilities to increase resistance of the coil
The practicalities for these methods are coils size depended, for small coils they could work, but for large coils the power required goes quickly into tens of MW.
Quench heaters have been used for HTS, but require a lot of power to quench in the required time [1].
Using external coils to induce a quench (e.g. E-CLIQ [2]) is possible but challenging in practice for HTS due to large enthalpy to quench.
Using external power sources (P Source) like capacitor bank as in CLIQ [3] or PSU as in FLIQ [4] is possible, but again large enthalpy margin and large coils requires large AC loss power for a effective protection.
E-CLIQ coil [2]
HTS quench heater [1]
CLIQ discharge cir. [3]
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 11: Some examples of how protection could be done in practice

## Slide 12
Quench heaters used as energy extraction resistor
Magnet stored energy is used as a power source
Might be challenging for protection at lower magnet currents
W. D. Markiewicz - Quench protection of HTS superconducting magnets, US20060291112A1
Coil
Heater and energy extraction resistor
Power source
EE switch
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 13
This method uses electrical energy extraction and magnetic coupling to the ‘co-wound’ coils
Such an additional coil works effectively like a quench heater
Step change of transport current is very beneficial for reducing the quench integral
M. Mentink et al. - Quench Protection of Very Large, 50-GJ-Class, and High-Temperature-Superconductor-Based Detector Magnets, IEEE App. SC 26 (2016) 4500608
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Step change of current
Active (requires quench detection)
Passive
Passive
Quench protection has strong influence on the conductor design and magnet design

## Slide 14
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
For HTS magnets that are difficult to protect the best strategy is to use as many methods from the above outlined approaches as applicable.
Active (requires quench detection)
Passive
Passive

## Slide 15
No Insulation / Partial insulation / Metal insulation - single pancake case
[1] S. Hahn et al. 45.5-tesla direct-current magnetic field generated with a high-temperature superconducting magnet, Nature, 570, 496–499 (2019).
[2] G. Brittles, R. Bateman, Stability and quench dynamic behaviour of REBCO coils for spherical Tokamaks R&D, WAMHTS-5, 2019, Budapest
Figure from [2]
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive
Very effective method for decreasing J flowing through a quench region, i.e. the left side integral is low, so resulting temperature increase is low
Current redistribution can create stress states during quench that are difficult to simulate and design for
Stored energy is predominantly deposited in cold mass
or quenched region
Figure from [1]
L
Rθ
RR
Power source
I

## Slide 16
Very effective method for decreasing J flowing through a quench region, i.e. the left side integral is low, so resulting temperature increase is low
[1] S. Hahn et al. 45.5-tesla direct-current magnetic field generated with a high-temperature superconducting magnet, Nature, 570, 496–499 (2019).
[2] G. Brittles, R. Bateman, Stability and quench dynamic behaviour of REBCO coils for spherical Tokamaks R&D, WAMHTS-5, 2019, Budapest
Current redistribution can create stress states during quench that are difficult to simulate and design for
Stored energy is predominantly deposited in cold mass
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
L
LC
M
Rθ
RR
RC
Power source
I
copper rings are magnetically coupled to the coil
Active (requires quench detection)
Passive
Passive
or quenched region
Figure from [1]
Figure from [2]
No Insulation / Partial insulation / Metal insulation - single pancake case

## Slide 17
Animation courtesy of T. Mulder
Pancakes in the stack are mutually coupled.
A decrease of current in one pancake causes increase of current in the others.
This leads to magnetic pumping and redistribution of energy density and force density.
One needs to be careful in limiting the deposited magnet energy or over-stress in the pancake that quenches last.
Placement of conducting elements at the end of the stack or around it (e.g. Cu tubes) is a good solution to absorb some of the stored energy by magnetic coupling.
L1
LC
M1c
Rθ
RR
RC
Power source
I
Ln
Rθ
I
RR
Mnc
M1n
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive
Multiple pancakes case

## Slide 18
L1
LC
M1c
Rθ
RR
RC
Power source
I
Ln
Rθ
I
RR
Mnc
M1n
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive
Multiple pancakes case - mitigations
Redistribution of energy density and force density
Deliberately quenching parts of the magnet at strategically chosen locations and time could be help with the above issue
Quench heaters or capacitor discharge can be effective
This would require quench detection
This would require external power sources
[1] A. Gavrilin et al. Comprehensive quench analysis of the NHMFL 32T all-superconducting magnet, CHATS 2015, Bologna, Italy
[2] E. Ravaioli. Optimisation of CLIQ for HTS, WAMHTS-2, 2015, https://indico.cern.ch/event/396905/contributions/1837520
HTS quench heater [1]
CLIQ connections [2]

## Slide 19: An example of how protection could be done in practice

## Slide 20
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive
R. Bateman, Overview of the HTS program for the fusion programs, HiTAT 2023, slide 12
Quench protection has strong influence on the conductor design and magnet design
Excellent example was show earlier today by Rob Bateman of Tokamak Energy

## Slide 21
Also, for NI HTS magnets that are difficult to protect (suffer from excessive stress or temperature), the best strategy is to add a level of control to the quench process by using some of the above outlined approaches, as applicable.
One needs to understand the issues (e.g. over-stress of the conductor, temperature) to be deliberate using these methods.
Magnet Stored Energy
Distribute (propagate)
Remove (extract)
Conductor
Heaters
Turn-to-turn layer
Coils
Increase resistance of the coil
Electric (via term.)
Magnetic (via coupling)
Res/Var-istors
Structures
Add. coils
Power Sources
By-pass
Active (requires quench detection)
Passive
Passive

## Slide 22: Conclusions
There are many approaches that can be followed to protect an HTS magnet.
Broadly, the approaches can be divided into distributing the energy inside the magnet or removing it.
These approaches are often not mutually exclusive and, if needed or required, can be used in conjunction.
This logic can be followed for NI magnets, for which it might be necessary due to the possibility of energy and force density redistribution during a quench.
Conductor design often is driven by a chosen protection scheme
Limits for protection for HTS are becoming increasingly complex and not well understood or defined.
Collaboration, teamwork, experimental data and simulations are needed to maximize progress in HTS protection development.