## Slide 1
TCAD analysis of leakage current and breakdown voltage in small pitch 3D pixel sensors
Jixing Ye, Abderrezak Boughedda, Gian-Franco Dalla Betta
University of Trento
TIFPA INFN
Fondazione Bruno Kessler

## Slide 2
Content
Introduction
Simulation of Existing Detectors
Influence of Geometrical Parameters
Summary
1

## Slide 3
1. Introduction
Geometrical parameters of small-pitch 3D detectors:
active thickness 150 μm;
nominal radius ~2.5 μm;
effective gap ~20 μm.
Smaller inter-electrode distance translates into:
lower event pile up;
stronger radiation hardness.
ATLAS ITk specifications:
Radiation tolerance up to 2*1016neq/cm2;
Operation voltage Vop < 250 V;
Power dissipation < 10 mW/cm2;
Hit efficiency > 97%.
2

## Slide 4
Objective:
Locate the origin of the breakdown;
Improve the breakdown voltage from geometry point of view.
1. Introduction
Beam Test Results:
At 1016 neq/cm2 a hit efficiency of 96% reached below 100V with perpendicular beam incidence;
Larger voltages (~150 V) required at 1.8x1016 neq/cm2.
Problem:
Breakdown voltage not large enough compared with the required voltage for the worst cases;
Power dissipation.
TCAD Simulation
Simulation domain
25×100-1E
Effective Gap
Model Used | Temp
Perugia Surface Damage Model | -25 ℃
Perugia Bulk Damage Model | -25 ℃
CERN Bulk Damage Model | -38 ℃
3

## Slide 5
Breaks down at the Tip with/without surface damage.
2. Simulation of Existing Detectors
Structure | 50×50-1E
Column radius | 2.5 μm
Effective gap | 20 μm
Temp | -25 ℃
Model Used | Perugia Surface Damage Model
k(I,V) = , kbd
Simulation in agreement with experiment before and after surface damage.
Same breakdown voltage with/without surface damage.
I-V simulation based on Perugia Surface Model
4

## Slide 6
I-V simulation based on Perugia Surface Model
After surface damage: Max impact ionization on the tip
Deviation from experiment probably due to column depths uncertainty of the fabrication.
Before surface damage: Max impact ionization on the surface
Breakdown shifts from the surface
to the Tip after surface damage
2. Simulation of Existing Detectors
Structure | 25×100-1E
Column radius | 2.5 μm
Effective gap | 20 μm
Temp | -25 ℃
Model Used | Perugia Surface Damage Model
Simulation in agreement with experiment (breakdown voltage ~130V).
5

## Slide 7
Irradiation | Fluence (neq/cm2) | Structure | α* Experiment (10-17A/cm) | α* Perugia Model (10-17A/cm) | α* CERN Model (10-17A/cm)
Neutron | 1.0×1016 | 50×50-1E | 6.92±1.14 | 5.54 | 4.87
 |  | 25×100-1E | 4.25±0.91 | 6.69 | 4.22
Calculated Damage Rate at Vb=100V, T=20℃
Comparison between simulation & experiments
2. Simulation of Existing Detectors
Structure | 50×50-1E
Temp | -25 ℃
Structure | 25×100-1E
Temp | -25 ℃
Simulation based on the CERN Bulk Damage Model used Temp=-38 ℃, the leakage current was then scaled to -25 ℃ using the SRH model.
Always breaks down at the Tip regardless of the bulk damage model used or the structure.
6

## Slide 8
Irradiation | Fluence (neq/cm2) | Structure | α* Experiment (10-17A/cm) | α* Perugia Model (10-17A/cm) | α* CERN Model (10-17A/cm)
Neutron | 1.5×1016 | 50×50-1E | 7.79± 2.53 | 10.74 | 7.65
 |  | 25×100-1E | 3.87±0.43 | 9.25 | 6.13
Calculated Damage Rate at Vb=100V, T=20℃
Comparison between simulation & experiments
2. Simulation of Existing Detectors
Structure | 50×50-1E
Temp | -25 ℃
Structure | 25×100-1E
Temp | -25 ℃
Always breaks down at the Tip regardless of the bulk damage model used or the structure.
7

## Slide 9
Perugia Model:
predicted breakdown voltage of both layouts before and after surface damage;
the prediction of breakdown voltage is still in good agreement with experiment after bulk damage;
the shape of the leakage current is different from the measured I-V curve.
CERN Model:
leakage current well predicted at low reverse bias when the fluence is low;
leakage current starts to deviate from measured results at high fluence;
over-estimates the breakdown voltage for all simulated scenarios, including different layouts and fluences.
2. Simulation of Existing Detectors
8

## Slide 10
Conclusion:
Breakdown voltage increases with the Radius and the Gap;
Always breaks down at the Tip, contribution from the surface gets more and more important;
The Radius & the Gap effect saturates.
Conclusion:
Always breaks down at the Tip;
Same breakdown voltage for both Doses due to long distance of the Tip from the surface;
Breakdown voltage increases with the Radius & the Gap.
3. Influence of Geometrical Parameters
Structure | 50×50-1E
Temp | 20 ℃
Structure | 50×50-1E
Model Used | Perugia Surface Damage Model
Designed Value
9

## Slide 11
Conclusion:
1): Breakdown voltage increases with the Radius;
2): The Radius & the Gap effect saturates.
Conclusion:
1): Breakdowns at the Tip after surface damage, thus same breakdown voltage for both Doses;
2): Breakdown voltage increases with the Radius & the Gap.
Structure | 25×100-1E
Temp | 20 ℃
Structure | 25×100-1E
Model Used | Perugia Surface Damage Model
3. Influence of Geometrical Parameters
Designed Value
10
Notes: The origin of the breakdown for the 25X100-1E structure is quite different from the 50X50-1E for pre-irradiation cases, we can see that the breakdown always happens at the surface when the Gap is large, this is reasonable since the inter-electrode is larger than that of the 50X50 ones. Thus the breakdown voltage only increases with the radius and the effect saturates.
After surface damage, the breakdown shifts from the surface to the Tip, and we can see a clear dependence of the breakdown voltage on the Radius and the Gap.

## Slide 12
Breakdown simulation With/Without Oxide
Safe to use only the bulk for breakdown prediction after radiation damage to boost the simulation.
Structure | 25×100-1E
TID | 20Mrad
Model Used | Perugia Surface&Bulk Damage Model
Difference in the breakdown voltage with/without Oxide is negligible;
The trend applies for the CERN Model as well.
3. Influence of Geometrical Parameters
11

## Slide 13
Conclusion:
1): Higher Fluence leads to higher breakdown voltage;
2): Breakdown voltage increases with the Radius & the Gap;
3): The Radius & the Gap effect saturates.
Structure | 50×50-1E
Model Used | Perugia Bulk Damage Model
Structure | 50×50-1E
Model Used | Perugia Bulk Damage Model
3. Influence of Geometrical Parameters
Designed Value
Only the Bulk
Breakdown voltage increased 12V by increasing the radius for 1μm
12

## Slide 14
Structure | 25×100-1E
Model Used | Perugia Bulk Damage Model
Structure | 25×100-1E
Model Used | Perugia Bulk Damage Model
Conclusion:
1): Higher Fluence leads to higher breakdown voltage;
2): Breakdown voltage increases with the Radius & the Gap;
3): The Radius & the Gap effect saturates.
3. Influence of Geometrical Parameters
Designed Value
Only the Bulk
Breakdown voltage increased 20V by increasing the radius for 1μm
13

## Slide 15
4. Summary
The Tip limits the breakdown voltage, especially after radiation damage;
25×100-1E has higher breakdown voltage due to larger inter-electrode distance;
Perugia Bulk Damage Model can predict the breakdown quite accurately, CERN Bulk Damage Model is better at predicting the leakage current;
It is possible to increase the breakdown voltage of both designs by increasing the Radius/Gap, but the Radius & the Gap effect saturates.
14

## Slide 16
Thank you for your time!

## Slide 17
Backup – Pre-irradiation
Structure | 25×100-1E
Column radius | 2.5 μm
Effective gap | 20 μm
Temp | 20 ℃
Structure | 50×50-1E
Column radius | 2.5 μm
Effective gap | 20 μm
Temp | 20 ℃

## Slide 18
Back – Surface Damage
Structure | 50×50-1E
Column radius | 2.5 μm
Effective gap | 20 μm
Temp | 20 ℃

## Slide 19
S. Terzo et al., Frontiers in Physics 9:624668
Backup - Power dissipation
At the voltages of interest for a high hit efficiency, the power dissipation is still low
FBK
CNM

## Slide 20
G. Bardelli et al., IWORID 2022
S. Terzo et al., Frontiers in Physics 9:624668
25x100-1E
RD53A assemblies with different 3D sensor geometries
At 1016 neq/cm2 a hit efficiency of 96% at normal beam incidence reached below 100 V
Larger voltages (~150 V) required at 1.8x1016 neq/cm2
Back – Efficiency of irradiated modules at beam test