## Slide 1: Overview of the ongoing studies for the 12T robust dipole
(from a student’s point of view)
Gianluca Vernassa
TE-MSC-SMT | Topical meetings 29.11.2022

## Slide 2: Outline
HFM and DAHLIA12
Quench protection
Electromagnetic design
Mechanical design
Introduction to the probabilistic approach 

## Slide 3: Context: MSC HFM activities
Scope of the 12 T Robust Dipole Magnet Program:
  prove robustness
  study industrialization
  and cost effectiveness
  of Nb3Sn technology for potential future large scale application
Cos-theta layout: proven maturity in accelerators and large scale industrialization
Considered structures:
  Collars-based
  Bladder & keys (attempt for a world’s first!)
Particular attention on:
  Effectiveness in coil pre-stress (respecting performance limits)
  Ability to cope with mechanical tolerances
[image 1] https://td.fnal.gov/wp-content/uploads/2016/02/Picture9-431x221.png
[image 2] https://cds.cern.ch/record/2773288/files/coupe%20dip%C3%B4le.JPG

## Slide 4: Context: MSC HFM activities
[plan] A. Ballarino, A. Devred – The MSC HFM activities: strategy and milestones – Part 1: Nb3Sn, EDMS Nr: 2680109
[images] M. Masci & P. Wachal
Build two double aperture cos-theta dipole magnet models each 1.5-2 m long. The best solution will be extrapolated to a long magnet (5~6 m), in view of an accelerator application.
Collared structure
Bladders & keys

## Slide 5: Functional specification (In Work)
Bore field and field quality
  Nominal B1 = 12 T (at 1.9 K)
  Woundability preferred over of field quality (still maintaining acceptable values for an accelerator magnet)
Maximum current allowed: 20’000 A
Aiming for high quality coils: avoiding pop-out’s, extensive practical tests, manual optimization of pole ends’ spacers,…
Maximum hotspot temperature: 150-200 K (as low as possible)
Option for separate layers with external/internal splice (integrated work with the HFM WP3.1)
[images] P. Ferracin - EUCAS 2017 - Superconducting Dipole and Quadrupole Magnets for Particle Accelerators

## Slide 6: Functional specification (In Work)
Geometrical parameters
apertures
yoke
beam to beam distance

## Slide 7: Quench protection (F. Mangiarotti)
Adiabatic calculation
observable during tests
known under certain assumptions
Depends on:
Quench propagation velocity
Quench Detection system
Quench Protection system “effectiveness”
Estimation with FalconD cable parameters: 40-54 MIITs
https://indico.cern.ch/event/1143493/

## Slide 8: Quench protection (F. Mangiarotti)
Sensitivity: Cu/Non-cu
we need more Cu!
Statistics on QPS:
above 300K (of AHST) magnets show degradation
FalconD

## Slide 9: Quench protection (F. Mangiarotti)
Sensitivity: Cu/Non-cu
we need more Cu!
Statistics on QPS:
we need QH + CLIQ
FalconD

## Slide 10: Electromagnetic design (L. Fiscarelli)
Started with FalconD values, and attempted to propose a new design
  40 strands
  Strand diameter 1 mm
  Height 21.42 mm
  Width 1.797 – 1.989 mm (after reaction)
  Aperture diameter 50 mm
  5 blocks (3 inner + 2 outer)
  36 turns
[ref] A. Pampaloni et al., "Preliminary Design of the Nb3Sn $\cos\theta$ Short Model for the FCC," in IEEE Transactions on Applied Superconductivity, vol. 31, no. 5, pp. 1-5, Aug. 2021, Art no. 4900905, doi: 10.1109/TASC.2021.3061334.
R 25
21.42
1
2
3
4
5

## Slide 11: Electromagnetic design (L. Fiscarelli)
Many optimizations tried with this cable and aperture radius (for field quality and test sensitivity)
  Introduction of wedges at midplane
  Splitting (i.e. adding) blocks
  Genetic algorithms for angles,...
What we learnt:
  This geometric parameters have strong limitations
  It becomes very difficult to wind and optimize
  Nb-Ti internal splice cannot work
  We need to investigate a different parameters’ space!

## Slide 12: Electromagnetic design (L. Fiscarelli)
We investigated:
  diameters between 50 – 66 mm
  strands of Ø 0.85-1.00 mm
  cables of 34-40 strands
We checked:
  field quality (b3, b5, b7, b9)
  operating current
  margin on loadline
We miss (in progress):
  Quench protection studies
Ø 50-66
# strands
Ø strands
cable:
- width
- height
Aperture Ø [mm] | Cable spec.’s [strands × Ø] | Loadline fraction | [kA] | turns
50 | 40 × 0.85 mm | 83.2 % | 17.6 | 37
56 | 40 × 0.85 mm | 82 % | 17 | 41
60 | 34 × 1.00 mm | 78.6 % | 19.5 | 35
Aperture Ø [mm] | Cable spec.’s [strands × Ø] | Loadline fraction |  | turns
50 | 40 × 0.85 mm | 83.2 % | 17.6 | 37
56 | 40 × 0.85 mm | 82 % | 17 | 41
60 | 34 × 1.00 mm | 78.6 % | 19.5 | 35
Proposed solutions from ELM design

## Slide 13: Mechanical design: two pre-stress paradigms
Collared bladders & keys
prestress

## Slide 14: Functional specification (In Work)
Mechanical specifications:
  Maximum value of compressive stress at RT : 100 MPa (σ3 > -100 MPa)
  Maximum value of compressive stress at cold : 120 MPa (σ3 > -120 MPa)
  Not clear in terms of Von Mises equivalent stress, but limit around 120 MPa
  Other materials’ properties and limits (in parenthesis at cold):

## Slide 15: Mechanical design: two pre-stress paradigms
40-50 MPa
Collared bladders & keys
[graph1] D. Perini - Mechanical structures for superconducting dipoles. Different configurations for different applications. https://indico.cern.ch/event/1192313/
[graph2] Mechanical Simulation of Nb3Sn Coils - G. Vallone - 37th EuroCirCol WP5 Coordination Meeting CERN, 22/05/2018

## Slide 16: Mechanical design
Mock-ups as part of the 12T Robust Dipole program
Our mock-ups will be slices of the whole X-sections of the two magnets.
DAHLIA11: we start taking the coils of the 11T magnet and we re-design the structure around.
Finally, we will move to the chosen X-section of the 12 T

## Slide 17: Mechanical design
Collared bladders & keys

## Slide 18: Splices: conceptual design (O. Bahmane)
https://indico.cern.ch/event/1185610/
We would prefer separate coils for inner and outer layer
Here the option of external splice

## Slide 19: Probabilistic approach to magnet design
Many unknowns inside a Nb3Sn magnet
For a robust magnet we must consider them since the design

## Slide 20: Probabilistic approach to magnet design
Reliability analyses: manipulation of the uncertainties to assess the system’s probability of failure.
Uncertain mechanical properties of the materials
Uncertain geometry of the components
Limit state
State space
CMM Coil 1
CMM Coil 5
CMM Coil 2
CMM Coil 7
Strain []
Stress [MPa]

## Slide 21: Thank you!

## Slide 22: messy references (sorry)

## Slide 23
Eurocircol: https://cordis.europa.eu/project/id/654305/it
B. Bordini - Conductor Activity within EuroCirCol - EuroCirCol WP5 Workshop - https://indico.cern.ch/event/572501/
Second review of the Eurocircol WP5 -https://indico.cern.ch/event/661257/

## Slide 24: Baseline conductor (S. Hopkins)

## Slide 25: Similar Cable/Strand Experience (1)
Baseline: 40-strand cable of 1 mm diameter strands
  FalconD Cable Spec: EDMS 2663170
  cf. HL-LHC, 108/127
Ref | Name | Keystone | Width (mm)* | Strand Types
C01 | FalconD | 0.5° | 20.95 | 162/169, R&D (TVEL, KAT)
H11 | FRESCA2 | 0° | 20.95 | 132/169, PIT
H19 | ERMC | 0° | 20.95 | 150/169, 120/127
* width spec for FalconD set to 20.95 mm to match production experience for ERMC, FRESCA2
https://indico.cern.ch/event/1135479/

## Slide 26: Similar Cable/Strand Experience (2)
RRP layouts with relevant cabling experience at CERN:
 | 108/127 | 132/169 | 150/169 | 162/169
Layout |  |  |  | 
Cu/non-Cu | 1.15-1.2 | 1.25 | 1 | 0.9
deff (µm) | 60 | 52 | 52 | 52
https://indico.cern.ch/event/1135479/

## Slide 27: Quench Protection (F. Mangiarotti)

## Slide 28: Adiabatic calculation
If a small volume L of a cable quenches, the temperature rise can be estimated as follows:
Re-arranging terms and integrating from the time of quench:
Copper
Superconductor
L
This part is (mostly) independent of time. For a given geometry and maximum T, it can be calculated. Assuming constant maximum magnetic field is conservative.
Quench integral (QI). This part depends on quench prop. velocity, QDS settings and QH effectiveness at quenching the full magnet
https://indico.cern.ch/event/1143493/

## Slide 29: Material dependent part
Zcu (T,B,100) ¦ Zcu (T,B,200) | T = 250 K | T = 280 K | T = 300 K | T = 330 K
B = 12.0 T | .1042 ¦ .1085 | .1110 ¦ .1153 | .1151 ¦ .1194 | .1207 ¦ .1251
B = 12.4 T | .1035 ¦ .1077 | .1103 ¦ .1145 | .1144 ¦ .1187 | .1201 ¦ .1244
B = 13.0 T | .1026 ¦ .1066 | .1094 ¦ .1135 | .1135 ¦ .1176 | .1191 ¦ .1233
Zsc (T,B,100) ¦ Zsc (T,B,200) | T = 250 K | T = 280 K | T = 300 K | T = 330 K
B = 12.0 T | .0753 ¦ .0789 | .0795 ¦ .0831 | .0820 ¦ .0856 | .0855 ¦ .0892
B = 12.4 T | .0747 ¦ .0782 | .0789 ¦ .0824 | .0814 ¦ .0850 | .0849 ¦ .0885
B = 13.0 T | .0739 ¦ .0772 | .0781 ¦ .0814 | .0806 ¦ .0840 | .0841 ¦ .0875
Z values in MA2s / mm4
Zsc values fixed on 13.05.2022
https://indico.cern.ch/event/1143493/

## Slide 30: Quench timeline
t<0: nearly constant current
quench
QDS threshold
(100 mV)
QDS validation window (~3 ms)
t>0: current decays due to QH
QH fire at around t=0 (typically t~2ms)
https://indico.cern.ch/event/1143493/

## Slide 31: Definitions
Vth
tv
tQ
I0
tQ = time of quench (-7 ms in the example)
tv = validation window (3 ms in the example)
Vth = QDS threshold (100 mV in the example)
I0 = initial current (11.5 kA in the example)
tQ-100mV = the time it takes the resistive voltage to reach 100 mV (4 ms in the example)
QPV. From simulations and/or measurements
QDS settings
QH effectiveness. From simulations and/or measurements
quench
https://indico.cern.ch/event/1143493/

## Slide 32: Current fit after QH trigger
Mechanism:
QPS (QH and PC FPA) are triggered
QH heat up (OL) coil
As coil gets warmer, it becomes resistive and the current starts decaying
At some point (almost) all the coil becomes resistive -> this is the peak dI/dt
From then onwards, the decay is roughly exp(-tR/L)
Phenomenological fit:
https://indico.cern.ch/event/1143493/

## Slide 33: Current fit results
Including data from:
MBH short models
MBH full length magnets
MQXF short models
MQXF prototype
Impregnated and non-impregnated QH
RRP and PIT cables
Average coil cu/no-cu from 0.96 to 1.27
Coils with missing QH strips/circuits
QH current from 150 to 200 A
Only tests at 1.9 K
https://indico.cern.ch/event/1143493/

## Slide 34: FalconD

## Slide 35
[ref] Riccardo U. Valente, Falcon Dipole: Electromagnetic design – 30-06-2020

## Slide 36
[ref] Riccardo U. Valente, Falcon Dipole: Electromagnetic design – 30-06-2020

## Slide 37
[ref] Riccardo U. Valente, Falcon Dipole: Electromagnetic design – 30-06-2020

## Slide 38: Electromagnetic design in ROXIE (L. Fiscarelli)

## Slide 39: Genetic algorithm in ROXIE
Cable 2x20 strands of 1 mm
2 layers, 7 blocks
Parameters:
  Number of turns per block
  Phi angle
  Alpha angle
  Mid plane wedge on outer layer
Objectives

## Slide 40: Splice design (O.I. Bahmane)

## Slide 41
https://indico.cern.ch/event/1185610/