## Slide 1
CERN MPT workshop (Micro Pattern Technologies)

## Slide 2: MPT activity
Chart: 
| STD PCB | MPGD | GEM | LHC related circuits | Inner trackers
Activities | 10 | 30 | 20 | 20 | 20
-20 persons.
-1400m2.
-100m2 clean room.
-Top class environnement protection:
-Waste water treatment plant.
-Large scrubbers for fume cleaning.
-Fire extinguisment water containment.
PCB: Printed Circuit Board
MPGD : Micro Pattern Gas Detectors
-GEM : Gas Electron Multiplier
-Micromegas or uMegas or MM: Micro mesh gaseous detector
-uRwell: Micro Resistive Well detectors

## Slide 3: Examples of MPT activities
LHC
  Quench heaters
  Power Thick film resistors
  Magnetic sensors calibration
  Flexible heaters
  Diamond beam monitoring detectors
  Many Chemical milling
  RF Fingers
GEM :
  Compass
  CMS GEM GE1/1
  CMS GEM GE2/1
  ALICE TPC GEM
  CBM GEM for Fair
  BM@N (Baryonic Matter at the Nuclotron Dubna)
  Low material budget detectors (Hampton university)
  Kloe
  Totem
  LHC-B
  Phoenix TPC (Brookhaven)
  SBS tracker (Jefferson Lab)
  EIC tracking detectors (Jefferson Lab)
  Etc…
Micromegas
  ILC Calorimeter
  Minos TPC
  T2K
  ATLAS NSW
  Cast
  Panda X uBulk detectors
  TrexDM uBulk detectors
  TPC’s for Nuclear physics
  Beam for School
  T2K upgrade
  Clas12
  Scanpyramid
  Etc…
Inner trackers
  ALICE Inner tracker Al Bus
  Phoenix TPC AL bus
  ATLAS IBL
  ATLAS ITK
  LHCB data flexes

## Slide 4: FSU Experts
-Photolithography (down to 30um line/space):
-Resist Lamination, spraying.
-UV exposure  LDI , STD , large , scanner.
-Resist Devellopment.
-Resist Stripping.
-Chemical etching:
-metals :Cu,Al,Ni,Au,Ti,W etc..
-Adam Drozd
-Guillaume Button
-Christophe Ferreira De Oliveira
-Pawel Dubert
-CNC Drilling/milling.
-Katia Jauregui
-Galvanic and chemical plating:
-Cu, Ni, Au, In.
-Xavier Thery
-Vacuum press gluing.
-Jorge Penedo
-Optical & Electrical tests
-Elise Pechaud
Adam Drozd FSU team leader
Benilde Martins Administration
-Detectors production
-Zafer Budun
-Paul N’Guyen
-Patrick Ferreira De Oliveira
-Ercan Budun

## Slide 5: CERN Staff experts
-Design Bertrand Mehl
- Gazeous Detectors R&D Alexis Rodrigues
Olivier Pizzirusso
Antonio Teixeira
-Thin Film , Thick Film R&D Antonio Teixeira
-Vacuum deposition R&D Serge Ferry
-Chemical analysis Alexandra Gris

## Slide 6: Introduction to MPGD detectors

## Slide 7
Gaseous Detectors principle
-
Anode
Cathode
+
+
+
+
+
-
-
-
-
Gas volume
Ionization
Charged Particles

## Slide 8
Gaseous Detectors principle
-
Small Electric field
(100V/mm)
moves the charges
-
-
-
-
+
+
+
+
-
Anode
Cathode
+
+
+
+
+
-
-
-
-
Gas volume
Ionization
Charged Particles

## Slide 9
Gaseous Detectors principle
-
Small Electric field
(100V/mm)
moves the charges
-
-
-
-
+
+
+
+
-
Anode
Cathode
+
+
+
+
+
-
-
-
-
Gas volume
Ionization
Charged Particles
-
Strong Electric field
(50kV/mm)
triggers an avalanche
multiplying electrons
Output signal

## Slide 10
Gaseous Detectors principle
-
Small Electric field
(100V/mm)
moves the charges
-
-
-
-
+
+
+
+
-
Anode
Cathode
+
+
+
+
+
-
-
-
-
Gas volume
Ionization
Charged Particles
-
Strong Electric field
(50kV/mm)
triggers an avalanche
multiplying electrons
Output signal
Any detector needs a low field region to do the ionization
and then move these primary charges in a high field region to amplify them

## Slide 11
Different ways to get these 2 fields
anode
anode
anode
anode
anode
cathode
cathode
cathode
V1
V1
V1
Cathode
Cathode
Cathode
Cathode
The 2 regions are naturally obtained
because the field increases close
to the small Anodes wires
The 2 regions are obtained by adding electrodes
and 3D structures
V2
V1
V1
anode

## Slide 12
MPGDs have detecting cells 10 times smaller than wire chambers structure
 photolithographic technics
Why MPGD ?
Micro Pattern Gas Detectors
Faster ion evacuation
Higher spatial resolution
Reduced multiplication region size
Wire chambers
slow ion evacuation
Limited read out granularity

## Slide 13: First MPGD  Micro Strip Gas Chamber (MSGC)
Pitch limited to 1 to 2mm due to mechanical and electrostatic forces.
Glass substrate with anode strips of 10 um with a pitch of 200 μm.
More simple than a wire Chamber.
A. Oed
Nucl. Instr. and Meth. A263 (1988) 351.
RESULT:
Spatial resolution ~50μm
Rate capability ~106 Hz/mm2

## Slide 14
Came a period where many different structures were tested by many labs to overcome such defects
But as everybody knows there is always a problem
Spark damages coming
with heavy ionizing particles
Unstoppable erosion of electrodes.
Too difficult to solve
Aging
Creation of dendritic deposits
reducing the gain.
Same problem in Wire chambers
Also difficult to solve

## Slide 15
AND MANY OTHERS ….

## Slide 16
GEM family
Micromegas family
GEM
Thick-GEM
uRwell
Micromegas
Resistive Micromegas
uBulk
Nowadays, I think we can consider that the winners are:

## Slide 17
GEM
Thick-GEM
uRwell
Micromegas
Resistive Micromegas
uBulk
GEM family
Micromegas family
Nowadays, I think we can consider that the winners are:

## Slide 18
GEM production
the beginning

## Slide 19: Interconnection technologies available at MPT in 1996
Screen printed circuits
PCB
Thick film technology
MCM/L laminated
MCM/C ceramic
Thin film technology
MCM/D deposited
200um
120um
90um
75um
50um
25um
20um
MCM: Multi Chip Module
PCB: Printed Circuit Board
Minimum line and space
Technologies name

## Slide 20: Interconnection technologies available at MPT in 1996
Screen printed circuits
PCB
Thick film technology
MCM/L laminated
MCM/C ceramic
Thin film technology
MCM/D deposited
200um
120um
90um
75um
50um
25um
20um
MCM: Multi Chip Module
PCB: Printed Circuit Board
Minimum line and space
Technologies name

## Slide 21: MCM / D
Conductor material
  AL 10um
  Vacuum deposited
Dielectric material:
  Photo-imageable Liquid polyimide (PI)
  20um thick
  deposited with a spinner
Photolithography:
  Minimum track 20um
  Minimum via hole 25um
Substrate :
  TPG (Thermally annealed Pyrolytic Graphite)
PI stripper :Ethylene Diamine (EDA)
But the important detail is :
liquid PI typical application:
-Chip Scale Package (CSP)
-or Chip passivation
PI 1
PI 2
Silicon Die (Chip)
Pb/Sn Bump
STD Wire-Bond Pad
Atlas strip detectors R&D

## Slide 22: Fabio Sauli visit in 1996
Fabio was originally looking for a electron preamplifier stage to improve MSGCs
Request : foil with small holes of 100 to 200um
Electrode on both sides
And large size : 20cm x 10cm !

## Slide 23
Survey on Polyimide etching with EDA
First type of polyimide:
Perfect anisotropic etching
No under etch
Perfect to make small holes
Second type of polyimide:
Fully isotropic etching
Not satisfactory
We were lucky to find
immediately a good candidate
since there is more than 50 different PI types on the market
OK
OK
bad
bad

## Slide 24: GEM Manufacturing Process
Applying Resist
Copper Etching
Resist Stripping
Polyimide Etching
and Cleaning
UV Exposure
& Development
Vacuum deposited
copper on polyimide
Bad
OK
OK
Optimum pattern for physics
Obtained after many trials
1
2
3

## Slide 25: Manufacturing Process
Image transfer
Copper Etching
PI Etching
2nd image Transfer
2nd copper etch
HV test
Resist lamination
2nd lamination
2 aligned films pocket
Chemical spray
Dead bath

## Slide 26: GEM first application
The GEM gas gain was only 10
Today the GEMs can reach easily a gain of many hundred
Reduce the spark risk on the MSGC by doing part of the amplification in the GEM
First real application:
Save the HERA-B Experiment
(300 GEMs)
200mm x 200mm

## Slide 27: Triple GEM = detector
A cascade of multiple GEMs permit to reach high gains (> 104) before discharges with lower voltage for each GEM.
Gain is increased by about one order of magnitude at each addition of a GEM.

## Slide 28
Compass settled all the parameters:
-GEM Segmentation
-HV distribution
-X/Y Read out board
-FE electronics
TOTEM
30cm diameter
Cylindrical R&D
40cm x 40cm
Triple GEM = detector

## Slide 29
But the community started to ask for larger detectors.
We tried to increase the mask size using the same technique.
We faced unsolvable problems with mask alignment.
The cost of glass mask is prohibitive
15 000 CHF for 1m x 0.6m.
We manage to patch GEMs but this was a bit too complex.
We then tried to use the best automatic alignment machine available on the market.

## Slide 30: LDI laser direct imaging
Top to bottom alignment :
Announced +/-15um
Real +/- 40 um
Corners of a 800mm x 400mm GEM
Direct laser exposure of resist
following a GERBER file.
Scanning process

## Slide 31: LDI laser direct imaging
Top Vs bottom alignment :
Announced +/-15um
Real +/- 40 um
Corners of a 800mm x 400mm GEM
Direct laser exposure of resist
following a GERBER file.
Scanning process

## Slide 32: Why not using only one mask to skip alignment?
1/ etch holes in the top copper with one mask
3/ etch the bottom copper through the PI holes
Problem  how to etch the bottom copper without etching the TOP copper ?
2/etch the Polyimide through the copper holes

## Slide 33: Differential etching
  Working but:
  -Large rims
  -Bad yield
  -Hole shape too conical
  -Charging up
  -Lower gain
Top
Bottom

## Slide 34: Differential etching
  Working but:
  -Large rims
  -Bad yield
  -Hole shape too conical
  -Charging up
  -Lower gain
Top
Bottom

## Slide 35: Top copper plating protection
Top
Bottom

## Slide 36: Top copper plating protection
Top
Bottom

## Slide 37: Invert a Copper plating bath
Top
Bottom

## Slide 38: Invert a Copper plating bath
Top
Bottom

## Slide 39: Electro protection & chemical etching
TOP
Bottom

## Slide 40: Electro protection & chemical etching
TOP
Bottom
Perfect

## Slide 41: Double Mask Vs single mask
Base material : Polyimide 50um + 5um on both sides
Same base material
Hole patterning in Cu
Polyimide etch
Bottom electro etch
Second Polyimide Etch
Limited to 40cm x 40cm due to
  Mask precision and alignment
Limited to 2m x 60cm due to
  Base material
  Equipment
Double mask
Single mask

## Slide 42
Single mask introduced cost reductions:
10cm x 10cm GEM example
The 10cm x 10cm double mask GEM cost is 300 CHF/piece
For 100 pieces with Single mask the cost dropped to 100 CHF/piece
For 10 000 pieces , less than 50 CHF

## Slide 43
CMS GE1/1 application
CMS nose
GE1/1 Muon detector
Triple GEM stack
Single GEM
Microscopic view
Cross section
CMS experiment
GE1/1  400 GEM (1.3m x 0.5m) made at CERN
GE2/1 1000 GEM (1.3m x 0.5m) CERN/Korea
GEM producers capabilities:
-CERN MPT : 500m2/year
-Mecaro Korea : 250m2/year
Mecaro will finish half of GE2/1 end 2023
MPT will finish the other half mid 2023

## Slide 44: And many many more
KLOE – Cylindrical Detector
ALICE TPC – 700 GEM
Future CMS ME0
-BM@N in Dubna
-SBS tracker Jefferson lab
-CBM at Fair
-BESIII China
-SOLID
-BONUS 12
-P-RAD
-S-Phenix TPC
-COMPASS upgrade
-GEM for nuclear physics TPCs
-ESS for neutron detectors
-and lot of small GEMs for academic purpose
Other detectors using single mask technique

## Slide 45: Micromegas
George Charpak and Ioannis Giomataris

## Slide 46: Principle

## Slide 47: Micromegas during early days
-Electro formed mesh stretch on frame
 ultra fragile
-Amplification gap defined with
fishing wires (really long & delicate job)
-Good detector but a pain to produce
-Low yield  small size
-Frame needed
PCB with R/O structure
-Thin patterned copper 5um  still fragile
-Amplification pillars attached to mesh by process
-Pillars done by photolithography techniques
-low yield also  small size also
-Frame still needed
frame
SACLAY
CERN
frame
PCB with R/O structure

## Slide 48: Interconnection technologies available at MPT in 1996
Screen printed circuits
PCB
Thick film technology
MCM/L laminated
MCM/C ceramic
Thin film technology
MCM/D deposited
200um
120um
90um
75um
50um
25um
20um
MCM: Multi Chip Module
PCB: Printed Circuit Board
Minimum line and space
Technologies name

## Slide 49: Interconnection technologies available at MPT in 1996
Screen printed circuits
PCB
Thick film technology
MCM/L laminated
MCM/C ceramic
Thin film technology
MCM/D deposited
200um
120um
90um
75um
50um
25um
20um
MCM: Multi Chip Module
PCB: Printed Circuit Board
Minimum line and space
Technologies name

## Slide 50: MCM/C
-High density
-High Thermal Conductivity
-Vacuum compatible
-Conductive Layers: noble metals
-Dielectrics : Ceramic
-Sequentially printed layers
-850 Degrees curing
-Precise deposition
-Small sizes : 20cm x 10cm max
Screen printing machine
Screen with a patterned
Photo-imageable emulsion
on the mesh
Principle

## Slide 51
Screen printing is quite common
Manual printing on a T-shirt
Semi automatic screen printing machine
Printing area 2m x 0.9m for posters (Satigny)
Semi automatic CERN machine 1.5m x 2m
General purpose
CERN precision machine 20cm x20cm
for Micro-electronic

## Slide 52: Why not using this type of mesh for MM ?
Mechanically robust
Low cost compared to Electroformed or etched
325 wires/inch  wire 24um  transparency 48%
400 wires/inch  wire 18 um  49%
640 wires/inch  wire 15um  39%
730 wires/inch  wire 13um  40%
Available in rolls of 1.2m up to 1.7m
The answer came from Patrick Janneret PHD student
@ Neuchatel university.
Even if the idea was in the air , he was the first to ask us
to put spacing pillars on a woven mesh and test them.
And the results were really good.
This was the important missing detail to go for the next stage.
Etched mesh
Woven mesh

## Slide 53: With I.Giomataris we decided to develop these 2 structures
BULK Micromegas
Developed in 1 week
Floating mesh Micromegas
The detectors behavior were really good !
The technology spreading was quite rapid

## Slide 54
BULK Micromegas detectors
ATLAS NSW R&D, Joerg Wotschack
1.5m x 0.5m plane
Single panel
Muon detector in LHC background
ILC DHCAL , M.Chefdeville
1m x 1m plane
With 6 detectors
T2K TPC ,J.Beucher
1.8m x 0.8m plane
With 12 detectors

## Slide 55
But during the early phase of ATLAS NSW R&D we rapidly faced a big problem.
In presence of LHC background the detectors were continuously sparking , compromising seriously the use of this technology in HEP applications .
In close collaboration with Joerg Wotschack we decided to add resistive layers.
It took us 12 iterations to understand how to use resistive layers

## Slide 56: R1-R2-R3-R4-R5-R6-R7
PCB
PCB
PCB
Several resistive values and
Shapes have been tested
Test : apply a voltage above the
breakdown voltage of the gas (Air), with a really high current limitation (10mA)
Resistive layer directly on R/O lines
All detectors died within a sec !
-Vertical resistive layer breakdown
-and massive Mesh melting

## Slide 57: Then R9-R10
PCB
Copper Strip 0.15mm x 100mm
Resistive Strip
1MOhms / cm
Coverlay
65um
Active area 100mm
PCB
Cross section

## Slide 58: Then R9-R10
PCB
Copper Strip 0.15mm x 100mm
Resistive Strip
1MOhms/cm
Coverlay
65um
PCB
For the fist time a structure survived our test for more than 1mn.
We have anyway been able to damage the detectors .
Damages were always near the connection between resistive strip and copper strip.
Cross section

## Slide 59: And finally R11-12
PCB
GND
Addition of an
embedded resistor
15 MOhms 5mm long

## Slide 60: And finally R11-12
PCB
GND
Perfect behavior, sparks were quenched
This helped us to validate our electrical model of the spark mechanism
Addition of an
embedded resistor
15 MOhms 5mm long

## Slide 61: Validation with Neutron irradiation on R11-R12 (protons effect)

## Slide 62: Validation with Neutron irradiation on R11-R12 (protons effect)
Nominal operation voltage

## Slide 63: Validation with Neutron irradiation on R11-R12 (protons effect)
Current peaks due to voltage ramp up
Peak current limited by the power supply
Increasing the current limit increases the peak currents
The real situation is even worse than this plot
Peak current is limited by the detector itself

## Slide 64
PCB + readout strips
50um Kapton + resistive strips
ATLAS NSW prototype production

## Slide 65
PCB + readout strips
50um Kapton + resistive strips
25um solid Glue

## Slide 66
PCB + readout strips
50um Kapton + resistive strips
25um solid Glue
High temp Gluing

## Slide 67
PCB + readout strips
50um Kapton + resistive strips
25um solid Glue
High temp Gluing
Pillars deposit

## Slide 68
PCB + readout strips
50um Kapton + resistive strips
25um solid Glue
High temp Gluing
mesh

## Slide 69
Real ATLAS NSW prototype 1m x 2m
Open
Open
Closed
Closed

## Slide 70
Atlas NSW
Close to 2000 Micromegas detectors produced with sizes up to 2m x 0.5m
PCBs with pillars built at ELTOS (IT) and ELVIA (FR)
Panels construction and detector Assy :
-Dubna
-INFN Frascati
-CEA Saclay
-LMU Munich
MPT participated largely to the R&D and was also involved in the mass production with industry
-Specification
-Companies selection
-Technology transfer

## Slide 71
Unfortunately for other applications, we were really limited with resistive values obtained by screen printing.
So the last evolution is the introduction of
Vacuum deposited resistive DLC layers (Diamond Like Carbon).
This is the result of a large collaboration effort :
We can now access nearly all resistive values
(from kOhms to Gohms per Square) .

## Slide 72
ESS
Kobe
China USTC
Chart: X-Axis
| 5 | 15 | 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95
5 | 532 | 615 | 708 | 554 | 467 | 430 | 360 | 339 | 290 | 293
15 | 526 | 625 | 708 | 559 | 442 | 384 | 348 | 350 | 286 | 270
25 | 525 | 597 | 712 | 556 | 462 | 377 | 342 | 346 | 305 | 270
35 | 520 | 600 | 726 | 512 | 431 | 376 | 327 | 338 | 293 | 278
45 | 546 | 623 | 728 | 570 | 453 | 380 | 349 | 328 | 282 | 267
55 | 537 | 599 | 721 | 532 | 425 | 383 | 360 | 332 | 283 | 296
Chart: X-Axis
| 5 | 15 | 25 | 35 | 45 | 55 | 65 | 75 | 85 | 95
5 | 540 | 593 | 723 | 512 | 430 | 378 | 345 | 329 | 281 | 255
15 | 554 | 599 | 742 | 526 | 419 | 392 | 342 | 333 | 282 | 264
25 | 569 | 593 | 738 | 516 | 432 | 378 | 348 | 354 | 287 | 273
35 | 570 | 625 | 745 | 565 | 445 | 380 | 360 | 340 | 275 | 275
45 | 547 | 615 | 733 | 532 | 460 | 403 | 368 | 370 | 283 | 296
55 | 582 | 642 | 765 | 561 | 472 | 398 | 365 | 334 | 280 | 292
Initial results: example of 1m x 0.6m foils 500Kohms/square +/-60%
The error dropped today to values around +/- 30%

## Slide 73
DLC brought new capabilities:
Possibility to make 2D Micromegas detectors.
Spark protection improvement.
Possibility to make High rate resistive detectors.
Better granularity thanks to the resistive spreading effect.
Removed the need of electronic FE protections.

## Slide 74
High rate resistive Micromegas
1 DLC layer without pattern
2 layers screen printed pads
2 DLC layers without patterns
Medium rate detectors 100kHz/cm2
Side evacuation of the charges
High rate detectors 10Mhz/cm2
Charge evacuation inside active area
Single layer screen printed strips
DLC and screen printed pads
Printed
DLC
Mix
LSBB
50cm x 50cm
X/Y 1mm/1mm
30M/Sqr DLC layer
Silver line evacuation
Best results

## Slide 75: uRwell Result of all the accumulated knowhow

## Slide 76: Initial Micro-well
-3 x 3 cm Micro-well detector
-Ronaldo Bellazzini idea 1997
-Produced at MPT with GEM processes
-Really simple but abandoned due
to the impossibility to mitigate spark damages
Close-up view
Square pattern used
in the early days
R/O lines
Anode
cathode
Cathode
Anode strips
Anode strips

## Slide 77: 15 years later: introduction of a resistive layer to control the sparks thanks to MM experience!
After vacuum gluing
‘Wellized’ with GEM process
Any PCB or flex with any kind of R/O structure
X/Y , UVW , Pads, Capacitive sharing etc..
DLC coated foil
Prepreg

## Slide 78
We have then explored different ways to improve the rate capability
DLC connected with Cu strips on the DLC
DLC connected by plated grooves or holes
High rate uRwell
1 DLC layer
Charge evacuation in the active area
Medium rate µRwell
Lateral evacuation of charges
10cm x 10cm µRwell detector
“STD kit”
2 DLC layers connected by plated holes

## Slide 79
Best compromise between performances & cost  PEP
Wellize
P Pattern top copper
E Etch the kapton
P Plate with copper

## Slide 80: uRwell advantages
Total control of the released energy during a spark.
The control is so good that we can use the sparks to clean the detectors !  We call it “E-cleaning”
The simplest uRwell is flexible  cylindrical detectors are easy to produce.
Low mass , low background
First time we have a detector production process fully compatible with mass production tools from PCB industry.
We are aiming to reach a point were one can buy a uRwell as a STD PCB ( Technology transfer on going )
Lower cost than GEMs or resistive MM

## Slide 81
CLAS12 R&D
2D PEP uRwell
Active area:
150cm x 50cm
PEP examples
Frascati R&D
1D PEP uRwell
Active area:
30cm x 30cm
Frascati R&D
1D PEP uRwell
Active area:
40cm x 5cm
CLAS12 uRwell
rolled in the oven
for E-cleaning

## Slide 82
Future
Vacuum deposition
Subtractive micro-structuring
    Chemical
    Laser
    Reactive Ion Etching Plasma (RIE)
    Directive RIE Plasma (DRIE)
Additive micro-structuring
    3D printing

## Slide 83: Pulsed DC magnetron reactive vacuum deposition machine @CERN
5 targets.
3 simultaneous deposition.
3 gas inputs for reactive deposits:
  H2,N2,02,C2H2,Ar etc..
300 deg in built heater.
In built plasma cleaner
Max foil size:
  -1.7m x 0.7m.
Useful size:
  -1.7m x 0.6m.
Budget:
-25% INFN
-25% CERN EP/DT group
-50% MPT self financing
Market survey  04/21
Invitation to tender  05/21
Purchase order  08/21
Delivery  10/22
Operation  11/22
Fantastic help during from:
  DLC collaboration team
Can deposit
  -metals
  -Dielectrics
  -alloys
  -Carbon structures

## Slide 84: Future Program for our vacuum deposition machine
-Aluminium GEMs
-Low mass detectors
-Continue to explore DLC possibilities
-Improve Uniformity : target  less than +/-5% error (1m x0.6m)
-DLC/Cr/Cu deposition needed for Micromegas high rate detectors and resistive GEM
-Study of strong photocathodes for PICOSEC detectors
-Neutron converter layers deposition like B4C
-Explore other resistive materials like Ge
DLC resistive GEM
Aluminum GEM

## Slide 85: Subtractive micro-structuring with chemistry (Polyimide etching)
Dead Baths in a dedicated hood with scrubber :
-EDA based chemistry
-Ok up to 1000m2 projects
-Strict safety procedures.
Now
Future
Automatic Horizontal etching line :
-10 000m2 projects.
-Still EDA based chemistry
-We are now finalizing the design (quite complex).
-Could be ready for production next year (2024).
-No more individual protective equipment's (IPE)
-Hermetic machine .
-Less handling  Production cost reduction expected

## Slide 86: Laser or plasma subtractive micro-structuring
C02 laser
UV laser
-Many possible base Materials.
-Holes perfectly clean.
-Small patterns
-Limited in size
-Machine cost
-Many possible base Materials.
-Machines can drill both metals and polymers
-Too slow! 200 Holes/sec max
-Limited in size
-Machine cost
-Carbonization
Large punching spot
Thin spiral cut
RIE Plasma
DRIE Plasma
-Modarate machine cost .
-Holes perfectly clean
-Not uniform on large size.
-Etching Isotropy too prononced.
-Perfect cylindrical holes.
-Holes perfectly clean
-Ultra precise patterns
-Sample size : dia 20cm max.
-Machine cost .
Really Interesting
Interesting

## Slide 87: Additive Micro-structuring ink-jet printers

## Slide 88: Many thanks for your attention !