## Slide 1: Manufacturing techniques: Photolithography Chemical etching Plating techniques Gluing techniques Drilling techniques
Tuesday 28 November 11h30
Building 40 - Salle Curie 40/S2-C01

## Slide 2: Production rules
IPC standard define the parameters
to check and set 3 levels of quality
Class 1: Worse level but the PCB
works  general electronic
Products.
Class 2: Industrial products for
which uninterrupted service
is desired but not critical.
Class 3: High reliability
electronics products.
No possibility to exchange boards
during its full life
Ex: lines quality

## Slide 4: Talk outline  4 Layer PCB production steps
Base material
Gluing
Drilling
Plating
External layers
patterning
Photolithography

## Slide 5: Photolithography basics
Photoresist deposition
UV exposure through a mask
Base material with copper
Resist development
Copper Etching
Resist Stripping

## Slide 6: Used for Printed Circuit Boards production
Creation of all the conductive tracks
Protective layers : soldermask & coverlay
Legend ink
Micro via patterning

## Slide 7: Chemical milling and electroforming
Wave guides
Meshes
Heat sinks
Ink jet nozzles
Optical parts
Fuel cell parts
Lead frames
Encoder discs
Flow sensors

## Slide 8: Semiconductor industry
Creation of metal lines for interconnection
Define areas for selective doping
Patterning of protective layers
Micromachining of silicon
  Ink jet printer heads
  Pressure sensors
  Accelerometers
  Magnetic sensors
  Actuators by electroforming magnetic materials

## Slide 9: 4 Layer PCB
Base material

## Slide 10: Substrates
Glass epoxy
  G10 , FR4, High TG, Low loss , low Dk , anti CAF , low CTE etc..
Aramid Epoxy
  Low CTE
Glass polyimide
  G30 ,High temperature , high reliability
Glass Teflon , ceramic Teflon
  High frequencies
  not good for high radiation dose.
Polyimide
  General flex application
Peek
  High reliability flex application
  low moisture absorption
  High frequencies
Bakelite
  Low cost
Example of data sheet

## Slide 11: 4 Layer PCB
Resist deposition

## Slide 12: Photo-imageable materials
Photo-imageable Cover-layer (not sacrificial)
  Protect lines on flexible boards
  Solid or liquid
  Typical thickness 30um
  Aqueous development
Legend inks (not sacrificial)
  Most of the time liquid
  Typical Thickness 20um
  Many colors
Polyimide (usually not sacrificial)
  Make 3D shapes , protect Chips
  liquid
  Thickness ranging from 1 to 30um
Epoxy (usually not sacrificial)
  Make 3D shapes
  SU8 , used in many MEMs
  Thickness ranging from 1 to 100um
Liquid resist
  Thicknesses ranging from 1um up to 5um
  Spin , spray ,deep , screen-printing coatings
  Aqueous or solvent development
  Fine lines , sub micron capabilities
Solid resist
  Thicknesses ranging from 15um up to 100um
  laminated
  Aqueous development
  Minimum line 20um
Solder-mask (not sacrificial)
  Protect external lines on rigid boards
  Solid or liquid
  Typical thickness 30um
  Many colors available

## Slide 14: Resist deposition
-Spinning - semiconductor production
  Thin layers, Highest resolution
-Dip coating - fine lines for PCBs or 3D objects
  Fine lines, large sizes
-Curtain coating - solder mask deposition
  Fast, not accurate, cheap
-Spray - liquid resist, solder mask deposition
  3D best coverage, best quality for solder mask
-Screen printing - solder mask deposition
  Ultra-fast but medium quality
-Dry film lamination- PCB production
  Fast, good resolution

## Slide 15: Spin Coating
Best deposition !
Deposition by centrifugation
Uniform thickness
Ultra-thin :down to 1 μm
Excellent repeatability
Clean room mandatory
Spin
Spin & spray

## Slide 16: Dip Coating
Really simple principle but difficult to tune
with small productions
Thin depositions
Fine patterns
Good for continuous mass production lines
1/vertical dryer
2/base material
3/tank with liquid resist

## Slide 17: Curtain coating
PCB
Liquid resist
PCB
Good for solder-mask deposition
-fast deposition
-thickness not really accurate

## Slide 18
Screen printing
CERN Semi automatic machine 1.5m x 2m
General purpose
CERN precise machine
20cm x20cm deposition
Good for solder-mask deposition
-fast deposition
-thickness not really accurate

## Slide 19: Hot roll lamination
Hot rubber roll
Hot rubber roll
PCB
Solid photoresist roll
Solid photoresist
Best speed Vs quality compromise !
Dry process
Medium class clean room
Large size
Precise thickness
Easy to process
Resolution 30μm line/space
Not compatible with 3D shapes

## Slide 20
Hot roll lamination deposition
Cu/Glass-Epoxy/Cu plate
Or flex
Plate + Photoresist
Resist deposition by Lamination

## Slide 21: 4 Layer PCB
UV exposure
Resist development

## Slide 22: Masks
Glass mask : Glass or Quartz
-Cr on thick soda lime glass
-Direct laser ablation of thin vacuum deposited Chromium
  -Sub-micron resolution possible
  -up to 1m x 0.6m
Polyester mask : 100um thick
  -Minimum line and width around 20um
  -up to 2m x 1.5m
  -Laser exposure of a photosensitive layer on a polyester film
Laser direct imaging : no mask
  -Minimum 15um strips
  -up to 80cm x 60cm
  -resist direct Laser exposure

## Slide 23
UCAM software (GERBER  DPF)
-Corrections for over etch
-DRC
-conversion to Plotter Format : DPF to raster file
start with GERBER file
Or DXF files
Laser photo plotter
Chemical Mask development
Mask
Polyester Mask production

## Slide 24: light diffusion problem
Collimated UV
Diffuse UV
From a neon tube

## Slide 25: light absorption problem
Thin layers ok
Problem with thick layers

## Slide 26: light diffraction problem
Ultra thin patterns
Micrometric range
Diffraction in glass or polyester
Less with quartz

## Slide 27
STD UV exposure
Two UV bulbs
Vacuum Drawer (open)
Sliding in the machine.
Stack up:
-Polyester foil
-Mask  manual alignment
-PCB with resist to pattern
-Glass plate
Deflectors to
Improve collimation

## Slide 28: Collimated UV lamps avoid diffuse light
UV Source alone for multipurpose application
or
Combined with a high precision mechanical
system for alignment: “Mask aligner”
Precise large size lens up to 12 inches
The lens quality is the base of this system

## Slide 29: LDI: laser Direct Imaging
LDI
Increasing local energy can beat the 3 problems
But with thick resist the absorption remains .
Precision: 0.5 μm to 2 μm
(depending on laser type)

## Slide 30: Electron beam exposure beats all the problems
Current dedicated systems have produced line widths of 10 nm or smaller
The primary advantage of electron beam lithography is that it is one way to beat the diffraction limit and make features in the nanometer regime
Angle due to Electron scattering in resist

## Slide 31: Advanced image transfer with X-ray exposure
LIGA technology uses X-ray lithography to obtain polymer structures with extremely high aspect ratios (lateral precision bellow 1μm in a 0.1 to 2mm thick polymer).
LIGA is a German acronym in English Lithography, Electroplating, and Molding.
Because of the high collimation of X-rays needed, the source must be synchrotron light.
This technology is the base for many MEMS,
It beats the limitation of light absorption in the photoresist.

## Slide 32: Cheaper way to avoid light absorption problem
Resist lamination
+ UV exposure
Second Resist lamination
+ second UV exposure
After development
That’s how we produce
Thick pillars for Micromegas

## Slide 33
After exposure Wet development
After Exposure
Development with NA2CO3
After Development

## Slide 34: 4 Layer PCB
Etching
Resist stripping

## Slide 35
Wet spray horizontal etching
Some examples of chemistries:
-Ferric Perchloride for Copper/SS/Aluminium
-Phosphoric/sulphuric/Fluoridric acid for Niobium
-Fluoridric acid for Titanium
-Potassium Ferrocyanide for Tungsten
-Iode/Iodine for Gold
-Iron nitrate for Silver etc.. etc..
After Etching
Resist Image
Wet spray Etching

## Slide 36: Anisotropic , Isotropic wet etching
Some exceptions
  Silicon etching is anisotropic due to its crystalline structure
  Polyimide etching can also be anisotropic
Anisotropic etching
Big limitation with thick layers
Minimum opening 3 to 4 time the thickness
Most metals can be wet etched
The etching is isotropic for nearly all of them
Most of the dielectrics are difficult to wet etch

## Slide 37
Polyimide wet etching , isotropic and anisotropic
First type of polyimide:
Perfect anisotropic etching
No under etch
Perfect to make small holes
Second type of polyimide:
Fully isotropic etching
Not satisfactory
Les than 10% of PIs available on the market are OK
OK
OK
bad
bad

## Slide 38: Laser etching
-Laser direct metal patterning is not yet used to make lines in PCBs.
-With thick layers ( above a few um), the speed /quality ratio is much worse than chemical etching.
-Powerful and fast laser ablation produces poor quality lines
-And to get good quality lines the throughput is too slow
-But laser is nice for repairs .
Full of shorts
Cleaned up
It looks simple but the process is complex

## Slide 39: Electroforming to beat wet etching isotropy
Thick resist
Electro plating
Resist stripping
Seed layer removal

## Slide 40
After wet etching  resist Stripping
After copper Etching
Stripping with:
NAOH
KOH
Solvents
After stripping

## Slide 41: After stripping  Automatic Optical inspection (AOI)
Compare the scanned image with the design file
Minimum track or space 20um
Minimum detectable defect around 5 um ( pixel 2.5um)
Cannot detect hole plating defect
Short circuit
Open
Bonding pad

## Slide 42: At the end Electrical test
Flying probe
2 in front 2 in bottom
AOI
Control netlist integrity
Including PTH this time

## Slide 43
Gluing

## Slide 44: First step prepare the metals
Some metals can be nearly directly glued:
- Aluminum , Titanium
Some need to be micro-structurized
- Copper and alloys
Other need to be chemically treated
- Ni, stainless steel
All of them need to be degassed
1/Detergent Cleaner
2/Pre-conditioning
3/Micro structurizing Chemistry
4/DI water Rinse
5/Dry

## Slide 45: Gluing Equipment
Isostatic press
Vacuum chamber
5 Heating plates
Mechanical Hydraulic pressure (40 Bars)
Plate size 600mm x 700mm
Presses with plates above 1m is exceptional
Short cycles
usually only used for flat plates
Autoclave
The parts to glue are in a vacuum bag
Pressure coming from compressed air (10 Bars)
STD size 2m x 1m
Machine with a length of 20m are existing
Long cycles
3D objects

## Slide 46: Glue
Liquid
  Rarely used
  Difficult to apply , difficult to clean , thicknesses not accurate
Prepregs
  Wowen glass impregnated with a bi-stage polymer glue (um precision thickness)
Cast
  Thin layer glue (solid) on a carrier (um precision thickness)
Cover-layer
  Polyimide layer with a thin layer of glue on one side
Bond-ply
  Polyimide foil with glue on both sides
Pressure sensitive adhesive
  Thin layer of adhesive on a carrier

## Slide 47: Gluing principle
Pressure (30 kg/cm2)
Thick Stainless steel
Stack under vacuum
Heat all the stack
PCB
PCB
glue
Metallic guiding pins
Thick Stainless steel

## Slide 48: Gluing principle
Pressure (30 kg/cm2)
Thick Stainless steel
Stack under vacuum
Heat all the stack
PCB
PCB
glue
Metallic guiding pins
Thick Stainless steel
Problem :
Flatness of the SS plates , press , PCB
Thickness uniformity of Prepreg , Glues
Thickness variation on a patterned PCB

## Slide 49: Release and conformal layers
Pacothane
  release sheet
Pacolon
  High temperature release sheet
Pacopads
  Melting with temperature  Planarity corrections up to 200um
PacoFlex
  Encapsulate strips , the coverlayer will follow the strips shape
Pacovia
  Melting and hermetic avoid glue coming out from buried holes
Pacotherm
  Large Planarity corrections up to 1mm
Typical Rigid PCB stack

## Slide 50: Others configuration
Typical Flex stack
Configuration to avoid glue bleeding

## Slide 51: Autoclave configuration
stack
Conformal
Foam

## Slide 52: Curing cycle
Cast
PrePreg

## Slide 53
Drilling

## Slide 54: Different type of holes
8 layers staggered vias
8 layers stacked vias

## Slide 55: Mechanical drilling
Xray Camera
Optical camera
Tool store
Spindle
0.15 mm tool minimum
Some machines can go below 100um
180 000 RPM
1.4m x 0.6m drilling area
Max rate 3H/s
Industry : 10 H/s

## Slide 56: Mechanical Milling
Tool store
Spindle
80 000 RPM
0.3mm min tool

## Slide 57: Chemical drilling  GEM
Base material : Polyimide 50um + 5um on both sides
Same base material
Hole patterning in Cu
Polyimide etch
Bottom electro etch
Second Polyimide Etch
Limited to 40cm x 40cm due to:
  The 2 masks alignment precision
  And Glass mask cost
30um hole minimum
Limited to 2m x 60cm due to:
  Base material
  Equipment
30um holes minimum
Double mask
Single mask

## Slide 58: Laser or plasma drilling
C02 laser
UV laser
-Many possible base Materials.
-Holes perfectly clean.
-Small patterns
-30um holes
-Not competitive with Wet drilling
-Many possible base Materials.
-Machines can drill both metals and polymers
-20um holes
-Not yet competitive with Wet drilling
Punching
Thin spiral cut
RIE Plasma
DRIE Plasma
-Moderate machine cost .
-Holes perfectly clean
-50um holes
-Not uniform on large size.
-Isotropic Etching
-Perfect cylindrical holes.
-Holes perfectly clean
-Ultra precise patterns
-20um holes
-limitation on size : dia 20cm max.

## Slide 59
Sand blast drilling
Anisotropic etching
Can treat nearly all materials
Smooth walls
Millimetric scale patterns

## Slide 60
Plating

## Slide 61
Plating
Electro-plating
Electroless plating
Vacuum plating
Screen printing

## Slide 62: Dielectric treatment before Electro-plating
1/Deasmear
  Remove the dust in holes
  Remove material burnt by drilling
  Come back to fresh dielectric
2/Deposit conductive material on dielectric:
  Nano Carbon deposition
  Or organic Palladium
Deasmear line:
Sweller
+ Potassium permanganate
Carbon line:
Detergent
Carbon full covering
Micro-etch to remove Carbon on Copper

## Slide 63: Electro plating
CU
NI
Au
Anode
Cathode
Filter/pump
Basket with copper balls
Solid piece
Copper plating Bath
2m x 0.6m panels

## Slide 64: Horizontal Ni or Cu or Ni/Cu line continuous deposition
Ni Bath
horizontal
Cascade Rince
spray
Cu Bath
Horizontal
Cascade Rince
spray
Dry  Blower
Passivation Spray
Rince  Spray

## Slide 65: Electro-less plating
Protect copper from oxidation
- Guaranty an easy soldering
- Allow Aluminum or Gold wire Bonding
ENIG : Electroless nickel (5um) , Immersion Gold (0.07um)
ENEPIG: Electroless nickel , electroless Palladium , Immersion Gold
Ag: Chemical silver less than 1um
Tin: Chemical Tin
Immersion Au
Electroless Ni

## Slide 66
70cm copper target
Drum unloading
after processing
Pulsed DC Magnetron vacuum
deposition machine
Vacuum plating

## Slide 67
Deposited Materials.
  Metals : Cu , Al ,Cr
  Resistive materials DLC, Si
  Converters B4C
Possibility to co-deposit 3 materials.
Possibility to sequentially deposit 3 materials.
Built in heater.
RF plasma cleaning.
3 gas inputs for reactive sputtering.
Can treat flex or rigid substrates.
Possibilities
Inner trackers
  Low mass flexes, Al conductors.
  Solid-state detectors embedded in flex.
MPGD
  Resistive protection layers.
  Layers for neutron detection.
  Photoelectric layers
Applications

## Slide 68: Thin film deposition Lift Off

## Slide 69: Thick Film Printing
High density
High Thermal Conductivity
Low Vacuum compatible
Conductive Layers: noble metals
Dielectrics : Ceramic
Sequential deposits by screen printing
Followed with 850 Celsius curing

## Slide 70: Resistive materials deposition
Full layer deposition
Pattern DLC with :
-sand blasting
-lift Off
50um Kapton
Direct screen printing
with resistive paste
ATLAS
NSW

## Slide 71
End of production
or back to the beginning

## Slide 72: Examples

## Slide 73: Interconnection technologies names
Screen printed circuits
PCB
Thick film
HDI circuits
MCM/C (ceramic)
Thin film
MCM/D (deposited)
Nominal line and space
200um
120um
100um
75um
50um
25um
20um
Technologies names
In green available at CERN
Cabling
Integrated
chips

## Slide 74
Inner Trackers  Low Mass Aluminium circuits
ATLAS IBL Low Mass 8 layers
ALICE inner tracker BUS (5 Aluminum layers)
Double-sided flex for ILC Vertex sensor
ALICE inner tracker

## Slide 75
Multi layer coils :
-1.5m long
-up to 40 layers
-30um maximum registration error
-Line and space down to 50um/50um
Magnets calibration  ultra precise field sensors
-Printed Coils are 10 time more accurate than
wounded structures

## Slide 76: LHC machine protection
Stainless steel or SS/Cu mix Quench Heaters
Long flexes up to 15m x 0.6m
Niobium Titanium supraconductor quench detector.
Others:
-Heating foils
-High power resistors
-Optical targets for UHV
-etc..

## Slide 77: HDI for ATLAS pixel detectors
Size in the range of 8cm x 2cm
Silicon pixel detector below
Output bus
control chip
bonding

## Slide 78: HDI CMS strip detectors
Size in the range of 10cm x 20cm
Front end Asics
Rigid flex
Glass pitch adaptor
Silicon strip detector

## Slide 79: PCB for CMS Pre-shower

## Slide 80: Full Aluminium flex with embedded silicon detector (R&D)
Top
bottom
Thinned chip 50um
100um thick end device
Full aluminium
No bonding

## Slide 81
CMS GEM with single Mask
CMS nose
GE1/1 Muon detector
Triple GEM stack
Single mask GEM
Microscopic view
Cross section
CMS experiment
GE1/1  400 GEM (1.3m x 0.5m) made at CERN
GE2/1 1000 GEM (1.3m x 0.5m) CERN/Korea
GEM producers' capabilities:
-CERN MPT : 500m2/year
-Mecaro Korea : 250m2/year

## Slide 82: And many more
KLOE – Cylindrical Detector
ALICE TPC  700 GEM
Future CMS ME0  1000 GEMs
-BM@N in Dubna (1.6m x 0.5m)
-SBS tracker Jefferson lab
-CBM at Fair
-BESIII China
-SOLID
-BONUS 12
-P-RAD
-S-Phenix TPC
-COMPASS upgrade
-GEM for nuclear physics TPCs
-ESS for neutron detectors
-and lot of small GEMs for academic purpose
Other detectors with GEM single mask technique

## Slide 83: BULK and Floating mesh Micromegas detectors
BULK Micromegas
Floating mesh Micromegas

## Slide 84
BULK Micromegas detectors
ILC DHCAL , M.Chefdeville
1m x 1m plane
With 6 detectors
T2K TPC ,J.Beucher
1.8m x 0.8m plane
With 12 detectors
CLAS 12
Cylindrical Micromegas bulk
Thin substrate
33 sectors , 12cm diameter detector
2.5mm dead space for sectorizing
1mm hole for HV connection
Early ATLAS NSW R&D
Joerg Wotschack
1.5m x 0.5m plane
Single panel

## Slide 85
PCB + readout strips
50um Kapton + resistive strips
25um solid Glue
High temp Gluing
Pillars creation
mesh
Introduction of a resistive layer in floating MM

## Slide 86
Atlas NSW
Close to 2000 Micromegas detectors produced with modules sizes up to 2m x 0.5m
PCBs with pillars built at ELTOS (IT) and ELVIA (FR)
Panels construction and detector Assy :
-Dubna
-INFN Frascati
-CEA Saclay
-LMU Munich
MPT participated to the R&D and was also involved in the mass production with industry
-Specification
-Companies selection
-Technology transfer

## Slide 87
All Resistive MM structures
1 full DLC layer
2 layers with screen printed pads
2 DLC layers without patterns
Medium-rate detectors 100kHz/cm2
Side evacuation of the charges
High-rate detectors 10Mhz/cm2
Charge evacuation inside active area
Screen printed resistive strips (ATLAS NSW)
or
or
2013
2015
2020
2015

## Slide 88: uRwell detectors
After vacuum gluing
Kapton etching with GEM process
Any PCB or flex with any kind of R/O structure
X/Y , UVW , Pads, Capacitive sharing etc..
Polyimide coated foil: copper top , DLC bottom
Prepreg

## Slide 89
DLC connected by plated grooves or holes
High rate uRwell
1 DLC layer
Charge evacuation in the active area
Medium rate µRwell
Lateral evacuation of charges
10cm x 10cm µRwell detector
“STD kit”
2 DLC layers connected by plated holes
Evacuation line

## Slide 90
CLAS12 R&D
2D PEP uRwell
Active area:
150cm x 50cm
uRwell examples
Frascati R&D
1D PEP uRwell
Active area:
30cm x 30cm
Frascati R&D
1D PEP uRwell
Active area:
40cm x 5cm
CLAS12 uRwell
rolled in an oven
for E-cleaning

## Slide 91: Thank you for your attention