## Slide 1
Mechanical Analysis of HTS Forced-Flow Cooled Cable for the Target Solenoid
J. Lorenzo, A. Portone, P. Testoni (F4E Barcelona)
In collaboration with C. Accettura, L. Bottura, A. Kolehmainen (CERN)
01/06/2023

## Slide 2
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 3
Introduction: HTS-based Target Solenoid
Coil | Rc [m] | Zc [m] | DR [m] | DZ [m] | NR | NZ | I [A] | It [MAt]
1 | 0.849 | -0.185 | 0.498 | 0.830 | 12 | 20 | 58905 | 14.137
2 | 0.870 | 0.665 | 0.540 | 0.830 | 13 | 20 | 60710 | 15.785
3 | 0.870 | 1.515 | 0.540 | 0.830 | 13 | 20 | 60392 | 15.702
4 | 0.808 | 2.365 | 0.415 | 0.830 | 10 | 20 | 51654 | 10.331
5 | 0.766 | 3.215 | 0.332 | 0.830 | 8 | 20 | 47469 | 7.595
6 | 0.704 | 4.065 | 0.208 | 0.830 | 5 | 20 | 46504 | 4.650
7 | 0.745 | 4.708 | 0.291 | 0.415 | 7 | 10 | 46293 | 3.240
8 | 0.704 | 5.423 | 0.208 | 0.415 | 5 | 10 | 53168 | 2.658
9 | 0.662 | 6.065 | 0.125 | 0.830 | 3 | 20 | 43280 | 2.597
10 | 0.662 | 6.915 | 0.125 | 0.830 | 3 | 20 | 42146 | 2.529
11 | 0.642 | 7.765 | 0.083 | 0.830 | 2 | 20 | 49452 | 1.978
12 | 0.642 | 8.615 | 0.083 | 0.830 | 2 | 20 | 44183 | 1.767
13 | 0.642 | 9.465 | 0.083 | 0.830 | 2 | 20 | 39567 | 1.583
14 | 0.642 | 10.315 | 0.083 | 0.830 | 2 | 20 | 32713 | 1.309
15 | 0.642 | 10.958 | 0.083 | 0.415 | 2 | 10 | 46717 | 0.934
16 | 0.642 | 11.673 | 0.083 | 0.415 | 2 | 10 | 45905 | 0.918
17 | 0.621 | 12.315 | 0.042 | 0.830 | 1 | 20 | 52310 | 1.046
18 | 0.621 | 13.165 | 0.042 | 0.830 | 1 | 20 | 56056 | 1.121
19 | 0.621 | 14.015 | 0.042 | 0.830 | 1 | 20 | 51602 | 1.032
20 | 0.621 | 14.865 | 0.042 | 0.830 | 1 | 20 | 51376 | 1.028
21 | 0.621 | 15.715 | 0.042 | 0.830 | 1 | 20 | 50471 | 1.009
22 | 0.621 | 16.565 | 0.042 | 0.830 | 1 | 20 | 52861 | 1.057
23 | 0.621 | 17.415 | 0.042 | 0.830 | 1 | 20 | 57438 | 1.149
Scope
Mechanical assessment of the proposed HTS design for the Target Solenoid following the Structural Design Criteria for ITER Magnets (ITER MSDC).
Bi = 20 T, Bf = 1.5 T, Lt = 15 m, -1 m < z < 15 m
Coil 1
Coil 23
Reference field (H. K. Sayed and J. S. Berg, 2014):

## Slide 4
Conductor features
  Diameter of central cooling channel = 8 mm.
  Cable diameter = 23.5 mm.
  Square steel jacket 39.5 mm x 39.5 mm (minimum thickness of 8 mm).
  1 mm thick turn insulation.
Cable features (parametric studies, 50 tapes/stack)
  Bonded/frictional stack-former contact.
  3/4/6/8 stacks of HTS tapes.
  3/4/6 mm wide HTS tapes.
HTS tape features (90 um thickness)
  44 um thick Hastelloy.
  20 um thick copper layers (x2).
  2 um thick silver layers (x2).
  1.6 um REBCO layer.
  0.4 um buffer layer.
Introduction: Conductor
Cooling Channel
Cable
Jacket
Turn Insulation
Void Filler
Copper Former
Steel Wrap
HTS Stack
Solder

## Slide 5
Introduction: Material Properties
 | Steel | Copper | Insulation | Filler | WP (smeared) | Solder | HTS Tape (smeared)
Ex [GPa] | 205 | 110 | 12 | 7 | 112 | 10 | 100
Ey [GPa] | 205 | 110 | 20 | 7 | 112 | 10 | 121
Ez [GPa] | 205 | 110 | 20 | 7 | 160 | 10 | 132
νxy [] | 0.29 | 0.33 | 0.33 | 0.3 | 0.25 | 0.33 | 0.25
νxz [] | 0.29 | 0.33 | 0.33 | 0.3 | 0.21 | 0.33 | 0.24
νyz [] | 0.29 | 0.33 | 0.17 | 0.3 | 0.21 | 0.33 | 0.30
Gxy [GPa] | 79 | 41 | 6 | 3 | 31 | 4 | 37
Gxz [GPa] | 79 | 41 | 6 | 3 | 42 | 4 | 46
Gyz [GPa] | 79 | 41 | 6 | 3 | 42 | 4 | 43
P. GAO, et al. Superconductor Science and Technology, 2020, vol. 33, no 4, p. 044015.
Properties of HTS tape obtained from smearing of isotropic properties of individual components at 77 K.

## Slide 6
Introduction: Loads
Coil | Rc [m] | Zc [m] | DR [m] | DZ [m] | NR | NZ | I [A] | It [MAt] | Fz [MN] | Fz [MN]
1 | 0.849 | -0.185 | 0.498 | 0.830 | 12 | 20 | 58905 | 14.137 | 251.2 | 251.2
2 | 0.870 | 0.665 | 0.540 | 0.830 | 13 | 20 | 60710 | 15.785 | 59.50 | 59.51
3 | 0.870 | 1.515 | 0.540 | 0.830 | 13 | 20 | 60392 | 15.702 | -101.0 | -101.0
4 | 0.808 | 2.365 | 0.415 | 0.830 | 10 | 20 | 51654 | 10.331 | -101.4 | -101.4
5 | 0.766 | 3.215 | 0.332 | 0.830 | 8 | 20 | 47469 | 7.595 | -58.48 | -58.48
6 | 0.704 | 4.065 | 0.208 | 0.830 | 5 | 20 | 46504 | 4.650 | -17.10 | -17.10
7 | 0.745 | 4.708 | 0.291 | 0.415 | 7 | 10 | 46293 | 3.240 | -16.60 | -16.60
8 | 0.704 | 5.423 | 0.208 | 0.415 | 5 | 10 | 53168 | 2.658 | -2.179 | -2.177
9 | 0.662 | 6.065 | 0.125 | 0.830 | 3 | 20 | 43280 | 2.597 | -5.691 | -5.69
10 | 0.662 | 6.915 | 0.125 | 0.830 | 3 | 20 | 42146 | 2.529 | -2.609 | -2.608
11 | 0.642 | 7.765 | 0.083 | 0.830 | 2 | 20 | 49452 | 1.978 | -1.687 | -1.686
12 | 0.642 | 8.615 | 0.083 | 0.830 | 2 | 20 | 44183 | 1.767 | -0.9150 | -0.9147
13 | 0.642 | 9.465 | 0.083 | 0.830 | 2 | 20 | 39567 | 1.583 | -0.7432 | -0.7428
14 | 0.642 | 10.315 | 0.083 | 0.830 | 2 | 20 | 32713 | 1.309 | -0.1610 | -0.1603
15 | 0.642 | 10.958 | 0.083 | 0.415 | 2 | 10 | 46717 | 0.934 | -0.8960 | -0.8958
16 | 0.642 | 11.673 | 0.083 | 0.415 | 2 | 10 | 45905 | 0.918 | 0.3742 | 0.3754
17 | 0.621 | 12.315 | 0.042 | 0.830 | 1 | 20 | 52310 | 1.046 | -0.3951 | -0.3941
18 | 0.621 | 13.165 | 0.042 | 0.830 | 1 | 20 | 56056 | 1.121 | -0.0839 | -0.08169
19 | 0.621 | 14.015 | 0.042 | 0.830 | 1 | 20 | 51602 | 1.032 | -0.0973 | -0.09354
20 | 0.621 | 14.865 | 0.042 | 0.830 | 1 | 20 | 51376 | 1.028 | -0.0427 | -0.03481
21 | 0.621 | 15.715 | 0.042 | 0.830 | 1 | 20 | 50471 | 1.009 | -0.0091 | 0.01137
22 | 0.621 | 16.565 | 0.042 | 0.830 | 1 | 20 | 52861 | 1.057 | -0.0188 | 0.06418
23 | 0.621 | 17.415 | 0.042 | 0.830 | 1 | 20 | 57438 | 1.149 | -0.9872 | -0.3138
No pre-compression needed to keep the coils together.
Gravity load is not considered.
Cool-down is not considered.
Only Lorentz forces applied.
No cyclic loading considered (fatigue).
Net Vertical Forces
(without chicane coils)
Net Vertical Forces
(with chicane coils)
Chart: Coil
| C1 | C2 | C3 | C4 | C5 | C6 | C7 | C8 | C9 | C10 | C11 | C12 | C13 | C14 | C15 | C16 | C17 | C18 | C19 | C20 | C21 | C22 | C23
w/ chicane | 251.2 | 59.51 | -101 | -101.4 | -58.48 | -17.1 | -16.6 | -2.177 | -5.69 | -2.608 | -1.686 | -0.9147 | -0.7428 | -0.1603 | -0.8958 | 0.3754 | -0.3941 | -0.08169 | -0.09354 | -0.03481 | 0.01137 | 0.06418 | -0.3138
w/o chicane | 251.2 | 59.51 | -101 | -101.4 | -58.48 | -17.1 | -16.6 | -2.178 | -5.691 | -2.608 | -1.687 | -0.9152 | -0.7434 | -0.1609 | -0.8964 | 0.3746 | -0.3954 | -0.08392 | -0.09731 | -0.04272 | -0.00908 | -0.01877 | -0.9872

## Slide 7
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 8
Analysis Strategy: Overview
2-D Axis. Global Electromagnetic Model
2-D Axis. Local Electromagnetic Model I
2-D Axis. Local Electromagnetic Model II
2-D Axis. Global Mechanical Model
2-D Axis. Local Mechanical Model I
2-D Axis. Local Mechanical Model II
3-D Homogenization Model
Nodal EM forces
Boundary conditions (Az)
Boundary conditions (Az)
Nodal EM forces
Nodal EM forces
Boundary conditions (ur, uz)
Boundary conditions (ur, uz)
Assessment Jacket and Turn Insulation
(ITER Magnet Structural Design Criteria)
Assessment HTS Tapes
(Tensile and shear stresses)
WP mechanical properties
(Ex, Ey, Ez, νxy, νxz, νyz, Gxy, Gxz, Gyz)
Fully parametric model automatized with ANSYS Parametric Design Language (APDL).
3-D Homogenization Model
Tape mechanical properties
(Ex, Ey, Ez, νxy, νxz, νyz, Gxy, Gxz, Gyz)
Magnetic Models
Mechanical Models

## Slide 9
Analysis Strategy: Global Models
Magnetic Field [T]
Displacement [m]
Homogenized WP.
Frictional contact between coils.
No pre-compression force applied.
Boundary Condition: uy = 0
Peak field in coils 2/3.
Smeared Properties
The global stiffness of the WP is modelled by means of a homogenized orthotropic material.
Nodal EM forces
Most loaded coil for detailed analysis
Global displacements

## Slide 10
Analysis Strategy: Local Models I
Magnetic Field [T] in Coil 2 cables
Tresca Stress [Pa] in Coil 2 jackets
Nodal EM forces
Frictional contact between cable and jacket
Fine distribution of magnetic field
Stresses in jackets and insulation

## Slide 11
a) Hoop Stress
b) Axial Stress [Pa]
Analysis Strategy: Local Models I

## Slide 12
Analysis Strategy: Local Models II
Magnetic Field [T] in tapes
Compressive/Tensile Stress [Pa] in tapes
Nodal EM forces
Shear Stress [Pa] in tapes

## Slide 13
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 14
Stresses in HTS Tapes
Stress components of interest in the HTS tapes (de-bonding, degradation):
  Tensile stress across HTS tapes.
  Shear stress in HTS tapes.
The tapes are modelled as relatively stiff components (~100 GPa) due to the large amount of hastelloy and copper.
The surrounding solder is modelled as a rather soft material (~10 GPa) due to the mix of Sn and Pb.
Parametric Analyses:
  Bonded/frictional stack.
  Number of stacks (3, 4, 6, 8).
  Width of stacks (3 mm, 4 mm, 6 mm).
SuperPower

## Slide 15
Bonded/Frictional Stack
Stack bonded to copper former.
Stack allowed to separate and slide in the copper former (μ = 0.2).
Tensile Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Shear Stress [Pa]
bonded stack
bonded stack
frictional contact
frictional contact
Contact Pressure [Pa]
~40 MPa
~30 MPa
Smaller tensile stress area with lower peak.
Lower shear stress in general.

## Slide 16
Stack Number (6 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
~30 MPa
~30 MPa
~30 MPa
Larger tensile stress area.
81 mm2
108 mm2
162 mm2

## Slide 17
Stack Number (4 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
~30 MPa
~30 MPa
~30 MPa
Larger tensile stress area.
72 mm2
108 mm2
144 mm2

## Slide 18
Stack Number (6 mm wide tape, frictional contact)
Shear Stress [Pa]
Contact Pressure [Pa]
Shear Stress [Pa]
Contact Pressure [Pa]
Shear Stress [Pa]
Contact Pressure[Pa]

## Slide 19
Stack Width (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Increased peak compressive stress.
Increased peak shear stress.
108 mm2
72 mm2
54 mm2

## Slide 20
Stack Width (6 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
Increased peak compressive stress.
Increased peak shear stress.
162 mm2
108 mm2
81 mm2

## Slide 21
Tape Thickness (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
108 mm2
108 mm2
50 tapes
thickness = 90 um
75 tapes
thickness = 60 um

## Slide 22
Solder Stiffness (4 stacks, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]
108 mm2
108 mm2
Esolder = 10 GPa
Esolder = 20 GPa
Larger tensile stress area.
Increased shear stress.
~30 MPa
~40 MPa

## Slide 23
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 24
Conclusions
A magneto-structural analysis of the Target Solenoid is presented, involving several nested global and local axisymmetric models with different level of detail. The analysis is fully parametric and automatized in APDL.
On the one hand, the conductor jacket and turn insulation are assessed according to the ITER Magnet Structural Design Criteria (backup slides).
On the other hand, the tensile and shear stress distributions in the stacks of tapes are analyzed. Parametric studies are carried out to understand the impact of bonded/frictional stacks, number of stacks, width of stacks, etc.
Stack allowed to slide and separate in the former grooves results in lower tensile and shear stresses. Tensile stresses in the tapes are generally below 10 MPa, shear stresses around 30 MPa.
If the stack is bonded to the groove shear stress regions up to 45 MPa. Softer solder yields lower shear stress.
Fewer stacks reduce the regions with tensile stresses.
Wider stacks result in lower peak compressive and shear stresses.
Fewer and wider stacks approach is deemed preferable from the parametric analyses.

## Slide 25
THANK YOU

## Slide 26
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 27
Stack Number (6 mm wide tape, frictional contact)
Tensile Stress [Pa]
Shear Stress [Pa]
Tensile Stress [Pa]
Shear Stress [Pa]

## Slide 28
Introduction
Analysis Strategy
Stresses in HTS Tapes
Conclusions
Structural Design Criteria & Assessment (backup)
Outline

## Slide 29
Structural Design Criteria & Assessment
ITER Magnet Structural Design Criteria:
  Part 1: Main Structural Components and Welds.
  Part 2: Magnet Windings (Radial Plates and Conductors) with High and Low Voltage Insulation and Epoxy Filler.
  Part 3: Bolts, Keys, Supports and Special Components.
  Part 4: Cryogenic Piping.
Jackets
Turn insulation
Only static stress limits are considered.
Relevance of fatigue stress to be discussed (cyclic loading?).

## Slide 30
Structural Design Criteria & Assessment: Stress Linearization
= membrane stress tensor (constant part).
= bending stress tensor (linear part).
Once membrane and bending stress tensors are known, von Mises/Tresca stresses can be computed as usual.
Von Mises/Tresca stresses do not vary linearly along the defined paths.
Source: ANSYS Theory Reference

## Slide 31
Structural Design Criteria & Assessment: Stress Classification
Primary Stress, P
  Stress developed by imposed loading.
  Necessary to satisfy laws of equilibrium.
  Not self-limiting.
  Result in failure/gross distortion if considerably exceeds yield strength.
  Thermal stress is not primary.
Secondary Stress, Q
  Stress developed by constrain of adjacent material or by self-constraint of the structure.
  Self-limiting.
  Thermal stress.
Rule of thumb:
  Thermal stresses are classified as secondary.
  Stresses induced by EM loads, inertial/gravity loads, pressure loads, etc., are classified as primary.

## Slide 32
Structural Design Criteria & Assessment: Metallic Components
ITER MSDC Part 2 for Metallic Components:
  Allowable stress:
  Primary membrane stress:
  Primary membrane + bending stress:
  Primary + secondary stress
depends on type of service conditions:

## Slide 33
Structural Design Criteria & Assessment: Metallic Components
ITER MSDC Part 2:
  Allowable stress:
  Primary membrane stress:
  Primary membrane + bending stress:
  Primary + secondary stress (not considered, no thermal load applied).
PATH

## Slide 34
Structural Design Criteria & Assessment: Metallic Components
Copper former is not intended to be a structural component in the cable but it reacts the magnetic load due to its relatively high stiffness (110 GPa vs. 205 GPa of steel).
The yield strength of copper is rather low compared to that of steel (factor ~3)), at least at room temperature (strength at cryogenic temperature needs to be investigated).
Frictional stacks
Frictional stacks
Bonded stacks

## Slide 35
Structural Design Criteria & Assessment: Non-Metallic Components
ITER MSDC Part 2 for High-Voltage Insulation:
  Allowable compressive stress normal to the reinforcing plane. The compressive static stress in the through-thickness direction of the insulating material is limited to 50% of the minimum ultimate compressive strength:
  Allowable tensile strain normal to reinforcing plane. No primary tensile strain is allowed in the direction normal to the adhesive bonds between metal and composite.
  Allowable shear stress. The allowable shear strength of an insulator depends on the applied compressive stress.
  Allowable strain in plane of reinforcing. The allowed tensile or compressive strain in the plane of the insulation material is in the range [-0.5%, 0.5%].

## Slide 36
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable compressive stress normal to the reinforcing plane.

## Slide 37
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable tensile strain normal to reinforcing plane.
Small spots in the corner regions show normal tensile strain likely due to the fact that bonded insulation layers are assumed, and no separation is allowed.

## Slide 38
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable shear stress.
A usage factor is defined as the ratio between element shear stress and allowable shear stress, which must be less than 1. Negative values correspond to tensile stresses that should be avoided, but these are likely due to the modelling of contact between adjacent insulating layers.

## Slide 39
Structural Design Criteria & Assessment: Non-Metallic Components
  Allowable strain in plane of reinforcing.