## Slide 1: Status of interaction region magnets (WP3) with focus on MQXF
E. Todesco, on behalf of HL-LHC WP3
KEK, Tsukuba, 13 January 2023

## Slide 2: List of contributors (from East to West)
KEK: T. Nakamoto, M. Sugano, K. Suzuki, N. Kimura et al.
IHEP: Q. Xu, Y. Wang, D. Ni, W. Wu, L. Li, Q. Peng, et al.
FREIA: K. Pepitone, R. Ruber, et al.
INFN-LASA: M. Statera, M. Sorbi, M. Prioli, S. Mariotto, et al.
INFN-Genova: P. Fabbricatore, S. Farinon, B. Caiffi, A. Bersani, R. Cereseto, et al.
CERN: S. Izquierdo Bermudez, E. Gautheron, G. Kirby, A. Foussat, J. Carlos Perez, F. Rodriguez Mateos, N- Lusa, E. Ravaioli, M. Bednarek, J. Ferradas Troitino, F. Mangiarotti, M. Bajko, A. Devred, H. Felice, D. Perini, G. Willering, S. Ferradas Troitino, H. Prin, A. Milanese, J. Ferradas Troitino, E. Takala, R. Principe, A. Ballarino, D. Tommasini, B. Bordini, J. Fleiter, C. Barth, S. Hopkins, F. Savary, D. Duarte Ramos, Y. Leclercq, M. Struik, L. Fiscarelli, S. Russenschuck, C. Petrone, G. de Rijk, L. Rossi, P. Fessia, S. Riebe, H. Garcia Gavela, L. Carlos, S. Fleury, G. Vandoni, L. Quain Solis, A. Dallocchio, P. Moyret, S. Sgobba, A. Moros, M. Crouvizier, B. Bulat, M. Guinchard and its team, et al.
CEA: H. Felice, D. Simon, et al.,
CIEMAT: F. Toral, C. Martins Jardim, J. Garcia Matos, et al.
AUP: G. Ambrosio, S. Feher, R. Carcagno, G. Apollinari, B. Ahia, P. Joshi, K. Amm, M. Yu, A. Nobrega, J. Schmalzle, M. Anarella, A Vouris, G. Chlachidze, S. Stoynev, R. Bossert, M. Baldini, P. Ferracin, D. Cheng, S. Prestemon, G. L. Sabbi, L. Cooley, V. Lombardo et al.,
In red: management at CERN and in collaborations

## Slide 3: CONTENTS
A short review of the interaction region magnets in the HL-LHC project
The short model program of MQXF
The US contribution (MQXFA)
The CERN contribution (MQXFB)

## Slide 4: Back to the 90’s: LHC vs SSC
At the beginning of the 90’s, two projects were in competition: SSC and LHC
LHC was designed to compensate the 3 times lower energy (7 TeV rather than 20 TeV) with 10 times higher luminosity (1034 cm-2 s-1 compared to 1033 cm-2 s-1)
  SSC ring: 83 km, 6 T Nb-Ti magnets at 4.5 K, 20 TeV, lumi 1033 cm-2 s-1
  LHC ring: 27 km, 8 T Nb-Ti magnets at 1.9 K, 7 TeV, lumi 1034 cm-2 s-1
  Cost escalation lead the US congress to cancel SSC in 1993
  LHC is approved in 1994
Therefore LHC design in terms of luminosity was considered extremely challenging
On the top of this, LHC also had an ultimate luminosity defined as twice the nominal:
2×1034 cm-2 s-1

## Slide 5: Let be even more light …
Notwithstanding the challenging design, at the beginning of the 21st century plans for further increasing LHC luminosity started
  More fuel (more protons per bunch)
  Burning more rapidly (smaller beam size)
Target: gather 10 times more data
  via 5 times increase: 1  5×1034 cm-2 s-1
Smaller beam size in the interaction
requires larger quadrupole magnets
just after the interaction
Double quadrupole aperture, half beam size,
four times larger luminosity
So the keyword of higher luminosity is
larger aperture triplet and IR magnets

## Slide 6: The US program for the luminosity upgrade
At the beginning of the 00’s, the US DOE launches a massive program to develop Nb3Sn quadrupoles for the LHC upgrade (LARP)
  Two structures to be compared, subscale models, radiation hard materials, quench protection, …
In eight years (2003-2011) LARP proves
  90 mm and 120 mm aperture quadrupoles reaching
  >80% short sample, 1.5 m long
  Preference for the Al ring structure with b&k loading
  Protection is at the edge, not redundant as needed for operation
  Scaling to 3.4 m long for Al structure,
  but without integration in cold mass

## Slide 7: S-LHC and PhaseI upgrade
The LHC upgrade was initially split in two
  PhaseI with Nb-Ti, to reach 2-3×1034 cm-2 s-1
  PhaseII with Nb3Sn to reach 5×1034 cm-2 s-1
An MQXC, 120 mm and 120 T/m Nb-Ti magnet was succesfully built (G. Kirby, P. Fessia, S. Russenschuck, J. C. Perez, et al.)
Some ideas were taken later in HL-LHC, as grouping correctors in the CP , nested collars for MCBX, superferric design for HO correctors
PhaseI upgrade was canceled in 2011
LHC
layout
PhaseI upgrade
layout

## Slide 8: LHC luminosity in the 10’s
In the 10’s, ultimate LHC luminosity was achieved (3.5 TeV, then 4 TeV, then 6.5 TeV) – the accelerator performs according to the most optimistic plans!
  PhaseI upgrade targets achieved in LHC operation in 2018
In 2022, first year of Run 3, ultimate luminosity achieved also at 6.8 TeV
LHC luminosity ramp up in the 10’s (M. Lamont, J. Wenninger, and many many others)
Nominal luminosity
Ultimate luminosity

## Slide 9: The HL-LHC project
Luminosity upgrade of LHC
  ~1 BCHF project, CERN flagship
L. Rossi steers the efforts from 2011,
and O. Bruning from 2021
  HiLumi design studies in 2012-2014
  Project approved in 2015
  Installation in 2026-28
  Larger aperture triplet and crab cavities are the enabling technologies
  SC technologies: interaction region magnets (this talk), MgB2 link to power the main magnets (A. Ballarino), 11 T dipoles (A. Devred, D. Perini, installation on hold)
IR magnets: replacing magnets in the 160 m left and right of ATLAS and CMS with larger (double) aperture magnets
  ~220 MCHF budget (w/o personnel), including 8 collaborations/in kind contributions

## Slide 10: Interaction region magnets: from LHC to HL-LHC
Triplet: from 70 mm aperture Nb-Ti quadrupoles (8.4 T peak field, two types MQXA and MQXB) to 150 mm aperture Nb3Sn quadrupoles (11.3 T peak field, two lengths with same cross-section, made at CERN and in the US
  Thanks to Nb3Sn, the triplet is only 19 m longer than in the LHC – space is given thanks to D1
MQXA cross-section
MQXF cross-section

## Slide 11: Interaction region magnets: from LHC to HL-LHC
Triplet design: scaling of LARP HQ design from 120 to 150 mm, Al ring structure with B&K loading, operating ≈80% of short sample, 110 MPa accumulated stress due to e.m. forces
In 2014, CLIQ is developed at CERN and provides protection with redundancy together with the QH (G. Kirby, E. Ravaioli, et al.)
MQXB cross-section
MQXF cross-section

## Slide 12: Interaction region magnets: from LHC to HL-LHC
LARP had already build 3.4 m long magnets, and proposed 4.2 m long magnets – a project of 8.5 m long magnet would have not been approved by DOE (16 magnets to install plus 4 spares)
CERN decided to go for 7 m long magnets to open a way for the final scaling to 15 m (8 magnets to install plus 2 spares)

## Slide 13: Interaction region magnets: from LHC to HL-LHC
D1 today is a resistive magnet, 6 module 3.4 m long, 1.28 T
The 10 m longer triplet makes use of this space, since the magnet is replaced by a Nb-Ti dipole with 5.6 T field, provided by KEK, Japan – very challenging magnet with 100 MPa e.m. stress

## Slide 14: CONTENTS
A short review of the interaction region magnets in the HL LHC project
The short model program of MQXF
The US contribution (MQXFA)
The CERN contribution (MQXFB)

## Slide 15: MQXF short model synoptic
6 short models built, 5 conform
T0: aperture and cable selection
2013
2014
2015
2016
2017
2018
2019
2020
2021
MQXFS1: ≥12.9 T
MQXFS3: ~10.6 T
MQXFS5: ≥12.7 T
MQXFS4: ≥13.1 T
MQXFS6: ≥13.4 T
MQXFS7: ≥12.7 T
T0+3
RED indicates conform magnets
2022
MQXFS8
2023

## Slide 16: MQXF short model results
  Ability to operate at nominal current both at 1.9 K and at 4.5 K
  Large margin: ability to achieve 1 to 2 T conductor peak field in excess of what required
  Perfect memory: no retraining after thermal cycle up to ultimate current
  Reproducibility: 5 out of 6 magnets reached operation >7.5 TeV
  Endurance (see next slides)
7.5 TeV
11.3 T peak field
7 TeV
13.4 T peak field
Preload experiment on MQXFS6 (S. Izquierdo Bermudez, F. Mangiarotti, et al.)

## Slide 17: CONTENTS
A short review of the interaction region magnets in the HL LHC project
The short model program of MQXF
The US contribution (MQXFA)
The CERN contribution (MQXFB)

## Slide 18: MQXFA synoptic
10 out of 22 magnets built and V tested (including 2 prototypes)
  6 conform
T0: aperture and cable selection
2013
2014
2015
2016
2017
2018
2019
2020
2021
MQXFAP1: ≥11.6 T, but electrical short
MQXFAP2: ~10 T, broken structure
MQXFA03: ≥11.6 T
MQXFA05: ≥11.6 T
MQXFA06: ≥11.6 T
T0+4
MQXFA07: ~10.7 T
DOE approval
10 magnet tested, 13 more new magnets to test (9 and 12-23), plus re-assemblies
2022
MQXFA08: <6 TeV
2023
MQXFA10: ≥11.6 T
MQXFA04: ≥11.6 T
MQXFA11: ≥11.6 T
MQXFA08b
Red: conform
Black: non conform
Grey: coming in 2022
2024

## Slide 19: MQXFA conform magnets
MQXFA program confirms
  Operation at nominal current plus 300 A, both at 1.9 K and 4.5 K
  Perfect memory, i.e. no retraining, and robustness
Powering test of conform MQXFA magnets (J. Muratore, B. Ahia, S. Feher et al.)
Non conform MQXFA11 transport

## Slide 20: MQXFA performance limitations
MQXFA07 and MQXFA08 showed performance limitations with reverse behaviour
  Issue identified in an asymmetry in the assembly, at the transition straight part-end
  MQXFA07 limiting coil has been inspected via tomography/mterialography at CERN: large number of longitudinal cracks in the filaments in that region
  Feedback on the assembly procedures was implemented starting from MQXFA10 that reached performance
Presence of cracks (red crosses) in coil 214 (M. Crouvizier, A. Moros, S. Sgobba)
Power test of MQXFA07 (J. Muratore, S. Feher, G. Ambrosio et al.)

## Slide 21: CONTENTS
A short review of the interaction region magnets in the HL LHC project
The short model program of MQXF
The US contribution (MQXFA)
The CERN contribution (MQXFB)

## Slide 22: MQXFB synoptic
3 prototypes and 1 series horizontally tested, directly in a cold mass
2013
2014
2015
2016
2017
2018
2019
2020
2021
MQXFBP1: ~10.5 T
MQXFBP2: ~11.2 T
T0+7
9 to 11 more magnets to test
2022
T0: aperture and cable selection
2023
MQXFBP3: ≥ 11.6 T
MQXFB02: ≥ 11.6 T

## Slide 23: MQXFB performance limitations
MQXFBP1 and MQXFBP2 were limited below nominal current
  Contrary to MQXFA, no reverse behaviour, i.e., 4.5 K performance consistent with 1.9 K (70% and 74% of short sample) – quenches in straight part
  MQXFBP1 was disassembled, and longitudinally broken filaments were found in the limiting coil, in agreement with quench antenna and voltage tap locations
MQXFBP1 and MQXFBP2 prototype performance
(F. Mangiarotti, S. Izquierdo Bermudez, et al.)
Broken filaments in coil 108, limiting MQXFBP1
(M. Crouvizier, A. Moros, S. Sgobba, et al.)

## Slide 24: MQXFB performance limitations
In April 2021, date of the test of second prototype, third magnet (MQXFBP3) was assembled and coils for the fourth (MQXFB02) were completed
Coil production was paused and a plan addressing possible causes were defined and addressed

## Slide 25: MQXFBP3
MQXFBP3 used a new procedure to weld the LHe vessel minimizing the mechanical coupling with the magnet
  Nominal plus 300 A reached during first powering with one training quench,
  At 4.5 K, we see the same type of limitation observed in MQXFBP1 and P2 but at much higher levels
  No degradation after three cool-downs
Test results of MQXFBP3 and comparison to MQXFBP1 and MQXFBP2, and short models
(PE: S. Izquierdo Bermudez, test eng.: F. Mangiarotti, et al.)

## Slide 26: MQXF temperature margin
  The collision debris coming from the interaction point heat locally the magnet to 2.2 K: therefore a temperature margin larger than 0.3 K is needed for operation
MQXF nominal current is at 78% of the loadline, corresponding to temperature margin of 5.0 K
  The presence of a temparture margin >2.6 K is checked for all magnets via a test at 4.5 K
  MQXFBP3 has 2.0 K temperature margin, all short models and US magnets have >2.6 K
Peak power density on the coil
(F: Cerutti, et al.)
Temperture map in the coil
(P. De Sousa, R. van Weelderen, et al.)

## Slide 27: MQXFB02
MQXFB02 used a revised procedure to assemble the magnet, reducing the peak stress
  (plus the LHe vessel welding procedure already implemented in MQXFBP3)
  Peak stress during assembly is now below 100 MPa, note that succesful short models were asselbmed with peak stresses up to 140 MPa – large margin in terms of prestress for the long magnets
  Nominal plus 300 A reached during first powering with two training quench,
  At 4.5 K same type of limitation observed in MQXFBP1 and P2 but with 2.6 K temperature margin
Test results of MQXFB02 (left) and peak stress during assembly (right)
(PE: S. Izquierdo Bermudez, test eng.: F. Mangiarotti, et al.)
Short models
MQXFBP1
MQXFBP2
MQXFBP3
MQXFB02
TEST ONGOING

## Slide 28: Coil manufacturing
Several actions ongoing to improve the coil manufacturing
  Analysis of 108 (limiting coil of MQXFBP1) shows that breakages are close to pole transitions
  Analysis of 126 shows that (few) events are also present in a virgin coil (not tested)
  Efforts are focusing on the «hump»
Fast-tracks have been defined to assess the performance of the two coils manufactured after the 1 year long pause
  MQXFBMT4 and MQXFBMT5, where new coils are assembled with existing coils – to be tested in April and August 2023
MQXFB03, the first magnet using 4 coils manufactured after the pause, will be tested at the end of the year 2023
The hump (S. Izquierdo Bermudez, A. Milanese, N. Lusa, et al.)

## Slide 29: Endurance tests
Degradation of Nb3Sn magnets after thermal cycle has become a major concern in the community after the results in 2018-2020 of the 11 T long magnets
  Three short models succesfully went through endurance tests: MQXFS1, MQXFS4, MQXFS6
  One full-length MQXFA magnet (without integration in the LHe vessel) succesfully went through endurance tests – no degradation observed after 5 thermal cycles and 50 quenches
Long magnet endurance test
(B. Ahia, S. Feher, G. Ambrosio, et al.)
Short magnet endurance test
(P. Ferracin, F. Mangiarotti , et al.)

## Slide 30: THE STRING COMING SOON
MQXFBP2 on assembly bench with
nested corrector MCBXFBP1 (H. Prin, et al.)
The string will assemble Q1 to D1 cryomagnets to test the system, to be commissioned in 2024 (M. Bajko)
First cryostating of MQXFB cold mass
(D. Duarte Ramos, et al.)
Alignment of first MQXFA cold mass
(S. Feher, et al.)

## Slide 31: CONCLUSIONS
MQXFS
  Short model program proved ability to reach 1-2 T in excess of requirements, and endurance
MQXFA
  Successful endurance test of the first Nb3Sn full length magnet – major milestone
  Six conform magnets, but integration in the cold mass still to be proven
  Issues with MQXFA07 and MQXFA08 performance seem to be understood and MQXFA10 is conform
  Next critical steps before end of the year: test of the first cold mass in horizontal position and validation of coil replacement in MQXFA08b
MQXFB
  Fully redundant protection has been proved
  Last prototype has achieved nominal plus 300 A, with memory and no degradation – first Nb3Sn magnet in a cold mass configuration
  Repeatability of this result is being assessed in test of MQXFB02
  Efforts still ongoing to improve coil manufacturing to have 7 m long magnet with the full performance shown in short models

## Slide 32: Interaction region magnets: from LHC to HL-LHC
D2 today is a Nb-Ti magnet, 2.8/3.5 T, 9.5 m long (from BNL, same design of BNL dipole coils)
D2 in HL-LHC is a Nb-Ti 4.5 T magnet, 7.9 m long (from INFN-Ge, similar design to SIS-300 dipole)
INFN-Ge and ASG make the magnet – cold mass, cryostating and horizontal test made at CERN

## Slide 33: Interaction region magnets: from LHC to HL-LHC
MCBX today is a Nb-Ti magnet, 3 T field, 2 T m integrated field, combined function H and V field
MCBXF is a Nb-Ti magnet, 2.1 T field, 2.5/4.5 T m integrated field, combined function H and V field
Double collared structure, very large aperture and thin coil, made in CIEMAT/Elytt
Integration in the cold mass, cryostating, V and H test at CERN

## Slide 34: Interaction region magnets: from LHC to HL-LHC
HO correctors, based on Nb-Ti superferric technology: nine magnets gathered in the corrector package
Design developed for S-LHC, CIEMAT, and adapted by INFN-LASA
Integration in the cold mass, cryostating, H test at CERN

## Slide 35: Interaction region magnets: from LHC to HL-LHC
D2 correctors (merged with Q4 in LHC) are 2.8 T magnets, 4.5 T m integrated field
CCT design was adopted, a prima for CERN – design and prototypes developed in 927
China in-kind contribution (magnets and V test), integration in D2 cold mass in 180

## Slide 36: D1 (see T. Nakamoto talk)
After the test of the prototype in vertical KEK test station (May 2021), past year has been dedicated to cold mass manufacturing and test facility upgrade
  Shipping to CERN before the end of 2022, and horizontal test in SM18 in early 2023
The winding at Hitachi of the coils of first (MXBF5) and second (MBXF1)
series magnet has been completed (1/3 of total production!)
  These coils had a fine tuning of cross-section to
  correct 5 units of b3 and -5 of b5
Collaring of MBXF5 completed, but issue
with procedures has been found  decollaring
  Vertical test of MBXF1 expected for end of 2022
Cold mass of MBXFP1 (T. Nakamoto, M. Sugano, K. Suzuki, H. Felice, et al)

## Slide 37: D2 (see B. Caiffi talk)
D2 prototype (fully made in ASG) test at 1.9 K in SM18 is ongoing
  Final cold mass configuration, with one D2 corrector from CERN and one from China in-kind contribution
  First use of cryostating tooling for HL-LHC at CERN
Manufacturing of first series coil completed
  Fine tuning of cross-section to optimize b3 and b5
  First series magnet at CERN in mid 2023,
  test in early 2024
D2 cold mass on the test bench in SM18 (S. Farinon, B. Caiffi, A. Bersani, A. Foussat, et al)

## Slide 38: Nested correctors (see F. Toral talk)
The performance limitation seen on the retraining after change of torque in prototype MCBXFBP1 and MCBXFBP2 (short nested correctors) was overcome after a design iteration executed on MCBXFB01
The second prototype had the inner layer changed with a new inner layer made by Elytt, both to validate the first production coils and to verify the reproducibility of the design change
  Magnet reached performance at 7.5 TeV equivalent without retraining after thermal cycle – second magnet conform
First short corrector fully manufactured in Elytt is being completed (MCBXFB02)
  To be tested in October 2022 at CERN
First long prototype to be assembled in October at CERN
Test results of MCBXFP2c
(S. Ferradas Troitino, F. Toral, J. C. Perez, C. Martins, et al)

## Slide 39: D2 correctors (see Q. Xu) talk
D2 correctors (see also A. Foussat talk on Wednesday at 9h)
  Issue of very long training at 4.5 K observed in inital production at BAMA has been solved (iteration on impregnation prodecures, and size of the channel gap)
  First fast training coils to be tested in MCBRD03
  MCBRD01 and 02 reached performance at 4.5 K in IMP (non conformity in retraining and HV test)
  MCBRD01 retested at CERN at 1.9 K and achieved training requirements – pending issue on insulation
  MCBRD02 to be tested at CERN in October 2022
  Additional magnet completed at CERN (MCBRDP4) - conform
Training of MCBRD01 (PE: Q. Xu, test: W. Wu, G. Willering et al)
Training of MCBRDP4
(WPE: A. Foussat, G. Kirby, test: G. Willering et al)

## Slide 40: High order correctors (see M. Statera talk)
Production completed in SAES-RIAL vacuum (54 magnets)
  37 magnets tested and accepted (2/3)
  Cold mass assembly operations started at CERN, including alignment
The nine high order correctors assembled in the prototype cold mass
(M. Statera, E. Gautheron, H. Prin, et al)