## Slide 1: NIOBIUM THIN FILMS:
Carlota Pereira, S. Leith, G. Rosaz, , M. Taborelli, M. Bonura, C. Senatore, S. Pfeiffer, A. -T. P. Fontenla, G. Belini, L. Ferreira, L. Vega-Cid, A. Bianchi, W. Venturini-Delsolaro
02/05/2023
CORRELATION BETWEEN MICROSTRUCUTRE AND SUPERCONDUCTING PROPERTIES

## Slide 2
Background & Motivation
Outline
Recent results 400 MHz SRF cavities
Summary
Additional studies for improving SRF cavity performance
Thin film optimization for superconducting radiofrequency (SRF) accelerating cavities
Summary

## Slide 3
Superconducting radiofrequency (SRF)
cavities
400 MHz cavity, LHC
Particle acceleration
Background

## Slide 4
Cu substrate
Nb coating
4.5 K
  ω - resonant frequency
  U - energy stored in the cavity
  P - dissipated power
Superconductor
Background: SRF cavities
Notes: Geometry Factor ranks the cavity's effectiveness of providing accelerating electric field due to the influence of its shape alone

## Slide 5
Cu substrate
Nb coating
4.5 K
Background: SRF cavities
  G – Geometry factor
  - surface resistance
Higher quality factor
Rs copper mΩ
Rs sc niobium nΩ
Superconductor
Notes: Geometry Factor ranks the cavity's effectiveness of providing accelerating electric field due to the influence of its shape alone

## Slide 6
Q0
LHC cavities Q vs Eacc @4.5 K
Eacc (MV/m)
LHC
2-cell
1-cell
Degradation of Q0 with increasing Eacc: Q-slope
FCC-ee 400 MHz Nb/Cu
Motivation

## Slide 7
Motivation
Q0
LHC cavities Q vs Eacc @4.5 K
Eacc (MV/m)
LHC
2-cell
1-cell
Degradation of Q0 with increasing Eacc: Q-slope
FCC-ee 400 MHz Nb/Cu
Cure Q-slope & extend field reach!
How?

## Slide 8
RF superconductivity
Magnetic flux lines
Meissner state
flux expulsion
Normal conducting
Mixed
state
flux pinning
Performance optimization
Defect density minimization
Pinning centers = defects in the layer
Under RF field, fluxon oscillation leads to energy dissipation
Superconducting

## Slide 9
SRF cavities R&D
Substrate
Interface
Thin film

## Slide 10: Thin film optimization
Coating technique

## Slide 11
Kr+
Nb atoms
LHC: DC Magnetron Sputtering
Coating technique
Switch deposition method
Nb target
HiPIMS
High Power Impulse
Magnetron Sputtering
Sheath
Sheath
Plasma
See talks by F. Avino, S. Fiotakis:
https://indico.cern.ch/event/876252/
https://indico.cern.ch/event/1129796/

## Slide 12
Kr+
Nb+
Pulsed sputtering
Target material becomes
ionized (~70%)
Plasma
Sheath
Nb+
Nb+
DC bias
power supply
-V
HiPIMS
Sheath
Coating technique

## Slide 13
Kr+
Nb+
Plasma
Sheath
Nb+
DC bias
power supply
-V
Nb+
biasing potential: allows the control of the particles’ trajectory and increases the incident bombardment energy
Energetic condensation
Sheath
HiPIMS
Coating technique

## Slide 14
Kr+
Nb+
Plasma
Nb+
DC bias
power supply
-V
Nb+
Sheath
Sheath
Energetic condensation
HiPIMS
HiPIMS
DCMS
1 µm
Coating technique

## Slide 15: Thin film optimization

## Slide 16
400 MHz
Correlate microstructure of HiPIMS Nb films with their superconducting properties and lower RF surface resistance
Scale-up
Current strategy
Optimize HiPIMS process
Small samples
1.3 GHz test cavities

## Slide 17
How to quantify film performance?
Q0
Eacc (MV/m)
LHC
Ultimate test
RF testing
400 MHz cavities: max 3/year
1.3 GHz cavities: max 15/year
Hard to single out the effects of an individual coating parameter
Intermediate method that could be used on samples

## Slide 18
Max current a superconductor can carry without breaking superconductivity
Critical surface of a superconductor
Depends on pinning centres (structural defects)
The higher the defect density, the higher the JC
Defect density minimization
JC minimization
Critical current density JC
Extracted using VSM SQUID measurements
How to quantify film performance?

## Slide 19
Bulk Nb
HIE-ISOLDE
4K, 250mT
HiPIMS +DC Bias
Nb/Cu samples
JC of our HiPIMS samples is orders of magnitude higher
There’s room for improvement
JC minimization
Bulk Nb: Eacc 49 MV/m with Q0 above 1010
HIE-ISOLDE reached fields up to 120mT (~30 MV/m in an elliptical cavity)

## Slide 20
JC minimization
Substrate treatment
Post coating annealing
Coating temperature
…
Thickness
Ion bombardment energy

## Slide 21: JC minimization vs thickness

## Slide 22
Bulk Nb
HiPIMS +DC Bias
Nb/Cu samples
HIE-ISOLDE
JC decreases with increasing film thickness
Independently of bias
JC minimization vs thickness
4K, 250mT
What morphological property is responsible for this?
i. e. which defect family disappears gradually with increasing thickness?
Notes: HIE-ISOLDE – Coated in diode mode w/ high pressure 10^-1 mbar and high temperature 300-650C. 80V bias

## Slide 23
Microstructure Analysis
Grazing incidence XRD
…
Focus Ion Beam
Optical profilometry
Evaluated films with different thicknesses:
Dislocation density
Grain size
Roughness
Impact on JC?

## Slide 24
Dislocation density,
We quantified the dislocations density in our Nb films through Grazing Incidence XRD
crystallite size,
microstrain,
lattice parameter,
b = Burger vector expressed as (m) for BCC materials
x103
20.0
10.0
40.0
60.0
80.0
2theta (degrees)
Intensity (a.u.)
Nb-bcc
Cu-fcc
Dislocation density

## Slide 25
Dislocations are driving defects for Jc minimization
Data from all films
Promising for optimization of RF performance
Dislocation density vs JC

## Slide 26: JC minimization vs DC bias

## Slide 27
Bulk Nb
4K, 250mT
HIE-ISOLDE
HiPIMS +DC Bias
Nb/Cu samples
Nonlinear relation:
optimum JC with
-75 V applied DC bias
JC minimization vs DC bias
Bias voltage applied UB changes the ion energy impinging the surface
Eion = |eUB|
-75 V bias corresponds to 75 eV of ion bombardment energy

## Slide 28
Ion bombardment energy vs JC
4K, 250mT
(same thickness)
Optimum JC for ion bombardment energy around 75 eV.
How are the different bombardment energies interacting with the growing film?

## Slide 29
{100}
{110}
{111}
surface
Ion bombardment energy vs JC
For each ion bombardment energy, we calculated the deposited energy at the surface and in the bulk of the film along the different crystalline planes
bulk
1 µm
Body-centered cubic unit cell

## Slide 30
[1] D. K. Brrce et al. Nuclear Instruments and Methods in Physics Research, 44 1989 68-78
[2] Z.Q. Ma et al. Applied Surface Science 137 1999 184–190M
Optimum Jc when the energy is equally spread among the {100} and {110} crystalline planes
*
binary collision approximation [1][2]
*
difference between deposited energy the {100} and {110} planes as a function of impinging ion energy @ the surface
4K, 250mT
{100}
(same thickness)
Ion bombardment energy vs JC

## Slide 31
Summary
performance boost achieve FCC-ee target
energetic condensation of the film
HiPIMS
JC
Bulk Nb
HiPIMS +DC Bias
HIE-ISOLDE
Better RF performance with:
Bombardment energy equilibrium across the {100} and {110} crystalline planes
Reduction of dislocation density
as a metric of thin film quality for SRF applications
Future work: study other deposition parameters on how they impact JC
Thin film optimization

## Slide 32: Additional ongoing studies
for SRF cavity performance optimization

## Slide 33
SRF cavities R&D
Substrate
Interface
Thin film
Post- coating processing

## Slide 34
Control system upgraded (ICM section, 2021)
30 min: no effect
(normal rinsing time)
Effect of HWPR duration on film surface?
(smoothening, hardening…)
5 h roughening
Frequency (1/mm)
Power Spectral Distribution (mm µm2)
1-2 h smoothens the surface
3-4 h improved
See talk by Joana Staniszewska
https://indico.cern.ch/event/1129767/
3-4h optimum
3 h rinsing to be implemented on future cavities
High Pressure Water Rinsing
Roughness

## Slide 35
SRF cavities R&D
Substrate
Interface
Thin film

## Slide 36
Suppress surface defects “propagation”
Produce flat layer independently of substrate’s roughness
Film planarization
(a)
(e)
(f)
(c)
-75V
(b)
(d)
-50V
-100V
-125V
-150V
-200V
-300V
Simulations
Experimental results

## Slide 37
SRF cavities R&D
Substrate
Interface
Thin film

## Slide 38
Seamless substrates + Electropolishing
Scaled FCC-ee
targets
@4.5 K
Recent RF results 1.3GHz test cavities
Cavities were coated with parameters found to optimize JC, -75 V DC bias and 6 µm thickness (cell)
seamless cavities (no welds)
Improved performance with minimum Q-slope
bulk machined + electroformed substrates
Electropolishing: see talk by Gloria Bellini
https://indico.cern.ch/event/1129762/
+ Electropolishing
+ Optimized recipe

## Slide 39
Seamless cavities + EP +
optimized coating recipe:
Improved performance
and minimized Q-slope
Substrate
Thin film
HPWR optimization:
3 h smoothening of the
surface
Nb planarization:
@ -300 V DC bias
Stop defects from propagating from substrate to film
Interface
Summary
Additional studies
Coating recipe to apply this to cavities under investigation

## Slide 40
400 MHz
Scale-up
1st HiPIMS-coated 400MHz SRF cavity
SUBU (not Electropolished)
Q0
1010
109
108
Eacc (MV/m)
0
2
4
6
8
10
12
14
16
FCC-ee
HiPIMS hardware limitations
@2K
@4.5K

## Slide 41
Thank You!