## Slide 1: ESD measurements from unbaked to baked samples
Paulina Gabriela Czapkowicz
Supervisor: Ivo Wevers
TE-VSC-BVO 26.09.2023

## Slide 2: Outline
Electron Cloud in the LHC
ESD Testbench – old design
ESD Testbench upgrade
Measurement procedure
ESD Results:
- Stainless steel
- Copper
- NEG coatings
- Carbon coatings

## Slide 3: Electron cloud in the LHC
Thermal load
Prim. e-
hν
Sec. e-
Primary electrons
Residual gas ionization
Photoelectric effect
Acceleration by proton
beam potential
Electron Stimulated Desorption
Collisions with vacuum chamber walls
Emission of
secondary electrons
Secondary Electron Yield
p+
p+
p+
p+
Based on data taken from V. Petit, Beam scrubbing and heat loads in the LHC arcs [1]

## Slide 4
Old design of the load-lock
ESD Testbench – old design
Old design of the ESD testbench, located in building 113

## Slide 5: ESD Testbench – old design
Dome
Old design of the load-lock
Old design of the ESD testbench, located in building 113

## Slide 6: ESD Testbench – old design
Load-lock
Dome
Old design of the load-lock
Old design of the ESD testbench, located in building 113

## Slide 7: ESD Testbench – old design
Load-lock
Dome
Old design of the load-lock
Not possible to bake samples due to:
Polymer seal in load-lock
Lack of heater
No direct temperature measurement of sample
Old design of the ESD testbench, located in building 113

## Slide 8: ESD Testbench – old design
Old design of the ESD testbench, located in building 113

## Slide 9: ESD Testbench – dome
Components of the testbench dome
1
2
3
4
5
Residual Gas Analyser (RGA)
NEG cartridge
Electron gun
Conductance
Vertical manipulator

## Slide 10
ESD Testbench – overview
Old design of the ESD testbench
New design of the ESD testbench

## Slide 11
ESD Testbench – overview
New design of the ESD testbench
Old design of the ESD testbench

## Slide 12
ESD Testbench – new design of load-lock
1 - viewport
2 – heater tectra HC3500
3 - horizontal manipulator
4 - PBR260
5 - thermocouple feedthrough
6 - thermocouple manipulator
7 - blank flange
8 - variable leak valve
New design of the load lock

## Slide 13: Load-lock temperature measurement
Temperature measurement in load-lock

## Slide 14
1
1 – heater (tectra HC3500)
Temperature measurement in load-lock
Load-lock temperature measurement

## Slide 15: Load-lock temperature measurement
1
2
1 – heater (tectra HC3500)
2 – sample holder
Temperature measurement in load-lock

## Slide 16
1
2
1 – heater (tectra HC3500)
2 – sample holder
Model of the new sample holder
Picture of the sample holder
Temperature measurement in load-lock
Load-lock temperature measurement

## Slide 17
1
2
Model of the new sample holder
1 – heater (tectra HC3500)
2 – sample holder
3 – thermocouple type E
3
Temperature measurement in load-lock
Load-lock temperature measurement

## Slide 18: Testbench after upgrade
ESD testbench located in building 113

## Slide 19: Sample characteristics
Sample dimensions: 4.5 x 3.5 x 1 cm
Irradiation area: 3.24
Tested materials: copper, stainless steel, carbon coatings, NEG coatings
Stainless steel carbon coated samples:
Stainless steel + 100 nm aC (substrate not vacuum fired),
Stainless steel + 100 nm aC,
Stainless steel + 400 nm aC,
Stainless steel + 100 nm aC + 200 nm Ti underlayer.
Coating thickness difference: ± 15%

## Slide 20: Measurement procedure of ESD
Venting load lock with N2
Sample insertion to load lock
Pumpdown
Sample heating (optional)
Transfer to dome
Sample positioning in dome
Measurement
Measurement settings:
P ≤ 5 ·
Ee = 300 eV

## Slide 21: Raw data of OFE copper baked at 150°C for 24h
Current collected on sample

## Slide 22: Raw data of OFE copper baked at 150°C for 24h
Current collected on sample
Pressure measured by Bayard-Alpert gauge in dome

## Slide 23: Raw data of OFE copper baked at 150°C for 24h
Current collected on sample
Data collected by RGA (for H2)
Pressure measured by Bayard-Alpert gauge in dome

## Slide 24: Raw data of OFE copper baked at 150°C for 24h
Current collected on sample
Data collected by RGA (for H2)
Pressure measured by Bayard-Alpert gauge in dome

## Slide 25: ESD measurement in function of temperature
Procedure:
Inserting sample
Unbaked sample measurement
Transfer to load lock for baking
Measurement of baked sample
Repetition of the steps 3 and 4 for all temperatures
Measurements parameters:
Electron bombardment: 60s
Ee = 300 eV
Emission current: 24 μA
Heating time: 2h

## Slide 26: Unbaked vs baked OFE copper
*research data from O. B. Malyshev, Beam induced desorption, CAS on Vacuum for Particle Accelerators 2017 [2].
Ee = 300eV
Emission settings:
24μA (25 min)
160 μA (1.5h)
650μA (24h)
Baking time: 2h
Heating temp.: 150°C, 300°C
24μA
160μA
650μA

## Slide 27: Influence of temperature on ESD of stainless steel 316LN
*Data taken from O. B. Malyshev; A. P. Smith; R. Valizadeh; A. Hannah, Electron stimulated desorption from bare and nonevaporable getter coated stainless steels, J. Vac. Sci. Technol. A 28, 1215–1225 (2010) [2]
[2].
Ee = 300eV
Emission settings:
24μA (25 min)
160 μA (1.5h)
650μA (24h)
Baking time: 2h and 24h
Baking temperatures: 250°C

## Slide 28: Influence of coating type on ESD of aC
*substrate not vacuum fired, rest of the substrates were vacuum fired.
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)
100 nm aC Average : 1.15
400 nm aC Average : 1.14
100 nm aC/Ti Average 1.16

## Slide 29: Influence of temperature on NEG samples
*Data taken from O. B. Malyshev; A. P. Smith; R. Valizadeh; A. Hannah, Electron stimulated desorption from bare and nonevaporable getter coated stainless steels, J. Vac. Sci. Technol. A 28, 1215–1225 (2010) [2]
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 30: Influence of temperature on NEG sample
Electron Desorption Yield of stainless steel coated with NEG in function of temperature
Ee = 300eV
Emission settings: 24μA (60s)

## Slide 31: Conclusion
Upgrade:
New load-lock design
Repeatable measurements
Programmable heater
Direct temperature measurement during sample baking

## Slide 32: Thank you for your attention!

## Slide 33: Bibliography
[1] V. Petit, Beam scrubbing and heat loads in the LHC arcs
[2] O. B. Malyshev, Beam induced desorption, CAS on Vacuum for Particle Accelerators 2017
[2] O. B. Malyshev; A. P. Smith; R. Valizadeh; A. Hannah, Electron stimulated desorption from bare and nonevaporable getter coated stainless steels, J. Vac. Sci. Technol. A 28, 1215–1225 (2010)

## Slide 34: SEY of carbon coatings
Average 1.15
Average 1.14
Average 1.16
100 nm aC
400 nm aC
100 nm Ti/aC
Data from TE-VSC

## Slide 35: CH4 - OFE copper
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 36: CO - OFE copper
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 37: CO2 - OFE copper
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 38
CH4 – aC coatings
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 39
CO – aC coatings
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 40: CO2 – aC coatings
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 41
CH4 - Stainless steel
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 42
CO - Stainless steel
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 43: CO2 - Stainless steel
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 44
CH4 - NEG
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 45: CO - NEG
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 46: CO2 - NEG
Ee = 300eV
Emission settings: 24μA (25 min)
160 μA (1.5h)
650μA (24h)

## Slide 47
CH4 - NEG
Ee = 300eV
Emission settings: 24μA (60s)

## Slide 48: CO - NEG
Ee = 300eV
Emission settings: 24μA (60s)

## Slide 49: CO2 - NEG
Ee = 300eV
Emission settings: 24μA (60s)