## Slide 1
Thin films vacuum coating
M.Taborelli on behalf of the TE-VSC-SCC section

## Slide 2
DC Magnetron sputter deposition:
-evacuate at p in 1e-8 mbar range and inject Ar (Kr) in 10-3 mbar range
-target at negative potential
-noble gas ionization by electrons
-magnetic field confines electrons and helps to sustain plasma
HIPIMS (High Power Impulse Magnetron Sputtering):
Same configuration, but pulsed high voltage (current) leading to ionized target species
PAr ~ 10-3 mbar
Physical Vapour Deposition by planar magnetron sputtering
substrate
Process gas
Cathode (target)
magnets
+
+
+
e
e
e
e
e
+
Ar+
+
-500V
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 3
up to 1 m length, on substrates of copper, aluminium, StSt, MoGr, graphite, alumina, some polymers, coatings of 1-5 m thickness typically
coatings to improve static/dynamic vacuum (NEG, a-C), for RF applications or reduction of impedance and charging (Cu, Mo, TiOx), for superconducting RF (Nb, Nb3Sn R&D) and more (Au, B4C, n-tof N and Cl rich target layers…), Al, Re…..
Thickness test on partially masked witness glass sample and profilometry on step or XRF
SMA18
SPS tunnel
«Small substrates»
SMA18
Ø 1500 mm
targets

## Slide 5
Up to 7 m length
Typically for TiZrV (Non Evaporable Getter for pumping) and a-C (low secondary electron yield)
Target made of intertwisted wires or rod, vertical to avoid sagitta
Coating method for long vacuum pipes
0.5-3 μm thickness for NEG and < 0.5 μm for a-C
Before coating
after coating
typically < 300G
Coating after pumping and bake out (below 10-8 mbar base pressure)
B-field
coil
Vacuum chamber
Notes: Appropriate situation with the CERN logotype
Mixture of different logotypes
All of them are circulating
All CERN clubs were also very creatives

## Slide 6
CAPE09 Cambridge M.Taborelli CERN
Coating plant bdg 181

## Slide 7
SMOG II cell
(a-C)
VELO RF boxes
(NEG)
Unusual geometries

## Slide 8
-“train” (modular in several coaches and moved along the pipe) with hollow cathode
-coated in LS2 95 QF quadrupoles of SPS and several dipoles “in situ”
Graphite targets
(cells)
6.5 meter
MBB dipole
Design, production and operation of custom made coating systems: in SPS
132 mm

## Slide 9
-coated the beamscreen of Q5L8 during LS2, to suppress e-cloud related heat load
Courtesy of B.Bradu
Design, production, operation of coating systems: Standalone magnet in LHC in situ
Titanium target
pump hydrogen
enhance adhesion
Graphite target
direction
100
mm

## Slide 11
  400 nm thick carbon foil (about 100ug/cm2)
  Development in progress as stripper foil for Linac 3
Combine coating and etching: carbon windows as ion stripping foils
Chemical etching of Cu (ammonium persulfate)
20 mm

## Slide 12
Thank you!
Questions?
Reference: Pedro Costa Pinto, Wilhelmus Vollenberg

## Slide 13: HiPIMS configurations
  Duty cycle : 1 kHz
  Main pulse (MP) : 30 ms
  Delay (D) : 4 ms
  PP duration (PP) : 20 – 250 ms
-550 V
~20 A
+50 V
PP
MP
D
+50V PP
no PP

## Slide 14
19 November, 2013
It is possible to set up a multitarget system to produce coatings of alloys
3* Ø 50 mm targets
For R&D purpose:
Small samples !!
Multicathode system