## Slide 1
Surface treatments at CERN
M.Taborelli on behalf of the TE-VSC-SCC section
TE-VSC
107
Service and R&D activity
Located at Bdg 107
Bdg 118
TE-VSC

## Slide 2
Wet surface treatments: cleaning, etching
-cleaning service of all Ultra High Vacuum components in detergents (chambers up to 7 m length) and solvents (Dualene 1601S modified alcohol)
-as preparation for other processes: PVD coating, welding, brazing
-chemical etching (acids, bases) and passivation, before plating,
PVD coating, welding or for thin film removal
NB: no clean room environment
Solvent based cleaning machine
Alkaline detergent bath

## Slide 3
Plating and electropolishing schemes
Anodes :
Cathodes:
M(s) M+q(aq) + qē
M+q(aq) + qē M(s)
2H2O 4ē + O2(g) + 4H+
2H+ + 2ē H2(g)
Water electrolysis
Can do electropolishing (dissolution) on this side
Can do plating and electroforming on this side
+
-
G
M+q
M+q
M+q
M+q
M+q
M+q
NB: the bath, the concentrations, the current density, the voltages, the temperature, the bath agitation are specific for each processes and material
M+q

## Slide 5
-on substrates like StSt, Cu, Al and their alloys
-by layers of Ni (pre-layer for Cu/StSt plating and StSt vacuum brazing…), Cu, Au, Rh, Ag
-typical thickness of 5-50 m depending on the material and goals
-copper plating of large objects in dedicated (built on purpose) vessels
Ag (RF fingers, screws, gaskets, pre-layer for brazing, …)
Au (RF fingers, current leads, beam-screen edges, pre-layer for Cu plating)
Rh (hard contact to RF fingers …)
Metal plating

## Slide 6
Chemical polishing and electropolishing
chemical and electropolishing of copper (for superconducting RF cavity substrates before Nb coating)
chemical polishing of Nb (CRAB cavities)
electropolishing/polishing machine for cavities
StSt electropolishing
if necessary simulations for R&D can be done by COMSOL
HIE full cavity polishing
Nb CRAB, polishing
Cu 1.3GHz, electrop.
polishing before assembly

## Slide 7
Cu electroforming: starting from an internal aluminium mandrel + thin copper coating by magnetron sputtering + electroplating of thick copper + mandrel removal by chemical etching
Electroforming: combining machining, plating and etching
1.3GHz RF cavity with integrated flanges
60 cm
Vacuum chamber (ondulator)
6mm diam, 0.2 mm wall thickness, integrated flanges and stiffener
80cm

## Slide 8
The thickness is uniform
Composition is uniform and correct
Some delay in activation temperature
A. E. Prodromides et al. Vacuum 60 (2001) 35, 41
Combination of different technologies: electroforming, etching,PVD

## Slide 9
Wet surface treatments: copper plating on 3D printed polymers
-in collaboration with EN-MME, TE-MSC polymer lab, EP-DT
-Mock-ups for low power RF testing and design validation
-3D printing in Accura polymer + 30 um copper plating on a pre-layer of chemical carbon based conductor
-complex configuration of electrodes to get a good thickness distribution

## Slide 10
Thank you!
Questions?
Reference persons: Leonel Ferreira, Marc Thiebert
Dedicated sharepoint to submit jobs (after getting access rights) : https://espace.cern.ch/TE-VSC-job-requests/Lists/Surface%20Treatment%202023/AllItems.aspx

## Slide 11
Electropolishing (EP) is an anodic dissolution process that reduces the roughness of a metal surface.
REF
anode
cathode
V
A
+
-
Electropolishing bath, bulk
diffusion domain:
- higher density
- higher viscosity
Anode = cavity surface
convection domain
R1
R2
R1 < R2
Saturated salt/oxide layer
Electropolishing
U
resistance
T = t0