## Slide 1
Thin film coating
Glass & ceramic machining
Optics Quality Control lab
Apprentice's training
General support to DT detector projects
See link=> https://ep-dep-dt.web.cern.ch/thin-film-glass-service
EP-DT Thin Film and Glass Service (TFG)
Jerome Noel
Thomas Schneider
Miranda van Stenis
More than 50 years growing experience
Production
Standard service
R&D
Apprentices & Graduates

## Slide 2
EP-DT-TFG Location
Optical QC lab
(optical spectrometer)
Optical QC lab
(Microscopes)
Clean room with 7 coating devices
Offices
Entrance area with ovens
and gluing facility
Building 3 R
Glass and Ceramic workshop
Entry
Building 108

## Slide 3
EP-DT-TFG Infrastructure
Building 3 R
Entry
Glass & Ceramics Workshop
Gluing area ( Fibre beam monitor)
Chemistry and cleaning
Ovens
laminar flow cabinets for assembly activities (ISO class 5)

## Slide 4
EP-DT-TFG Infrastructure
Optical Quality Control equipment
Keyence VR3000 3D
measurement system (μm)
OGP 3D metrology
Different microscopes
Perkin Elmer spectrometer for spectral/diffuse reflection and transmission (200-900nm)
BRUKER Profile-meter
DEKTAK for measurement in nm scale

## Slide 5
Metrology
VELO Substrate metrology
(Keyence VR3200)
Microchannel planarity measurement after soldering and before place front end components.

## Slide 6
Thin Film Thickness characterization
DEKTAK XT Stylo-meter
(Bruker )
Thin Film Thickness measurement <10nm
Roughness measurement down to few nm

## Slide 7
EP-DT-TFG general support
List of detector groups or users profiting of our infrastructure (~last 5 years):
NA62 Giga Tracker (assembly, cleaning and metrology in cleanroom)
LHCb SciFi (close collaboration, QC tools)
LHCb SciFi/RICH (Carbon filter regeneration)
LHCb SPACAL R&D (fibre machining/prototype assembly)
LHCb Velo (component cleaning/surface metrology)
LHCb Muon (microscopic chamber inspection)
CMS HGCal (large silicon sensor cleaning)
TE-VSC (ceramic machining/spectroscopy)
CAST –CAPP (repair of turning mechanism for cavity)
Student workshop (Optics lab of TFG)
Neutrino platform (PM QE measurements)
BE-BI (Fibre detector production)
ATLAS ITk (cleaning/surface metrology)
DT µ-channel cooling (cleaning/surface metrology)
DT µ-fabrication facilities (cleaning/surface metrology)
Picosec project with RD51 (machining/handling of photocathodes)
The Perkin Elmer spectrometer (UV-VIS) is used by various CERN users
Open lab?!

## Slide 8
EP-DT-TFG coating facilities
PVD thin film coating devices
WLS/Zinc coater
Small CSI coater
Upgrade big production coater (1m diameter)
Big CsI coating unit
Generic coating unit (Balzers 1957!)
New state of the art coating unit

## Slide 9
EP-DT-TFG PVD coating technology
Motivation for vacuum thin film coating:
High purity thin layers <=vacuum environment
Low cost of material <=thin layers with same performance as bulk material
Good reproducibility <=precise control of process parameters
Different kind of technologies available:
Physical Vapour Deposition (PVD):
Resistive
Thermal Evaporation (30th)
  (EP-DT) E-beam
Cathodic
Sputtering (70th)
  (TE-VSC) Magnetron
Chemical Vapour Deposition (CVD)
Thermal vs sputtering
“Thermal evaporation is the more mature technology...it allows coating almost all materials needed for “standard” coating applications”
+high flexibility in substrate material and
geometry
+Also exotic material can be coated (low
temp)
=>Best candidate for R&D device in TFG lab
-need high vacuum level ( ~10-7mbar)
-lower energy coating (packing
density/adherence)

## Slide 10
EP-DT-TFG PVD schematics
concept for uniform large area coating:
Increase distance source –substrate
Rotate substrate
Position source most excentric
Uniformity of layer thickness is key issue

## Slide 11
EP-DT-TFG R&D LHCb RICH Photonic crystal
Two multi-layer samples successfully manufactured.
61 layers 57 layers
SiO2 substrate
Chrome
SiO2
TiO2
SiO2
TiO2
SiO2
TiO2
Coater calibrated with single layer couples of SiO2 and TiO2.
Dissertation Michele Blago 2021

## Slide 12
EP-DT-TFG PVD optical coatings
Optical coatings
Enhanced reflective coatings
Anti reflective coatings
NA62 RICH UV mirror system
Mylar foil coating for NA62 RICH optical feed trough
AR quartz window for LHCb RICH1
Geometer target

## Slide 13
EP-DT-TFG LHCb RICH1 enhanced mirror coating
COATING
The LHCb RICH1 upgrade is certainly the Flagship project of our coating service. Enhanced Reflective coating (Cr/Al/SiO2/HfO2) has been applied to spherical composite substrates (1m diameter)

## Slide 14
EP-DT-TFG PVD coating application
Other light related coatings
Wavelength shifter coatings (WLS)
Photocathode layers (PC)
Compass Thick-gem PC coating (CsI)
PM wavelength shifter coating (TPB)

## Slide 15
EP-DT-TFG PVD coating application
Very reactive coating service along the different test beam Periods. Developed base line recipe:
3.8nm Cr (transparent + conductive)
100nm Cr (outer border region)
18nm CSI (Photocathode layer)
Pico-sec R&D (close collaboration with GDD)
=>
Scale up
=>

## Slide 16
EP-DT-TFG optical Fiber activities
Construction and installation of ATLAS ALFA detector (initially started with lateral fibre coating)
Demonstrator construction for AX-PET
Strongly involved in LHCb SciFi development
Development and construction of 15 Fibre beam monitors for Neutino Platform (collaboration with BE-BI)
Contribution to prototype of E-cal LHCb
Individual fibre polishing for various detector groups (fibre–fin)
Competencies:
Individual fibre polishing
Fibre gluing
Fibre detector construction
Reflective (Al) lateral fibre coating
Fibre end coating

## Slide 17
EP-DT-TFG PVD coating application
Functional layers
Pre-coating of conductive layers
Transparent conductive layers
De-moulding layers
Zinc layer for isotropic radicals
Micro buses de-molding layer (Au)
Conductive layer (Cu) on ceramics
Zinc layer on gold plates for MEDICIS (Medical Isotopes Collection ISOLDE)
Titanium (conductive) spirals on CLOUD UV sabre

## Slide 18
End ?questions? End