## Slide 1: PUMA vacuum system
Jose A. Ferreira
Data contributed by Anke Stoeltzel, Alexandre Obertelli, Alexander Schmidt and Jonas Fischer
14.02.2023

## Slide 2: Introduction
Vacuum requirements at PUMA trap
Cryo-pumping
Isotherm measurements
ELENA vacuum layout
ISOLDE vacuum layout
Summary

## Slide 3: Vacuum requirements at PUMA trap
Langevin cross section (ion-atom interaction) [1]:
[1] X. Fei, Trapping Low-Energy Antiprotons in an Ion Trap., Harvard University, 1990. https://ui.adsabs.harvard.edu/abs/1990PhDT.......101F
Other gases (using same formulas):

## Slide 4: Cryo-pumping
Except H2 and He, all the gases have an equilibrium vapour pressure <10-17 mbar at 4.2K
At 4.2K all these gases can be pumped without limit
H2 and He <1ML for pressure < 10-17 mbar  Adsorption Isotherm
At cryogenic temperature Dubinin-Radushkevich isotherm describes the adsorption process
Open question, is DR isotherm valid at arbitrary low pressure (Henry’s law) [2]?
Ref [3]
[2] J.P. Hobson, Journal of Vacuum Science and Technology 3, 281 (1966)
[3] Handbook of Vacuum Technology, 1st ed. (John Wiley & Sons, Ltd, 2016)

## Slide 5: Cryo-pumping
Low temperature gas adsorption modelled with Dubinin–Radushkevich (DR) isotherm
Available data
  H2 from [4]: T0=209 K ML=0.645×1015 cm-2
  He from [5]: T0=67.8 K ML= 1.27×1015 cm-2
[4] F. Chill, S. Wilfert, and L. Bozyk, J. of Vac. Sci. Technol. A 37, 031601 (2019)
[5] E. Wallén, J. Vac. Sci. Technol. A 15, 265 (1997)

## Slide 6: Cryo-pumping
Low temperature gas adsorption modelled with Dubinin–Radushkevich (DR) isotherm
Available data
  H2 from [4]: T0=209 K ML=0.645×1014 cm-2
  He from [5]: T0=67.8 K ML= 1.27×1015 cm-2
[4] F. Chill, S. Wilfert, and L. Bozyk, J. of Vac. Sci. Technol. A 37, 031601 (2019)
[5] E. Wallén, J. Vac. Sci. Technol. A 15, 265 (1997)

## Slide 7: Cryo-pumping H2
COMSOL model: PH2=10-11mbar
Acceptable antiproton lifetime in reservoir trap and collision trap
After 100 days almost no degradation
Target the lowest achievable pressure at the entrance of the trap

## Slide 8: Cryo-pumping He
COMSOL model: PHe=10-11mbar
Acceptable antiproton lifetime in reservoir trap and collision trap
After 7 days almost no degradation
Acceptable level 2×higher than H2

## Slide 9: Isotherm measurements
Option 1: Isosteres (pressure over temperature scans at a constant coverage)  several isosteres can be used find the fit parameters of adsorption isotherm models
Option 2: Gas propagation at constant sample temperature with a continuous injection  can be used to test the isotherm parameters in simulations and reproduce the gas propagation
[6] A. Stöltzel, Sub-monolayer adsorption isotherms and gas propagation of H2 and He in cryogenic copper tubes. https://indico.cern.ch/event/1129799/#1-gas-propagation-in-cryogenic

## Slide 10: Isotherm measurements: Hydrogen
Dubinin–Radushkevich (DR) isotherm
Measured values:
T0=204.7 K ML= 2.67×1015 cm-2
From [4] T0=209 K ML= 0.645×1015 cm-2
Values used for simulations are coherent with last measurements  Monolayer coverage more conservative

## Slide 11: Isotherm measurements: Hydrogen
Dubinin–Radushkevich (DR) isotherm
Measured values:
T0=204.7 K ML= 2.67×1015 cm-2
From [4] T0=209 K ML= 0.645×1015 cm-2
Values used for simulations are coherent with last measurements  Monolayer coverage more conservative

## Slide 12: Isotherm measurements: Helium
Dubinin–Radushkevich (DR) isotherm
Measured values:
T0=74.8 K ML= 1.72×1015 cm-2
From [5] T0=67.8 K ML= 1.27×1015 cm-2
Values used for simulations are coherent with last measurements

## Slide 13: Isotherm measurements: Helium
Dubinin–Radushkevich (DR) isotherm
Measured values:
T0=74.8 K ML= 1.72×1015 cm-2
From [5] T0=67.8 K ML= 1.27×1015 cm-2
Values used for simulations are coherent with last measurements

## Slide 14
Cold shutter to reduce gas flow when not in operation [8]
Carbon coating to increase the number of sites ×100 [7]
[7] R. Salemme, et al. "Vacuum Performance of Amorphous Carbon Coating at Cryogenic Temperature with Presence of Proton Beams.“ (IPAC'16), Busan, Korea, May 8-13, 2016
[8] A. Obertelli et al. PUMA, SPSC report on the activities of 2022

## Slide 15: ELENA vacuum layout
ELENA: At the end of LNE51
Pressure at transfer lines ≈10-10 mbar range
Pressure ring <10-11 mbar

## Slide 16: ELENA vacuum layout
PUMA trap
ELENA ring
LNE50
LNE51 (CERN)
PDT and instrumentation
Offline ion source (RFQ)
Handover point
NEG coatings
≈5×10-11 mbar
≈1×10-11 mbar
≈6×10-11 mbar
≈1.5×10-11 mbar

## Slide 17: ELENA vacuum layout
PUMA trap
ELENA ring
LNE50
LNE51 (CERN)
PDT and instrumentation
Offline ion source (RFQ)
Handover point
NEG coatings
Measured ≈5×10-11 mbar
≈1×10-11 mbar
≈6×10-11 mbar
≈1.5×10-11 mbar

## Slide 18: ELENA vacuum layout
COMSOL model to validate assumptions for last chamber
OG of sector valves 3×10-9 mbar×l/s
NEG coating sticking factor 0.008
H2 injection results vs simulation
≈1×10-11 mbar
≈1.8×10-11 mbar
≈1×10-10 mbar

## Slide 19: ELENA vacuum layout
PUMA trap
ELENA ring
LNE50
LNE51 (CERN)
PDT and instrumentation
Offline ion source (RFQ)
Handover point

## Slide 20: ISOLDE vacuum layout
RC6

## Slide 21: ISOLDE vacuum layout
RC6 beam line
Paul trap
Ion source
MR-TOF
Handover point
Three sections, ISOLDE, unbaked all metal seals, baked section
The line is under definition
Vacuum system still to be optimized. Some gas sources still to be defined (i.e. diagnostics with limited baking temperature)
Main challenge: pump Helium injected in Paul’s trap

## Slide 22
ASACUSA
LNE.VGPB.0643
Example Helium propagation

## Slide 23
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
Example Helium propagation

## Slide 24
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
Example Helium propagation

## Slide 25
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
LNS.VGPB.0030
Example Helium propagation

## Slide 26
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
LNS.VGPB.0030
LNE.VGPB.0002
Example Helium propagation

## Slide 27
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
LNS.VGPB.0030
LNE.VGPB.0002
LNR.VGPB.0411
Example Helium propagation

## Slide 28
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
LNS.VGPB.0030
LNE.VGPB.0002
LNR.VGPB.0411
Example Helium propagation

## Slide 29
ASACUSA
LNE.VGPB.0643
LNE.VGPB.0608
LNE.VGPB.0020
LNS.VGPB.0030
LNE.VGPB.0002
LNR.VGPB.0411
≈ 20 m between the experiment and the ring
XHV machine not well suited for He pumping (chemical pumping)
7 times higher pressure at ELENA
>20% beam lost
Example Helium propagation

## Slide 30: ISOLDE vacuum layout: MIRACLES at LA2
LA2

## Slide 31
Injection optics
Paul trap (300K)  10-2 mbar
2-keV extraction
Quadrupole bender
Offline ion source
30 deg bender
Reacceleration
2 keV  50 keV
MR-ToF mirror
Optical detection region
MR-ToF mirror
Laser
ISOLDE vacuum layout: MIRACLES at LA2

## Slide 32: ISOLDE vacuum layout: Helium propagation
Paul trap at 10-2 mbar
Gas propagation along the line  ≈7×10-9 mbar at hand over point
Simulation to be cross checked with in situ measurements

## Slide 33: ISOLDE vacuum layout
For the design of ISOLDE line main problems to address are outgassing and Helium propagation
Pumping He will require turbopumps (with high compression). Areas with high throughput and areas with limited ultimate He pressure (type of primary pump? ballast? Small booster TMP to increase compression ratio?)
[3] Handbook of Vacuum Technology, 1st ed. (John Wiley & Sons, Ltd, 2016)

## Slide 34: Summary
Cryo-pumping concept validated by isotherm measurements. Mitigations (increase number of sites and cold shutter) will help to address the unknown behaviour at very low pressures
ELENA beam transfer line almost completed
Cross in front of PUMA trap validated against previous assumptions
ISOLDE beam line under definition.
Helium propagation can be an issue difficult to handle. Consider positions for extra pumping may be required along the line
Benchmarking of the simulations of MIRACLS at LA2 will help to define the pumping required in the line

## Slide 35: Thank you!