## Slide 1
High Gradient and Q-factor SRF Performance at 1.3 GHz and 650 MHz
Daniel Bafia
IMCC’23
June 21st, 2023

## Slide 2: Introduction to Bulk Nb SRF Cavities
Nb SRF cavities: most efficient engineered EM resonators ever created
Mature, proven technology
  LCLS-II + HE
  EXFEL
RF power injected at resonant frequency
Performance governed by microscopic properties within the first ~100 nm from inner surface
650 MHz – 9 GHz

## Slide 3: Surface Engineering of Nb SRF Cavities
Goal of SRF research: tailor surface properties via chemical and baking treatments to yield high Q0 and Eacc
  Higher Q  lower cryogenic costs
  Higher gradient  less $$$ OR higher energy
f0 = 1.3 GHz
T = 2 K
Nb SRF Cavities Post State-of the-Art Surface Treatments

## Slide 4: “2/6” Nitrogen-Doping Treatment
Nb
Slide adapted from M. Martinello
800C UHV, 3 hours
800C UHV, 6 minutes
UHV cooling
5 um EP
N
Final RF Surface
800C UHV, 6 minutes
UHV cooling
5 um EP
800C N2
p = 25 mTorr 2 minutes
800C N2
p = 25 mTorr 2 minutes
N Interstitial
NbxNy
6/19/2023
Depth profile of Nitrogen impurities
Instead of N, recently learned that we can use O!

## Slide 5: Outline
Introduction to SRF
Fundamental R&D Toward Improving Bulk Nb SRF Cavity Performance
  Key Materials Science findings
  Optimizing 1.3 GHz cavity performance
  Applying findings to 650 MHz cavities
  Optimizing EP for 650 MHz
Key Technological Advancements Towards High Gradients
  +50 MV/m recipe: cold EP + 2-step low-temp bake
  Extending gradients further with the traveling wave design
  Plasma processing
Conclusions

## Slide 6: Coupling RF and Material Studies to Improve SRF Cavities
A. Romanenko, TTC’2020, CERN
EP
LTB
TOF-SIMS Data on Cavity Cutouts
RF Data on Variously Processed Cavities to be Cut
A. Romanenko et al., SRF’19, THP014
Material science is critical to understand sources of improved SRF cavity performance
Identified O as a key impurity in enabling high gradients and Q in cavities
Can we tune cavity performance by tailoring O impurity profile?

## Slide 7: Tuning Cavity Performance with Oxygen Impurities
Single cavity subjected to sequential baking and RF testing to study the evolution of cavity performance
O diffusion: ability to tune between high Q0 or high gradient!
Q vs E Evolution with Increasing O Diffusion
D. Bafia et al, Proceedings of SRF’2021, THPTEV016
2K
1.3 GHz
One key parameter:

## Slide 8: Optimizing Cavity Q0 By Tailoring O Impurity Profile
Maximizing Q0 requires minimizing RBCS
Gradually introduced more oxygen into the RF surface of cavities and tracked RBCS evolution
  100+ cavity RF tests
2 K
1.3 GHz
D. Bafia, TTC’22

## Slide 9: Optimizing Cavity Gradient by Tailoring O Impurity Profile
D. Bafia, TTC’22
Gradually introduced more oxygen into the RF surface of cavities and tracked quench
Found a peak in quench field when oxygen diffuses 46 nm!
Quench Peak
Mid-T Bake data comes from S. Posen et al., PRA 13, 014024 (2020)
f0 = 1.3 GHz

## Slide 10: Application of Quench Peak Findings to 650 MHz Cavities
Subjected a 650 MHz cavity to a surface treatment which introduced O to a depth of 46 nm
From 1.3 GHz studies expect high quench field:
  We achieved get 44 MV/m!
Quench optimization studies on 1.3 GHz are applicable to 650 MHz
Non-optimal electropolishing likely limiting performance
Near record quench in 650 MHz!
D. Bafia, LCWS’23

## Slide 11: Improving 650 MHz Performance Further via Optimized EP
Proper electropolishing (EP) is critical in enabling excellent cavity performance
  Smooth surface, minimal uptake of H
Developed a novel cathode and optimal EP parameters for 5-cell 650 MHz cavities for PIP-II
V. Chouhan, to be presented at SRF’23
Cathode Structure
Patented
Optimized design and parameters yields unprecedented performance in high-β 650 MHz EP’d cavities!
f0 = 650 MHz

## Slide 12: Outline
Introduction to SRF
Fundamental R&D Toward Improving Bulk Nb SRF Cavity Performance
  Key Materials Science findings
  Optimizing 1.3 GHz cavity performance
  Applying findings to 650 MHz cavities
  Optimizing EP for 650 MHz
Key Technological Advancements Towards High Gradients
  +50 MV/m recipe: cold EP + 2-step low-temp bake
  Extending gradients further with the traveling wave design
  Plasma processing
Conclusions

## Slide 13: New Cold EP + 2-Step Low-Temp Bake Enabling 50 MV/m
Transferred recipe to 9-cell cavities as part of ILC Cost Reduction effort
Average Eacc = 40.4 MV/m!
Ultra-high gradients of 50 MV/m!
Confirmed by other labs!
+
Cold EP
=
1-cell cavity
9-cell cavities
Grassellino et al. https://arxiv.org/abs/1806.09824
Courtesy of S. Posen

## Slide 14: Extending Gradients Further with the Traveling Wave Design
Standing wave Nb cavities limited Eacc by Hsh
Alternative: Niobium traveling wave structure
  RF power returned via feedback Nb waveguide  Lowers peak fields in cavity
  Possible to achieve Eacc > 70 MV/m!!
Current Status:
1-cell: designed, treated (BCP), and tested
  Achieved 26 MV/m in RF testing
3-cell: designed and treated (BCP)
  Tuning just completed
  RF testing scheduled for this summer
  TW operation demonstrated at room temp!
0.5 m structure currently being designed in collaboration w/ Cornell
V. Yakovlev, LCWS’23
*Euclid Techlabs DOE SBIR DE-FG02-06ER84462 and DE-SC0006300.

## Slide 15: Plasma Processing Applied to LCLS-II-HE vCM
RF test after plasma processing demonstrated that:
vCM performance is preserved
Plasma processing did not introduce any contamination: vCM still FE-free
Plasma processing can also eliminate multipacting:
Possible to address both FE and MP in situ in CMs  decreased CM testing and commissioning time, increased reliability during machine operation
B. Giaccone, et al. arXiv:2201.09776 (2022)
Plasma processing procedure for 1.3GHz CMs is fully validated
S. Posen et al. PRAB 25, 042001 (2022)

## Slide 16: Conclusions & Future Directions
Bulk Nb SRF cavities are a mature, ready-to-go technology for use in a muon collider
Recent advancements in R&D push the limits of cavity performance
Impurity tailoring enables tuning cavity performance for high gradient or high Q
Electropolishing optimization shown to extend gradient reach
Cold EP + 2-step baking yields gradients above 50 MV/m
Initial traveling wave cavity demonstrate promising results, opening the door to > 70 MV/m
Plasma processing enables in situ mitigation of FE and MPing in CMs

## Slide 17: Thank you for your attention!