## Slide 1
Sergio Calatroni – CERN
With contributions from many Collaborators
Prospects of Cryo-Cu and HTS high gradient RF cavities

## Slide 2: Motivation
Muon cooling system requires RF cavities operating at high-gradient AND in a strong magnetic field.
Normal conducting copper, possibly cryo: see next talks
Superconducting: High-Temperature Superconductors (HTS) ?

## Slide 3: Outline
HTS cavities in a strong magnetic field
HTS cavities at high-gradient
HTS cavities in both strong field and high-gradient
Future steps

## Slide 4: Outline
HTS cavities in a strong magnetic field
HTS cavities at high-gradient
HTS cavities in both strong field and high-gradient
Future steps

## Slide 5: Reference case
Typical SRF accelerator cavities are made of niobium
Effect of external magnetic field on SRF accelerating cavities is mostly due to flux pinning, weak pinning in bulk Nb and strong in Nb/Cu
Niobium critical field Hc2 < 1 T, superconductivity is lost at higher fields
Strong magnetic shielding needed
Limited or no magnetic shielding

## Slide 6: Some theory background: fluxon motion in RF
The motion of the rigid fluxon lattice behaves as a harmonic damped oscillator
(neglecting thermal creep)
The “depinning frequency”
Gittleman and Rosenblum: Phys Rev. Lett. 16, 734 (1966)
Calatroni and Vaglio, IEEE Trans. Appl. Supercond. 27 (2017) 3500506
Coffey, Clem PRL 67, 386 (1991)
Brandt PRL 67 2219 (1991)
Silva et al, PRB 78, 094503 (2008)
d
Chart: 
Pinning centers
B field is normal to surface: worst case
Surface resistance

## Slide 7: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Jc may vary of orders of magnitude.
Hc2 has much smaller variation.
YBCO most promising candidate
NbTi – NbTiN possible candidates at B < 10T
Nb3Sn for B < 15 T

## Slide 8: Validation of RF performance (UPC - ICMAB)
In house developed 8.05 GHz cavity resonator compatible with 25mm bore 9 T magnet at ICMAB
REBCO CCs outperform Cu at 50K and up to 9T
RS is microstructure dependent
Puig et al, SuST 32, 094006 (2019)
Surface currents equivalent to 0.1 MV/m of a typical accelerating cavity

## Slide 9: HTS coated conductor soldering and delamination
Ag
Substrate
Buffer layers
Ag
REBCO
Cu
Surface to coat
Cu
Solder
Cu
Ag
REBCO
Surface to coat
Cu
N. Lamas et al., to be published
Developed in the context of FCC-hh impedance reduction by coating the beam screen with HTS tapes

## Slide 10: First real cavity, f9 GHz
We have developed a technology for applying 2D HTS tapes to 3D RF “RADES” cavities demonstrating the potential of HTS for RF applications J. Golm et al., IEEE TAS, Vol. 32, No. 4, (2022) 1500605
2x improvement of RF quality factor compared to copper
(newer prototype 5x improvement)
RADES cavity for axion searches
12 mm-wide HTS tapes

## Slide 11: Scaling to lower frequency
REBCO scaled to 1 GHz at 50 K
x100 improvement over Cu at 50 K
Romanov et al, SciRep 10:12325 (2020)
For HTS Rs scales as
For Cu Rs scales as
GHz
38x12 mm samples
50 mm bore
16 T
at all frequencies
A parallel-plate resonator is being commissioned to test samples at ~1 GHz
Will demonstrate real experimental frequency scaling on samples

## Slide 12: Outline
HTS cavities in a strong magnetic field
HTS cavities at high-gradient
HTS cavities in both strong field and high-gradient
Future steps

## Slide 13: Potential motivation: linear colliders
Linear collider studies fall essentially in two categories
Linear collider studies result in roughly similar power consumption for equivalent machines (ie ILC vs CLIC)
We want to see if HTS in pulsed RF mode allows an optimal gain compared to both Nb and Cu
Superconducting niobium, CW
Normal conducting copper, pulsed

## Slide 14: Cryo-cooled copper -> HTS ?
The C3 study aims at cryogenically cooled copper, to attain a larger gradient and save cost in the RF power stations
A further advantage could come from combining the advantage of higher gradients at lower temperatures, with the higher Q factor of HTS coatings -> energy efficiency
E. Nanni et al., PRAB 24, 093201 (2021)
SRF temperature | Ratio W300K/Wcryo
77 K | 13
50 K | 20
4.2 K | 230
1.9 K | 920
Cryoplant efficiency (Carnot + engineering)
Thanks to T. Koettig, CERN
A factor x10 improvement in Q factor compared to copper could pave the way for significant energy savings

## Slide 15: Low-power measurments
A potential improvement at least x10 compared to copper (Rs=8m) has been measured on samples of tapes (8 GHz) at low RF power
(adapted from Romanov et al, Sci. Rep. (2020) 10:12325)
Cu

## Slide 16: HTS tape at 8 GHz (dielectric resonator)
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 17: Literature review - I
There are very few measurements on HTS at high RF currents (mostly microstrip resonators). But physics is proven.
~1011 A/m2 RF current (microstrip resonator, 200 µm, 350 nm thick, 8 GHz)
Powell et al. Journal of Applied Physics 86, 2137 (1999)
For 1 µm thickness this is equivalent to 105 A/m ( 0.1 T  25 MV/m)
in the “high-gradient” range

## Slide 18: Literature review - II
From: M. Hein, “High-Temperature-Superconductor Thin Films at Microwave Frequencies” (Springer Tracts in Modern Physics, 155)

## Slide 19: High-gradient testing at SLAC – supported by I.FAST IIF
Demountable high-power RF cavity
Can achieve Hpeak of about 360 mT using 50 MW XL-4 Klystron.
High-Q X-band hemispheric cavity with a TE032-like mode at 11.4 GHz.
Zero E-field on the sample
Maximum H-field on the sample
Sample accounts for ⅓ of total cavity loss
Goal: demonstrate high-gradient pulsed operation of HTS, at cryo-temperatures, and develop large size coatings (50 mm wide tapes)
HTS-coated sample
By CERACO
HTS-coated with tapes
By CSIC-ICMAB

## Slide 20: First results at SLAC
Cu and Nb reference measurements
HTS measurements
High-gradient tests foreseen shortly

## Slide 21: First device validation – supported by I.FAST Innovation Fund
Device approach: X-band pulse compressor (SLAC) as first “real” device
Coated with small tapes by CSIC-ICMAB for device validation
Future goal: full device with large-size tapes (or directly coated on copper, ideally)
Max surface field 3.126 MA/m
Courtesy Greg LeSage, SLAC

## Slide 22: Outline
HTS cavities in a strong magnetic field
HTS cavities at high-gradient
HTS cavities in both strong field and high-gradient
Future steps

## Slide 24: Outline
HTS cavities in a strong magnetic field
HTS cavities at high-gradient
HTS cavities in both strong field and high-gradient
Future steps

## Slide 25: Possible test in a dedicated RF stand
See talk of Dario Giove later today
Availability of a high-field / high-gradient test stand foreseen within the MuCol study could be beneficial for the entire HTS-HFF community
SC HTS coils
Pillbox test cavity
RF Wave guide
Sc magnet/cryostat sketch by M. Castoldi & Stefano Sorti, UMIL & INFN-LASA
(RF drawing by Guillaume Ferrand –CEA)

## Slide 26: Possible practical implementation of HTS tape-coated cavities
How could a future cavity look like? Bimetallic cavities
J. Haimson, WEPMS085, PAC07 (s.steel inserts)
CLIC Mo-iris prototype
P. McIntyre et al., IEEE TAS 19 (2009) 1380
Composite cavities exist and have been demonstrated.
Joints at low-current regions are standard practice even in SRF cavities (ie QWRs)
Segmentation at zero-current region is possible, see device being designed at SLAC
SC
NC
B

## Slide 27: Final remarks
No data for HTS at high-gradient and in strong magnetic field exist (either samples or cavities): experiments needed
Overall energy efficiency would have to be studied, taking into account: operating temperature, cryo-efficiency, possible Q-factor, pulsed operation
Fabrication technologies for real cavities have to be assessed: wider soldered tapes, or develop a direct HTS coating technique?

## Slide 29: Effect of magnetic field: fluxon losses in RF
Surface resistance, reactance due to vortex motion
To maximize f0 and minimize fluxon losses we need high Jc materials
“safe” zone
“unsafe” zone

## Slide 30: HTS for the FCC-hh beam screen
Recent work motivated by the need of HTS materials for replacing copper in the FCC-hh beam screen, to reduce beam coupling impedance.
Beam produces RF fields
Extremely challenging requirements:
  HTS must operate at 50 K and 16 T
  Critical fields Hc2 , Hirr >> 16T
  Jc > 25 kA/cm2 (2.5x108 A/m2)
  Surface resistance Rs better than for copper
Compatible with accelerator environment
  Minimize dipole field distortion due to persistent currents (Note 1)
  UHV compatible, low SEY, lifecycle assessment, etc..
16 Tesla !
Calatroni, IEEE TAS 26, 3500204 (2016)
Calatroni et al, SuST 30, 075002 (2017)

## Slide 31: How to make it in practice ?
Coat the inside of the screen
with Tl-1223 films
Manufacture the screen using REBCO tapes soldered to the screen

## Slide 32: Zoo of superconductors
https://nationalmaglab.org/magnet-development/applied-superconductivity-center/plots
Pinning force

## Slide 33: Predicted surface resistance of HTS in 16 T field
YBCO | Tc=92K | T=50K | B0=16T | Jc(50,16)=7.5x109Am-2 | Bc2(50)=40T | n=60cm | f0=10GHz
Tl-1223 | Tc=125K | T=50K | B0=16T | Jc(50,16)=1x1010Am-2 | Bc2(50)=80T | n=80cm | f0=14GHz
For HTS the Rs scales as
For Cu the Rs scales as

## Slide 34: Cryogenic losses: SRF aimed at energy saving compared to NRF
Carnot efficiency
Cryoplant efficiency
30%
Power consumption for 1 W @ 77 K | 13 W
Power consumption for 1 W @ 20 K | 50 W
Power consumption for 1 W @ 4.2 K | 230 W
Power consumption for 1 W @ 1.9 K | 920 W
Thanks to T. Koettig, CERN

## Slide 35: Test of Nb3Sn films up to 12 T
15 GHz

## Slide 36: HTS coating technologies
Patrick Krkotic, PhD dissertation, UPC Barcelona 2022

## Slide 37: INFN: NbTi and NbTiN cavities for axion searches
x10 improvement over copper at 4.2 K

## Slide 38: Nb3Sn @ 3.9 GHz in strong magnetic field: FNAL results
Ideally, Nb3Sn from vapor tin diffusion should then be compared to Nb3Sn from sputtering
Cigar-shaped cavity 3.9 GHz
1-cell ILC type 3.9 GHz
S. Posen et al. ArXiv 2201.10733

## Slide 39: NbTi / NbTiN and Nb3Sn at high RF field
NbTi 500 MHz
NbTiN 500 MHz, 4.2 K
S. Calatroni et al., Proc of the SRF 91
S. Posen – FNAL (TTC 2019 talk)