## Slide 1: The construction of the prototypes and series of the HOCM
LASA – Feb 17th 2022
Marco Statera and Marco Prioli
on behalf of the LASA team
INFN Milano - LASA

## Slide 2: OUTLINE
Scope: the High Order correctors magnets
Highlights from EM and mechanical design
Highlights of prototypes and series production
Selected results
Conclusions

## Slide 3: SCOPE - High Order Correctors
The INFN-LASA follows the design, construction and test of the 5 prototypes of the High Order (HO) corrector magnets for the HL interaction regions of HL-LHC. KE2291
The INFN-LASA follows the series production of the 54 HO corrector magnets for the HL interaction regions of HL-LHC. KE3085
INFN delivers the magnets, the vertical test of all magnets, and collaborates to the integration in the cold mass by CERN

## Slide 4: THE LOW BETA SECTION and the High Order Correctors
~70 m
a2
b6
a6
b5
a5
b4
a4
b3
a3
By H. Prin

## Slide 5: SUPERFERRIC DESIGN
NbTi coils
Racetrack
Insulation by S2 glass reinforced material
Superferric design
Compact and modular
Strong contribution of the iron poles
Field quality influenced by the shape of the poles
Quench protection
No energy extraction (but 4P)
60% margin @ 1.9 K
magnet | Integrated strength | Ic @ 4.2 K | Margin @4.2 K | Margin @1.9K
4P S | 0.700 Tm | 315.5 A | 42.3 % | 57.1 %
6P | 0.095 Tm | 225.5 A | 53.4 % | >60 %
8P | 0.069 Tm | 230.2 A | 54.4 % | >60 %
10P | 0.037 Tm | 255.7 A | 58.9 % | >60 %
12P N | 0.086 Tm | 232.6 A | 54.9 % | >60 %
12P S | 0.017 Tm | 230.2 A | 54.4 % | >60 %
Longitudinal dimension
Quench protection
Small dimension: 84 kN series production mass (54 magnets)
constraints
First superferric magnets in a high energy accelerator

## Slide 6: HO Corrector Magnets Zoo
a5
b5
MCDXF
a6
b6
MCTXF
a3
b3
MCSXF
OD320
a4
b4
MCOXF
MQSXF
OD460
a2
Design
Construction & Test
5 prototypes
54 series magnets
6P 8P 10P +50% Bdl
Round Coil Superconducting Magnet
MgB2demonstrator
Prototypes tested 2016-2020
Geometrical lengths:
200 mm - 265 mm
12P, S4P: 540 mm – 580 mm

## Slide 7: MECHANICS
pole shape
coils
ARMCO
iron
non magnetic
wedges
modifed ideal n= 2; 3
maximum area n > 3
ideal shape
pole
flux return plates
Racetrack coils
sketch by G. Volpini
3D modelling of the coils for stress managenment
wedge
coil
a.u.
Wedges prestress
Avoid movements/falling
1D model

## Slide 8: ASSEMBLY
Procedure developed at LASA on prototypes
6P, 8P, 10P assembled at LASA
12P and 4P assembled in industry
lamination
alignment frame
bridge
upper PCB
lower PCB
PCBs fixing
Pole laminations
Inner CuBe rods-loading
Coils centering and fixing
Connections
Final laminations
Outer CuBe rods-loading
CuBe rods
coil
wedge
Longitudinal support

## Slide 9: Prototypes
Sextupole Octupole and Decapole
Coils production and assembly at LASA
Normal Dodecapole and skew Quadrupole
Coils production and assembly in SAES Rial Vacuum
8P test
First components QC
Sextupole assembly
Skew Quadrupole handling in SRV

## Slide 10: The Electrical Connections
The coils are connected in series
Duratron disks
copper thick laminations (1 mm)
Duratron support disk
Printed Circuit Boards
Thin Cu on PCBs
PCB box
On duratron columns

## Slide 11: Coils
Racetrack, same design, but 6 families
Single wire up to 750 turns
External S2 reinforced material
Production learning curve in industry
QA at in industry during production
130 mm
498 mm
457 mm
Machined from bulk
out
1.0 mm
0.15 mm
sheet
insert
1.5 mm
in

## Slide 12: The Load Lines
What happens if something goes wrong?
6P, 8P and 10P may be installed as normal or skew
Many designs, one wire
Different designs, same protection scheme
Except for the skew quadrupole
Working point
4P working point
Analysis by Sorbi-Prioli-Mariotto
Mitigation: input wire additional protection layer

## Slide 13: COILS
Racetrack, same design, but 6 families
Single wire up to 750 turns
External S2 reinforced material
Production learning curve in industry
QA at in industry during production
130 mm
498 mm
457 mm

## Slide 14: QC coils
Produced coils 508
29 NC (6%)
QC developed by LASA
Measurements in industry
The number of turns is checked through a custom measurement setup
Surge test at V0 = 2 kV to detect internal insulation defects
Voltage to ground tests
Mechanical dimensions
Learning curve
Percentage of conform coils vs produced coils
Inter-turn short
One turn less

## Slide 15: Major Design iterations
Wedges additional supports fixed by spring washers to improve wedges stability in octupoles and quadrupoles 4P and 8P
Splices mechanical protection box

## Slide 16: Status of Production and test (magnets)
Produced magnets
Legend
done/tested
Test ongoing
re-assembly
Coils produced at SAES Getters Lainate (Milano, I)
Last coils delivered in July 2021
Magnets Assembled at SAES Rial Vacuum (Parma, I)
Last 10 produced magnets delivered to LASA in Oct 2021
End of tests Feb 2023
1 batch
½ production
100%

## Slide 17: The test station at LASA
Four HO correctors cooled at 4.2 K
  Each magnet powerd individually
  Magetic Measurements
Power converter 600 A
  Dump resistance 1 W or 1.5 W
  IGBT polarity switch by LASA
  IGBT for quench protection
Field probe for the series by CERN
  Each magnet measured individually
  No cross talk

## Slide 18: Test results
Powering (M. Prioli)
Training (both polarities)
Endurance test 1h at ultimate
Magnetic field measurement
(E. De Matteis, S. Mariotto)
Field integral 1% to 3% wrt simulations
Field integral reproducibility <0.1%
Field quality high reproducibility
Transfer function very good agreement with simulations, high reproducibility
Quenched coil recostruction via Magnetic Measurements (S. Mariotto)
By R. Valente
Round Coil Superconducting Magnet
2 MgB2 coils
Reached 230 A (1.5 Inom)
96 Thermal cycles
See 3LOr2B-02
S. Mariotto

## Slide 19: Training in last 12 months

## Slide 20: Magnetic Measurements Example
Allowed harmonics 100 U
Integrated field repeatibility 0.1% at nominal current
Second assembly repeatibility 0.05%(measured)
Integrated field simulated vs measured 2% or lower for all HO correctors
Calculated
Reproducibility 0.2%
The measurement of the 12p was a challenge

## Slide 21: Quenched Coil(s) Measurement
Superconductors get magnetized during operation due to the Persistent Screening Currents in the filaments of the conductors
Transition to normal resistive state cancel the magnetization
Quenched coils will not have residual magnetization
Post quench fourier analysis of the remnant magnetic field
S. Mariotto and M. Sorbi. SuST, 35(1):015006, nov 2021.
Multiple coils quench in quadrupole observed
The system is able also to localize quench coils in multiple ways:
Shape of Flux is different
Harmonics Amplitude depends by:
  Number of quenched coils.
  Position of the coils.
Harmonic Phase combination reconstruct uniquely the different quenched coils
1
4

## Slide 22: Integration
Mechanical integration
Assembly in building 180, CERN by H. Prin
Alignment measurement by C. Petrone
More in next presentation by E. Gautheron
by E. Todesco
9 correctors alligned
beampipe
46 HO Correctors
delivered to CERN

## Slide 23: Integration
Mechanical integration
Assembly in building 180, CERN by H. Prin
Alignment measurement by C. Petrone
More in next presentation by E. Gautheron
by E. Todesco
9 correctors alligned
beampipe
46 HO Correctors delivered to CERN
MCDXF01 first test in Jul 2020

## Slide 24: CONCLUSIONS
The HL-LHC corrector design is solid
Construction of 54 HO Correctors in industry
All HOC are powered at cold, 54 magnets have been successfully tested
Magnetic Measurements are performed
The results are very reproducible for each family with a good agreement with simulations
An innovative quench recostruction method has beed developed
The integration in the first cold mass started
First superferric magnets in a high energy collider

## Slide 25
LASA team
F. Broggi, E. De Matteis, S. Mariotto, A. Paccalini, A. Pasini, D. Pedrini, A. Leone, A. Palmisano, M. Prioli, M. Sorbi, S. Sorti, M. Statera, M. Todero, R.U. Valente
CERN
E. Gautheron, A. Musso, E. Todesco
SAES Getters and SAES Rial Vacuum
F. Gangini, P. Manini, C. Santini,
M. Canetti, M. Campaniello, A. Zanichelli
THANK YOU