## Slide 1: Nanostructured photocathodes development
Overview and link to breakdown studies.

## Slide 2: Electron Sources
1
Types of electron sources:
Thermionic emitter
Field emission gun
Photoemission cathodes
Notes: Electron sources have become a common day application. Used in every day application, such as a microwave oven, or in something complicated, like an accelerator!
There are essentially three main electron sources. Thermionic, which requires the heating of a filament to release electrons and is a common source. There is also field emitter, which you all are very farmiliar with already... There is also photocathodes, which is the focus of this talk!

## Slide 3: Basic Physics Behind Photoemission
1
Figurex : Taken from [1]
Three step model:
Photon absorption
Electron migration
Potential barrier esape
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.

## Slide 4: Basic Physics Behind Photoemission: Three Step Model
1
is reflectance
= available states at energy
occupied states at energy = scattering probability depending on wavelength and angle
Equation can be greatly simplified, but is just important you know it exists
Notes: REMEMBER TO MENTION THE ASSUMPTION OF THE MODEL

## Slide 5: Basic Physics Behind Photoemission: Fowler Dubridge
1
Fowler Dubridge assumptions:
Fermi-Dirac distribution
Uniform momentum space distribution
Photon absorption is independent on the electron’s initial energy state
Only the normal momentum is affected
Escape is possible if the normal momentum is larger than the work function
material constant
refletivity
120 A/cm2/K2
temperature
Fowler’s function
work function
boltzmann constant
laser energy
Notes: REMEMBER TO MENTION THE ASSUMPTIONS OF THE THEORY

## Slide 6: Basic Physics Behind Photoemission: Quantum model
1
Interesting model trying to explain what happens in the limit between photoemission and field emission
The different electrons can tunnel or reflect when they hig the boundary
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.

## Slide 7: Basic Physics Behind Photoemission: Quantum model
1
From this, different probabilities for processes can be found
0> multiphoton absorption
0= tunneling
0< n multiphoton emission
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.

## Slide 8: Basic Physics Behind Photoemission: Materials
1
Negative Electron Affinity
Metal
Two main groups
Semiconductor
Positive Electron Affinity
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.
Figures taken from [4]

## Slide 9: Basic Physics Behind Photoemission
1
Negative Electron Affinity
Metal
Two main groups
Semiconductor
Positive Electron Affinity
Materials:Cs2Te, K2CsSb, Cs3Sb
Quantum Efficiency: High
Lifetime: Short
Wavelength: Visible
Emitance: High
Vaccum sensitive: Yes
Materials: Cu, Mg Quantum Efficiency: Low
Lifetime: Long
Wavelength: UV
Emitance: Low
Vaccum sensitive: No
Materials: GaAs, GaN,AlGaN Quantum Efficiency: High
Lifetime: Short
Wavelength: Visible
Emitance: High
Vaccum sensitive: Yes
OBS! Needs an activation layer to lower the potential barrier!
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.

## Slide 10: Photocathode used at CERN
1
Figurex : Taken from [3] and [2] and [5]
At CERN: Cs2Te (PEA) photocathode.
Quantum efficienty of ~10%
Requires good vacuum and
Cannot be exposed to atmospheric conditions.
Want to move on to pure copper (metal) cathodes.
Notes: Electrons are struck with a photon, giving them energy. Thereafter, the electron has to move towards the surface without collision not to lose its additional energy At the last step, it must have enough energy to escape the potential barrier it is facing.
Several other theories exist to this day, like Fowler Dubridge and also newer quantum mechanical models regarding photoemission.

## Slide 11: Laser Induced Periodic Surface Structure (LIPPS)
3
Ultra fast lasers
Surface plasmons
Surface structures
Increased QE
Not caused by LIPPS pattern!
Caused by nanospheres!
Notes: By employing ultra fast lasers onto the surface of the metal, surface plasmons are induced, leading to periodic structures

## Slide 12: Laser Induced Periodic Surface Structure (LIPPS)
4
Small nanospheres occured as a bi- product.
Gives off a field enhancment generating hot electrons!

## Slide 13: Laser Induced Periodic Surface Structure (LIPPS): Potential LES studies
4
Structuring LES cathode
Test field emission form nanospheres
Can make distinguish between photo and field emission
Exposure to high electric field (arrow) will they survive in real RF structure?

## Slide 14: Nanopatterns into LES
7
Semiconductor nanostructures has been tested in the LES more than 10 years ago!
Data shows staircase steps in field emission
Caused by resonance tunneling? (likely not...)
Discrete distributions of beta
Only probing the high betas in an area
Notes: There could be a rich Mo area on top of the pillars, leading to a resonance tunneling effect there.
Only probing the high betas in an area IS JUS LIKE THE LIGHT EMISSIONE XPERIMENT!!!!

## Slide 15: Semiconductor nanopillars: GaSb
6
Same nanopillars tested in the LES
Ellipsometry data recorded for the system
Simulations indicate much absorption in the UV range
Could be an interesting photocathode candidate

## Slide 16: UV Low Reflectance Copper
8
Nanostructured metallic photocathodes
Low UV reflectance.
Potential metamaterial effect!
Period p
Width w
Height h
Fill factor f = w/p

## Slide 17: Looking for field emitters!
8
Is field emission (and light from field emission) dominated by field emitters?
Using the same camera to detect breakdowns, maybe we can detect field emitters!
Location of peak helps us triangulate the signal!

## Slide 18: Looking for field emitters!
8
Initial testing of CuBe shows the measurement to be dominated by noise…
Some small feature was observed during high voltage, but cannot be distinguished from noise!
…
…
Camera 1
Camera 2

## Slide 19: Looking for field emitters!
A few locations was estimated using the data.
Spectroscopic investigation revealed no additional features…

## Slide 20: THANK YOU!
8

## Slide 21: References
1
[1] https://journals.aps.org/prab/pdf/10.1103/PhysRevSTAB.12.074201
[2] file:///C:/Users/victormb/Documents/Papers/1-s2.0-0168900294912939-main.pdf
[3] https://accelconf.web.cern.ch/ipac2016/papers/thpow015.pdf
[4] https://psec.uchicago.edu/library/photocathodes/loch_thesis_CsTe.pdf
[5] Hot Electron enhanced photoemission from laser fabricated plasmonic cathodes
[6]https://pubs.aip.org/aip/jap/article/127/16/164903/153446/A-quantum-model-for-photoemission-from-metal