## Slide 2: Work Package WP2.2 (HTS conductor, cables & associated technologies)
Date: 02.05.2023
Author: Christian Barth on behalf of the TE-MSC-HSD section

## Slide 3: Introduction
Objective:
Demonstrator of 5 T in a background field of 15 T
Work Package 2.2:
Specification and procurement of tape.
Generate material database
Development of electrically insulated cables. Target: 10 kA @ 20 T, 5 kV .

## Slide 4: Scope of Work Package 2.2
Exploration of REBCO tapes for suitability for fields > 16 T.
   Establish REBCO characterization capabilities
   Derive tape specifications, procure tape
Development of cables, cabling and other associated technologies including insulation
Establish cabling & insulation capabilities
  Establish cable characterization capabilities

## Slide 5: Characterization of REBCO tapes #1
Automated 8-channel, 77 K, self-field, Ic test station developed
  in operation, also used for HL-LHC
  for REBCO cable QC: extracted tapes Ic measurements
Reel-to-reel tape QC system in development
  will be used to precisely map Ic along tape length

## Slide 6: Characterization of REBCO tapes #2
‘U’-shape adapter to characterize REBCO tapes in 15 T wire test station developed (B || c)
  in operation
‘1-turn’ adapter to characterize REBCO tapes in 15 T wire test station developed (B || ab)
  in fabrication

## Slide 7: Characterization of REBCO tapes #3
‘Compact sample holder for high-field tests (LNCMI) developed (B || c, or B ||ab)
  being assembled
Large-bore, 20 T test station with VTI will be installed at CERN for high field characterizations
  ~100 mm Ø targeted
Split-coil test station with VTI will be installed at CERN for variable angle characterizations
  ~10 T targeted, feasibility study with suppliers

## Slide 8: Characterization of REBCO tapes #4
Field, angle & temperature scaling relations for REBCO tape of different industrial suppliers
  SuperPower, Fujikura, SST, SuperOx, Theva
  Released as internal note (EDMS: 2747837)
Examples:

## Slide 9: Other superconductors
Future collaboration CERN/CNR-SPIN – Iron Based Superconductors
  drawing machines
  groove rolling machines
  flat rolling machine
CNR- SPIN, Genova
Courtesy A. Malagoli

## Slide 10: Cabling & insulation capabilities #1
Round, insulated power transmission cables
  operational, used for HL-LHC
‘Stack’ type cables
  14 tapes + insulation, torque control only: operational
  7 tapes, precise tension control: being upgraded to 15 tapes + insulation

## Slide 11: Cabling & insulation capabilities #2
Kapton tape wrapping for round and ‘stack’ cables
  operational, long lengths possible
‘c-shape’ Kapton tape insulation for ‘stack’ cables
  operational, long lengths possible

## Slide 12: Characterization of cables #1
Intertape resistance measurement setup (77 K, self-field) developed
  in operation

## Slide 13: Characterization of cables #2
In-field characterization of cables with the FRESCA & FRESCA2 test stations
  FRESCA (9.6T, 1.9K & 4.2K): in operation
  FRESCA2 (13T, 1.9K & 4.2K & gas-flow): being commissioned
Dedicated test station for splice & current lead characterization
  in development